## Slide 1: Development of ultra-low optical and mechanical loss aSi coatings using novel ECR ion beam deposition Optical absorption of amorphous silicon coatings Stuart Reid / Iain Martin (UWS/GU)
Ross Birney 1, Des Gibson1, Jim Hough2, Sean MacFoy1, Iain Martin2, Peter Murray2, Stuart Reid 1, Raymond Robie2, Sheila Rowan2, Jessica Steinlechner2, Simon Tait1, Zeno Tornasi2, David Vine1
1SUPA, Institute of Thin Films, Sensors and Imaging, University of the West of Scotland,
2SUPA, Institute for Gravitational Research, University of Glasgow
LIGO-G1601200

## Slide 2: “Take home message”
Recent results from UWS/UG suggest:
It is possible to reduce optical absorption in IBS aSi coatings, whilst maintaining low f.
Heated deposition of IBS aSi films likely to gain similar benefits in atomic structure/mechanical loss as heated e-beam deposition (as observed by Berkley group).

## Slide 3: Background
Original requirements for aLIGO (at 1064nm):
Absorption < 0.5 ppm required (goal < 0.3 ppm)
Scatter < 2 ppm required (goal < 1 ppm)
ITM transmission: (5 ± 0.25) × 10-3.
ETM transmission: < 10 ppm (goal < 5 ppm)
Test Mass HR matching = 2 (T1-T2)/(T1+T2) < 1 × 10-2 required (goal 5 × 10-3)
AR reflectivity: 200 ± 20 ppm
Mechanical loss: 3 × 10-5 (goal 1 × 10-4)
Likely requirements for aLIGO+ and beyond?
IBS
???

## Slide 4: PVD (Physical vapour deposition)
The continued challenges in PVD technology
-> Uniform deposition on large area : difficult
-> Multi component deposition: even more difficult
Evaporation
Pulsed Laser Deposition
(PLD)
Magnetron sputtering
substrate
ions
substrate
substrate
+
_
substrate
Ion Beam Deposition
(IBD)
Deposition profile/conditions is somewhat fixed and
limited by the geometry of the process

## Slide 5: Ion beam deposition (IBD)

## Slide 6: ECR ion source at UWS

## Slide 7: Development of ECR-IBD
ECR plasma cavity
(microwave)
Divergent Ar ion beam
focus
ground

## Slide 8: Development of ECR-IBD
z
Bz
BECR
Forward diffusion
inside the magnetic field
Area of maximum
power
coupling
~ l / 4 ~ 3 cm at 2.45 GHz
Extraction plane
Bmax
Antenna
Couplers
Compact l/4 microwave cavity
filament-free
maintenance free
low current
extraction potential 0-20 kV

## Slide 9: Comparison to standard IBS
Filament and extractor grid provide high-current
(possible contamination and expensive running costs)
50 to 1500eV and 75 to 700mA (for Veeco 16cm RF)

## Slide 10: Development of ECR-IBD

## Slide 11: Development of ECR-IBD

## Slide 12: Absorption measurements - Glasgow
Pump beam, 1550 nm
Probe beam,
1620 nm
Lock-in amplifier
sample
detector
A. Alexandrovski et al. Proc. SPIE 3610, Laser Material Crystal Growth and Nonlinear Materials and Devices, 44 (May 26, 1999);
Photo-thermal commonpath interferometry (PCI)
Slides courtesy of J. Steinlechner (IGR, Glasgow)

## Slide 13: Absorption measurements - Glasgow
Pump beam changes refractive index of an element in the probe beam
Dn
Slides courtesy of J. Steinlechner (IGR, Glasgow)

## Slide 14: Absorption measurements - Glasgow
Pump beam changes refractive index of an element in the probe beam
The wavefront from this element is different from the rest of the beam
We measure this phase difference by imaging the plane 1 Rayleigh range from the intersection point
(virtual detection plane)
Dn
Slides courtesy of J. Steinlechner (IGR, Glasgow)

## Slide 15: Absorption measurements - Glasgow
Pump beam changes refractive index of an element in the probe beam
The wavefront from this element is different from the rest of the beam
We measure this phase difference by imaging the plane 1 Rayleigh range from the intersection point
(virtual detection plane)
Dn
Getting absorption by comparing signal to calibration substrate with known absorption
Slides courtesy of J. Steinlechner (IGR, Glasgow)

## Slide 16: aSi coatings fabricated using ECR-IBD
20mm JGS3 silica witness samples
(optical characterisation and absorption)
Cross-section SEM image

## Slide 17: aSi coatings fabricated using ECR-IBD
silica cantilevers, coated with aSi

## Slide 18: Absorption measurements on aSi – 1550 nm
Description
Chart: heat treatment temperature [C]
| 20.0 | 120.0 | 200.0 | 300.0 | 400.0 | 450.0 | 500.0 | 600.0 | 700.0 | 800.0 | 900.0 | 1000.0
ATF | 6762 | 6357.4 | 2849 | 1783.6 | 1180.2 | 1057 | 1086.4 | 1204 | 6659.8 | 5955.6 | 20879.6 | 6868.4
UWS | 540.1515 | 131.5152 | 84.5455 | 35.2273 | 14.0909 | 46.9697
1550 nm
Absorption significantly lower than for ATF coatings
Refractive index ~3.4 from transmission measurements
UWS measured on a ~660 nm layer
ATF measured on a 500 nm layer → both scaled to HR coating
1000 ppm
< 20* ppm
* measurement limited by substrate absorption

## Slide 19: Absorption measurements on aSi – 1064 nm
ppm
m

## Slide 20: Mechanical loss
Description
Initial mechanical loss measurements on silica cantilevers
Chart: Mechanical Loss of aSi
| 0.0 | 15.0
 | 0.00024 | 0.00024
As Deposited | 0.00023016 | 0.00015493 | 0.00019914 | 0.00015129
 | 3.4201e-05 | 5.3335e-05 | 3.1836e-05

## Slide 21: Berkeley high temperature deposition
Description
X. Liu, F. Hellman, et al, PRL 113, 025503 (2014)
As discussed by M. Fejer yesterday (see G1601192-v1)
Heated deposition reduces mechanical loss much further than post- heat treatment alone.
~10-4 vs ~10-6
Surface mobility during deposition: - sound velocity approaches asymptote - distribution of bond angles narrows - density increasing - Heat capacity approaches bulk silicon value
Open question – similar benefits for IBS?
annealed 350C
deposited 350C

## Slide 22: High-temperature deposition
Description

## Slide 23: High-temperature deposition - absorption
Description
Strong evidence that room temperature coatings have been contaminated – strangely reducing the absorption further – however index also lower than expected
Random spread in absorption – no clear benefit in heated deposition in initial tests

## Slide 24: High-temperature deposition – mechanical loss
Description
Chart: Mechanical Loss of aSi
| 0.0 | 15.0
 | 0.00024 | 0.00024
As Deposited | 0.00023016 | 0.00015493 | 0.00019914 | 0.00015129
 | 3.4201e-05 | 5.3335e-05 | 3.1836e-05
So what happens???

## Slide 25: High-temperature deposition – mechanical loss
Description
Difficult (but good!) problem:
funcoated = 1.86x10-6
250s ringdown
1550Hz
150s ringdown
1550Hz
fcoated = 1.64x10-6
fcoating = 8.6x10-6
uncoated cantilever – annealed twice at 400C
coated cantilever – annealed at 400C

## Slide 26: High-temperature deposition – mechanical loss
Description
Chart: Mechanical Loss of aSi
| 0.557125 | 1.559813 | 3.059438 | 5.056344 | 7.636156
 | 7.2742e-05 | 0.00010022 | 9.9378e-05 | 9.4812e-05 | 0.00011033
 | 0.00024 | 0.00024
As Deposited | 0.00023016 | 0.00015493 | 0.00019914 | 0.00015129
 | 3.4201e-05 | 5.3335e-05 | 3.1836e-05

## Slide 27: High-temperature deposition – mechanical loss
Annealing the 200C aSi coating at 400C, measurement approaching experimental uncertainty, at the level of 1x10-5.
Chart: Mechanical Loss of aSi
| 0.557125 | 1.559813 | 3.059438 | 5.056344 | 7.636156
 | 7.2742e-05 | 0.00010022 | 9.9378e-05 | 9.4812e-05 | 0.00011033
 | 0.00024 | 0.00024
As Deposited | 0.00023016 | 0.00015493 | 0.00019914 | 0.00015129
 | 3.4201e-05 | 5.3335e-05 | 3.1836e-05
 | 9.0879e-06 | 1.403e-05
Likely factor 25 reduction in loss achievable

## Slide 28: High-temperature deposition – mechanical loss
Description
Results are on the way!

## Slide 29: Characterisation – bandgap associated absorption
Description
Chart: hn
Tauc plot – UWS aSi

## Slide 30: Characterisation – bandgap associated absorption
Description
Chart: hn
Tauc plot – UWS aSi
Average bandgap energy 1.4eV (commonly reported 1.1-1.5eV for a-Si)

## Slide 31: Characterisation – Raman
See poster by Zeno Tornasi (Glasgow)

## Slide 32: Thermal noise
Description
We can use a multi material design
Some bilayers of SiO2 and Ta2O5 are used to reduce the laser power
In lower layers amorphous silicon can be used to improve thermal noise due to a high refractive index and low loss
Jessica Steinlechner

## Slide 33: What does this mean for thermal noise? … if we want less than 1ppm absorption from the aSi:
Description
Jessica Steinlechner
At 1064 nm RT:
We need 8 bilayers of SiO2 and Ta2O5 to reduce the laser power
For an ITM with T= 1.4% we can’t improve the coating using aSi in lower layers
For an ETM with T = 6 ppm we need 4 bilayers of SiO2 and aSi
Thermal noise improvement* compared to a pure SiO2 and Ta2O5 coating:
Room temperature: ITM: - 0% ETM: - 28% total: -18%
*Loss for aSi: 1.2e-4 measured on UWS aSi coatings at room temperature
21.5%
5x10-5
Almost no improvement by reducing mechanical loss further (limited by silica loss and ITM thermal noise)

## Slide 34: What does this mean for thermal noise? … if we want less than 1ppm absorption from the aSi:
Description
Jessica Steinlechner
At 1550nm RT:
We need 5 bilayers of SiO2 and Ta2O5 to reduce the laser power
For an ITM with T= 6000 ppm we need 2 bilayers of SiO2 and aSi
For an ETM with T = 6 ppm we need 5 bilayers of SiO2 and aSi
Thermal noise improvement* compared to a pure SiO2 and Ta2O5 coating:
120 K 20 K ITM: -21% -20% ETM: -38% -36% total: -32% -31%
*Loss for aSi: values from commercial coatings; no cryogenic measurements on UWS coatings

## Slide 35: Conclusion from UWS + GU investigations using ECR-IBD
Description
aSi attractive high-index material choice for aLIGO+ and beyond
  Optical absorption of 20ppm for HR stack feasible (reason due to unique dep parameters – low dep rate + high ion energy)
  Mechanical loss ~ 5x10-5 (room temp deposition + heat treatment at 400C)
Heated deposition
  First evidence that heated substrates + ion-beam deposition can reduce mechanical loss below that achievable through same temperature post-deposition annealing
  Mechanical loss ~1x10-5 for aSi deposited at 200C then heat treated to 400C
Future work
  Complete studies on aSi deposited at elevated temperatures
  Investigate effect of elevated temperature on Ta2O5
  Investigate effect of shifting bandgap absorption edge in aSi through doping (H, Al, N etc) – with particular relevance to 1064nm use.

## Slide 36: Towards a more ordered future…
Description

## Slide 37: MBE developments (UWS+GU+Stanford+GSS)
Plan to develop AlGaP interference coatings on silicon
Key milestones:
March 2016: all equipment delivered (P cracker, P recovery system, auxillary equip.)
June 2016: installation of P cracker and recovery system
August 2016: test growths of AlGaP begin

## Slide 38: Conclusion from UWS + GU investigations using ECR-IBD
Description
aSi attractive high-index material choice for aLIGO+ and beyond
  Optical absorption of 20ppm for HR stack feasible (reason due to unique dep parameters – low dep rate + high ion energy)
  Mechanical loss < 1x10-4 (room temp deposition + heat treatment at 400C)
Heated deposition
  First evidence that heated substrates + ion-beam deposition can reduce mechanical loss below that achievable through same temperature post-deposition annealing
  Mechanical loss ~1x10-5 for aSi deposited at 200C then heat treated to 400C
Future work
  Complete studies on aSi deposited at elevated temperatures
  Investigate effect of elevated temperature on Ta2O5
  Investigate effect of shifting bandgap absorption edge in aSi through doping (H, Al, N etc) – with particular relevance to 1064nm use.
  Further low temperature absorption and thermal noise evaluation.