## Slide 1: Silicon sensors with internal gain: Optimizing for charged particle fast timing Characterization of Deep Diffused APDs (non-irradiated) devices from RMD
RD50 Workshop June 2016, Torino, Italy
OUTLINE:
Concept of Deep Diffused APDs (“Hyperfast Detectors”)
First measurements: Study on homogeneity of response
Simulation of charged particle fast timing
Outlook
RD50
Ashutosh Bhardwaj (Delhi), Ranjeet Dalal1 (Delhi), Marco Fernandez Garcia (Santander), Geetika Jain (Delhi), Changuo Lu (Princeton), Michael Moll (CERN), Kirti Ranjan (Delhi), Sofia Otero Ugobono (CERN), Sebastian White (Princeton, CERN)

## Slide 2: Concept of Deep Diffused APD
Deep Diffused APD from RMD (Radiation Monitoring Devices Inc.)
  n-type NTD-doped silicon from Topsil
  Grooving wafer
  Deep diffusion of p-type dopants
    Gallium used as dopant
  Etching of surface layer
[2006, McClish et al., IEEE TNS, 53, 3049 ]
[2004, McClish et al., IEEE TNS]

## Slide 3: Charge Multiplication and Gain
Deep Diffused APDs
  Amplification deep inside the bulk of the sensor
  Requires high voltage (1700-1800V)
  Delivers high gain and fast response time
[2015, N.Cartiglia, DESY seminar]
Comparison: Reach-through APD; LGAD
TCAD Simulations
  Doping profile based on measured data (literature) used to simulate E-Field

## Slide 4: Motivation: Time resolution
References to previous work
  By SAMPIC team and S.White [D.Brenton et al., Elba conference 2015]
    RMD Mesh-APD
    VCSEL, 980nm; Amplifier: Wenteq, 50dB (316) gain
    SAMPIC system (Sampling rate = 6.4 GSample/s )
~ 1 MIP
~ 15ps
  More details on previous work and collaboration working on the subject :
    S.White, CERN Detector Seminar, 25.09.2015 [ https://indico.cern.ch/event/439571/ ]

## Slide 5: Homogeneity of response (Charge)
Homogeneity scan on 2 RMD devices
  2mm x 2mm RMD Deep Diffused APDs
  TCT with IR (1064 nm) pulsed laser - integration of pulse over 25ns
Sample 02
Sample 01 [mounted not planar to PCB]
1700 V
1750 V
1750 V
1700 V
1800 V
Note: Different amplifier setting for sample 01 and 02 (arb. Charge values given)

## Slide 6: “Charge collection” outside active area
Signal observed outside active are of device
The glue around the sensor causes the laser to reflect and enter the APD, thus explaining the charge collection observed outside the sensor.
1700 V – IR laser
Signal disappears when Glue covered with tape

## Slide 7: Pulse shapes
IR laser pulses
Red laser pulses (front illumination); “electron injection”
Sample 02
Sample 02
Sample 01
Sample 01
Measurements: 10-1800V (10V steps)

## Slide 8: APD with mesh for readout
Proposed configuration for fast timing
  Deep Depleted APD with mesh readout (“Hyperfast Detectors”) [White at al. ]
  2 Kapton layer thicknesses tested (2 and 5 mil, i.e. 51 and 127 mm)
  IR and Red laser scans performed at -1776V
15 μm
15 μm
57 μm
49 μm
Low resolution scan (100mm)
High resolution scan (100mm)
  Irradiation and further test to be done.
-1776 V
Mesh: connected to amplifier
GND

## Slide 9: TCAD simulations (Silvaco)
Device: Deep Diffused APD
  200 mm thick APD (p-in-n) represented in simulator by 1x1x200 µm3 volume
  Error function deep diffused p-doping profile; bulk n-doping: 1.4 x 1014 cm-3
  Junction at depth of 57 mm
  TCT with three different laser wavelength (670nm, 980nm, 1060nm)
  External circuit (Bias T) implemented for transient simulation
  Carrier lifetime set to 100ms; Charge integration for gain plots: 20ns
p+
n
~15µm on front side not depleted
Increasing bias: field extending towards n-side

## Slide 10: TCT simulation
TCT (front side illumination) [670nm, 980nm, 1060nm]
  Very fast initial peak for all wavelengths due to drift component of current
    For charge created in depleted layer
  Large (and slow) diffusion component for 670nm
    almost all charge deposited in un-depleted layer on front side (needs diffusion)

## Slide 11: TCT simulation
TCT (front side illumination)
  Very strong dependence on applied voltage and bulk doping concentration!
  Simulation predicts pulse length of 2-3ns
    Measurements showed slightly larger pulse length (approx. 4ns)
Voltage dependence
Dependence on bulk doping

## Slide 12: TCT simulation
Gain predictions
  Gain defined as: Signal with impact ionization / signal without impact ionization (It’s a simulation )
  Higher bulk doping results in higher gain
    less depleted volume with higher E-Field
  Highest gain for lowest wavelength
    (higher fraction of generated carriers undergo amplification)
200mm APD thickness
200mm APD thickness

## Slide 13: TCT simulation
Simulated gain versus measured gain
  Gain for measured data (IR, red laser) defined as integrated signal / <integrated signal (1000V)>
Simulation reproduces data trend (gain vs. voltage) quite well
  Need to normalize simulation data and measured data in same way
  Test measurements at 480nm provide a signal while the simulation with the present TCAD device model would give no signal at all for 480nm: Indication that the surface layer to the front is thinner than in the model, which however for the infrared laser measurements/simulations has no impact.
preliminary
preliminary

## Slide 14: Simulation: Edge-TCT configuration
Simulation parameters:
  Laser 1060nm, beam width 1 µm, 1ps risetime
  Depth position 1µm to 170µm (5 µm step)
  Junction depth: 57mm;
  Bulk doping (n-type): 1.4e14cm-3
5 mm
170 mm

## Slide 15: Simulating energy-loss fluctuations
Calculations based on two simulations:
  TCAD edge-TCT simulation
    provides wave forms for charges generated for every 5 mm slice of the detector.
  Bichsel charged particle energy straggling calculations
    Theory and Fortran code by H.Bichsel [Bichsel, Straggling in thin silicon detectors, 1988,Rev. Mod. Phys. 60, 663 ]
    Provides probability density function for a slice of 5 mm silicon
Voltage: 1800 V
16 positions (16 slices)
1 GeV muon, 5mm silicon
[PDF provided by Su Dong, Stanford, USA]
Deposited Charge [KeV/5mm silicon]
PDF
Histogram based on PDF

## Slide 16: Simulating energy-loss fluctuations
Note that the Bichsel PDF for thin sensors is not a Landau Distribution !
  For 5 mm Silicon & 1 GeV muon
1 GeV muon, 5mm silicon
[PDF provided by Su Dong, Stanford, USA]
Deposited Charge [KeV/5mm silicon]
Bichsel PDF
Histogram from Landau
Landau fitted to Bichsel PDF
    based on [[Bichsel, 988,Rev. Mod. Phys. 60, 663 ]

## Slide 17: Simulating energy-loss fluctuations
Comparison of test beam data versus simulation [pulse heights distribution]
  Full size sensors
1 GeV muon
6 GeV pions, test-beam 2015
preliminary

## Slide 18: Simulating energy-loss fluctuations
Comparison of test beam data versus simulation [pulse heights distribution]
1 GeV muon
6 GeV pions, test-beam 2015
preliminary

## Slide 19: Simulating energy-loss fluctuations
Comparison of results [Prelimary]
  Comparing the different PDFs (Landau and Bichsel) result in significantly different time jitter
  Landau: 47 ps
  Bichsel: 30 ps
  Conclusion: Comparison with test-beam data needed.
preliminary
preliminary

## Slide 20: Test beam ongoing
Sunday 5.6.2016
  Sensors with Sampic readout installed …. data for next RD50
1. Signal trace @ 1800V and 50 dB preamp with MCP-PMT signal
2. Setup showing both the Si telescope on right and the SAMPIC on the left

## Slide 21: Conclusions and Outlook
Previous works showed excellent timing performance ~15ps
First measurements on Deep Diffused APDs performed at CERN SSD
  Some in homogeneities (up to factor 2) for collected charge seen over active surface
  ToDo: Perform same scan for time jitter
Wider multiplication zone then in LGAD/standard APD devices
  Increased multiplication zone with high bias leads to the good timing performance
  ToDo: Understand optimum configuration of deep diffusion vs. bulk doping
First simulation study on time jitter arising from energy-loss fluctuations performed using TCAD wave forms (e-TCT) and Bichsel or Landau PDFs
  Bichsel distribution vs. Landau distribution results in less time jitter
All results obtained on non-irradiated devices
  Need to perform irradiation tests to study feasibility for high radiation environments!

## Slide 22: Comparison: LGAD – DD APD
TCAD simulation
  LGAD structure (with peak p-well doping of 9.75e16 cm-3, see R.Dalal last RD50) and thickness of 150 µm is used for simulation
  APD structure of 200 µm is used (depletion width ~ 140 µm)
TCT signal evolution of APD and LGAD is compared
  TCT peak for LGAD is peaking after 1.8 ns (for example see blue curve for 1500V)
  TCT signal peak for APD is peaking after ~ 0.9 ns after laser fire
  Electrons from bulk have to move to front side p-well region for charge multiplication but in APD charge multiplication is happening around junction region.

## Slide 23: E field for different bias
E-field as function of bias
  With increase in bias, Depletion region mainly expand in backside bulk
  Should not expect much improvement with bias for front diffusion component !
  No multiplication beyond about 100 micron depth (this number depends on bias)