## Slide 1
Radiation Damage TCAD Analysis of
Low Gain Avalanche Detectors
F.R. Palomo1, M. Carulla2, S. Hidalgo2 ,G. Pellegrini2 ,I. Vila3,
rogelio@zipi.us.es
salvador.hidalgo@csic.es
1Departamento Ingeniería Electrónica, Escuela Superior de Ingenieros
Universidad de Sevilla, Spain
2Instituto de Microelectrónica de Barcelona, Centro Nacional de Microelectrónica, Barcelona, Spain
3Instituto de Física de Cantabria, Santander, Spain

## Slide 2
Sentaurus TCAD Simulation SetUp
Mixed Simulation Setup:
Red Pulsed Laser: 670 nm, 10 mm spot, 1e4W/cm2, 50 ps, BackIllumination at Device Center
ReadOut: gain unity current amplifier (Rf=1), AC (1 nF) coupled
2D detector model: 1 mm in Z direction, 3 mm in X direction,
300 mm in Y direction)
P-Stop
Collector
Ring
C-Stop
Low Gain Avalanche Detector (LGAD)
cross-section
ReadOut Simulation Setup
Doping profiles under confidenciality rules
Red Pulsed
Laser
Simulation
Setup
x
y
z

## Slide 3
LGAD Bias Analysis: 250V, 450V, 650V, Gain shows a linear increase with bias
The equivalent PiN is an LGAD device without Pwell (gain well)
4,26
5,52
4,88
Gain=(QLGAD/QPiN )|bias
LGAD current transient, variable bias
& Total transient charge
LGAD

## Slide 4
Radiation Damage Models
Simulation of Silicon Devices for the CMS Phase II Tracker Upgrade CMS Note 250887
CMS Proton Model
CMS Neutron Model
Four damage models
Pennicard Model f =1e12 up to 1e14 neq/cm2
CMS Proton and Neutron model f = 1e14-1e15 neq/cm2
Delhi Model Proton f = 1e14-1e15 neq/cm2
New Perugia Model f =1e12 up to 2e16 neq/cm2
Combined effect of bulk and Surface damage on strip insulation properties of proton irradiated n+-p silicon strip sensors, R.Dalal et al. JINST 2014 9 P04007
Delhi Model
N(cm-3)=gint x f
Pennicard Model
Simulations of radiation-damaged 3D detectors for the Super-LHC, D.Pennicard et al. NIMA 592(1-2), 2008, pp16-25
N(cm-3)=hint x f
New Perugia
Modeling of radiation damage effects in silicon detectors at high fluences
HL-LHC with Sentaurus TCAD, D.Passeri et al, NIMA 824 (2016), 443-445

## Slide 5
LGAD
Pulsed red laser transient, current amp readout (gain=1)
Pennicard Damage Model
## Putting traps in Silicon region only
## Trap concentrations found from Petasecca model and modified by
D. Pennicard, Fluence=1E14
Physics (material="Silicon") {
# Putting traps in silicon region only
# Modified Perugia model with trapping times at reported value
Traps (
(Acceptor Level EnergyMid=0.42 fromCondBand Conc=1.1613E14 Randomize=0.29 eXsection=9.5E-15 hXsection=9.5E-14) #Conc=Fluence*1.1613
(Acceptor Level EnergyMid=0.46 fromCondBand Conc=0.9E14 Randomize=0.23 eXsection=5E-15 hXsection=5E-14 ) #Conc=Fluence*0.9
(Donor Level EnergyMid=0.36 fromValBand Conc=0.9E14 Randomize=0.31 eXsection=3.23E-13 hXsection=3.23E-14 ) #Conc=Fluence*0.9
)
}
Pennicard model valid up to 1e14 neq/cm2.
It shows that LGAD does not experiment a significative gain reduction up
to 1e14. At 1e14, gain decreases 29%.
LGAD 400V Bias
Fluence | Gain
0 | 4,80
1e12 | 4,72
1e13 | 4,54
1e14 | 3,36
(Reference PiN Charge 50.9 fC)

## Slide 6
LGAD
Pulsed red laser transient, current amp readout (gain=1)
CMS Neutron Damage Model
## Putting traps in Silicon region only
## Trap concentrations found from CMS Two level neutrons
#Fluence=1E14
Physics (material="Silicon") {
# Putting traps in silicon region only
Traps (
(Acceptor Level EnergyMid=0.525 fromCondBand Conc=1.55E14 eXsection=1.2E-14 hXsection=1.2E-14)
(Donor Level EnergyMid=0.48 fromValBand Conc=1.395E14 eXsection=1.2E-14 hXsection=1.2E-14)
)
}
Fluence | Charge (fC) | Gain
0 | 244,0 | 4,80
1e14 | 186,1 | 3,66
1e15 | 30,7 | 0,60
PIN DIODE
Non Irradiated

## Slide 7
LGAD
Pulsed red laser transient, current amp readout (gain=1)
CMS Proton Damage Model
## Putting traps in Silicon region only
## Trap concentrations found from CMS Two level protons
#Fluence=1E14
Physics (material="Silicon") {
# Putting traps in silicon region only
Traps (
(Acceptor Level EnergyMid=0.525 fromCondBand Conc=1.8344E14 eXsection=1E-14 hXsection=1E-14)
(Donor Level EnergyMid=0.48 fromValBand Conc=1.6390E14 eXsection=1E-14 hXsection=1E-14)
)
}
Fluence | Charge (fC) | Gain
0 | 244,0 | 4,80
1e14 | 186,7 | 3,67
1e15 | 24,6 | 0,48
PIN DIODE
Non Irradiated

## Slide 8
LGAD
Pulsed red laser transient, current amp readout (gain=1)
Delhi Damage Model
## Putting traps in Silicon region only
## Trap concentrations found from Delhi Two level
#Fluence=1E14
Physics (material="Silicon") {
# Putting traps in silicon region only
Traps (
(Acceptor Level EnergyMid=0.51 fromCondBand Conc=4E14 eXsection=2E-14 hXsection=3.8E-15)
(Donor Level EnergyMid=0.48 fromValBand Conc=3E14 eXsection=2E-15 hXsection=2E-15)
)
}
Fluence | Charge (fC) | Gain
0 | 244,0 | 4,80
1e14 | 124,6 | 2,45
1e15 | 9,4 | 0,18
PIN DIODE
Non Irradiated

## Slide 9
LGAD
All Models show a similar panorama
CMS Model
Electric Field along Y axis
At 1e15 a double junction appears at P+ volumen (device back side)
Electric Field Profiling
Back side detail
Front side detail
1e15
1e15
Back side
Front side

## Slide 10
LGAD
Delhi Models
Electric Field Profiling
At 1e15 a double junction appears
at P+ volume
Back side detail
Front side detail
Electric Field along Y axis
1e15
1e15
Back side
Front side

## Slide 11
LGAD7859D10-3
CV analysis
Now, we analyze a real device, the PAD LGAD7859D10-3
It has JTE’s, 300 mm thickness one extraction ring.
CV Analysis with:
New Perugia Model:
  Fresh
  2. 1e13-1e14-1e15-7e15-2e16 n/cm2
Temperature = 20ºC
This LGAD is fully depleted past 70V
Capacitance shows a clear increase beyond 1e15 n/cm2
1/C2 formula is not clear beyond 1e14

## Slide 12
IV Analysis with:
New Perugia Model:
  Fresh
  2. 1e13-1e14-1e15-7e15-2e16 n/cm2
Temperature = 20ºC
LGAD7859D10-3
CV analysis
IV plots show problems starting at 1e15, the leakage grows a lot and even the general curve is different. This is coincident with the previous models.

## Slide 13
IV Analysis with:
New Perugia Model:
  Fresh
  2. 1e13-1e14-1e15-7e15-2e16 n/cm2
Temperature = 20ºC
LGAD7859D10-3
CV analysis
IV plots show problems starting at 1e15, the leakage grows a lot and even the general curve is different. This is coincident with the previous models.

## Slide 14
IV Analysis with:
New Perugia Model:
  Fresh
  2. 1e13-1e14-1e15-7e15-2e16 n/cm2
Temperature = 20ºC
LGAD7859D10-3
CV analysis
IV plots show problems starting at 1e15, the leakage grows a lot and even the general curve is different. This is coincident with the previous models.

## Slide 15
IV Analysis with:
New Perugia Model:
  Fresh
  2. 1e13-1e14-1e15-7e15-2e16 n/cm2
Temperature = 20ºC
LGAD7859D10-3
CV analysis
IV plots show problems starting at 1e15, the leakage grows a lot and even the general curve is different. This is coincident with the previous models.

## Slide 16
Laserback LGAD7958D10-3 20ºC
Fluence n/cm2 | Charge LGAD (nC) | Charge PIN (nC) | Gain Qlgad/Qpin
0 | 1,538 | 0,460 | 3,34
1e13 | 1,510 | 0,456 | 3,31
1e14 | 1,265 | 0,421 | 3,00
1e15 | 0,358 | 0,153 | 2,34
7e15 | 0,005 | FAIL | ---
2e16 | 0,002 | FAIL | ---
Equiv. PIN Detector,
700V bias (an LGAD without mult.P layer)
LGAD Detector
300 mm
700V bias
(We compare LGAD and PIN at same fluence to obtain a practical Gain Definition)
Refined models show same conclusions: beyond 1e15 n/cm2 the 300 mm LGAD has problems (but for PIN are worst!)

## Slide 17
Fluence n/cm2 | Charge LGAD (nC) | Charge PIN (nC) | Gain Qlgad/Qpin
1e13 | 1,743 | 0,4502 | 3,87
1e14 | 1,454 | 0,4222 | 3,53
1e15 | 0,561 | 0,2477 | 2,17
7e15 | 0,065 | 0,0175 | 3,61
2e16 | 0,028 | FAIL | ---
Laserback LGAD7958D10-3 -20ºC
Lowering to 253 K improves the radiation hardness, as expected, but avoid false friends (7e15 case, PIN is failing)
(We compare LGAD and PIN at same fluence to obtain a practical Gain Definition)
PIN Detector
700 V bias
(LGAD without
mult. P Layer)
LGAD Detector
300 mm
700V bias

## Slide 18
LGAD7859D10-3 50 mm thickness
CV analysis
Displacement damage scalates down with decreasing device thickness, so let’s explore that avenue: we have gain so signal volumen reduction is compensated by the linear avalanche. The CV for fluence panoplia shows a full depleted device beyond 40V in a thinned LGAD7859 (50 mm thickness).
New Perugia Model:
  Fresh
  2. 1e13-1e14-1e15-7e15-2e16 n/cm2
Temperature = 20ºC
This LGAD is fully depleted past 35V
Capacitance shows a moderate increase beyond 7e15 n/cm2
1/C2 formula is not clear beyond 7e15

## Slide 19
50 mm IV
IV Analysis with:
New Perugia Model:
  Fresh
  2. 1e13-1e14-1e15-7e15-2e16 n/cm2
Temperature = 20ºC
IV plots shows a promising behaviour even at 7e15 n/cm2. These are good news so it’s worth to look at the simulated back laser experiments.

## Slide 20
50 mm IV
IV Analysis with:
New Perugia Model:
  Fresh
  2. 1e13-1e14-1e15-7e15-2e16 n/cm2
Temperature = 20ºC
IV plots shows a promising behaviour even at 7e15 n/cm2. These are good news so it’s worth to look at the simulated back laser experiments.

## Slide 21
50 mm IV
IV Analysis with:
New Perugia Model:
  Fresh
  2. 1e13-1e14-1e15-7e15-2e16 n/cm2
Temperature = 20ºC
IV plots shows a promising behaviour even at 7e15 n/cm2. These are good news so it’s worth to look at the simulated back laser experiments.

## Slide 22
50 mm IV
IV Analysis with:
New Perugia Model:
  Fresh
  2. 1e13-1e14-1e15-7e15-2e16 n/cm2
Temperature = 20ºC
IV plots shows a promising behaviour even at 7e15 n/cm2. These are good news so it’s worth to look at the simulated back laser experiments.

## Slide 23
LGAD Detector
50 mm
150V bias
Laserback 50 mm (thinned) LGAD7958D10-3 20ºC
Fluence n/cm2 | Charge LGAD (nC) | Charge PIN (nC) | Gain Qlgad/Qpin
0 | 1,337 | 0,456 | 2,93
1e13 | 1,331 | 0,455 | 2,93
1e14 | 1,282 | 0,474 | 2,74
1e15 | 0,934 | 0,384 | 2,43
7e15 | 0,349 | 0,212 | 1,65
2e16 | 0,137 | 0,045 | 3,04
Thinning the LGAD it is a game changer for radiation hardness if we trust Synopsys TCAD. Experiments will tell.
Equiv. PIN Detector,
150V bias
(We compare LGAD and PIN at same fluence to obtain a practical Gain Definition)

## Slide 24
Conclusions
LGAD model from CNM, with JTE, guard rings,
p-stops and c-stops.
The 300 mm device withstand radiation damage up to 1e14 neq/cm2, fails approaching 1e15 neq/cm2
Main fail mechanism: double junction
The 50 mm device withstand radiation damage
beyond 7e15 neq/cm2, moderate fail at 2e16 neq/cm2.
Could it be the solution?, Experiments will tell

## Slide 25
Thanks for your attention
fpalomo@us.es