## Slide 1
First measurements on “NitroSil” diodes
Alexander Dierlamm, Pawel Kamiński, Kevin Lauer, Alexander Lawerenz, Ralf Röder, Tobias Wittig
Image credit: Andre Holzner

## Slide 2: Introduction
The “NitroSil” project evaluates the improvement of radiation hardness of nitrogen doped silicon
Material:
  6mm x 6mm diodes made from n-type FZ, FZ:O and FZ:N wafers (300µm)
Irradiations are preformed at JSI (neutrons) and KIT (23MeV protons)
Here I concentrate on diodes irradiated and measured at KIT!

## Slide 3: Initial characterization
Currents < 1.5nA@250V
Ubreak > 400V
Ufd ~ 145V
FZ:N

## Slide 4: I vs. T
I vs. T might reveal off mid-gap defects generating current, if Eeff differs from 1.21eV
Deviation from linear slope at low T hints to surface currents on all materials
In general, Eeff higher than 1.21eV (~1.4eV)
  FZ:N shows largest Eeff of 1.48eV
Diode | U in V | E in eV
DR1610 | 150 | 1.37
DR1610 | 170 | 1.45
DR1610 | 200 | 1.18
DO1617 | 150 | 1.42
DO1617 | 170 | 1.41
DO1617 | 200 | 1.16
DN161 | 150 | 1.48
DN161 | 170 | 1.48
DN161 | 200 | 1.48
0°C
-20°C
+20°C
I~T2exp(-Eeff/(2 kB T))

## Slide 5: Irradiations
For the NitroSil project KIT irradiated 5 sets of up to 10 diodes with 23MeV protons
  Set 1 (5 diodes): 0.5x1014neq/cm²
  Set 2 (10 diodes): 1.0x1014neq/cm²
  Set 3 (10 diodes): 5.0x1014neq/cm²
  Set 4 (10 diodes): 1.0x1015neq/cm²
  Set 5 (10 diodes): 5.0x1015neq/cm² (1 irradiation session to come)
Irradiation was performed cold (<-20°C); practically no annealing

## Slide 6: Characterization after irradiation
Set 2: 1.0x1014neq/cm²
  Currents very similar (~1.5µA@150V)
    alpha: ~7.8x10-17 A/cm (guard ring floating, no annealing…)
  Ufd
    ~135V for FZ:N and FZ:O
    ~150V for FZ

## Slide 7: Characterization after irradiation
Set 3: 5.0x1014neq/cm²
  Currents very similar (~7.5µA@600V)
    alpha: ~7.8x10-17 A/cm (guard ring floating, no annealing…)
  Ufd
    ~700V for FZ:N and FZ:O
    ~640V for FZ

## Slide 8: TCT measurements
IR laser to extract CCE and compare among the different materials
In preparation…

## Slide 9: Summary and Outlook
Irradiated diodes of FZ, FZ:O and FZ:N material in hands
First measurements done
  Quality of diodes very good
  Differences in currents and full depletion voltages not large up to now
Next:
  Complete initial IV and CV measurements
  Add annealing steps
  Perform TCT measurements to extract CCE

## Slide 10: Acknowledgment
The studies were partially supported by the Polish Centre for Research and Development within the framework of the NitroSil project (ID: 208346) financed by the Program for Applied Research under Contract No. PBS2/A9/26/2014.

## Slide 11
Status “NitroStrip” Project
Alexander for the NitroStrip Collaboration
Image credit: Andre Holzner

## Slide 12: Introduction
“NitroStrip” is the extension of the “NitroSil” project, which studies the mitigation of radiation damage in silicon by introduction of nitrogen
“NitroSil” concentrated on production of FZ:N wafers, defect measurements which High-Resolution Photoinduced Transient Spectroscopy (HRPITS) and characterization of diodes
“NitroStrip” will perform charge collection measurements on strip sensors

## Slide 13: Status of “NitroStrip”
The RD50 Project “NitroStrip” has been approved!
n-type wafers (300µm) for sensor production are at D&T Microelectronics
  6x FZ
  6x FZ:N
  6x FZ:O (oxygenation of wafers finished at D&T)
  6x MCz
RD50-C masks with small modifications are used to mainly produce mini-strip sensors (80µm pitch, ~1cm length, 26 per wafer)
  masks are produced and ready to use
Production will start soon, but last ~3-4 months due to heavy load of production line and holiday period…

## Slide 14: “NitroStrip” activities
Activity | Institute | Leader
Mask design | CNM | G. Pellegrini
Oxygenation and processing | D&T Microelectronics | J. Rafi
Electrical characterization | CERN, UFR, UHH, KIT | S. Kühn
CC measurements | CERN, UFR, KIT | A. Dierlamm
TCT measurements | CERN, UHH, KIT | M. Moll
TSC measurements | UHH | E. Fretwurst
e-TCT measurements | CERN | M. Moll
Irradiations | KIT, CERN | A. Dierlamm
Estimated project costs: 26.5k€
Granted RD50 funds: 18.5k€

## Slide 15: Mask details
Metal strips with overhang (11µm)
Wider wire-bond pads (50µm)

## Slide 16: Oxygenation results
12h @1150ºC in O2 (Oxygenation) + 48h @1150ºC in N2 (Diffusion)
Resistivity reduced to ~50%
  Already observed previously
Before
After Oxygenation (-50%)
Microelectronics Reliability 40 (2000) 791±794

## Slide 17: Irradiation plans
Materials:
  FZ, FZ:N, FZ:O, MCz
  4x6 wafers: ~150 strip sensors and 120 diodes for each material
Fluences:
  1x1013 (diodes only for TSC,) 1x1014, 5x1014, 1x1015, 5x1015neq/cm²
Particles:
  25MeV protons (KIT)
  24 GeV protons (CERN)
  reactor neutrons (JSI)
  Co-60
Initial program:
  2 sensors (plus 2 diodes) each irradiated with single particle type
    Total: 4 x 4 x 4 x 2 = 128 sensors (1/4 of production)

## Slide 18: Measurements
Sensor characterization
  IV, CV on all
  Strip measurements on samples
Read out strip sensors with
  ALiBaVa setup
  Sr90 source
  @ -20°C
CC, cluster size, noise
  vs. voltage
  vs. annealing min. steps: initial, 2w@RT, 20w@RT
Min. program ~2 days per sensor!
ALiBaVa setup @ KIT
ALiBaVa setup @ KIT

## Slide 19: Outlook
Wafer production will start soon
Production time ~3-4 months
Initial characterizations in autumn
…

## Slide 20: spares

## Slide 21: Materials from Microelectronics Reliability 40 (2000) 791±794

## Slide 22: Reminder V distribution