## Slide 1
E-TCT measurements of irradiated HV-CMOS test structures
I. Mandić1, G. Kramberger1, V. Cindro1, A. Gorišek1, B. Hiti1, M. Mikuž1,2, M. Zavrtanik1, et al.
1Jožef Stefan Institute, Ljubljana, Slovenia
2Faculty of Mathematics and Physics, University of Ljubljana, Slovenia

## Slide 2
TCT measurements with HVCMOS structures made on different substrate
resistivities from different foundries:
AMS: 20 Ohm-cm
  G. Krambergeret al, Charge collection studies in irradiated
  HV-CMOS particle detectors, 2016 JINST11 P04007
  I. Perić et al. , Active pixel sensors in high-voltage CMOS
  technologies for ATLAS, 2012 JINST 7 C08002.
  ……..
X-FAB :100 Ohm-cm, Silicon On Insulator, SOI
  S. Fernandez-Perez et al., Charge collection properties of a depleted monolithic active pixel
  sensor using a HV-SOI process, 2016 JINST 11 C01063
  T. Hemperek et al, A Monolithic Active Pixel Sensor for ionizing
  radiation using a 180 nm HV-SOI process, NIMA 796(2015)8-12
LFoundry: 2000 Ohm-cm, with and without back plane processing
  Piotr RYMASZEWSKI et al., Prototype Active Silicon Sensor in 150nm HR-CMOS
  technology for ATLAS Inner Detector Upgrade, 2016 JINST 11 C02045
All devices are made on p-type substrates
These samples are being investigated as candidates for HV-CMOS detectors for trackers at HL-LHC
From: S. Fenandez-Perez, TWEPP 2015
Buried oxide
electronics

## Slide 3
Edge TCT
( more details: www.particluars.si )
HV
scope
GND
Substrate (p-type)
Pixels (n-well)
Beam direction
Detector connection scheme:
x
y
TCT measurements with passive pixels (no amplifier in the n-well)
 collecting electrode connected to amplifier

## Slide 4
CHESS1, not irraidated
Charge (25 ns), Bias = 120 V
Depth
Laser beam direction
Chip surface
Scan across pixel:
2.5 µm steps in y
5 µm steps in x
Edge-TCT
Charge:
integral of induced current pulse
Induced current after laser pulse

## Slide 5
Charge collection profile, AMS (20 Wcm)
Reactor neutrons, steps: 2e14, 5e14, 1e15, 2e15, 5e15, 1e16
Depth
Chip surface
Scan direction
charge collection width increases with fluence up to ~ 2e15 n/cm2
 initial acceptor removal
charge collection width falls with fluences above ~ 2e15 n/cm2
 initial acceptor removal finished, space charge concentration increases with irradiation
at 1e16 charge collection width still larger than before irradiation

## Slide 6
Charge collection profile, Xfab (100 Wcm)
Reactor neutrons, fluence steps: 2e14, 5e14, 1e15, 2e15, 5e15
large increase of charge collection region at lower fluence than AMS
at 5e15 charge collection region narrower than before irradiation, but still 40 µm at 300 V
chip surface

## Slide 7
Charge collection profile, LFoundry (2000 Wcm)
Reactor neutrons, fluence steps: 1e14, 5e14, 1e15, 2e15, 5e15
no increase of charge collection width after irradiation seen
no significant difference between samples with and without back plane (BP)

## Slide 8
LFoundry
Xfab
w0 and Neff free parameters
works for AMS and LFoundry
X-FAB: can’t fit with sqrt(Vbias)
estimate Neff from width at 300 V
AMS: large increase of width at low bias
Xfab: “knee” at low bias
0 width up to 100 V at 5e15
Fit:
Charge profile width vs. bias voltage
AMS chess1

## Slide 9
acceptor removal
Radiation introduced deep
acceptors: g ~ 0.02 cm-1
Nc,Neff0 and c free parameters, g fixed
Nef vs fluence
Fit:
LFoundry: no removal (Nc ~ 0), fit:
AMS and XFab:
Neff0 and g free
AMS
(CHESS and HV2FEI4)
from:
G. Kramberger et al.,
2016 JINST11 P04007

## Slide 10
 larger width than the largest after neutrons (at 2e15 n/cm2)
AMS CHESS1 chips (20 Wcm) irradiated with PS protons
24 GeV protons, 1 MeV eq. fluences : 3.3e14 n/cm2 and 4.6e14 n/cm2

## Slide 11
fit compatible with Neff ~ 2e13 cm-3
less than after ~2e15 n/cm2 reactor neutrons (Neff ~ 3e13 cm-3)
 faster initial acceptor removal
 large rise of profile width low bias
neutrons
Irradiation with PS protons
Very fast rise at
low bias voltage

## Slide 12
This work,
protons 80 V
E-TCT with HVCMOSv3, (AMS 180 nm, 10 Ohm-cm)
irradiated with PS protons and neutrons:
M. Fernandez, RD50 meeting, December 2015:
Larger depleted depth (lower Neff) at lower fluence than after neutron irradiation:
 larger acceptor removal constant c (and smaller gc ) after proton irradiation
 measurements in agreement with M. Fernandez et al.
Calculate depletion depth from Neff using:
Neutrons: c = 3e-15 cm2, gc = 0.02cm-1
Protons would fit c ~ 1e-14 cm2 or larger
Irradiation with PS protons
Bias = 120 V

## Slide 13
Acceptor removal
AMS (20 Ωcm, NA0 ~ 1015 cm-3): c ~ 4·10-15 cm2, Nc/Neff0 ~ 1, PS protons: c ~ 1·10-14 cm-2
X-FAB (100 Ωcm, NA0 ~ 1014 cm-3 ): c ~ 1.3·10-14 cm2, Nc/Neff0 <~ 1
LFoundry (2000 Ωcm, NA0 ~ 6·1012 cm-3 ), acceptor removal not observed in this study
 deep acceptor introduction rate comparable or faster than removal rate
 initial acceptor concentration low  difficult to observe reduction of a small value
 removal not complete Nc/Neff0 < 1 and/or small c to be observed in this measurement
Blue marker – charged hadron irradiated
Red marker – neutron irradiated
X-FAB, neutrons
G. Kramberger et al, 10th Trento Meeting, Feb. 17-19, 2015
AMS, PS protons
AMS, neutrons
c [cm2]

## Slide 14
Charge collection profile - annealing
Measurement before and after 80 minutes at 60 C
 10% to 20 % increase of charge collection width after annealing
Xfab
2e14
1e14
1e15
5e14
5e15
5e14
1e15
2e15
5e15
Lfoundry:
2e15

## Slide 15
Not irradiated
2e15
gaps before irradiation
guard ring gaps smaller after 2e15
gaps better seen again after 1e16
1e16
Beam
to HV and readout
(via Bias-T)
to ground
Scan across pixel array: AMS (20 Wcm)
Bias = 120 V, all 9 pixels connected to readout, charge (25 ns)
Chip surface
Depth

## Slide 16
BP, 40 V, Φ = 0
No BP, 40 V, Φ = 0
LFoundry, Structure F, all pixels read out
 no significant efficiency gaps between pixels
 no large difference between BP and no BP devices
Chip surface
Depth
Structure F, 3x3 pixels,
125 µm x 33 µm
Laser
BP, 5e15
No BP, 5e15

## Slide 17
2e14
Before irradiation
5e15
X-FAB: 100 Wcm, 4x4 pixel array, Bias = 300 V
HV
scope
HV
Buried oxide
Low charge
High charge
 gaps less evident after high fluence
Efficiency gaps between pixels after irradiation
 nuch smaller gaps at 500 ns integration
 carriers drift to the oxide between n-wells
 behaves as “parasitic AC coupled electrode”
 more detail showed at Trento workshop, Paris 2016:
https://indico.cern.ch/event/452766/contributions/1117348/

## Slide 18
Summary
Edge-TCT measurements with passive test structures made on 3 different substrate resistivities:
  AMS : 20 Ωcm, X-FAB: 100 Ωcm, LFoundry: 2000 Ωcm
   charge collection profiles measured up to 1e16 n/cm2
   significant charge collection width after highest fluence in all samples
AMS and X-FAB: large increase of charge collection width after irradiation with neutrons
dependence of charge collection width with fluence consistent with effective acceptor removal
 acceptor removal in X-FAB faster than in AMS  faster removal at larger initial resistivity
AMS: large increase of charge collection width after irradiation with PS protons
 increase larger and at lower fluence than for neutrons
 faster acceptor removal and smaller deep acceptor introduction rate
 fast increase of charge collection width, faster than sqrt(V) at low bias voltage (seen also after
neutron irradiation)
LFoundry: charge collection width decreases with increasing fluence
 introduction of deep acceptors faster than removal of initial acceptors
  removal not complete Nc/Neff0 < 1 and/or too slow
  compensated material? (donoros and acceptors removed at different rate  we only see the sum)
 no significant difference between samples with and without back plane contact
 no significant efficiency gaps between pixels
X-FAB: large efficiency gaps between pixels after irradiation (at 25 ns integration times)
   low efficiency between n-wells due to parasitic charge collection