## Slide 1: Frontier Applications of Metamaterials to Magnetic Confinement Fusion
F.A. Volpe
Columbia University, New York, NY
Presented at ICFDT5 – 5th International Conf. on Frontiers in Diagnostic Technologies, Frascati, Itay
October 4, 2018

## Slide 2: Plasmas and metamaterials have a long history of flirting with each other
Artificial dielectrics [Kock 1946] applied to plasma diagnostics in 1980-90’s (e.g. [Volpe-Laqua 2003] and refs. therein).
In plasmas and, at , , as later realized in metamaterials.
Similar to metamaterials, optical properties of plasma can be “engineered” by proper choice of , , , , and their gradients.
Pendry’s 1996 seminal work on metamaterials mentions ‘plasma’ and ‘plasmons’ 42 times.
Plasmons and magnetoplasmons reminiscent of plasma waves and Electron Bernstein Waves in plasmas

## Slide 3: Outline
Motivation
Reverse chromatic aberration
Metamaterial lens
Numerical opimization
Ink-jet manufacturing
Rapid frequency-controlled steering

## Slide 4: Example of special needs of plasma diagnostics that can be addressed by metamaterials
Electron Cyclotron Emission is microwave emission from gyrating electrons in magnetized plasmas
Important for temperature measurement
Emission at different frequencies f originates at different locations  Challenge for focusing:
focal length should vary dramatically (increase) with f
This “reverse” chromatic aberration cannot be obtained with convergent lenses of conventional materials.
It can be obtained with a metamaterial lens.

## Slide 5: High sensitivity of focus to f might find application in survey, satellite observations, directed energy.
If object to be detected/irradiated is
  Moving
  Non-monochromatic
And sensor/receiver is rapidly (electrically) tunable
Then rapid change of f  rapid change of focus
No moving parts in the optics

## Slide 6: Control of chromatic aberration at design stage and rapid inexpensive ink-jet manufacturing also have numerous applications
Reverse chromatic aberration lens can compensate for regular chromatic aberration of other lenses in optical system
Flat lens of zero chromatic aberration can be designed and manufactured by same methods
Ink-jet printing can be applied to RF IC circuits, antennas, magnetic sensors, etc.
It can allow rapid prototyping, manufacturing and customization to specific frequency, polarization, focus etc.

## Slide 7: What is “reverse” Chromatic Aberration?

## Slide 8: What is “reverse” Chromatic Aberration?

## Slide 9
Sandwiches of inductive and capacitive layers behave like LC transmission lines

## Slide 10: 2D array of LC filters imparting different Df behaves like a Fresnel lens

## Slide 11: 2D array of LC filters imparting different Df behaves like a Fresnel lens
Designed, built and testing a 7 zone RCA lens for 8-12 GHz.
Designed an 83 zone RCA lens for 80-130 GHz.

## Slide 12: Reverse Chromatic Aberration is obtained by imposing vast zone-to-zone variation of Df at low f and more uniform response at high f

## Slide 13: Geometrical dimensions can be analytically optimized to obtain desired Df(f) in each zone

## Slide 14: …or problem can be solved numerically
Single cell of dimensions D, w, g1, g2, etc. is modeled with finite element code (CST).
Transmittance T and phase-shift Df at various frequencies f1, f2, etc. are stored.
Calculation is repeated for various D, w, g1, g2, etc. Database is built.
For each zone, we pick D, w, g1, g2, etc. yielding best match between calculated T and Df and desired T and Df
Contours of Df(deg) at f=10GHz
(mm)
(mm)
(mm)

## Slide 15: Numerically optimized Df(f) matches desired Df(f) for RCA at f=8-12GHz
W.J. Capecchi et al., Optics Express 20, 8761 (2012)

## Slide 16: Database was also built for f=80-130 GHz (ECE at DIII-D)

## Slide 17: Relaxing constraints on absolute phase improves agreement with desired Df(f)
Only relative phase (zone-to-zone) matters
G=“Goal function” (the smaller the better)
K.C. Hammond et al., J Infrared Milli Terahz Waves 34, 437 (2013)

## Slide 18: Individual fine-tuning of geometrical parameters in each layer further improves the agreement

## Slide 19: Optimized cells put together and treated as attenuated and delayed dipole-emitters  Interference pattern  Global lens response

## Slide 20: Obtained desired RCA for maximum transverse resolution in ECE at at DIII-D. A single lens focuses different f at different locations where that f is EC-emitted.

## Slide 21: Sidelobes were explained with non-uniform transmissivity across zones  grating  diffraction maxima

## Slide 22: Simulations show that varying the lens aperture changes its focal length  a diaphragm acting as a zoom!

## Slide 23: EC-emitting locations are always in focus, with metamaterial lens. They are not in focus with present mirror.
B=-2.0T
B=-1.56T
EC-emitting locations
Regions of good focusing

## Slide 24: Ink-jet printing is capable of 1-5mm details
K. Takano et al., Applied Phys. Expr. 2010
Sjctechnology.com
Silver, lines: 3mm, spacing: 15mm
Gold, lines: 5mm, spacing: 50mm
Conventional printer CAD Super-fine Printer

## Slide 25: Low-power 8-12 GHz lens manufactured using an ink-jet printer and silver-nanoparticle ink
(show samples)
Ink = liquid suspension of ~5nm Ag nanoparticles
Resistivity 3mWcm after 1h sintering at 150-200oC (bulk Ag 1.6mWcm).
Printed circuit board (PCB) techniques (e.g., laser) also under consideration
80-130 GHz might require lithography, laser raster or integrated circuit (IC) nano/microfabrication techniques
Tests of 8-12 GHz lens starting soon

## Slide 26: Extension to high power requires modified design and materials
Some motivations:
  Tunable gyrotrons
  Rapid steering of ECCD for NTM stabilization w/o moving mirrors in vessel
  Collective Thomson Scattering
Simple! Replace:
  plastic dielectric  recirculating cooling fluid (freon FC-75)
  Square patches  stripes (2 sets, orthogonal)

## Slide 27: Frequency-controlled Steering
Same num. technique can be used:
  Prescribe Df(f) for each cell
  Different spatial profiles of Df(f)
“Super-diffractor”: diffraction grating of metamaterial-enhanced resolving power
High sensitivity to f important

## Slide 28: Conclusions
Proper array of microfabricated phase-shifters acts as a lens.
Optimizing its dimensions allows to match a desired dependence of focal length on frequency, including extreme and reverse chromatic aberration.
Numerical example for 8-12 and 80-130 GHz.
Lens for 8-12 GHz was manufactured by ink-jet printing (with silver nanoparticle ink) on dielectric substrate.
  Inexpensive, fast, suited for low-power, low-frequency.
  Alternatives at high-power and/or high-frequency were discussed.
Numerical technique can be extended to:
  aberration-free lens
  rapid frequency-controlled steering
With different designs and materials, manufacturing can be extended to high-power heating, current drive & active diagnostics.