## Slide 1: Fondazione Bruno Kessler Centre for Materials and Microsystems

## Slide 2
SiPM Technology at FBK
A. Gola, F. Acerbi, A. Ferri, A. Picciotto, C. Piemonte, G. Paternoster, G. Zappalà, N. Zorzi
gola@fbk.eu, piemonte@fbk.eu
IFD 2014 – Trento – March 11-13, 2014

## Slide 3
Original technology
FBK technology evolution
2006
RGB-SiPM
(Red-Green-Blue SiPM)
excellent breakdown voltage uniformity
low breakdown voltage temperature
dependence
higher efficiency
very low dark noise
2010-11
NUV-SiPM
(Near-UV SiPM)
excellent breakdown voltage uniformity
low breakdown voltage temperature
dependence
high efficiency in the near-ultraviolet
very low dark noise
2012
2012
RGB-SiPM HD
(Red-Green-Blue SiPM – high density)
small cell size with high fill factor
electric field
engineering
new cell
border
new
junction
IFD 2014 – Trento – March 11-13, 2014

## Slide 4
RGB-HD
high density
IFD 2014 – Trento – March 11-13, 2014

## Slide 5
Why small cells?
1. Lower correlated noise, because of lower gain (lower Cd):
- lower afterpulsing
- possibly lower direct and delayed Optical CT
- lower external Optical CT (with scintillator).
2. Larger linear dynamic range.
3. Faster recharge time.
- reduced pile-up
- useful with «slow» scintillators (CsI) for further extended dynamic range
All are important to optimize spectroscopic and timing
performance.
IFD 2014 – Trento – March 11-13, 2014

## Slide 6
We completely re-designed the cell border structure of the RGB technology to have small cells with high fill factor using trenches.
RGB-HD structure: L < 2 um (originally it was 7 um).
L is the dead border region around a cell
Difficult? Yes.
The Fill Factor (FF), also called geometrical efficiency, is the ratio:
New Technology
Old Technology
IFD 2014 – Trento – March 11-13, 2014

## Slide 7
RGB-HD optimal cell size
For a given border dead space, the choice of the optimal cell size is not obvious:
Larger cells provide higher Fill Factor (FF) and thus higher PDE.
Smaller cells reduce the correlated noise, which ultimately limits the over-voltage and thus the PDE.
We produced many cell sizes and characterized their performance experimentally.
(measurements are ongoing)
IFD 2014 – Trento – March 11-13, 2014

## Slide 8
RGB-HD Layouts
All are much smaller than the traditional 50 um (67 um) cells!
Very good linearity!
High Fill Factor
IFD 2014 – Trento – March 11-13, 2014

## Slide 9
Photo Detection Efficiency (PDE)
30 um cell
Without correlated noise!
RGB SiPM technology:
Peak PDE in the blue/green
IFD 2014 – Trento – March 11-13, 2014

## Slide 10
Photo Detection Efficiency
591 nm
(without correlated noise)
Larger cells and FF, same technology
IFD 2014 – Trento – March 11-13, 2014

## Slide 11
Gain
Smaller cells
Old Technology
IFD 2014 – Trento – March 11-13, 2014

## Slide 12
Excess Charge Factor (ECF)
The ECF can be considered an upper bound for the Excess Noise Factor.
Smaller cells
IFD 2014 – Trento – March 11-13, 2014

## Slide 13
PDE/ECF
Quantifies the worsening of the Poisson statistics due to the photo-detector  “effective” PDE
591 nm
At high VOV, smaller cells are more efficient than larger ones due to ENF
IFD 2014 – Trento – March 11-13, 2014

## Slide 14
VBD Uniformity and Temp. Stability
Breakdown voltage (VBD)
uniformity
Breakdown voltage variations with T
ΔG/G < 1%/°C is possible!
Gain temperature stability
VBD variations <  150 mV inside the wafer and between wafers.
Important at the system-level
IFD 2014 – Trento – March 11-13, 2014

## Slide 15
Temperature dependence of DCR
Arrhenius plot of SiPM reverse current
20 um cell
4 VOV
Fast DCR reduction with T
≈ Eg/2
Electric Field Engineering for
low band-to-band tunneling
IFD 2014 – Trento – March 11-13, 2014

## Slide 16
Signal Shape
Very fast single cell response (SCR)
Response to fast light
pulse from LED
t = 9ns
15 um cell
Response to LYSO (511keV)
t = 43ns
Thanks to the fast SCR, the LYSO decay time constant is preserved.
IFD 2014 – Trento – March 11-13, 2014

## Slide 17
Radiation Damage in SiPMs
The main effects of radiation damage, in SiPMs, are:
Increase in the primary noise (DCR).
Increased afterpulsing (increased number of traps).
PDE loss due to cells busy with dark counts.
Increased power consumption due to higher DCR.
Mitigation of the effects of rad. damage with RGB-HD:
E field engineering allows a steeper reduction of DCR with cooling.
Low gain reduces afterpulsing (for a given number of traps).
Many, smaller cells with faster recharge are less sensitive to the phenomenon.
Lower gain means less current (for a given DCR).

## Slide 18
Measurements after Irradiation
Measurements carried out by Y. Musienko and A. Heering @CERN, with a dose of 1012 n/cm2.
After irradiation:
Dark current increased up to 450 μA
Gain*PDE change is < 10%
PDE change is < 10%
ENC(50ns gate) ~ 20 p.e. RMS
Noise increase
PDE loss
Parameters measured at VOV=2.7 V (PDE(515 nm)=15%)
IFD 2014 – Trento – March 11-13, 2014

## Slide 19
Thank you!

## Slide 20
Timing Resolution (hints)
FWHM ≈ 20 ps!
Single photon time resolution
10 um SPAD
Time resolution vs. number of photons
1x1 mm2 SiPM – 50 um cell
30 ps FWHM
~1/sqrt(N)
Measurements on older RGB-SiPM technology at 23 °C.