## Slide 1: Brazing, Copperplating, Vacuum Design
C. Roncolato

## Slide 2: Vacuum Brazing

## Slide 3: Physical Issues
Brazing does not involve any substantial melting of the base metals
Maintain closer assembly tolerances and to produce a cosmetically neater joint without costly secondary operations.
Brazing makes it possible to join dissimilar metals (or metals to ceramics). Therefore, steel can be brazed to copper as easily as to another steel.
Brazing also generally produces less thermally induced distortion. An entire part can be brought up to the same brazing temperature.
Brazing readily lends itself to mass-production techniques. In fact, given the proper clearance conditions and heat, a brazed joint tends to make itself and is not dependent on operator skill, as are most fusion welding processes.
As a rule, the HAZ produced during brazing is wider and less sharply defined than those resulting from other fusion-related processes.
Main Features:

## Slide 4: Brazing Filler Metal (BFM)
 | Ag | Pd | Cu | Tsol | Tliq
 | % | % | % | °C | °C
Palcusil 10 | 58 | 10 | 32 | 824 | 852
Palcusil 5 | 68 | 5 | 27 | 807 | 810
Cusil | 72 | 0 | 28 | 780 | 780
Three different alloys can be used to joint parts in several steps.
The amount of Palladium determines the eutectic temperature and the joint performances.
Ternary Phase Diagram for Cu-Ag-Pd

## Slide 5: Technological Issues
Electrode
Base
Water Channel
Water Connection Plug

## Slide 6: Welding Analysis
Copper
Stainless Steel
Voids
BFM
BFM
The Brazing Filler Metal (BFM) is positioned in the grooves.
After the melting for capillarity flows in the joint gaps, leaving a holes.
In red are shown some points for measurements

## Slide 7: Eutethic Phase Formation
Point 1 with 200x
Point 1 with 830x
This redistribution is accomplished by atomic diffusion. The microstructure of the solid that results from this transformation consists of alternating layers or zones of the Ag and Cu phases that form simultaneously during the transformation. This microstructure is called a eutectic structure.

## Slide 8: EDAX Analysis
Cu
Ag
Pd
Fe
Ni
Cr
It is possible to show where the chemical elements are positioned in the joints. Selective scanning are taken, while measuring a particular x-ray emission energy.

## Slide 9: Effect of Cleaning Process
BEFORE
AFTER

## Slide 10: Copper Plating

## Slide 11: Physical Issue
Electroplating
Buffer Layer
Substrate
Layer
Material
Copper
Nickel / Copper
Stainless Steel AISI 316L / Mild Steel
Thickness
x3÷x4 skin depth = 30 mm
2÷4 nm
≈ 50 mm
 | Frequency | Skin Depth
SPES | 80 MHz | 7.38 mm
r (resistivity) = 1.72 mW-cm

## Slide 12: Experience at CERN (substrate is AISI 316L) 1/3
Ultrasonic Degreasing
detergent NGL 17.40 spec. ALU III: 10 gm/lt
temperature: 50 – 60°C
time: 30 – 120 minutes
frequency: 25 kHz
Cathodic Cleaning
Detergent: Cleanor GL 301: 80 gm/lt
Temperature: 30 - 35°C
Voltage: 5 – 8 V, current density: 5 – 7 A/dm2
Time: 30 – 60 s
Small Parts
Jet rinsing, followed by dipping in water.

## Slide 13: Experience at CERN (substrate is AISI 316L) 2/3
Jet rinsing, followed by dipping in water.
Anodic Etching
Sulfuric acid 20% v/v
Temperature: Ambient (20°C)
Voltage: 5 – 6 V
Time: 10 – 15 sec.
Jet rinsing, followed by dipping in water.
Activation
Cloridric Acid 50% v/v
Temperature: Ambient (20°C)
Time: 5 sec.
Small Parts
No rinsing, afterwards! Nickel plating strightaway
Power Supply
+ −
−
+
+
Heater
Sample (Cathode)
Anode(Nickel)
Movement
Nickel Plating (Wood’s Bath)
Nickel Cloride: 300 gm/lt
Boric Acid : 30 gm/lt
Cloridric Acid : 50 ml/lt
Temperature: 50°C
Voltage: 1.5 – 3.5 V
Current Density: 4 – 10 A/dm2
Time: 1-2 min (pari a 3-5 mm)

## Slide 14: Experience at CERN (substrate is AISI 316L) 2/3
Jet rinsing, followed by dipping in water.
Small Parts
Copper Plating
Copper Sulfate CuSO4 • 5 H2O: 75 g/l
Solforic Acid (conc.): 100 ml/l
Cloride: 0.075 g/l
Voltage: 1.5 – 3.5 V
Temperature: 20-30°C
Current Density: 2 A/dm2
Time: 75 minuti (pari a 30 mm)
Air blowing for mixing
Bath is filtered

## Slide 15: Experience at CERN (substrate is AISI 316L) 2/3
Small Parts
Jet rinsing, followed by dipping in water and cathode removal
Deoxidize
Cloridric Acid 50% v/v
Temperature: Ambient (20°C)
Time: 10-20 sec.
Jet rinsing, followed by dipping in water
Copper Passivation
Jet rinsing, followed by dipping in water
Ultrasonic cleaning in demineralized water
Rinsing with ethyl alcohol folloed by drying with nitrogen

## Slide 16: Calculations

## Slide 17: Experience with Nichel Plating at LNL w/ «First» External company
AISI 316LN
Nickel Plating
scratch test
Scratch test parameters
Type : Progressive
Begin Load (N) : 0
End Load (N) : 30
Loading rate (N/min) : 60
Speed (mm/min) : 13.62
Length (mm) : 7
AESensitivity : 5

## Slide 18: SEM Imaging after scratch test. Head diameter 100mm
Plastic deformation of the film with cracks

## Slide 19: SEM Imaging after scratch test. Head diameter 50mm
Film is already cracked. Cracks are through all the thickness
The smaller head creates a deeper groove. Part of the films are removed generating flakes.

## Slide 20: Chemical Analysis with EDS a 20kV
Chart: Canale
The Nickel plating seems to be contaminated with Zinc.
Principio EDS
Tempo acquisizione = 42s

## Slide 21: Deposition from the «second» Company
SEM Imaging after scratch test. Head diameter 100mm

## Slide 22: SEM Imaging after scratch test. Head diameter 50mm

## Slide 23: Thickness Calibration
2.5mm
Chart: Deposition Time [min]
| 15 | 20 | 25 | 30
 | 2.5 | 3.5 | 4 | 5
6.25 min/mm

## Slide 24: Chemical Analysis with EDS
12 kV
20 kV

## Slide 25: Coppert Plating Analysis (1/2)
Chart: Deposition Rate
| 18 | 36 | 54 | 72 | 90
 | 8.783 | 23.4117 | 30.9017 | 40.4745 | 54.6465
J = 2.7 A/dm2
The actual thickness of the deposit on the plates were measured with a profile meter. The plates are masked in a way to have a “sharp” step between the Cu layer and the substrate.
The interpolation shows the current density.

## Slide 26: Coppert Plating Analysis (2/2)
EDS Principle
Copperplating is free of other elements (1% range)

## Slide 27: Scratch Test & SEM analysis
Micro Scratch Test with head of 100μm

## Slide 28: Scratch Test & SEM analysis
Micro Scratch Test with head of 50μm

## Slide 29: EDAX Scan Analysis

## Slide 30: Other example of copper plating

## Slide 31: Electroplating Recipe
Buffer layer is made of copper

## Slide 32: Problem with plating
Choose a proper
Curvature Radius
Solution?
Reversing
Solution?

## Slide 33: Quality Assurance
Outgassing Rate Test
Preparation for testing
The requirement to performance an “Outgassing Rate Test” will be specified prior to manufacture by the VG.
The total out-gassing rate of a vessel or assembly shall be measured after 10 hours of pumping from atmosphere. The measured outgassing rate shall be <10-10mbar l/s cm2.
A hydrocarbon free dry pumping unit and a Residual Gas Analyser (RGA) must be used for these tests.
Testing Requirements
The mass spectrum over the mass range of 1-100 u is to be recorded after 10 hours of pumping from atmosphere.
The “hydrocarbon” content, recorded by the RGA, must not exceed 10% of the maximum allowable outgassing rate.
This can be calculated by summing all the hydrocarbon peak heights >40 u and expressing them as a fraction of the total peak height. From the total measured outgassing rate.
The outgassing rate due to hydrocarbon (HC) is to be calculated as follows:
Hydrocarbon outgassing (%) = Sum of HC peaks / sum of all peaks x measured outgassing rate
Peaks at 17, 18, 28 and 40 u are deemed to be non-hydrocarbon.

## Slide 34: RFQ tank for SPES
Mechanical Specifications:
no. 6 tanks
FInt = 754 mm
Length ≈1150 mm
Weight 990 kg (approx)
General Requirements:
Operating Pressure < 1x10-8mbar
Cleanliness from dust particles and oil
Limited Vibration
No Maintenance

## Slide 35: Back-of-The-Envelope Calculation