## Slide 1: Development of CdTe Pixel Detectors combined with Aluminum Schottky sensor and Photon-Counting ASICs
H. Toyokawa1, C. Saji1, M. Kawase1, S. Wu1, Y. Furukawa1, K. Kajiwara1, K. Osaka1, M. Sato1, T. Hirono2, A. Shiro3, T. Shobu3, A. Suenaga4, H. Ikeda5
1Japan Synchrotron Radiation Research Institute, 2Universitaet Bonn,
3Japan Atomic Energy Agency,
4Howa Sangyo Co., Ltd., 5Japan Aerospace Exploration Agency
H. Toyokawa, PIXEL2016, Sestri Levante, Italy, 5-9 Sep. 2016

## Slide 2: Overview
Motivation and Design Concepts
SP8-04F10K detector
  Threshold trimming
  Bias voltage
  Long term stability
  Laue diffraction measurements
  Large area detector
Summary and outlook

## Slide 3
March 2012
SACLA (XFEL) 8 GeV Linac
SPring-8
8 GeV Storage Ring
Oct. 1997
We have been developing 2D-type high energy X-ray detectors combined with CdTe Schottky diode sensors and photon-counting readout ASICs in use for synchrotron radiation experiments.
H. Toyokawa, PIXEL2016, Sestri Levante, Italy, 5-9 Sep. 2016

## Slide 4: Pixelated sensor structures
 | CdTe | CZT | Ge | Si
density (g/cm3) | 5.85 | ~5.8 | 5.33 | 2.33
atomic number | 48, 52 | 48, 30, 52 | 32 | 14
band gap energy (eV) | 1.44 | ~1.65 | 0.67 | 1.12
Ionization energy (eV) | 4.43 | ~5.0 | 2.96 | 3.62
resistivity (Ωcm) | 109 | 109~1011 | 3900 | 1400
μe (cm2/V・s) | 1100 | 1000 | 3900 | 1400
μh (cm2/V・s) | 100 | 50~80 | 1900 | 480
τe (s) | 3×10-6 | 3×10-6 | >10-3 | >10-3
τh (s) | 2×10-6 | 10-6 | 1×10-3 | 2×10-3
Chart: Detection Efficiency
| 0 | 5 | 10 | 15 | 20 | 25 | 30 | 35 | 40 | 45 | 50 | 55 | 60 | 65 | 70 | 75 | 80 | 85 | 90 | 95 | 100 | 150 | 200
CdTe 750μm | 1 | 1 | 1 | 1 | 0.99999 | 0.99814 | 1 | 1 | 0.99998 | 0.99959 | 0.99723 | 0.98951 | 0.9727 | 0.94486 | 0.90647 | 0.85983 | 0.80794 | 0.75367 | 0.69937 | 0.64673 | 0.59684 | 0.28025 | 0.16203
Si 320μm | 1 | 1 | 0.92308 | 0.53477 | 0.27777 | 0.15686 | 0.097985 | 0.06685 | 0.049049 | 0.038175 | 0.031157 | 0.026412 | 0.023075 | 0.020647 | 0.018827 | 0.017427 | 0.016325 | 0.015439 | 0.014713 | 0.014108 | 0.013596 | 0.010861 | 0.0096024
Si 450μm | 1 | 1 | 0.97287 | 0.65908 | 0.36721 | 0.21332 | 0.13499 | 0.092714 | 0.068281 | 0.053264 | 0.043535 | 0.036941 | 0.032296 | 0.028912 | 0.026374 | 0.02442 | 0.022881 | 0.021642 | 0.020628 | 0.019783 | 0.019067 | 0.015239 | 0.013477
Si 1mm | 1 | 1 | 0.99967 | 0.90849 | 0.6383 | 0.41327 | 0.27549 | 0.19444 | 0.14544 | 0.11453 | 0.094179 | 0.080243 | 0.070355 | 0.063116 | 0.057666 | 0.053458 | 0.050136 | 0.047459 | 0.045263 | 0.04343 | 0.041878 | 0.033549 | 0.029702
Ge 750μm | 1 | 1 | 1 | 1 | 1 | 0.99989 | 0.99569 | 0.97055 | 0.91069 | 0.82309 | 0.72436 | 0.62793 | 0.54094 | 0.46586 | 0.40256 | 0.34982 | 0.30606 | 0.26977 | 0.23958 | 0.21437 | 0.19321 | 0.09388 | 0.043604
Pt
Al
h
e-
ASIC
X-ray
- Bias voltage
Pt/CdTe/Al-pixel
CdTe sensor is generally fabricated with a metal/CdTe/metal structure.
We have investigated Pt/CdTe/Al-pixel configuration by using high resistivity p-type CdTe wafers 750 μm in thickness.
This configuration has the advantage of providing a high Schottky barrier formed on the Al/CdTe interface, and, hence, a benefit to operate the CdTe as an electron-collecting pixelated diode.

## Slide 5: Upgrade to SP8-04 ASIC
 | SP8-01 | SP8-02 | SP8-02B | SP8-03 | SP8-04 (final)
pixel size (μm2) | 200 × 200 |  |  |  | 
format | 16 × 16 | 20 × 50 |  |  | 20 × 50 A1K 20 × 100 W2K 95 × 50 L5K 95 × 100 F10K
preamp | high / low gain |  |  | tunable gain | 
comparator | upper / lower |  |  | upper/lower×3 | 
counter | 20 bits |  |  | 24 bits | 
process | 0.25 μm (TSMC) |  |  | 0.18 μm (TSMC) | 
 | Cybershuttle |  |  |  | Full wafer run
2010
SP8-01
16×16 pixels
2011
SP8-02
20×50 pixels
2012
SP8-02B (optimized ASIC)
20×50, 41×50 pixels
2013
SP8-03 (3-window comp.)
20×50 pixels

## Slide 6: Bump-bonding
SP8-01, 02, 02B, 03
SP8-04
Au-stud bonding
Bi-Sn solder bonding

## Slide 7: SP8-04F10K single chip detector
Thickness : 750μm
Pixel size : 200μm2
Format : 95×100

## Slide 8: Threshold scan (W fluorescence, untrim)
Total counts
Pixel (20,65)
Threshold dispersion Kα edge
Thr = -90 mV
Kα

## Slide 9: Threshold scan (W fluorescence, trimed)
Total counts
Pixel (29,60)
Thr = -90 mV
Kα
Threshold dispersion Kα edge

## Slide 10: Depletion voltages (W theshold scan)
-50 => -400 V
-400 => -600 V

## Slide 11: Comparison of CdTe and Si detector
CdTe
PILATUS
CeO2 diffraction pattern and line profile at 70 keV

## Slide 12: Water-cooled detector

## Slide 13: Stability measurement @ 20 degrees
0.6%
Pb fluorescence
Temperature = 20 degrees
HV = 500V
Threshold = -90 mV
Lower threshold scan
10 sec
10 min

## Slide 14: Micro white-Xay Laue diffraction
Experimental setup with Al sample

## Slide 15: Energy measurement with comparator scan
Comparator threshold
Experimental setup with Al sample

## Slide 16: Grain boundary imaging with SP8-02B
white x-rays
10×10μm2
silicon steel plate
40×30 positions
0.25mm steps

## Slide 17: 2 × 2 single-board detector

## Slide 18: 2 × 2 ASICs large area detector
CdTe
190 × 200
pixels
SP8-04 F10K
95×100
pixels
4 cm
3.8 cm

## Slide 19: Summary and Outlook
We have been developing 2D high energy X-ray detectors combined with CdTe Schottky diode sensors and photon-counting readout ASICs in use for synchrotron radiation experiments.
SP8-04 ASICs have been processed with TSMC 180 nm technology and F10K ASIC single-chip detector could function as designed.
2 x 2 ASICs large area detector has been newly developed and performances are investigated currently.
2-side buttable design could achieved 8cm x 8cm area detector.
For going to further large are detector, 4-side buttable module will be designed next step.

## Slide 20
Thank you for your attention!
H. Toyokawa, PIXEL2016, Sestri Levante, Italy, 5-9 Sep. 2016