## Slide 1: A novel Transient-Current-Technique based on the Two- Photon-Absorption process for the characterization of the HV-CMOS deep n-well
PIXELS 2016, September 5th, 2016
M. Fernández1, J. González1, R. Jaramillo1, M. Moll2, R. Montero3, F. R. Palomo4, I. Vila1
1Instituto de Física de Cantabria (CSIC-UC)
2CERN
3Universidad del Pais Vasco (UPV-EHU)
4Universidad de Sevilla (US)

## Slide 2: Transient-Technique Basics
Study of transient current of laser-generated non-equilibrium carriers provides information of many internal diode’s characteristics: space-charge geometry, trapping times, CCE, mobility,...
Capital tool for the understanding of the detector’s radiation tolerance
From G. Kramberger, Advanced TCT systems, Vertex 2014
Notes: Time resolved measurement of the current induced the transient of the non-equilibrium carriers created by a laser pulse.
Mainstream tool for the radiation tolerance assessment.
Edge-TCT configuration as tool for mapping the electric field
Laser light is injected through the edge of the sensor and the current induced in a microstrip on top of the laser beam focus is measured

## Slide 3: Transient-Current Technique Basics (2)
Ideally, a TCT technique with non-equilibrium free carriers generation in a very localized volume (micrometric-scale voxel) should allow the best E field mapping and geometry determination of the semiconductor junctions with very small size features of the new generation of position-sensitive-detectors
Let’s see what non-linear optics can do for us…
Notes: Limitation – electron-hole generate along the whole laser optical path (proportional to the laser intensity)

## Slide 4: Two-Photo-Absorption Process in Semiconductors 101
Predicted in 1931 by
Maria Goppert-Mayer
1963 Nobel Prize in Physics
In fluorescent molecules, two photon pumping was demonstrated by Webb et al in 1990.
Notes: Single-photon
Virtual electronic states with a very short lifetime with energy level within the bandgap

## Slide 5: Two-Photo-Absorption Process in Semiconductors 101 (2)
TPA-TCT is a way to generate very localized electron-hole pairs in semiconductor devices (microscale volume).
TPA-TCT simplifies the arrangement to inject light into the device and the unfolding of the device internal Electric field and other relevant parameters of the theoretical model.
"A picture is worth a thousand words”
Notes: Bottom microscope objective single photon absorption is possible.
top

## Slide 6: TPA-eTCT on a HV-CMOS: Set-up

## Slide 7: TPA-eTCT on a HV-CMOS: Set-up (2)
Analog readout of of the laser-induced signal collected by deep N-Well (no on-chip amplification)
Notes: Study of the radiation tolerance of a HV-CMOS charge collecting juntion, the deep n-well (buried n-in-p diode)
Measuring the analogue current out to the n electrode. Edge injection.

## Slide 8: TPA-eTCT: Charge Collection Efficiency.
Fast transient current ( 1ns) to estimate the E field.
TPA provides a much better “E field” mapping resolution than Single-Photon Absorption.
TPA
SPA
Notes: Raster scan to map in a plane parallel to the device edge - mapping the value of the charge at 1ns
Potato shape.

## Slide 9: TPA-eTCT: Collection Time (95% signal)
Distinct waveform shape depending on zone of illumination.
  Drift region: fast
  Diffusion region: slow
  At the implant double peak observed in the waveform (two contributions one for drift and another from diffusion).
Diffusion region
Drift region
Implant region

## Slide 10: TPA-eTCT: Depletion depth vs Vbias
Doping estimation (resistivity) Assuming abrupt n-in-p junction.

## Slide 11: TPA-eTCT: Implant depth (along Z)

## Slide 12: TPA-eTCT: Neutron Irradiated HV-CMOS
7×1015 neq/cm2 (Caveat: high leakage current 620 mA @50 V)
VERY PRELIMINARY
Dedicated TPA-eTCT characterization campaign going on this week on irradiated
HV-CMOS samples.

## Slide 13: Other possible (exclusive) application
First sub-bandgap laser-induced signals in diamond detectors.
3D diamond detector provided by A. Oh (U. Manchester)
Quick and simple test.

## Slide 14: Summary
Development of a TPA based TCT technique validated both on non-irradiated and irradiated sensors.
Localized charge carrier generation: High-resolution 3D mapping of the charge collecting junction and simpler unfolding of sensor’s performance characteristics.
First distinct determination of the deep n-well on HV-CMOS devices and precise determination of its sensitive volume and resistivity
New opportunities: dedicated studies on diamond sensors, active-edge pixels, signal amplification junctions, …

## Slide 15: Thank you !
F. Rogelio et al, Two Photon Absorption and carrier generation in semiconductors
https://indico.cern.ch/event/334251/contributions/780784/
I. Vila et al, A novel Transient Current Technique based on the Two Photon Absorption (TPA) process
https://indico.cern.ch/event/334251/contributions/780782/
I. Vila et al, Investigation on the radiation resistance of HV-CMOS and pin diodes using a Transient Current Technique based on the Two-Photon-Absortion Process
https://indico.cern.ch/event/452766/contributions/1117347/
M. Fernández et al, High-resolution three-dimensional imaging of a depleted CMOS sensor using an edge Transient Current Technique based on the Two Photon Absorption process (TPA-eTCT)
(http://www.sciencedirect.com/science/article/pii/S0168900216304569).