## Slide 1
Wafers available
 | Purchased | Used | Available
DWB 100 um | 25 | 3 (planar) + 4 (3D) | 18
DWB 130 um | 30 | 6 (planar) + 11 (3D) | 13
SOI 100 um +5e14 B/cm2 back implant | 15 | 1 (SRP) | 14
SOI 130 um +5e14 B/cm2 back implant | 15 | 1 (SRP) | 14

## Slide 2: Some considerations
Three batches still to go:
  1st PAE (2015-2016)
  2nd 3D (2016-2017)
  2nd PAE (2016-2017)
Due to deep Boron diffusion, SOI option not so interesting for 3D sensors
I would go with more SiSi DWB of 130 um thickness and maybe another thickness (to be chosen)