## Slide 1: Stato dell’analisi dei test su fascio
Vannuccini Elena
On behalf of the Florence group

## Slide 2: Sommario test su fascio
Feb 2013  Test su fascio all’SPS del CERN
  (Pb+Be)  Ioni A/Z=2 @13-30 GeV/u
  Prima versione del prototipo 14 piani
Lug 2014  Test su fascio di elettroni alla BTF di Frascati
  Elettroni multipli 1500  400300 MeV
  Studio del regime di transizione di CASIS tra alto e basso guadagno e della dipendenza della risposta dalla tempistica del segnale
Feb 2015  Test su fascio all’SPS del CERN
  (Ar+Polyethylene)  Ioni A/Z=2 @19-30 GeV/u
  Upgrade: cristalli schermati per eliminare cross-talk ottico + 15° piano equipaggiato con «cristalleria»
Aug/Sep 2015  Test su fascio all’SPS del CERN
  Elettroni, muoni e adroni fino a 350 GeV
  Upgrade: rivestimento cristalli ottimizzato (vikuiti) e implementazione PD di piccola superficie (basso guadagno)

## Slide 3: Feb2013  Single crystal signal
All events
Not-interacting 4He
4He
2H
Test 2013
Pb+Be
30 GeV/u
hig gain | low gain
Signal of the first crystal along the beam direction
log(ADC counts)
Hit  5RN cut

## Slide 4: Feb2013  Ionization signal –vs– Z2
O
|
F
|
Ne
|
|
Cl
O
|
F
|
Ne
|
|
Na
Ionization signal
Cross-talk signal
Equilized ADC counts
Equilized ADC counts
Linear fit from He to O
Linear fit from Na to Cl
Na
|
Non-linearity in scintillator response to high-Z ions
Non-linear behaviour for higher Z  not instrumental but physical effect
Courtesy of Pisa/Siena group

## Slide 5: Feb2013  Ionization signal –vs– Z2
17%
discrepancy
 Central crystal (gaussian fit)
 Total over layer
MC tuning:
14% optical cross talk  to match cube/layer signal ratio for C
4.5% additional gaussian spread to single-crystal signal  to match ionization-signal spread
Not-interacting ions
30.0GeV/u
(2013 test)
Discrepancy between beam-test and MC data
Prototype calibrated with He
MC normalized to MIP

## Slide 6: Feb2013  Showers: beam-test –vs– MC data
Beam test
MC
+1%
-5%
+5%
-3%

## Slide 7: Feb2013  Showers: energy resolution –vs– A
Showers starting on layer 3
 Beam test 2013
 MC
12.8 GeV/n
30 GeV/n

## Slide 8: Feb2013  Beam-test –vs– MC data
 Beam-test
 MC
12.8 GeV/n
30.0 GeV/n
Beam test
MC
+4%
-10%
+6%
-14%

## Slide 9: Feb2013  Energy resolution –vs– A
 Beam test 2013
 MC
Showers starting on layer 1
12.8 GeV/n
30 GeV/n

## Slide 10: Feb2013  conclusions
First prototype exposed to ions of total energy ranging between  202000 GeV (DFe)
Study of detector response to ionization energy deposits
  Non-linear Z2 dependency found
Study of shower classification and energy resolution
  MC tuned on 2013 data  agreement MC/data within 15%
  Difficulty in MC tuning due to optical cross-talk

## Slide 11: The Feb-2015 setup
Assembly
  CsI(Tl) cubes 3.6 cm side
    diffusive (Teflon tape) wrapping
    + absorber layer (Tedlar film) to shield optical cross-talk
  3314 elements (0.4 cm gap)
    1.5 RM containment
    active depth 27 X01.3 lI
  Spare 33 layer with test crystals
Sensors
  VTH2090H PDs
    Active area 84.6 mm2  0.3 A/W @550 nm
FE electronics
  CASIS
Teflon wrapping
+
black Tedlar film

## Slide 12: The Feb-2015 setup
BEAM TRACKER (BT)
4 Si-pixel matrixes + 8 Si-strip layers
CALORIMETER
3314 CsI:Tl crystals
SPARE PLATE
33 test crystals
ION
BEAM
ION
BEAM
FRONT exposure
BACK exposure

## Slide 13: Feb2015  Single crystal signal
All events
Not-interacting 4He
4He
2H
Test 2015
Ar+Polyethylene
30GeV/u
hig gain | low gain
log(ADC counts)
Signal of the first crystal along the beam direction
Hit  5RN cut

## Slide 14: Feb2015  Calibration
Scan of 33 column with ion beam
  FRONT + BACK exposure
Iterative selection of not-interacting He (standalone calorimeter)
  Events with interacting ions accepted up to 1-layer before interaction point
  First iteration  topological selection (cube-to-layer fraction > 90%)
  Second iteration  + charge selection (signal  MP1.5SIG)

## Slide 15: Front exposure
Candidate He event
Accepted up to layer 11
0
1
2
3
4
5
6
7
8
9
10
11
12
13
14

## Slide 16: Front exposure
Candidate He event
Accepted up to layer 5
0
1
2
3
4
5
6
7
8
9
10
11
12
13
14

## Slide 17: Front exposure
Candidate D
Accepted up to layer 3
0
1
2
3
4
5
6
7
8
9
10
11
12
13
14

## Slide 18: Back exposure
Candidate He event
Accepted up to layer 8
0
1
2
3
4
5
6
7
8
9
10
11
12
13
14

## Slide 19: Front exposure
Heavy ion (Ar? Si?)
Accepted up to layer 5
0
1
2
3
4
5
6
7
8
9
10
11
12
13
14

## Slide 20: Back exposure
Heavy ion (Ar? Si?)
Accepted up to layer 11
0
1
2
3
4
5
6
7
8
9
10
11
12
13
14

## Slide 21: Feb2015  Calibration parameters
19 GeV/u front ~ 1050
30 GeV/u front ~ 974
30 GeV/u back ~ 1069

## Slide 22: Calibration parameters (2013)
Gain dispersion ~14%
Gain +50%

## Slide 23: Maximum gain
19 GeV/u (front)

## Slide 24: Minimum gain
19 GeV/u (front)

## Slide 25: Maximum statistics (@first layer)
19 GeV/u (front)

## Slide 26: Minimu statistics (n.entries>1000)
19 GeV/u (front)

## Slide 27: Feb2015  Parameter comparison
19 GeV/u
front
30 GeV/u
front
30 GeV/u
back
Weighted ratios:
1.019
1.004
1.028

## Slide 28: Feb2015  Statistical errors
19 GeV/u front
30 GeV/u front
30 GeV/u back

## Slide 30: 19 GeV/u front –vs– 30 GeV/u front

## Slide 31: Gain dispersion
(Spare plane with test crystals)
CsI(Tl) with diffusive+reflective wrapping (Teflon+Vikuiti)
RMS  21%
Merging of front&back data-set @30 GeV/u
Crystal responses equalized by normalizing to 4MIP the ionization energy deposit of 4He (@peak)
2015 
Lower signal and larger dispersion due to absorber wrapping
ADC counts
Feb2013
1510
Feb 2015
1050
(preliminary)

## Slide 32: 2013 –vs– 2015 prototype
33.8%
33.5%
preliminary
(Z-tagging from first calorimeter layer )
beam-test 2015
beam-test 2013
Showers starting on layer 2
He @ 30.0 GeV/n

## Slide 33: Test of scintillating materials
Test of 9 scintillating materials
  CsI:Na, CsI:Tl, YAG:Ce, BaF2, YAP:Ce, LuAG:Ce, BSO, BGO, LYSO:Ce
  Teflon+Vikuiti+Tedlar wrapping
Z-tagging from BT+CAL
Study of the ionization signal –vs– Z2
BEAM TRACKER (BT)
4 Si-pixel matrixes + 8 Si-strip layers
CALORIMETER
3314 CsI:Tl crystals
SPARE PLANE
33 test crystals
ION
BEAM

## Slide 34: «Cristalleria»
 | Density (g/cm3) | l (cm) | X0 (cm) | l/X0 | RM (cm) | Cube side (cm) @ 2t | Total n.int.lengths @ 2t | Total n.rad.lengths @ 2t | W.L. max. emission (nm) | D.time (ns) | L.Y. (%) @300K |  | Cherenkov | L.Y.*VTH2090 Sp.Res. / W.L.max | ... * RM/16.1
CaF2:Eu | 3,18 | 34 | 3,1 | 11 | 3,7 | 86 | 2,5 | 28 | 435 | 940 | 50 | Scionix |  | 25,3 | 18,4
CsI | 4,5 | 40 | 1,9 | 21 | 3,6 | 76 | 1,9 | 41 | 310 | 10 | 5 | DETEC | ? | 1,6 | 1,6
CsI:Na | 4,5 | 40 | 1,9 | 21 | 3,6 | 76 | 1,9 | 41 | 420 | 630 | 88 | DETEC | ? | 43,0 | 43,0
CsI:Tl | 4,5 | 40 | 1,9 | 21 | 3,6 | 76 | 1,9 | 41 | 550 | 1250 | 165 | DETEC |  | 100 | 99,8
YAG:Ce | 4,57 | 25 | 3,5 | 7 | 2,8 | 76 | 3,0 | 22 | 550 | 70 | 40 | Crytur | ? | 24,2 | 19,5
BaF2 | 4,89 | 31 | 2,0 | 15 | 3,1 | 74 | 2,4 | 37 | 300 | 630 | 36 | Scionix |  | 10,5 | 9,9
YAP:Ce | 5,5 | 22 | 2,7 | 8 | 2,4 | 71 | 3,3 | 26 | 370 | 27 | 47 | Scionix |  | 19,9 | 16,3
LuAG:Ce | 6,73 | 21 | 1,5 | 14 | 2,2 | 67 | 3,3 | 46 | 535 | 70 | 20 | Crytur |  | 11,9 | 11,0
BSO | 6,8 | 22 | 1,1 | 20 | 2,2 | 67 | 3,0 | 60 | 480 | 100 | 6 | MolTech |  | 3,3 | 3,0
BGO | 7,13 | 23 | 1,1 | 20 | 2,2 | 65 | 2,9 | 58 | 480 | 300 | 21 | CERN |  | 11,6 | 11,4
LYSO:Ce | 7,4 | 21 | 1,1 | 19 | 2,1 | 65 | 3,1 | 59 | 402 | 40 | 85 | Cinesi |  | 39,7 | 37,8
PWO | 8,3 | 21 | 0,9 | 23 | 2,0 | 62 | 3,0 | 70 | 425 | 5 | 0,3 | MolTech |  | 0,1 | 0,1

## Slide 35: Segnali attesi
Z  | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8
CaF2:Eu | 18 | 74 | 166 | 295 | 461 | 664 | 904 | 1181
CsI | 2 | 6 | 14 | 25 | 39 | 56 | 77 | 100
CsI:Na | 43 | 172 | 387 | 687 | 1074 | 1546 | 2105 | 2749
CsI:Tl | 100 | 399 | 898 | 1596 | 2494 | 3592 | 4889 | 6386
YAG:Ce | 19 | 78 | 175 | 312 | 487 | 701 | 954 | 1246
BaF2 | 10 | 40 | 89 | 159 | 248 | 357 | 486 | 634
YAP:Ce | 16 | 65 | 146 | 260 | 407 | 586 | 798 | 1042
LuAG:Ce | 11 | 44 | 99 | 175 | 274 | 394 | 537 | 701
BSO | 3 | 12 | 27 | 49 | 76 | 110 | 149 | 195
BGO | 11 | 46 | 103 | 183 | 286 | 411 | 560 | 731
LYSO:Ce | 38 | 151 | 340 | 604 | 944 | 1360 | 1851 | 2417
PWO | 0 | 0 | 1 | 1 | 2 | 3 | 4 | 5
Segnale di ionizzazione atteso (% del CsI:Tl), tenendo conto della risposta spettrale del PD, della LY, delle dimensioni e della densità del cristallo, in funzione dello ione.
CsI(Tl)  S/N>10 @mip (CERN 2013)
Evidenziati gli ioni dai quali ci si aspetta un segnale rivelabile (S/N>5)
X
X
X
X
X
X
X
X
X

## Slide 36: Signals
CsI:Na
CsI:Tl
YAG:Ce
BaF2
YAP:Ce
LuAG:Ce
BGO
LYSO
All events
Non-interacting He

## Slide 37: Crystals
 | Expected |  | Measured |  |  | 
 | Z=1 (a.u.) | Z=2 (a.u.) | Z=2 (ADC counts) | Relative width | Norm. @CsI:Tl (a.u.) | Measured/Expected
CsI:Na | 43 | 172 | 1336 | 8,3% | 229 | 1,3
CsI:Tl | 100 | 399 | 2330 | 7,6% | 399 | 1,0
YAG:Ce | 19 | 78 | 642 | 9,4% | 110 | 1,4
BaF2 | 10 | 40 | 95 | 14,6% | 16 | 0,4
YAP:Ce | 16 | 65 | 316 | 13,7% | 54 | 0,8
LuAG:Ce | 11 | 44 | 674 | 9,1% | 115 | 2,6
BSO | 3 | 12 | - | - | - | -
BGO | 11 | 46 | 312 | 13,4% | 53 | 1,2
LYSO:Ce | 38 | 151 | 759 | 7,6% | 130 | 0,9
(preliminary)
LuAG
YAP

## Slide 38: Next steps
Implementation of BT information, under progress
Shower analysis:
  Comparison of energy resolution for individual ions with Feb2013 results
  Tuning of MC model (no OCT) and comparison with beam-test data
Test crystals:
  Study of ionization signal with Z-tag given by BT