## Slide 1: WP13 – JRA 1
Status of the innovative gas detectors work package WP13
Silvia Dalla Torre, Imad Laktineh

## Slide 2: DELIVERABLES

## Slide 3: MILESTONES
MS13.8
A report is already ready. It will be soon submitted

## Slide 4
WP13-2-1
Establishing new resistive materials for high rate RPCs
-Low resistivity materials like HPL, Glass, Ceramics are inventoried. New materials are developed.
-Their resistivity (bulk, surface) and homogeneity are studied as well as their ageing properties due to large integrated doses.
RPC built a new plastic (peek doped with CB)
Detector with electrodes made of Ceramics
Detectors made of low-resistivity glass exposed to GIF++ source and SPS beam
Si3N4/SiC

## Slide 5
WP13-2-2
Fast timing, high rate large RPC
New PCB with pick-up strips read from
both sides. This allows to determine Y:
Y= L/2-v*(t2-t1)/2.
resolution can be measured:
(t1+t2)- L/v
Excellent time resolution thanks to
the PETIROC ASIC, the Tsinghua TDC and
well matched strips of the PCB: 20-30 ps
The PCB will be inserted in between two gaps
of one large RPC.
20-30 ps
32 strips of 3 mm width
(4 mm pitch)
Return strips outside
the detector
petiroc
Tsinghua
TDC
50 cm
Test points
Large 2-gap chambers are built using small plates of low-resistivity glass
Gluing method
Fixation method

## Slide 6
WP13-2-3
High rate and fine space resolution RPCs operated with eco-gases
New “ecological” gases for RPC to replace the high GWP (R134A and SF6) currently used. HFO is a good candidate but could not be used as the only gas, at least for the RPCs currently used. R134A is still needed. Helium could help to reduce the streamer component. Many mixtures are being tested.
Streamer probability
HV
New gap layout
50 x 100 cm2
1 mm gas gap
1.2 mm electrode
new FE Board
2D readout
Resistive electrode :
1011 W . cm
Exposure to GIF++
infinite
100
33
10
3

## Slide 7
WP13-4-1
Large RPC detector preserving mechanical precision
Development of integrated mechanical support and Faraday cage for large-area thin RPC chambers for future collider detectors and development of mechanical assembly procedures and tools for large-scale production.
Drawings of the Faraday cage and mechanical support are ready
Triplet of new RPCs with 1mm gas gap
support frame and Faraday cage with
only 48 mm overall thickness.
First module to be built and tested in 2016
INFN activity

## Slide 8
WP13-4-6
Preparation for large RPC series production
Construction of large size RPC using different kind of electrodes : HPL, Glass
Definition and developing of common tools for QC & QA procedures are under preparation at CERN. This is crucial to guarantee uniformity on each detectors components
Large Bakelite RPC chamber with thinner electrodes and gas gap than those currently used in CMS
Large Glass RPC built from small pieces of low resistivity glass
INFN activity

## Slide 9
WP13.2.4
The µ-RWELL performance: Beam Tests
the µ-RWELL detector
tracking
efficiency
vs resistivity
Ar/ISO=90/10
Ar/ISO=90/10
At low resistivity the spread of the charge (cluster size) on the readout strips increases, thus requiring a higher gain to reach the full detector efficiency.
Resistive stage
segmentation in
preparation: next step
INFN activity

## Slide 10
WP13.2.5
DISCHARGE STUDIES IN THGEMs
In parallel: polishing protocol to increase THGEM production yield
Hybrid Detector
(2 THGEMs + Micromesh)
Chart: Pressure X Gap in Torr-Inch
| 2.8585099999999999E-2 | 5.9146600000000001E-2 | 0.117537 | 0.18329799999999999 | 0.28585100000000002 | 0.59146600000000005 | 1.17537 | 1.8329800000000001 | 3.0990500000000001 | 6.1584799999999982 | 11.7537 | 17.604099999999999 | 29.763500000000001 | 59.146600000000007 | 122.38200000000001 | 176.041 | 309.90499999999992
 | 4052.61 | 674.108 | 410.449 | 366.046 | 380.286 | 426.417 | 624.569 | 727.576 | 987.359 | 1446.18 | 2467.55 | 3102.51 | 5095.45 | 8055.22 | 15411.5 | 20914.2 | 37073.3
TOOL: the phenomenological Paschen curve
The breakdown V vs P, electrode distance and specific gas
THGEM
Paschen measurements
Correlation between the Paschen measurements and the discharge rates
Before polishing
MAX V: 1390 V
After polishing
MAX V: 2180 V
INFN activity

## Slide 11
WP13.3.1
Interfacing FE-chips specific to gas detectors to the Scalable Read-out System (SRS)
New design from A. Rusu
Design of the new SRS Hybrid with wire bonding finalized.
Interfacing VMM2 /VMM3
SRS Readout Electronics for
VMM 128 (laboratory setup)
Intermediate Interface CARD (keeping the AGH hybrid)
Final Hybrid
First Step
GEMROC
+
Integration of TIMEPIX3 starting now
VMM

## Slide 12
WP13.3.2
Development of cheap, standard MPGD dedicated laboratory instruments
 | Task 13.3.2
Deliverable [M24] | High Voltage Power Supply for MPGD
 | (Floating) Pico ammeter
 | Signal Processing
 | Monitoring and Control Unit
 | Regeneration Gas System
AVD (Active Voltage Divider)
Suitable for multistage MPGDs
FemtoBox: femto-ammeter et al.
APIC: Charge Preamplifier – Shaper Amplifier Chain
CERN
Chips commercially available
INFN activity

## Slide 13
WP13.3.3
Development of a general purpose readout electronics for MPGDs
Test set –up for the
MultiChip Module (MCM)
Adaptor board
Top side
Bottom side
Upper surface
of adaptor
board with
mounted
SALTRO-chip
(12 x 8.9 mm2)
Carrier Board ok but some problems related to soldering.

## Slide 14
WP13.4.2
Resistive anode Micromegas
Production by silk screen printing
The machine and associated equipment, are also used for other WP13 activities :
Tests on about 30 glass plates, combining
  3 pastes : RS 12115 (100 kΩ/sq) , RS 12116 1 MΩ/sq + bi component from IN2P3
  3 glasses : Leroy-Merlin 2 mm, IN2P3, « chinese » 1 mm thick
  Several baking temperatures around 200 °C during 4 hours
Resistivity meas. on Carbon-Loaded Kapton with a circular probe and with the strip method.

## Slide 15
WP13.4.3
Control of foil/micromesh mechanical tensioning by optical inspection
Moire’ interferometry for large area surfaces:
Phase shift algorithm double n. of fringes, lowers noise enhances contrast: fraction of fringe can be appreciated
WITH PHASESHIFT
W/T PHASESHIFT
+-30um RESOLUTION
MILESTONE 13.8 - M12
Report ready
FBG sensors embedded
in MPGD detectors
INFN activity

## Slide 16
WP13.4.4
LEOPARD scanning system for THGEMs/GEMs
Small size prototype of optical / gain scanning, high resolution
DAQ with RPi
Position resolution:
FWHM = 60 mm
INFN activity

## Slide 17
WP13.4.5
Design of an automatic system to ensure the electrical integrity of electrode patterns by pulse reflection method
A quality assurance test setup
    Time Domain Reflectometer Method
    FPGA implementation
Objectives: cost-effective, flexibility, modular, fast, precise
EXAMPLE:
2D readout geometry
EXAMPLE:
2D readout geometry
ISSUE: Temperature stability:
  The only reliable method is to put one TDC/channel
INFN activity

## Slide 18
WP13.4.7
MPGD detectors to industry
2D RESISTIVE MICROMEGAS
Area of 50 x 50 cm2
2D readout with resistive anodes
Bulk technique
Industrial transfert to Elvia
On-going production (Elvia/Cern) of 16 detectors
QA/QC and follow up of the production will be setup
THGEM INDUSTRIAL TRNSFER
THGEM prototypes: (LEMs from WA105)
  10x10 cm2, thickness 1 mm
  Hole pitch 800 µm and diameter 500 µm
  Rim 40 µm (micro-etching)
  Techno transfer to Elvia (4 protos)
THGEM for COMPASS RICH produced by ELTOS
30x60 cm2, thickness 0.4 mm
  Hole pitch 800 µm and diameter 400 µm, no rim

## Slide 19
Conclusions
A lot of activities in the different subtasks
Increasing synergy among the different groups
New groups are joining the activities
First milestones and deliverables are expected to be on time