## Slide 1
DANE-L end stations
of interest for the CERN-LNF collaboration
R. Larciprete
CNR-Istituto del Sistemi Complessi, Roma
e
LNF-INFN Frascati
Meeting CERN-LNF , Frascati 14/10/16

## Slide 2
Experimental hall
XUV1
60-1000 eV
XUV2
30-200 eV
Meeting CERN-LNF
R. Larciprete

## Slide 3
Material Science Laboratory @ INFN-LNF
ultra high vacuum systems
background pressure 1x10-10 mbar
Meeting CERN-LNF
R. Larciprete
small area (1x1 cm2) sample

## Slide 4
Material Science Laboratory @ INFN-LNF
main chamber
preparation
chamber
fast-entry lock
Meeting CERN-LNF
R. Larciprete

## Slide 5
secondary electron yield
Material Science Laboratory @ INFN-LNF
Meeting CERN-LNF
R. Larciprete

## Slide 6
Technical samples and
atomically clean surfaces
SEY measurements
Equipment : Electron gun, Faraday cup
Meeting CERN-LNF
R. Larciprete
R. Cimino et al. Phys. Rev. ST 18, 051002 (2015)

## Slide 7
Technical samples and
atomically clean surfaces
SEY measurements
Equipment : Electron gun, Faraday cup, cryostat
Low-energy SEY
R. Cimino et al. Phys. Rev. ST 18, 051002 (2015)
Meeting CERN-LNF
R. Larciprete

## Slide 8
Technical samples and
atomically clean surfaces
SEY measurements
Equipment : Electron gun, Faraday cup, cryostat
Low-energy SEY
R. Cimino et al. Phys. Rev. ST 18, 051002 (2015)
LA Gonzales et al. AIP Adv. 6, 095117 (2016)
Meeting CERN-LNF
R. Larciprete

## Slide 9
Technical samples and
atomically clean surfaces
SEY measurements
Equipment : Electron gun, Faraday cup, cryostat
Low-energy SEY
R. Cimino et al. Phys. Rev. ST 18, 051002 (2015)
LA Gonzales et al. AIP Adv. 6, 095117 (2016)
Meeting CERN-LNF
R. Larciprete

## Slide 10
secondary electron yield
Material Science Laboratory @ INFN-LNF
10 K closed-cycle refrigerator
Meeting CERN-LNF
R. Larciprete

## Slide 11
Technical samples and
atomically clean surfaces
SEY measurements
Equipment : Electron gun, Faraday cup, cryostat
Low-energy SEY
Low-temperature SEY
R. Cimino et al. Phys. Rev. ST 18, 051002 (2015)
LA Gonzales et al. AIP Adv. 6, 095117 (2016)
15
Ar
Cu
Meeting CERN-LNF
R. Larciprete

## Slide 12
SEY measurements at 10 K
Meeting CERN-LNF
R. Larciprete
Ar
Cu

## Slide 13
SEY vs. thermal desorption
Meeting CERN-LNF
R. Larciprete

## Slide 14
X-ray photoeletron
spectroscopy
UV photoeletron
spectroscopy
secondary electron yield
Material Science Laboratory @ INFN-LNF
Meeting CERN-LNF
R. Larciprete

## Slide 15
electron
analyzer
KE: kinetic energy
BE: binding energy
φ: work function
KE=hv-BE-φ
XUV1 exp. station
AlK (1486 eV) and MgK (1253 eV)
HeI (21.2 eV) and HeII (40.8 eV)
Electron energy analyser
X-ray and UV Photoelectron Spectroscopy
XPS and UPS
XUV1 exp. station
HeI (21.2 eV) and HeII (40.8 eV)
Monochromatized
Angle resolved electron energy analyser
Angle Resolved
PhotoElectron Spectroscopy ARPES
Photoelectron spectroscopy @ LNF
Meeting CERN-LNF
R. Larciprete

## Slide 16
Cu 3p3/2
C1s
O1s
oxide
metal
C-O
C-C sp3
C-H
O-C
O-Cu
R. Larciprete et al. Phys. Rev. ST 16, 011002 (2012)
R. Cimino et al. Phys. Rev. Lett. 109, 064801 (2012)
Surface characterization by XPS and SEY
Meeting CERN-LNF
R. Larciprete

## Slide 17
C1s
O1s
C-O
C-C
C-H
O-C
O-Cu
Cu 3p3/2
oxide
metal
E=500 eV
I=5A
Q=1.2x10-3 C/mm2
R. Larciprete et al. Phys. Rev. ST 16, 011002 (2012)
R. Cimino et al. Phys. Rev. Lett. 109, 064801 (2012)
Surface characterization by XPS and SEY
Meeting CERN-LNF
R. Larciprete

## Slide 18
C1s
O1s
C-O
C-C
C-H
O-C
O-Cu
Cu 3p3/2
oxide
metal
E=500 eV
I=5A
Q=1.2x10-3 C/mm2
R. Larciprete et al. Phys. Rev. ST 16, 011002 (2012)
R. Cimino et al. Phys. Rev. Lett. 109, 064801 (2012)
Surface characterization by XPS and SEY
Meeting CERN-LNF
R. Larciprete

## Slide 19
X-ray photoeletron
spectroscopy
UV photoeletron
spectroscopy
secondary electron yield
Material Science Laboratory @ INFN-LNF
material growth
Meeting CERN-LNF
R. Larciprete

## Slide 20
Larciprete et al. Appl. Surf. Sci 328, 356 (2015)
SEY vs. graphitization for a-C films
RF magnetron sputtering 50W p(Ar) 6x10-2 mbar
a-C (~ 20 nm)/ poly Cu
SEY
Meeting CERN-LNF
R. Larciprete

## Slide 21
SEY vs. graphitization for a-C films
Larciprete et al. Appl. Surf. Sci 328, 356 (2015)
Meeting CERN-LNF
R. Larciprete

## Slide 22
P
3-zone furnace Tmax 1200°C
Quartz Tube
Gas inlet
Vacuum
Pressure
Controller
Tube furnace for material growth
Meeting CERN-LNF
R. Larciprete

## Slide 23
CH4 + H2+Ar
gas phase precursors
S0lid precursors
S + MoO3 powder
Graphene monolayers on Cu foils
MoS2 mono and multi-layers on
Si and SiO2 substrates
High pressure material growth
Controlled annealing processes of large scale samples
Meeting CERN-LNF
R. Larciprete
Tube furnace for material growth

## Slide 24
Material Science Laboratory @ INFN-LNF
2D band
Raman microscope
Raman image
optical image
scanning tunneling/atomic force
microscope STM/AFM
Meeting CERN-LNF
R. Larciprete

## Slide 25
Material tests and characterization
(in UHV: SEY, XPS, UPS, STM/AFM; in air: Raman)
In UHV:
Radiation (electrons, photons, ions) induced surface modification
Thermal programmed desorption (combined with XPS)
Photon induced desorption (conventional sources)
Film growth for SEY optimization
In the tube furnace:
High pressure material growth
Controlled annealing processes of ‘large’ scale samples
With the DANE beam available:
X-ray beam induced surface chemistry
X-ray beam induced desorption
Feasible experimental activity
Meeting CERN-LNF
R. Larciprete

## Slide 26
PhD students, post-doc and associated collaborators
Mario Commisso
Davide Remo Grosso
Roberto Flammini
Luis Gonzales
Antonio Di Trolio
Alessandra Di Gaspare
Marco Angelucci
Eliana La Francesca
Tecnical staff of DANE-L
Antonio Grilli
Marco Pietropaoli
Agostino Raco
Giacomo Viviani
Vittorio Sciarra
Vinicio Tullio
Meeting CERN-LNF
R. Larciprete
People

## Slide 27
Collaborations
CNR Istituto dei sistemi Complessi
IMM
IFN
ENEA - Frascati
UNI Napoli
Uni Luis
Sin generali che con Garfield
CNR
ENEA
UNI
Thanks for your attention!