## Slide 1: Status Report ALICE ITS @ LNF
Federico Ronchetti, INFN-LNF
ALICE ITS Meeting 25/10/2016
Schedule
Welding tests ----------------------
Assembly Report (Emiliano)
Quark Matter 2018
News from the ALICE CB (Valeria)

## Slide 2
Bari for MOSAIC Eleuterio, Marco T, Pavel
Bari for Glass Dummies Daniele, Marco T.
Full Mechanical Stave Alignment w/ Stefania Beole’
Vitrinite Dummies to start Module Alignment

## Slide 3
Full Mechanical Stave Alignment w/ Stefania Beole’
ITSU Plenary

## Slide 4
Leica MZ6 binocular microscope:
FoV: 50°
Real FoV: 10 50 mm
Hand supports
Vacuum rail
Working height
Soldering machine:
METCAL MX-PS5000 with
MX-H2-UF handpiece

## Slide 5: Raw setup in our lab (2)
Home-made tool to block the bridge

## Slide 6
Solder wires used:
  Metaux Blancs Ouvres (MBO): Sn63Pb37 ø=0.35 mm T= 183˚C
  RS 756-8907 : Sn60Pb40 ø=0.38 mm T= 183-188˚C
  EDSYN : Sn62Pb36Ag2 ø=0.35 mm T= 183˚C
  LOCTITE C51196SC :Cu95.5Ag3.5 ø=0.23 mm T= 217˚C
Tips used ( all T=412˚C)
  UFTC-7CNB04 (ø=0.4 mm) (Tip 04)
  UFTC-7CN02 (ø=0.2 mm) (Tip 02)
  UFTC-7CN01 (ø=0.1 mm) (Tip 01)
Solder wire and tip details

## Slide 7
Soldering quality evaluation
Electrical test (ET): measure bridge resistance with multimeter before stripping
Mechanical test (MT): visual inspection of each pad after stripping
Example
ET=bad, MT=bad (1 fail)
ET=good, MT=bad (2 fails)
ET=good, MT=bad (1 fail)
ET=good, MT=good

## Slide 8
LNF: Soldering quality evaluation
LNF

## Slide 9
LNF: Tests with fluxing liquid
LNF

## Slide 10
Test with tip 02 - EDSYN – tip deoxidizer Y/N (stripping)
i - No Deox
l - No Deox
m - No Deox
n - No Deox
o - Yes Deox
p - Yes Deox
q - Yes Deox
r - Yes Deox
Tot ET fails = 0, Tot MT fails = 4
Tot ET fails = 0, Tot MT fails = 0

## Slide 11
  Best tip : UFTC-7CN02 (ø=0.2 mm) (Tip 02)
  Best solder wire: EDSYN (Sn62Pb36Ag2 ø=0.35 mm T= 183˚C)
  Best tip cleaning technique: using solder tip deoxidizer
  Note: remember to position the bridge with the trace between the pads on the bottom side. (This guarantee a faster and better soldering of the bridge)
  Remove hole from bottom pad
  Make slimmer bridge with half hole to allow “soldering knee” as suggested by Luciano
  Redesign of test structures ongoing in TO
  More tests and tooling ongoing at LNF
Conclusions (TO + LNF)