## Slide 1: GIF++ 2016
Ezio Torassa
(INFN Padova)
TOP Italy meeting November 29th 2016

## Slide 2: Belle II GIF++ test August 2015
Lens/Fiber Distance Rad measured Rad estimation
source - fiber from 26/8 to 1/9 from 26/8 to 1/9
Position 1 1.5 m 1.75 Gray
Position 2 3.2 m 0.53 Gray
Position 3 5.8 m 0.12 Gray 0.12 Gray

## Slide 3: Belle II GIF++ test August 2015
Fiber transparency
Wavelength (nm)
Attenuation @1.8 Gray: 28%
Lens transparency
Attenuation @ 400 nm and 1.8 Gray: 7%
Lens producer:
Attenuation @ 400 nm and 10 Gray: 17%

## Slide 4: Belle II GIF++ test November 2016
1
2
3
4
Z distance:
1: 0.46 m
2: 2.15 m
3: 3.05 m
4: 5.25 m
Z
X

## Slide 5: Position of samples
1
2
3
4
Z = 0.46 m
X = 0 m
q = 0o
Z = 2.15 m
X = 1 m
q = 25o
Z = 3.05 m
X = -1 m
q = -18o
Z = 0.46 m
X = 0 m
q = 0o
Due to the presence of angular correction filters the intensity of the radiation decreases with a factor 1/z2 in spite of 1/r2

## Slide 6: Radiation dose
Radiation dose:
1: 340 Gray
2: 15.6 Gray
3: 7.7 Gray
4: 2.6 Gray
Radiation measured in position 1: 340 Gray
( integrated from Nov. 16th to Nov. 22° 2016 )

## Slide 7: Radiation dose errors
Position 1:
The radiation was measured, the error is due to the different position between sensor, lens and fiber roll.
1 cm difference = 5% error for the radiation
The radiation was extrapolated with the factor 1/z2.
In locations with the same absolute value of the z-coordinate, the measured dose rates at various x positions differ up to 20%. (arXiv:1611.00299v1)
Position 2,3,4:
Radiation dose:
1: (340 ± 17) Gray
2: (15.6 ± 3.1) Gray
3: (7.7 ± 1.5) Gray
4: (2.6 ± 0.5) Gray

## Slide 8: Backup

## Slide 9: Rad hardness test (neutrons)
In the backward region of the TOP detector the expected radiation flux is:
1010 neutrons/cm2/year =
2.54 108 neutrons/lens/year
(section of the lens: 0.0254 cm2)
2.54 1011
10%
LNL June 2015
2H+ beam, Be target
A neutron ux 103 times larger than expected will produce a transparency reduction of 10%.
Numerical aperture not affected by neytron flux
(lens 12 not irradiated, lens 1 higher flux