## Slide 1
LOW SECONDARY EMISSION SURFACES
FOR MULTIPACTOR SUPPRESSION IN SPACE
G. Troncoso, C. Morales, V.C. Nistor, L.A. González, L. Galán, L. Soriano
Grupo de Recubrimientos, Intercaras y Nanoestructuras (GRIN)
Departamento de Física Aplicada and
Instituto de Ciencia de Materiales “Nicolás Cabrera”
Universidad Autónoma de Madrid
Madrid, Spain

## Slide 2
Background for anti-multipactor coatings in space
Coatings proposed fo.r the M-ERA.net project
Other studies for the M-ERA Net project
Acknowledgments
Anti-multipactor materials and coatings
OUTLINE

## Slide 3
High-power RF equipment in communication space satellites
High-energy particle accelerators
Magnetically confined fusion apparatus
High-power RF vacuum devices (klystrons and others)
and may become destructive (Corona discharge) if outgassing is produced
For mitigation, it is always necessary to decrease SEY in critical parts
Electron cloud and Multipactor discharge affect severely normal operation of:
ELECTRON CLOUD AND MULTIPCTOR

## Slide 4
In the central part of the wave-guide, in the reduced gap, the electric field is maximum, as it is the multipactor susceptibility.
Multipactor in space is mainly produced by the acceleration of electrons by the RF electric field in the wave guides.
MULTIPACTOR IN SPACE
The accelerated electrons impinge the wave-guide walls creating more electrons by secondary emission, thus generating a cascade resulting in an electron cloud
Internal volume space of a multipactor sample: reduced height gap transformer waveguide, WR75 12 GHz. The waveguide is split in two halves In order to facilitate the surface treatment of internal space

## Slide 5
In critical conditions, the electrons impinge the wave-guide surface and more electrons are ejected by secondary emission
MULTIPACTOR IN SPACE
secondary emission
UV light
wave guide
wave guide
electromagnetic field
exponential growth of electron cloud
electron trajectory
second mode multipactor discharge

## Slide 6
In order to have only one parameter to define the goodness (low SEY) of a surface, the parameter E1/ σmax is defined
The secondary emission yield coefficient determines the number of emerging electrons per incident electron
SECONDARY EMISSION YIELD (SEY)
The most important parameters for SEY are:
E1= Cross over energy
σmax = max value of the SEY coefficient
Em = Energy for the maximum SEY value

## Slide 7
Effect of SEY in Multipactor power level
Simulation results with MEST
multipactor power threshold increases 8 & 12 dB
by nanostructuring Cu surface
SEY AND MULTIPACTOR

## Slide 8
SEY AND MULTIPACTOR FOR ALODINE:
SIMULATION AND EXPERIMENT
Good agreement experiment-simulation

## Slide 9
1) low SEY to avoid multipactor
Requirements for anti-multipactor coatings:
ANTIMULTIPACTOR COATINGS
2) low RF surface resistance to avoid insertion losses
3) inertness, stable under exposure to the air, slow aging
4) practical deposition techniques and surface treatments
5) good adhesion
(3) is critical in space applications because no in situ conditioning is possible
(1) and (2) are becoming more demanding

## Slide 10
Suitable surface material:
Best materials: do not deteriorate in air (aging)
aging increases SEY and decreases conductivity
have high conductivity
Good materials : Alodine, graphite, TiN, Au, Ag, …
SEY can be reduced by:
Suitable surface morphology:
high-density high-aspect-ratio pores or roughness
might increase surface RF resistance (skin effect)
however SEY reduction due only to shape of roughness
surface; RF resistance due to size and shape
it is possible to reduce resistance reducing the size
SEY REDUCTION
Best a combined approach!

## Slide 11
RF currents are superficial, thus surfaces require good conductivity
SKIN EFFECT: Why size of roughness has to be reduced?
Skin depth:
o(Ag) = 0.58 m
1(Au) = 0.69 m
f = 12 GHz
 = rms roughness
IL of Au-coated grooved Ag relative to flat Ag
Numerical approximate results
Goal
Excess of roughness leads to increase of surface resistance

## Slide 12
Reference anti-multipactor coatings for space applications. Multipactor
Approximate experimental reference data from ESTEC - ESA
Device bulk material
Electrolytic Ag plating
Chromate conversion coating
Multipactor power level increase: 1.8 & 3.0 dB
ECSS-E-20-01A
ANTIMULTIPACTOR COATINGS

## Slide 13
Reference anti-multipactor coatings for space applications. Roughness
Electrolytic Au plating
Surface morphology
SEM
ANTIMULTIPACTOR COATINGS

## Slide 14
Reference anti-multipactor coatings for space applications. Roughness
Electrolytic Ag plating
Surface morphology
SEM
ANTIMULTIPACTOR COATINGS

## Slide 15
Reference anti-multipactor coatings for space applications. Roughness
Alodine
Surface morphology
SEM
Composition:
Al oxides and hydroxides (~ 98 %)
Cr oxides and hydroxides (~ 1 %)
Compounds of Al, Cr, O, N, C, Cu,
Zn, Mn, Ca, Ti, Si
Cr 6+
ANTIMULTIPACTOR COATINGS

## Slide 16
INSERTION LOSSES
Reference anti-multipactor coatings for space applications. Insertion Loss
Relative IL and RF surface resistance at 9.5 GHz
Silver 1
Gold 1.24
Alodine 3.8
For a waveguide, insertion loss IL = 10·log(Pthruout/Pin) depends on geometry, frequency f, and surface resistance Rsurf .
IL  Rsurf

## Slide 17
AGING
Reference anti-multipactor coatings for space applications. Aging
Notes: 17

## Slide 18
Aluminum alloy
device bulk
Silver
Nickel (P)
Gold
10 μm
Conductive
2 μm
Adherence
Roughness
Passivation, conductive
20 μm
Gold-coated chemically-etched Silver. Structure
NEW COATINGS 1
Notes: 18

## Slide 19
Aluminum alloy
device bulk
Silver
Nickel (P)
Gold
10 μm
Electroplating
2 μm
Electroplating
Chemical etching
Magnetron sputt.
20 μm
NEW COATINGS 1
Gold-coated chemically-etched Silver. Structure
Notes: 19

## Slide 20
Aluminum alloy
device bulk
Silver
Nickel (P)
Gold
10 μm
2 μm
20 μm
Silver
Gold-coated chemically-etched Silver. Structure
NEW COATINGS 1
Notes: 20

## Slide 21
Aluminum alloy
device bulk
Silver
Nickel (P)
Gold
10 μm
2 μm
20 μm
Gold-coated chemically-etched Silver. Structure
NEW COATINGS 1
Gold
Notes: 21

## Slide 22
Gold-coated chemically-etched Silver. Multipactor and Insertion Loss
NEW COATINGS 1
Aluminum alloy
device bulk
Silver
Nickel (P)
Gold
10 μm
2 μm
20 μm
Insertion Loss enhancement factor = x 2.6 (12 GHz)
important drawback
Power enhancement = 3.7 - 12.7 dB
Notes: 22

## Slide 23
Very good behaviour in air
Aluminum alloy
device bulk
Silver
Nickel (P)
Gold
10 μm
2 μm
20 μm
Gold-coated chemically-etched Silver. Aging
NEW COATINGS 1
Important aging effect
Notes: 23

## Slide 24
Roughened Ag by Masking Double Ion Beam Sputtering. Experimental setup
Substrate: Ag (soft)
Masking material: Ti: (hard)
NEW COATINGS 2
Notes: 24

## Slide 25
Roughened Ag by Masking Double Ion Beam Sputtering. Structure
1st step:
Ag roughened by ion etching while Ti masking by magnetron deposition
2nd step:
Au magnetron deposition
while ion induced diffusion
NEW COATINGS 2
Notes: 25

## Slide 26
Roughened Ag by Masking Double Ion Beam Sputtering. Structure
1st step:
Ag roughened by ion etching while Ti masking by magnetron deposition
2nd step:
Au magnetron deposition
while ion induced diffusion
NEW COATINGS 2
Notes: 26

## Slide 27
Roughened Ag by Masking Double Ion Beam Sputtering. Properties
Reference Ag plated harmonic low-pass corrugated filter for 12 GHz
Multipactor power level enhancement = 7 dB: excellent, practical suppression
Insertion Loss enhancement = x 1.1: excellent, in the limit
Aging: apparently not so good
Multipactor power level ≈ 1/time (approx.)
NEW COATINGS 2
The incorporation of Titanium in the coating and its progressive oxidation in atmosphere (aging) leads to increase both, SEY and surface resistance (insertion losses)
Notes: 27

## Slide 28
NEW COATINGS PROPOSED FOR M-ERA-Net
New rough Ag anti-multipactor coatings with no insertion loss and aging drawbacks
The method proposed is the same followed before but changing seeding with Carbon instead of Titanium

## Slide 29
Several reasons exists to substitute Titanium by Carbon for improvement of the anti-multipactor coating:
The intrinsic SEY of Carbon is very low (lower than for Au and Ag)
Carbon is a hard material with very low sputtering coefficient
NEW COATINGS PROPOSED FOR M-ERA-Net
The electrical conductance of Carbon is acceptable
Carbon is inert material which does not oxidize easily in air, thus no fast aging is expected. Besides, passivation with gold could be avoided

## Slide 30
The goal is to obtain the best growth parameters to obtain the roughness with the lowest SEY
Ion gun
Magnetron sputtering
Valve
Rotable sample-holder
Gas inlet
pump
pump
Valve
The main growth parameters for the experimental setup:
Magnetron Power (PM) wat
Ion voltage (Vion) V
Ion intensity (Iion) mA
Etching time (t) min
Other geometrical parameters will be also tested: Ion etching incidence angle, distances to the sample, etc.
NEW COATINGS PROPOSED FOR M-ERA-Net

## Slide 31
Preliminary results:
NEW COATINGS PROPOSED FOR M-ERA-Net
Lowest SEY

## Slide 32
Preliminary results:
NEW COATINGS PROPOSED FOR M-ERA-Net
Lowest SEY

## Slide 33
Coatings with Ag nano-columns
Growing by magnetron sputtering at grazing angles with respect the sample surface, ordered nano-columns can be obtained
1108
NEW COATINGS PROPOSED FOR M-ERA-Net

## Slide 34
Empirical study of the effects on SEY of surface roughness using model surface geometries
The goal is to obtain model surfaces with controlled aspect ratio to study its influence on SEY
We have used Cu surfaces with pores made by laser lithography:

## Slide 35
Empirical study of the effects on SEY of surface roughness using model surface geometries
We have also used Al surfaces mechanically drilled at different depths, i.e. different aspect ratios:
Diameter of the pores: 500µ

## Slide 36
OTHER POSSIBLE STUDIES FOR THE MERA-Net
Study of the effect of Graphene on the anti-multipactor sufaces
Study of the effect magnetic nanoparticles on the anti-multipactor sufaces

## Slide 37
GRIN-Space Group, UAM, Madrid, Spain
ACKNOWLEDGMENTS
Gonzalo Troncoso
Undergraduated student
Valentín Nistor
Post Doc.at CERN
Luis Antonio González
Post Doc.at CERN
Luis Galán
Hononary Professor
Carlos Morales
PhD student

## Slide 38
THANK YOU VERY MUCH
FOR YOUR ATTENTION