## Slide 1
Graphene Nanostructures As Terahertz Photedetectors
Alessandra Di Gaspare
28/03/2017

## Slide 2
The THz Gap
Limited by parasitic
RC time constant
Limited by band-gap and thermal Energy
(1 THz = 4 meV)
THz Sources
Output Power
LNF, 28/03/2017

## Slide 3
THz radiation applications
THz range offers many opportunities for applications
Security
Body scanner to reveal concealed weapons
Availability of sensitive detectors: main technological bottleneck
In R&D: new approaches and devices based on interaction between THz radiation and technologically important materials
THz Time Domain Spectroscopy:
dynamics of electrons, holes, phonons
Fundamental Science
Industrial Process monitoring, food contamination
Inspection of Material Devices, …
LNF, 28/03/2017

## Slide 4
OUTLINE
Semiconductors Nanostructures and Terahertz Radiation
  Systems and State of the Art
  Detection in Field Effect Transistors: theory and some experimental results
Low dimensional semiconductrors nanostrucures as effective active material for THz detection
  Graphene, 1D systems
Reaching the photon-counting level in the THz range
LNF, 28/03/2017

## Slide 5
THz Detection: figures of merit
Responsivity (R) [A/W] or [V/W]
Noise Equivalent Power (NEP) [W/Hz-1/2]
Response Time (t)
Portable/Integration On-chip/Scalable/Price
Electrical Output
Input Power
Noise Spectral Density
Responsivity
[Max. modulation freq.]-1
LNF, 28/03/2017

## Slide 6
THz Direct Detectors
Hot Electron Bolometers
NEP = 3 x 10-19 WHz-½
QWIPs
Pyroelectric
NEP = 3 nWHz-½
CMOS Multipixel Camera, Schottky Diodes
NEP = 100 pWHz-½
1-Portability
2-In electronic systems, time response very fast
T < 10 K
Higher performances, cryo needed
LNF, 28/03/2017

## Slide 7
LNF, 28/03/2017
THz Detection in FETs
Rectification of THz plamsa waves in the 2D active channel
(Dyakonov and Shur, PRL 1993)
1-Low-dimesnional systems, 2DEG (Two-dimensional electron gas) gas of electrons free to move in two dimensions, quantum-confinement in the third dimension...
2- 2D plasmons @ THz frequencies can be coupled to radiation provided there is a wave vector defined by geometry (grating or antenna) to compensate for the momentum mismatch
Confinement of THz radiation in subwavelenght cavity
Tunability of the plasma frequency in 2D systems
F. Evangelisti, JAP 2013

## Slide 8
LNF, 28/03/2017
Why FETs for THz detection?

## Slide 9
LNF, 28/03/2017
Plasma wave devices
Exeprimental approach: fabrication of field effect transistors whose conducting channel is a 2DEG, integrated with a planar antenna
λplasmon/2
The 2DEG channel realizes a
plasmonic microcavity
SOURCE
DRAIN
GATE
PLASMON MICROCAVITY
semi-insulating substrate
n-AlGaAs
GaAs
λphoton/2
SOURCE
DRAIN
GATE
Charge modulation in time and space at w  2DEG in hydrodynamic regime

## Slide 10
LNF, 28/03/2017
Self-mixing in FETs (Dyakonov-Shur mechanism) THz modulation of the channel charge density imposed by the gate terminal
Intrinsic nonlinearity in the 2DEG-hydrodynamic response
Heating of the 2DEG
…
Inversion symmetry of the E field must be broken (antenna, channel design)
Absorption of THz radiation
THz-down conversion: DC photocurrent
Damped (broadband) detection
Resonant detection
µ
µ

## Slide 11
LNF, 28/03/2017
Spectral Response
50 mm
undoped GaAs
substrate
LSD
W
Lg
10 mm
Two perpendicolar linear dipole antenna
S
D
50 mm
Two-terminal device with asymmetric design
Hydrodinamic regime of the ungated 2DEG in the investigated spectral range
Strong indication of plasma waves
Modes assignement:
interaction btewteen 2DEG gated and ungated (hybrid cavity)
Activation of optically inactive mode
A. Di Gaspare, APL 2012
A. Di Gaspare, J. Opt 2013
V. Giliberti, PRB 2015
Optical inactive even mode
with asymmetric E distribution
hybrid gated cavity
m=2
m=3
m=1
G

## Slide 12
LNF, 28/03/2017
The Terahertz gap & graphene
50 mm
THz modulation
B. Sensale-Rodriguez et al., Nature Commun. 3, 780 (2012)
B. Sensale-Rodriguez et al., Nano Lett. 12, pp. 4518–4522 (2012)
THz detection
THz plasmonic devices
A. N. Grigorenko et al,Nature Photon., vol. 6, pp. 749–758 (2012)
Y. M. Bahk et al, ACS Nano, 2014, 8 (9), pp 9089–9096
THz generation
THz metamaterials
N. Papasimakis et al., Light: Science & Applications (2013) 2, e78

## Slide 13
LNF, 28/03/2017
Graphene-based devices as THz detectors
Electrons
Holes
Works only for Graphene in the
THz Range
L. Vicarelli et al, Nat. Mater. 11, 865 (2012).
D. Spirito et al, Appl. Phys. Lett. 104, 061111 (2014).
A. Zak et al, Nano Lett. 14, 5834 (2014).
A. V. Muraviev et al, Appl. Phys. Lett. 103, 181114 (2013).
M. Mittendorff et al, Appl. Phys. Lett. 103, 021113 (2013).
X. Cai et al., Nat. Nanotechnol. 9, 814 (2014).
Koppens et al, Nature Nanotechnology 2014

## Slide 14
LNF, 28/03/2017
Graphene
HfOx
Substrate
Epitaxial and CVD graphene
Exfoliated graphene
Epitaxial growth
CVD growth
Antenna coupled Graphene-FET
Device development@NEST
Antenna Integration
S
D
G
G
S
D
Broadband Asymmetric coupling
Top-gate G-FET
S
D
G

## Slide 15
LNF, 28/03/2017
Antenna coupled Graphene-FET
L.Vicarelli, Nat. Nano 2012
Maximum responsivity :
R = 0.05 V/W
Minimum Noise Equivalent Power:
NEP = tens of nW/
Exfoliated SL Graphene
Maximum responsivity :
R = 1.2 V/W
Minimum Noise Equivalent Power:
NEP = 2 nW/
D. Spirito, APL 2014
Broadband detection
C ~ 10-4 V2
efficiency of the antenna coupling and the FET impedance
= 1/Rsd
source/drain conductance
Photovoltage (a.u.)
CNP
j = e ⟨n(t)·v(t)⟩2π/ω
Exfoliated BL Graphene
DU=C*s-1*ds/dVG
0.3 THz

## Slide 16
LNF, 28/03/2017
QCL radiation detection by GFETs
at 3.4 THz
S
D
G
Detection speed:
250 kHz
Limit imposed by presently used experimental set up
Expected maximum speed > 1 MHz
Non-resonant plasma wave rectification
Maximum responsivity :
R = 1 V/W
Minimum Noise Equavalent Power:
NEP = 10 nW/Hz-1/2

## Slide 17
LNF, 28/03/2017
Epitaxial graphene FET
Max responsivity R = 0.25 V/W
NEP = 80 nW/√Hz
F. Bianco, APL 2015
2 Competing detection mechanism
Sug
DT
Sg
p
p/n

## Slide 18
LNF, 28/03/2017
Resonant Detectors (work in progress)
Encapsulated graphene
Large scattering time, High mobility
Exfoliated hBN
Cr-seeded CVD grown
single crystal graphene array
Cr
Graphene
Cu foil
Graphene on hBN
Top hBN
G
S
D
45 nm-thick hBN flake
G
D
hBN
flake
Graphene
flake
15 nm-thick hBN flake
Vsd = 1 mV
m = 33000 cm2/Vs
n0 = 5.71012 cm-2
Rc = 95 W
Vd = 3.7 V
S

## Slide 19
LNF, 28/03/2017
Van Der Waals Heterostructures:
the Flat Land
Improved material properties by
creating the «ideal» environment
BORON NITRIDE is a promising candidate:
Impervious to water and oxygen
High k dielectric
No dangling Bonds
Examples:
hBN/Graphene/hBN samples
hBN/BP/hBN Heterostructure
High Mobility
High Stability
[L.Viti, Adv. Mater. 2016]
µ > 105 cm2/Vs

## Slide 20
LNF, 28/03/2017
THz Detection in nanostructures: Nanowire-FETs
Viti et al., Nanoscale Research Letters 7, 159 (2012)
Vitiello et al., Nano Letters 12, 96 (2012)
Vg
Vout
Room temperature
THz detectors
0.3 – 3.5 THz range
Optimization: materials, device design, antenna (Vitiello M.S., APL Materials 2015)
300 GHz
Homogeneous and Gradient-doped
tapered
InAs NWs
InAs NanoWires-FETs
Asymm. Broad Band
Symm. Broad Band
Asymm. Narrow Band

## Slide 21
LNF, 28/03/2017
Sensing single photons at THz
Detector Scheme for free-space THz beams: quasi optical approach
bolometer phototransistor Schottky diode
Used also Photo-Conductive Antenna generators
THz beam is focused, collected and converted by the antenna
THz field is confined in a sub-wavelength region hosting the sensing element
for certain applications an ultimately high sensitivity reaching a photon-counting level is required (direct detection of dark matter in a region of the parameters space difficult to reach with different techniques)
in THz range E< 124 meV, l> 10 µm: the single-photon detection is not trivial
With the available detector technologies, attainable sensitivities are currently far below the level of single-photon detection

## Slide 22
LNF, 28/03/2017
Graphene Bolometers
Key points:
strong light-matter interaction and collective effects (plasma waves in the 2DEG)
Transport dominated by Hot-Carrier
Study on the thermal properties indicated the possibility to reach very high sensitivity as both a bolometer and as a calorimeter
General Advantages
Low Noise, Broadband absorption
Challenge: material purity, fabrication; many device contraints
T increase:
4 µm2 channel, 100mK,
Superconding contatcts, el-phonon coupling very weak
…

## Slide 23
Nanostructured systems for THz Photon Counting
quantum devices based on nanostructured semiconductors have demonstrated single-photon detection capabilities in the THz range
Classical photodetector
Isig=Gpc*e*(hPin/hn), Gpc<1 (gain)
R= Isig/Pin = 8 A/W
1photon – 1 electron, E=124 meV
Responsivity is limited, some Gain enhancement is needed
LNF, 28/03/2017

## Slide 24
LNF, 28/03/2017
Nanostructured systems for THz Photon Counting
quantum devices based on nanostructured semiconductors have demonstrated single-photon detection capabilities in the THz range
Classical photodetector
Robust and reliable metrologies for single-THz photons are still lacking
Why not to implement device concepts on QD+new materials?
Novel nanostructure-based detector
1-QD charging by 1-photon abs
2-sensing the 1QD via conductance in QPC or SET
DQD Det.
Pin10-18W
every skip is single photon!
Dark count 10-2 s-1
Komiama, IEEE JSTQE 2011,
See also F. Gatti talk

## Slide 25
Conclusion
Detection demonstrated from 0.2 THz up to 3.4 THz in Semiconductor Nanostructures (2D systems, Graphene, Nanowires)
NW-FETs
Gr-FETs
LNF, 28/03/2017

## Slide 26
Conclusion
Detection demonstrated from 0.2 THz up to 3.5 THz in Semiconductor Nanostructures (2D systems, Graphene, Nanowires)
NW-FETs
Gr-FETs
LNF, 28/03/2017

## Slide 27
LNF, 28/03/2017
Detection demonstrated from 0.2 THz up to 3.5 THz in Semiconductor Nanostructures (2D systems, Graphene, Nanowires)
Detection signals related to plasma wave effects in the 2D electronic system, but also other contributions
Antenna, device design and material are degrees of freedom for detectors optimization
Present-days performances enabled most of room-T applications
Quantum confinement in nanostrucutured and/or intrinsic low-dimensional materials is a potential playground for photon counters in the terahertz range
Conclusion

## Slide 28
Prof. Alessandro Tredicucci
Tredicucci’s Group@NEST, Federica Bianco
Miriam Vitiello, Leonardo Viti, THz Group@NEST
Camilla Coletti, Graphene Group@IIT NEST
Aknowledgments
LNF, 28/03/2017

## Slide 29
LNF, 28/03/2017
Conclusion
Detection demonstrated from 0.2 THz up to 3.5 THz in Semiconductor Nanostructures (2D systems, Graphene, Nanowires)
Detection signals related to plasma wave effects in the 2D electronic system, but also other contributions
Antenna, device design and material are degrees of freedom for detectors optimization
Present-days performances enabled most of room-T applications
Quantum confinement in nanostrucutured and/or intrinsic low-dimensional materials is a potential playground for photon counters in the terahertz range

## Slide 30: High mobility AlGaAs/GaAs heterostructure
with
Resonant plasmons: reduced electron-phonon scattering suppresses the plasmon-phonon decay channel
Heterostructure provided by CNR-IOM, Trieste, Italy
Notes: In order to realize the condition for observation of resonant plasmons we used an ultra-high mobility AlGaAs/GaAs heterostructure, whose succession of epilayers is reported in this figure. The ultra high mobuility is needed to reduce phonon-electron scattering and increase the lifetime of the collective excitations. At 10 K the mobility is around 300000 cm2/Vs and for a 10 um plasmon microcavity, around 200 ghz, the decay time of plasma waves is almost 2 times the transit time of the microcavity, hence

## Slide 31: Antenna integrated-HFET
50 mm
Ohmic contact: evaporation of metal (Ge/Au/Ni multilayer )
and Rapid Thermal Annealing
Electrical isolation of devices: ion implantation
Gate contact: evaporation of Ti/Au
undoped GaAs
substrate
LSD
W
Lg
10 mm
2 DEG
(n) Al0.33Ga0.67As
S
D
G
Undoped GaAs
Two perpendicolar linear dipole antenna: one connected to the source and drain terminals, and the other connected to the source and gate terminals.
S
D
50 mm
THz excitation of a “2DEG diode”
Two-terminal device with asymmetric design
Hydrodinamic regime of the ungated 2DEG in the investigated spectral range
Notes: The chosen design of the antenna, shown in this scanning electron microscope image, is two perpendicolar linear dipole antenna centered at 300 Ghz: one connected to the source and drain terminals, and the other connected to the source and gate terminals. Here is shown an image of the plasmon microcavity and these are the dimensions. Taking into account the frequency range of our tunable THz source Virginia diodes multipliers, which is 0.15 to 0.4 THz, we have designed a transistor with a distance between source and drain of L=10 um. The dimensions are limited by our technological capability. It is important to note that the gate is shifted towards the source contact and is very short compare to the source and drain lenght. In this way the plasmon dispersion is almost aneffected by the presence of the gate electrode.

## Slide 32
Plasma wave devices
LNF, 28/03/2017
Electrodynamics equations for the 2DEG
F. Evangelisti, Journal of Applied Physics 114, 124506 (2013)
Equivalent Circuit:
The 2DEG impedance oscillates as function of frequency