## Slide 1: Cryogenic SEY measurement Facility at Daresbury
Taaj Sian
Reza Valizadeh, Oleg Malyshev

## Slide 2: Motivation
LASE is the baseline for FCC-hh e-cloud mitigation
My PhD project is part of EuroCirCol WP4
  Optimising LASE surfaces on Cu with various lasers and parameters to create surfaces with SEY < 1
  Testing these surfaces at room temperatures
  Testing the best surfaces at cryogenic temperatures with and without cryosorbed gasses

## Slide 3: Sample Production
Produced and tested more than 100 different LASE samples
  With different laser parameters treated with the following lasers:
    Nanosecond 355 nm
    Nanosecond 1064 nm
    Picosecond 355 nm
    Picosecond 1064 nm
  In different atmospheres:
    Air
    Ar
    CH4
More than 40 samples have SEYmax<1
  More in talk my R. Valizadeh
What about cryogenic temperature and condensed gas?

## Slide 4: Cryogenic Experiment Schematic
Known amount of gas injected Q=P1* (V1 + V2 + V3)
All volumes are known
After opening valve 2 while Ts =T2:
Then sample temperature is reduced to 4.2 K< Ts < 80 K to cryosorb the gas.
Surface coverage is: , where A is the sample area
V1
V2
V3
V4
T1
T2
TS
P1
Valve 1
Valve 2

## Slide 5: Sample Holder
Sample at 4-80 K
Bottom flange of test chamber at 60-80 K
2nd stage
Conductor
from 1st stage
to a sample
Easy to design but
It took 8 months to manufacture
this piece (and delayed the
research programme)
Thin stainless steel tubes used to reduce conductance to sample
Holes near the sample holder for the supports for the Farraday cup
1 mm gap between the flange and sample to reduce lost gas

## Slide 6: Initial Design
Bellows
Conductor
from 1st stage to heat shield
Insulation vacuum
1st stage
2nd stage
Test chamber
  RDK-305D 4K Cryocooler (RDK-305D Cold Head with CNA-31C/D Compressor)
Electron Gun, Gauge,
RGA, Pumping,
Gas injection

## Slide 7: Current design
Bellows
Conductor
from 1st stage to heat shield
Insulation vacuum
1st stage
2nd stage
Test chamber
Faraday cup

## Slide 8: Injection line
Baratron
Small Volume
Large Volume
Gauge
Gasses (CO, CO2, CH4, N2, Ar and H2)
Pumps

## Slide 9: Conclusions
SEY < 1 has demonstrated on more than 40 samples produced with different lasers and various parameters
A new facility for SEY studies will allow the measurement of LASE surfaces at cryogenic temperatures with and without cryosorbed gasses
Facility will be tested shortly after this workshop