## Slide 1: Coupler Operation Experience at IMP
Tiancai Jiang, Ruoxu Wang, Shenghu Zhang
SRF Group
On behalf of ADS Linac Team
Institute of Modern Physics, CAS

## Slide 2: Outline
Introduction
Impact of Field Emission on coupler ceramic
Temperature-rise of the Cold Window
Summary

## Slide 3: The demo 25 MeV SRF linac
RFQ
ECRIS
HEBT
162.5 MHz HWR010
162.5 MHz HWR015
MEBT
IHEP
IMP
TTF III-like
Double Warm Ceramics
12 Double Warm Ceramic Couplers - IMP
5 TTF III-like Couplers - IMP
6 Single Choke Couplers - IHEP

## Slide 4
10 MeV operation for 2 months, ceramic windows of 2 couplers were leaking each CM.
Cracks of ceramic window
10 MeV coupler operation
(a)Single chock window (b) Fixed Qe (c)No bias
Outer conductor: helium cooling, thermal sink. Inner conductor: water cooling
12 single window couplers

## Slide 5: HWR010 field emission

## Slide 6
Field emission on coupler
emitters
FE hitting on Window
Trajectory of FE
window
EP 25MV/m, Energy of FE ~400KeV
EP 25MV/m (Cavity), local EP 15MV/m

## Slide 7: Field emssion on pick-up port
Pick up from
cavity
Forward
RF signal
Reflected
RF signal
*More details will be present in the talk “Troubleshooting and stability analysis of CW RF operation at China ADS front-end demo linac”.
Coupler Port
Pick-up Port

## Slide 8
FE simulation
Difficult to braze
Not easy for the clean of the space between the dual windows
windows
Solutions

## Slide 9
HWR010 coupler replacement
Replacing coupler in line
New couplers has worked for more than 1 year, no leak was found, and the new couplers work very well.
Replacing coupler in clean room

## Slide 10: Taper HWR015 feild emission
Donut Ring
Cold window
Warm window
80 K (Temperature Sensor)
4.2K
FE electrons cannot reach the window due to donut ring shape
Couplers has worked for about 1 year, no leak was found.

## Slide 11: Temperature-rise of the cold window
Chart: Time (min)
| 0 | 5 | 10 | 15 | 20 | 25 | 30
EPK=0 | 133.8 | 133.74 | 133.6 | 133.5 | 133.42 | 133.34 | 133.27
EPK=4.5 | 133.18 | 133.05 | 132.97 | 132.91 | 132.87 | 132.81 | 132.74
EPK=10 | 137.22 | 138.32 | 139.27 | 140.24 | 141.11 | 141.94 | 142.66
EPK=12 | 148.21 | 150.11 | 151.65 | 152.88 | 154.06 | 154.67 | 155.64
Chart: Time (min)
| 0 | 5 | 10 | 15 | 20 | 25 | 30
Ep=0 | 144.92 | 144.3 | 143.57 | 143.09 | 142.71 | 142.34 | 142.11
Ep=5 | 142.8 | 141.89 | 141.61 | 141.47 | 141.38 | 141.32 | 140.99
Ep=10 | 149.03 | 153.07 | 158.01 | 162.84 | 165.65 | 167.81 | 170.81
Ep=13 | 184.14 | 188.45 | 191.68 | 194.8 | 197.23 | 199.94 | 202.56
Chart: Time (min)
| 0 | 5 | 10 | 15 | 20 | 25 | 30
EPK=0 | 130.07 | 130.13 | 130.19 | 130.25 | 130.29 | 130.29 | 130.34
EPK=5 | 130.48 | 130.57 | 130.61 | 130.67 | 130.76 | 130.8 | 130.83
EPK=10.5 | 130.9 | 130.94 | 130.98 | 131.02 | 131.07 | 131.11 | 131.13
EPK=16 | 131.25 | 131.3 | 131.34 | 131.37 | 131.4 | 131.43 | 131.48

## Slide 12: Resonance & off-resonance
Resonance (Short)
Off-Resonance (Open)
L
H
0
Resonance
Temperature-rise of cold window caused by copper sputtering during RF conditioning.
After repairing the solenoid, RF conditioning the coupler was carried out at room temperature without opening valves of CM.

## Slide 13: Summary
The ceramic windows can be charged by FE electrons from cavity, which may cause the ceramic windows to be broken.
The temperature-rise of cold window supposed to be caused by copper plating on the surface of ceramic.

## Slide 14
Thanks for your attention