## Slide 1: Nb3Sn Coatings from Cornell
Ryan Porter Cornell University
Supported by:
U.S. DOE award DE-SC0008431.
This works make use of: Center for Bright Beams , NSF Award PHY-1549132
Cornell Center for Materials Research, NSF MRSEC program (DMR-1120296)

## Slide 2: Outline
Introduce Nb3Sn—why we care and how we make it
How it currently performs
  Current quality factors
  Current field limits
Advancing maximum fields and current work
Conclusion/Future outlook

## Slide 3: Properties of Nb3Sn
Parameter | Niobium | Nb3Sn
Transition temperature | 9.2 K | 18 K
Superheating field | 219 mT | 425 mT
Energy gap Δ/kbTc | 1.8 | 2.2
λ at T = 0 K | 50 nm | 111 nm
ξ at T = 0 K | 22 nm | 4.2 nm
GL parameter κ | 2.3 | 26
Blue: tin
Red: niobium
Higher critical temperature
→ Operation at 4.2 K
Higher superheating field
→ Double the limit of niobium
Lower losses
Higher gradients
~90 MV/m

## Slide 4: Cornell Nb3Sn Program
We have a program at Cornell for creating Nb3Sn coatings
Coat Nb with 2-3 µm of Nb3Sn
  Vaporize tin in high temperature vacuum furnace
Can (currently) coat:
  samples
  ~1.3 GHz single cells

## Slide 5: Before/After Coating
Doesn’t look that much different than before coating…
Before
After

## Slide 6: Comparison to niobium
20× more efficient than Nb at 4.2 K!

## Slide 7: Current performance
Data taken at 4.2 K
1.3 GHz ILC single-cells

## Slide 8: Limitations in quench field
Nb3Sn cavities quench consistently at fields between 14 and 18 MV/m in continuous wave operation, even in spite of some perturbations to the coating recipe.
The superheating field suggests we can achieve fields up to 90 MV/m!

## Slide 9: Pulsed quench field
Continuous→17 MV/m
Pulsed→26 MV/m

## Slide 10: Localised quench
Nb3Sn cavities are limited by a quench at a defect
What sort of defect could be at fault?

## Slide 11: Tc suppression
A tin depletion of only 3% reduces Hsh by 75%
Flux entry could occur at tin-depleted surface defects

## Slide 12: Tin-depletion in grains
Cross-section of the Nb3Sn RF surface
Grain boundary
Have only about 1% Sn depletion → more statistics needed

## Slide 13: Near quench behavior
Measure temperature of sensor near the quench point as field is increased
Sudden jumps in temperature
Temperature
Max Field
Time

## Slide 14: Near quench behaviour
The sudden nature of these jumps and hysteresis strongly suggests flux entry
2 K

## Slide 15: Grain boundary flux penetration
Increasing current across boundary
Power dissipated
Ahmad Sheikhzada and Alex Gurevich
Physical Review B 95, 214507 (2017)
arXiv:1702.02843

## Slide 16: Grain Boundaries
Looking at grain boundaries
  SEM scan with atomic resolution
  Sn concentration across grain boundaries
  More investigation needed
1 nm
Chart: 
5 nm

## Slide 17: Layer growth during ramp
2 μm
Pre-anodised
Not anodised
Start
500°C
800°C
950°C
1120°C

## Slide 18: What is happening at the surface?
We cut out this region and examined it with microscopy
Nothing suspicious except jump
  Rough Surface
Nb3Sn surface
Nb substrate grain boundary?
Quench Site

## Slide 19: Surface Roughness
Nb3Sn we create is rougher than electropolished Nb
  ~1 µm peak to peak
This causes large enhancement of the surface magnetic field

## Slide 20: Field Enhancement
1% of the surface has surface fields at least 50% higher than for a flat surface
  Limits maximum quench fields 60 MV/m for perfect surface
  Lowers field before defects become an issue

## Slide 21: Surface Treatment
Developing surface treatments to reduce surface roughness
Early results found oxypolishing could half roughness and surface field enhancement while removing < 1 µm

## Slide 22: Conclusions
Can reach 2·1010 at 4.2 K
Achieve 16-17 MV/m in continuous mode
Achieve 26 MV/m in pulsed mode
Have identified main sources of performance limitations
  Quench Fields
    Surface roughness
    Vortex entry (at grain boundaries?)

## Slide 23: Looking Forward
Reducing surface roughness may gain us 50% improvement in quench fields
  Continuous: 17 MV/m → 25 MV/m
  Pulsed: 26 MV/m → 39 MV/m
If we can fix grain boundaries
  Continuous & pulsed: → 90 MV/m?
Improving in magnetic shielding and cooldown could ~1.5x Q at 4.2 K

## Slide 24: Acknowledgements
Prof. Matthias Liepe
Prof. Tomas Arias
Prof. David A. Muller
Prof. James P. Sethna
Danilo Liarte
Daniel Hall
Paul Cueva
Nathan Sitaraman
James Maniscalco
James Sears
Greg Kulina
John Kaufman
Holly Conklin
Terri Gruber
with special thanks to
The Cornell Nb3Sn program is primarily supported by the U.S. Department of Energy