## Slide 1: IFMIF HWR cryomodule and magnetic shield properties
Ttc meeting
08 February 2018, MILANO
Juliette PLOUIN
Caifu FAN (Master Student)

## Slide 2: outline
CARACTERISATION OF IFMIF MAGNETIC SHIELD
CARACTERISATION OF CYLINDRICAL SAMPLES
  In ambient field at room temperature
  In variable field at room temperature
  In ambient field at cold temperature

## Slide 3: CRYOMODULE FOR THE IFMIF LIPAC
Cryomodule for the IFMIF LIPAC: 9 MeV, 125 mA
8 Half Wave Resonators
8 solenoids
8 RF couplers
1 overall magnetic shield

## Slide 4: Magnetic shield for the ifmif/lipac cryomodule
Mumetal magnetic shield with thickness 2 mm
Target : field lower than 2 micT
Measured field inside : 0.2 – 0.5 micT
Estimated mr ~ 150000

## Slide 5: Samples for magnetic shield qualification
Diameter : D=155 mm
Length 600 mm
Thickness : e = 2 mm
3 batches of thermal treatment (TT) same receipe
3 types of welding
1 batch of thermal treatment (TT)
3 types of welding

## Slide 6: Samples for magnetic shield qualification
Diameter : D=155 mm
Length 600 mm
Thickness : e = 2 mm
1 batch of thermal treatment (TT)
3 types of welding
TYPE III longitudinal full welding
TYPE II
radial full welding
TYPE I longitudinal spot welding

## Slide 7: Cylindrical samples in ambient field at RT  effect of TT and welding type
No effect of thermal treatment batch for IFMIF (was expected..)
No effect of welding type.
  in particular, no enhancement of the B field in the full radial welding region
Shield position
Shield position
TYPE II
radial full welding

## Slide 8: Cylindrical samples in ambient field at RT  estimation of permeability values
Permeability would be around 50000… Quite low.
Remark : measured B-fields are very low (<0.1 mT = 1 mG)… values are probably overevaluated by probes.

## Slide 9: mu-H curve used FOR simulations
M. Masuzawa, SRF 2013
Measurements on small ring sample

## Slide 10: Definition of a « equivalent permeability »
Transverse earth field applied
Permeability of the material varies along the shield material
Local permeability is not measurable with our sample
Simulation with OPERA software
For further sim/exp comparison we define:
We are in this region

## Slide 11: Magnetic shield caracterisation in variable field : setup
Experiments during JT60SA tests
Toroidal coil for fusion tested in Saclay cryostat.
Current goes from up to 27,5 kA
Magnetic field goes to 2.7 T
In this area, B goes up to 7.5 mT, transverse to shield and ~homogen
We measured field inside/outside the shield

## Slide 12: Magnetic shield caracterisation in variable field : results
Magnetic shield is magnetized after solenoid switch off
Measurements at low field unaccurate because probe offset seems to have changed during measurements…
Hysteresis effect observed
50 mT (earth field)
2.5 mT

## Slide 13: Magnetic shield caracterisation at low T in ambient field
Measurements during warm up in air : shield temperature is homogen.
Permeability tends to decrease with temperature, for both materials, maybe a bit more clearly for Mumetal.
What happens at lower temperature ?

## Slide 14: Effect of shield thermal gradient ?!
Measurements during warm up in air : shield temperature is homogen
Measurements during cool down in LN : high temperature gradient measured between shield top and bottom parts
ESS sample
Strange behavior in presence of thermal gradient… Due to differential stress in material (permeability change with temperature is due to magneto-strictive effect) ??
How is shield temperature gradient in cryomodules ??

## Slide 15: summary
Magnetic shields can provide magnetic field lower than 1 microtesla close to cavities
Key elements for achievement of high Q cavities
Magnetic shields can be magnetized by mT fields (e.g. field from solenoids).
Important to anticipate material behavior and properties for proper design
Equivalent permeability
Behavior at low temperature, in cryomodules