## Slide 1
UNIVERSITA’ DEL SALENTO
Facoltà di Scienze Matematiche, Fisiche e Naturali
Dottorato in Fisica and Nanoscience-XXIX Ciclo
Development and Production of Multifunctional Bio-Nano-engineered Drug Delivery Systems Loaded by TGF ß1 inhibitors for delivering into Hepatocellular Carcinoma Cells.
RELATORI:
Chiar.ma Prof.ssa Rosaria Rinaldi
Professor Stefano Leporatti
DOTTORANDO:
Nemany AbdelHamid Nemany Hanafy

## Slide 2
OUTLINE
Fabrication of CaCO3 and magnetic nanoparticles
Fabrication of Nano-Micelles
Fabrication of Hybrid Nanoparticles
Conclusion
Background
Hepatocellular Carcinoma Animal Model
Our Contributions
Acknowldegment
Hepatocellular Carcinoma (HCC)
Chapter 1
Chapter 2
Chapter 3
Chapter 4

## Slide 3
1-separation
2-Migration
3-Diffusion
4-Movement
5-Diffusion
6-Tumour
7-Angiogenesis
Modification from Geho et al.,2013
Hepatocellular carcinoma
Background

## Slide 4
Cell takes rounded shape (A), then psedudopodia are formed like protrusion (B) .Cytoplasm is extended (C ),(D) and takes shell shape (D), cytoskeleton remodels forming rod connected structure extended from nucleus and cover all cytoplasm (E) finally the cells are attached together to form colony (F)
Phenotype alteration of HCC

## Slide 5
Tight Junction
Adherent Junction
Desmosomes
Down- regulation
Claudin
Occludin
zonula
E-Cadherin
Desmoplakin
Plakophilin
Extracellular changes
Actin cytoskeleton filaments
Intracellular changes
MMP
Collagen fibers
Fibronectin
Up- regulation
TGFβ
TJ
AJ
DS
Golgi
Apparatus
pSmad 2&3
P-17
ALK1fc inhibitor
SHT-DNA& siRNA
ALK5
Stimulation cell to move
Modification from Xu,J. et al., Cell Res. 2009;19(2):156-72.

## Slide 6
Challenge of therapeutic agents
Oral dose
Injected dose
Disadvantages
Salivary amylase
Acidic pH of stomach
Alkaline pH of Colon
Poor adsorption
Disadvantages
Immunosystem attack
Not targeted dose
Diluted by blood plasma

## Slide 7
Fabrication of Micro/Nano-templates to obtain capsules as vehicles for drug delivery
Homogeneous population of particles
Separated particles
Small diameter
Charged particles
Optimization
LbL polyelectrolyte multilayers
No aggregation
Small diameter
Efficient core removal
Hollow capsules
Templates
Capsules
dissolution
Alternate LbL Abosrption
1
2
3
4
Core
Polymers
Functionalization

## Slide 8
Ca +CO3
Nucleation
Chemicals
Crystallization
Physical mechanism
Ca2+
CO3-
Aggregation
Same solution
Chemical mechanism
CaCO3 fabricated in presence of distilled water (B and D) and in the absence of distilled water (A and C).
The high magnification (2.500X) showed aggregated calcite in both samples (C and D)
CaCO3 Fabrication
Chapter:1 section 1

## Slide 9
Separated particles.
Homogenous population.
Charged particles
Spherical shape (mostly)
No aggregation
Chitosan
Poly(sodium 4-
styrene-sulfonate)
Poly acrylic acid
Poly(allylamine
hydrochloride)
Control CaCO3 fabrication by adding polymers
Elemental distribution of calcium and carbon atoms in different conditions

## Slide 10
PSS and PAA particles are negatively charged and final capsules are positively charged.
PAH particles are positively charged whereas final capsules are positively charged.
Chitosan particles is negatively charged and final capsules are positively charged.
SEM at low magnification showed no aggregated capsules in each polymers used after dissolving the core.
High magnification showed hollow capsule
Alternate Layer by Layer Assembly
Chitosan
Poly(sodium 4-
styrene-sulfonate)
Poly acrylic acid
Poly(allylamine
hydrochloride)

## Slide 11
DAPI
TRITC
FITC
Merge
DAPI
FITC
TRITC
Merge
A
B
4
3
2
1
CaCO3 Micro/Nano-Rods
TEM images of (A) elongated CaCO3 micro rods (about 1–2 µm). (B) elongated Nano CaCO3 rods (57 nm)
Cellular uptake after 6 h
Cellular uptake after 24 h

## Slide 12
FeCl3
FeCl2 + 2NaOH Fe(OH)2 + 2NaCl
Dissolved
O2
2Fe2O3
Fe3O4
Iron (II) Hydroxide
(Greenish colour )
Iron (II) oxide
(Blackish brown colour)
Iron (III) oxide
(dark-Black colour)
Iron oxide nanoparticles (NPs) fabrication
Fabrication of Magnetic NPs
A
B
C
FITC
Chapter:1 section 2

## Slide 13
Fe
Fe
Fe
Fe
Fe
A
B
C
D
20µm
A
B
C
Characterization of Fluoro-Magnetic Nanoparticles
Fabrication and characterization of Fluoro-Magnetic nanoparticles
Notes: Figure 1: TEM characterization of iron oxide NPs A) spherical iron oxide NPs without FITC; B) elongated iron oxide nanoparticles with FITC. EDX analysis show C) Low (wihout FITC) and D) High (with FITC) concentration of iron atoms. Squares indicate area of EDX analysis

## Slide 14
1
2
3
4
5
6
200
150
100
75
50
37
25
15
ALK1
ALK1
Cytoplasmic internalization
Nuclear internalization
Mitochondrial internalization
A
B
C
PEG
PEG
PEG
CMC-ALK1fc
CMC-ALK1fc
Fluoro-MNPs
PEG
PEG
Fluoro-MNPs
CMC
CMC
PEG
Magnetic nanoparticles
Functionalization

## Slide 15
Immune fluorescence assay: Anti-TGFβ1
Control HLF cells
Control ALK1fc
Control Nanoparticles
Encapsulated ALK1fc

## Slide 16
Nanoparticles
Functionalization
A
FA+D.W
FA+DMSO
B
C
D
Folic acid as ligand for folate receptors
Behaviour of activated folic acid. A) Photograph of folic acid dissolution. B) Folic acid absorbance. C) FTIR of Folic acid bands modification. D) Fluorescence intensity of folic acid.

## Slide 17
Behaviour of polygalacturonic acid and poly acrylic acid at different pH
Polygalacturonic acid
A
B
C
D
A) Distilled water; B) pH 10; C) pH 7.2; D) pH 3.
F
E
E) Alkaline pH 10
F) Acidic pH 3
Poly acrylic acid
Polymeric Nano-Micelles
Chapter: 2

## Slide 18
Polymeric –Nano-Micelles fabrication and functionalization

## Slide 19
Characterization of Nano-Micelles
Nano-Micelles characterization
PAA
PgA
Marker
Drug
Ligand
biodegradable
Increasable time circulation
Specific for cancer cells
Increasable rate of cellular uptake
Shrinkable inside stomach and extendable inside
colon
Nano-sized carrier 50-100nm
Folic acid in DMSO
Active Folic acid
Free R6G
Free FITC
Micelles with RG6
Micelles with FITC
At colon pH
At stomach pH

## Slide 20
Morphological ultrastructure of Golgi apparatus. A) Control HLF; B) Free LY2157299 incubated with HLF cells (swelling Golgi apparatus); C) Free LY2157299 incubated with HLF cells (many secreted vesicles); D) Free micelles incubated with HLF cells; E) Encapsulated LY2157299 incubated with HLF cells (swelling Golgi apparatus); F) Encapsulated LY2157299 incubated with HLF cells (many secreted vesicles).
TEM images of Golgi Apparatus Ultrastructure
A
B
D
C
E
F

## Slide 21
H
Bovine serum albumin
Bovine serum albumin /Folic acid
+
+
Folic acid
N-hydroxysuccinimide
EDAC
N-hydroxysuccinimide ester of folic acid
+
Polyethylene glycol
Pterin ring
PABA
Glutamate
α
γ
O
FA-BSA-PEG
HPNP-FA
Hybrid Polymeric Nano-Protein-FA Assembly
Scheme of Hybrid polymeric Nano Protein –FA Fabrication
Chapter:3

## Slide 22
Conjugation of folic acid with albumin
100 nm
A
B
15 nm
14.5 nm
17 nm
FA in D.W
FA in DMSO
Active FA
HPNP
HNPN- FA
HNPN- FA
HPNP
HNPN- FA
Active FA
HPNP
FA in DMSO
FA in DMSO
FA in D.W
1
2
UV analysis
Bio Rad analysis
Coomassie stain
TEM Image
AFM Image
FTIR:BSA/FA
FTIR: HPNP/HPNP-FA

## Slide 23
TEM photomicrograph and TGFβ assay
High-resolution TEM images of polymeric nano-protein carriers. A) Free capsules; B) SHT-DNA encapsulated; C) siRNA encapsulated; D) P-17 encapsulated.
EN-SHT DNA
EN-siRNA
EN-P-17
Control
Control anti-TGFβ
Control capsules
Effect of encapsulated P-17 on phosphorylation of SMAD2 in
presence and in absence of exogenous TGFβ1.

## Slide 24
Hepatocellular carcinoma animal model
Bio-luminescence IVIS analysis. A) Control group. B) Oral LY. C) LY-loaded Nano micelles.
qPCR analysis. A) TGFβ1 mRNA analysis. B) TGFβR1 mRNA analysis; C) TGFβR2 mRNA analysis. Vh: Control; Ly OS: Oral administered LY; Ly iv: LY-loaded nano-micelles.
Chapter 4:

## Slide 25
Where are we Now????
Fabrication and functionalization of drug delivery systems starting from selection of suitable templates until to obtain layered capsules and self assembly are gained.
Homogenous colloidal calcium carbonate has been fabricated, Alternate polymers were assembled onto their surface by using Layer- by-Layer (LbL) technique.
Magnetic nanoparticles (MNPs) were designed by grafting with fluorescent molecule. Then, they were coated by biocompatible and biodegradable polymers.
Polymeric micelles optimized by control their chemical composition, exhibit good stability and capacity as drug delivery system.
Hybrid polymer integrated biological molecules such as lipid or protein were functionalized
Previous results indicate that integration cargo molecule compounds inside layer-by-layer assembly can protect them from the external environment or from the adverse conditions and enable their controlled release.
What is the next?????
Chemotherapy causes many physiological disorders for cancer patients due to non-selectivity for their targets leaving patients to suffer a lot. The aim in future is to prevent the normal cells to obtain the desired therapeutic response completely by using dual or triple combination of specific ligands and molecules. In addition we are planning to use animal model experiments to exploit direction of new drug delivery system.

## Slide 26
Third EBTN Best Oral Presentation
Nemany A. Hanafy, Concetta Nobile, Maria Luisa De Giorgi, Bhavna Ran, Yuan Cao, Gianluigi Giannelli and Stefano Leporatti “ LY2157299-Loaded Carriers Inhibiting Wound Healing in Hepatocellular Carcinoma” European Biotechnology Congress 2014, Lecce 15th -18th May 2014 (Oral Communication,)
Young investigator Bursary registartion
Nemany A. N. Hanafy, Alessandra Quarta, Riccardo Di Corato, Luciana Dini, Concetta Nobile, Maria Luisa De Giorgi , Sonia Carallo, Mariafrancesca Cascione, Rosaria Rinaldi, Isabel Fabregat, Stefano Leporatti.” ENCAPSULATION OF SHT-DNA, SIRNA AND POLYPEPTIDE -17 INSIDE HYBRID POLYMERIC NANO-PROTEIN FOLIC ACID (HPNP-FA) CARRIER AS TARGETED TGFΒ INHIBITOR FOR HEPATOCELLULAR CARCINOMA” Intentional EASL conference 2016, Barcelona 13th -17th April (Bursary) .
Awards
Grants
Membership of the European Association for the Study of the Liver 2016 and is entitled to all association membership benefits.
Membership of the European Association for the Study of the Liver 2017 and is entitled to all association membership benefits.
Invitation for chapter/2018
Special Issue Nanocolloids for Nanomedicine and Drug delivery, http://www.mdpi.com/journal/nanomaterials/special_issues/Nanocolloids_Nanomedicine
Our Contributions

## Slide 27
Nemany A. N. Hanafy, Alessandra Quarta, Riccardo Di Corato, Luciana Dini, Concetta Nobile, Maria Luisa De Giorgi , Sonia Carallo, Mariafrancesca Cascione, Rosaria Rinaldi, Isabel Fabregat, Stefano Leporatti. Encapsulation of SHT-DNA, SIRNA and polypeptide -17 inside Hybrid polymeric nano-protein folic acid (HPNP-FA) carriers as targeted TGF beta inhibitor for Hepatocellular carcinoma. J Mater Sci: Mater Med (2017) 28: 120.
N.A.N. Hanafy, A. Quarta, M.M. Ferraro, L. Dini, C. Nobile, M.L. De Giorgi, S. Carallo, C. Citti, G. Cannazza, R. Rinaldi, G. Giannelli and S. Leporatti. Polymeric Nano-micelles as Novel cargo-carriers for LY2157299 Liver Cancer Cells Delivery. Nano medicine, 2017 (under correction).
Nemany A. N. Hanafy, Maria Luisa De Giorgi, Concetta Nobile, Mariafrancesca Cascione, Ross Rinaldi and Stefano Leporatti. CaCO3 rods as chitosan polygalacturonic acid carriers for brompyruvic acid delivery. Science of Advanced Materials Journal. 2016. 8(3);514-523.
Nemany A.Hanafy, Marzia Maria Ferraro, Antonio Gaballo, Luciana Dini, Vittorianna Tasco, Concetta Nobile, Maria Luisa De Giorgi, Sonia Carallo, Ross Rinaldi and Stefano Leporatti. Fabrication and Characterization of ALK1fc-Loaded Fluoro-Magnetic Nanoparticles Rods for Inhibiting TGF β1 in HCC. RSC Adv., 2016, 6, 48834–48842.
Chiara Dionisi, Nemany Hanafy, Concetta Nobile, Maria Luisa De Giorgi, Ross Rinaldi,Sergio Casciaro, Member, IEEE, Yuri M. Lvov, and Stefano Leporatti. Halloysite Clay Nanotubes as Carriers for Curcumin: Characterization and Application. Nanotechnology, IEEE. 2016; 15(5):720-724.
C. Buccoliero, D. Consolante, F. Dituri, S. Mancarella, N. Hanafy, A. Mancinelli , P. Trerotoli , S. Leporatti4 , C. Pisano , G. Giannelli . FRI-053 A TGF-Β RECEPTOR I KINASE INHIBITOR, GALUNISERTIB (LY2157299) INHIBITS HEPATOCELLULAR CARCINOMA PROGRESSION IN IN VIVO EXPERIMENTAL MODELS. Journal of Hepatology 2016 vol. 64 | S425–S630.
Nemany Hanafy, Concetta Nobile, Maria Luisa De Giorgi , Ross Rinaldi and Stefano Leporatti “Control of Colloidal CaCO3 suspension by using biodegradable polymers during fabrication” Beni-Suef University Journal of Basic and Applied Sciences, 2015;4: 60-70.
Our Publications

## Slide 28
8) N.A.N. Hanafy, M.L. De Giorgi, C. Nobile, G. Giannelli, A. Quarta, S. Leporatti P0253: Inhibition of glycolysis by using nanolipid bromopyruvic chitosan carrier is a promising tool to prevent HCC invasiveness Journal of Hepatology 2015; 62: S401.
9) Nemany A. Hanafy, Concetta Nobile, Maria Luisa De Giorgi, Bhavna Ran, Yuan Cao, Gianluigi Giannelli and Stefano Leporatti “LY2157299-Loaded Carriers Inhibiting Wound Healing in Hepatocellular Carcinoma. Journal of Biotechnology, Special Issue EuroBiotech abstract, published, 2014.
10) Nemany A. Hanafy, Concetta Nobile, Maria Luisa De Giorgi, and Stefano Leporatti “Curcumin bio\nano-template for building layer by layer capsules” Nanomedicine conference Mod. S5 Rev. 3 del 24/07/2014.
http://www.iss.it/binary/tesa/cont/Modulo_S5.Programma_Convegno_Rev3_Nanomedicine_17_19_settembre_2014_1.pdf.
11) del Mercato, L.L., Leporatti, S., Ferraro,M., Hanafy,N.A., Rinaldi,R., Parak, W.J., Carregal-Romero, S., Multilayer Polyelectrolyte Capsules for Sensing and Drug Delivery: Fundamentals and Application, submitted 2014 by Pan Stanford Publishing Pte Ltd www.panstanford.com.
Other Publications
SAFER, A.M., M. AFZAL,M., Hanafy, N.A., SOSAMMA,O., and MOUSA,S.A. “Green tea extract therapy diminishes hepatic fibrosis mediated by dual exposure to carbon tetrachloride and ethanol: A histopathological study. EXPERIMENTAL AND THERAPEUTIC MEDICINE, 2015; 9: 787-794.
A.M. Safer, Anindito Sen , Nemany Hanafy and Shaker Mousa. Quantification of the healing effect in hepatic fibrosis induced by Chitosan Nano-encapsulated Green Tea in Rat Model Studied – at Ultrastructural level. Journal of Nanoscience and Nanotechnology, 2015; 15:1–7.
Abdel Majeed. M. Safer, Nomany Hanafy, Dhruba J. Bharali, Huadong Cui, and Shaker A. Mousa. Effect of Green Tea Extract Encapsulated Into Chitosan Nanoparticles on Hepatic Fibrosis Collagen Fibers Assessed by Atomic Force Microscopy in Rat Hepatic Fibrosis Model. Journal of Nanoscience and Nanotechnology, 2015; 15:1–8.

## Slide 29
Workshops
Marie Curie fellowship
1-Workshop entitled “Omics meet translational research” organized by the Marie Curie ITN action “ITLiver” – IDIBELL and the Societat Catalana de Biologia (SCB) September 25-26th 2013, Barcelona, Spain. Organizer: Dr. Isabel Fabregat, Bellvitge Biomedical Research Institute (IDIBELL).
2-Workshop entitled “3dimensional (3D) cell cultures and drug discovery”. Location: Vienna, Austria. Organizer: Dr. Wolfgang Mikulits, Medical University of Vienna, 2014.
3-Workshop entitled “Intellectual property and commercialization”. Location: LUMC, Netherlands, 2014 . Organizer: Dr. Peter ten Dijke.
4-Workshop entitled “HCC From Molecular Pathogenesis to Targeted Therapy”. Location: Fulda, Germany, 2015. Organizer: SFB/TRR77 and Dr. Steven Dooley, University of Heidelberg.
5-Workshop entitled “Management of chronic liver diseases in the clinic”. Location: Bari, Italy. Organizer: Dr. Gianluigi Giannelli, University of Bari, 2015. Department of Internal Medicine (UB).
PhD fellowship
1-Workshop entitled “National School of Optical Biosensors and Bio photonics” Location: Otranto, Italy, 2014.
2- Workshop entitled “School of Nano medicine” Location: Bari, Italy, December 2-4, 2015.

## Slide 30
Conferences
1.Nemany A. Hanafy, Concetta Nobile, Maria Luisa De Giorgi and Stefano Leporatti "Novel multidrug model carrier for cancer cells treatment” “IT-Liver Meeting” and International Workshop ” 3 Dimensional Cell Cultures and Drug Discovery” Vienna (Austria) , 27-28 February 2014 (Poster Communication)
2.Nemany A. Hanafy, Concetta Nobile, Maria Luisa De Giorgi and Stefano Leporatti “ Control of Colloidal CaCO3 suspension during template fabrication by using biodegradable polymers” 2nd International Basic and Applied Sciences (ABAS) AIN-Sokhna Egypt, 2-4 April 2014 (Oral Communication)
3.N. A. Hanafy, C. Nobile, M.L. DeGiorgi and S. Leporatti "Encapsulation of curcumin inside carriers doped with poly (acrylic acid)" BioNanomed2014, Krems (Austria) 26-28 Marzo 2014 (Poster Communication) Topic: Nanomaterials for Biomedical Application
4.Nemany A. Hanafy, Concetta Nobile, Maria Luisa De Giorgi, Bhavna Ran, Yuan Cao, Gianluigi Giannelli and Stefano Leporatti “ LY2157299-Loaded Carriers Inhibiting Wound Healing in Hepatocellular Carcinoma” European Biotechnology Congress 2014, Lecce 15th -18th May 2014 (Oral Communication, Awarded as Third EBTN Best Oral Presentation)
5.Nemany A. Hanafy, Concetta Nobile, Maria Luisa De Giorgi, and Stefano Leporatti “Curcumin bio\nano-template for building layer by layer capsules” Nanomedicine, Viterbo (Italy), 17th-19th September 2014,(Oral presentation).
6. Nemany A. Hanafy, Concetta Nobile, Maria Luisa De Giorgi, and Stefano Leporatti“ Polymeric Nanocarriers: from Production to Medical application “European Biotechnology Days, Cluj-Napoca/ Romania , 9 - 11 October, 2014, Oral Communication.
7.Nemany A. Hanafy, Concetta Nobile, Maria Luisa De Giorgi, and Stefano Leporatti“ Novel CaCO3 rods as templates for producing chitosan-polygalacturonic acid micro/nanotubes and to encapsulate bromopyurvic acid“Nanotech. Italy 2014, Venice 26-28 November 2014.
8-Nemany A. Hanafy, Concetta Nobile, Maria Luisa De Giorgi, Ross Rinaldi, and Stefano Leporatti "Novel CaCO3 rods as templates for producing chitosan-polygalacturonic acid micro/nanotubes and to encapsulate bromopyurvic acid” NanotechItaly 2014, Venice 26th-28th November 2014 (Poster Communication).
9-Nemany A. Hanafy, Concetta Nobile, Maria Luisa De Giorgi and Stefano Leporatti“Encapsulation of Curcumin inside Carriers Doped with Poly(acrilyc acid)” BioNanoMed 2014, 5th International Congress Nanotechnology, Medicine & Biology 26th- 28th March, Krems 2014 (Poster Communication).
10-Nemany Hanafy, Chiara Dionisi, Concetta Nobile , Maria Luisa De Giorgi, Ross Rinaldi, Stefano Leporatti. Nanocarriers for cancer therapy. CNR meeting, Italy 2015.
11-Chiara Dionisi, Nemany A.N. Hanafy, Viviana Vergaro, Yuri M. Lvov and Stefano Leporatti “Halloysite Clay Nanotubes as Novel Carriers for Drug Delivery Euroclay 2015, Edingburgh 6th -10th July 2015 (Keynote Talk)
12-Nemany Hanafy, Concetta Nobile, Maria Luisa de Giorgi, Ross Rinaldi, and Stefano Leporatti “Nanocarriers per la Nanomedicina” Notte dei Ricercatori, Lecce, 2015.(Outreach).
13-Nemany A. Hanafy, Marzia Maria Ferraro, Antonio Gaballo, Luciana Dini, Concetta Nobile, Maria Luisa De Giorgi, Sonia Carallo, Ross Rinaldi and Stefano Leporatti. Fabrication and Characterization of ALK1fc-Loaded Fluoro-Magnetic Nanoparticles for Inhibiting TGF β in Hepatocellular Carcinoma (HCC). School of Nano medicine.Bari/Italy. December 2-4, 2015.

## Slide 31
Prof. Stefano
leporatti
Nemany Hanafy
Team Work
Prof. Isabel Fabregat
Dr. Maria Luisa De Giorgi
Dr. Concetta Nobile
Prof. Rosaria RINALDI
Prof. Luciana Dini
Prof. Antonio Gaballo
Dr. Alessandra Quarta
Couple: Dr Luigi Carbone
and Betty Perrone
Prof. Gianluigi Giannelli
First secondment
Second secondment

## Slide 32
Acknowldegment
Financial support of the REA research grant n° PITN-GA-2012-316549 (IT LIVER) from the People Programme (Marie Curie Actions) of the European Union’s Seventh Framework Programme (FP7/2007-2013) is gratefully acknowledged.
THANK YOU FOR YOUR ATTENTION !