## Slide 1: pp accelerator challenges and new technologies (magnets et al.)
Lucio Rossi
High Luminosity LHC Project Leader
I2FEST2019 - INFN&IHEP@Torino18Feb2019 - Cavallerizza Reale

## Slide 2: Content
FCC nominal parameter for hadrons
Critical Technologies (other than Magnets)
  Vacuum & Synchrotron radiation handling
  Cryogenics
  Beam handling (absorber, dump)
Magnets
  LHC and HL-LHC
  Roadmap for higher field in Europe: Nb3Sn
  HTS?

## Slide 3
parameter | FCC-hh |  |  | HE-LHC | HL-LHC | LHC
collision energy cms [TeV] | 100 |  |  | 27 | 14 | 14
dipole field [T] | 16 |  |  | 16 | 8.33 | 8.33
circumference [km] | 97.75 |  |  | 26.7 | 26.7 | 26.7
beam current [A] | 0.5 |  |  | 1.1 | 1.1 | 0.58
bunch intensity [1011] | 1 |  | 1 | 2.2 | 2.2 | 1.15
bunch spacing [ns] | 25 |  | 25 | 25 | 25 | 25
synchr. rad. power / ring [kW] | 2400 |  |  | 101 | 7.3 | 3.6
SR power / length [W/m/ap.] | 28.4 |  |  | 4.6 | 0.33 | 0.17
long. emit. damping time [h] | 0.54 |  |  | 1.8 | 12.9 | 12.9
beta* [m] | 1.1 | 0.3 |  | 0.25 | 0.15 (min.) | 0.55
normalized emittance [mm] | 2.2 |  |  | 2.5 | 2.5 | 3.75
peak luminosity [1034 cm-2s-1] | 5 |  | 30 | 28 | 5 (lev.) | 1
events/bunch crossing | 170 |  | 1000 | 800 | 132 | 27
stored energy/beam [GJ] | 8.4 |  |  | 1.3 | 0.7 | 0.36
FCC-pp collider parameters

## Slide 4
Beam vacuum induced dynamic effects [WP9]
Beam vacuum Magnet Cold Bore (Eurocircol WP4) [WP1]
CryoPlants efficiency [WP2]
Beam transfer devices [WP3]
Manufacturing technologies [WP4]
Robotics [WP14]
Surface-Vacuum parameters for beam-induced effects [WP13]
Architecture for magnets & machine protection [WP12]
Radiation Hardness Assurance [WP11]
Cryomagnet insulation vacuum [WP10]
Normal conducting magnets [WP5]
Transverse feedback [WP6]
Beam dumps [WP7]
Beam instrumentation [WP8]
FCC Special Technologies
JM Jimenez – FCC Amsterdam

## Slide 5
FCC-hh: beam screen evolution & tests
Simplified BS design in view of:
Mass production
Impedance optimization
e- cloud mitigation
latest version to be tested summer ‘18
Design optimisation:
Ribs removed; Optimization of thickness of copper and steel
Connection absorber/cooling tube, and welding positions
Measurements at KARA/KIT (pressure evolution) confirm MC vacuum simulations
Confident to use simulations for all vacuum design
Cold Sprayed Isolated Electrode
(e-cloud mitigation option)
M. Benedikt –
FCC Amsterdam

## Slide 6: Surface-Vacuum parameters for beam-induced effects
R&D for HL-LHC first, and further development for FCC-hh

## Slide 7: CryoPlants efficiency
CryoPlant efficiency is certainly a must: 30% possible gain
JM Jimenez – FCC Amsterdam

## Slide 8
Beam power handling: robust low-loss collimation
Complete designs of collimation insertions, main issue: sustain beam lifetime of 12 mins (12 MW loss)
260 kW
225 kW
1 MW
50 kW/m
<5 kW
Primary Collimators
Active length halved
Max. power reduced from 260 kW to 80 kW
50 to 100 kW considered OK
Old design
max power density
800 Wcm-3
total power
225 kW
total power
92 kW
New design
max power density
115 Wcm-3
1st Secondary Collimator
FLUKA simulations highlighted four critical points
Arc protection Protection design offers sufficient margin
M. Benedikt –
FCC Amsterdam

## Slide 9: Hadron Colliders are ruled by: Ebeam = 0.3 R * B (TeV; km; T)
< 10 y to double field: 2 T MR 4 T Tevatron
> 20 y to double again in SC:  8 T of LHC
Consideration on LHC
Designed for 8.33 T (14 TeV c.o.m.) with margin to go to 9 T (15 TeV c.o.m)
Today operating at 7.75 T (13 TeV)
8.33 T in 2021 possibly
9 T may be in 2026/2030 with HiLumi but very difficult (trade off with loss of lumi)

## Slide 10: The 25 y LHC construction time line
Striking: only 2 y to make a design «near to final». The conductor was almost there! (thanks to SSC)

## Slide 11: The key factor: superconductor (but not the only factor!)
Developing SC is the key in SC accelerators.
The perfection of LHC superconductor is such that we basically «forget» the SC effects and is the base of the repeatibility and optimal performance of the collider

## Slide 12: High Luminosity LHC -1 New Triplets IT QUADs
SC Links
D1
DFX
CP
Q3
Q2b
Q2a
Q1
Service gallery (UR)
Connection to LHC (UL)
TAXS
DFM

## Slide 13: High Luminosity LHC – 2 New Matching section
Crab cavities
D2
Collimators
TAXN
Service cavern
UA gallery
Q4
(BBLR)

## Slide 14: 16 Sept 2018
  China will provide 12 units of CCT magnets for HL-LHC before 2022
  A 0.5m model is under construction, and 2.2m prototype to be fabricated and tested by June 2019

## Slide 15: High Luminosity LHC 11 T dipole in the DS7
Present layout of the DS region:
New layout with one collimator and two 11T dipoles:
15.660 m
15.660 m
11 T dipole
11 T dipole
By-pass with collimator
LHC layout
HL-LHC layout

## Slide 16: First 11 T prototype (full size) on test @ CERN
Result not positive (<10 T)
Magnet under rework to test second aperture alone

## Slide 17: Review of 11 T results
Results on short models before test of long proto
Result of the first «new design» to cure «erratic» behaviour (July 2018)

## Slide 18: Now 11 T in full swing for production great care in QA given the sensitivity of Nb3Sn

## Slide 19: IT quadrupole. Increase in field btu also in size wrt LHC. Very relevant also for FCC magnets

## Slide 20: Result of IT quadrupoels
Best HF magnet ever tested in terms of behaviour (not max field)
Final conductor, final prestress procedure
This magnet had a too high prestress The last higher quench have fast ramp rate
All magnets have exceptional memory (no low current quench after thermal cycle)

## Slide 21: Construction of the 1st and 2nd long (7.5 m!) IT Quad in full swing (also in USA)
Making long magnets in Nb3Sn is not granted but we are confident for Hilumi: the project is big but not enormous (about 30 magnets of 4.2, 5.5 and 7.2 m length)

## Slide 22: A step between HL-LHC and a post-LHC?
Report under editing (by O. Bruning) in 2018 (not yet published).
Pushing to 15 TeV (ultimate dipole field of 9 T): not impossible, in the HiLumi time, sensible less availability, trade off with less lumi maybe not convenient, TBD
Pushing the energy using 11 T as middle cell dipole (1/3) gaining 11% energy: 15.5-16.6 TeV (nominal-ultimate field).
  Most probably not convenient in terms of cost, personnel resources,time (big installation) and very difficult for optics. I think is impossible to «touch» only the magnets. And needs at least a design revision of the HiLumi 11 T.
  Not for tomorrow, not easy, not cheap, not «transparent» for other CERN development, not a terrific gain…
Personal opinion: forget it
Personal opinion: unlikely

## Slide 23
FCC-hh injector options: a 1.3 TeV injection may allow smaller cheaper HE magnets
Baseline:
LHC @ 3.3 TeV
Alternative:
scSPS @ 1.3 TeV
Total of O(5.5 km) superconducting bends in transferlines from LHC, at 7.2 T
O(6.5 km) normal-conducting bends from SPS, at 1.8 T
Current baseline:
Injection energy 3.3 TeV LHC
 Field-swing FCC-hh like LHC
Alternative options:
Injection from SPSupgrade around 1.3 TeV
SPSupgrade could be based on fast-cycling SC magnets, 6-7T, ~ 1T/s ramp, cf. SIS 300 design
SPSupgrade would also be an ideal injector for HE LHC (as alternative to the 450 GeV SPS)
Better option than keeping alive LHC

## Slide 24
The critcal point to reach 16 T: superconductor!
Worldwide FCC Nb3Sn program
Main development goal is wire performance increase:
Jc (16T, 4.2K) > 1500 A/mm2 50% increase wrt HL-LHC wire
Reduction of coil & magnet cross-section
3150 mm2
~1.7 times less SC
~10% margin
HL-LHC
~10% margin
FCC ultimate
5400 mm2
Conductor activities for FCC started in 2017:
Bochvar Institute (production at TVEL), Russia
KEK (Jastec and Furukawa), Japan
KAT, Korea
Columbus, Italy
University of Geneva, Switzerland
Technical University of Vienna, Austria
SPIN, Italy
University of Freiberg, Germany
  In addition, agreements under preparation:
  Bruker, Germany
  Luvata Pori, Finland
This is difficult
Notes: New slide from Davide.
Showing that conductor development is launched at international level, Russia, Japan, (Korea and Europe in preparation)
Underline importance of that development as main cost driver for the hadron collider machine.

## Slide 25
16 T dipole design activities and options
Cos-theta
Blocks
Common coils
Short model magnets (1.5 m lengths) will be built from 2018 – 2022
Russian 16 T magnet program launched by BINP recently.
Swiss contribution
Canted
Cos-theta
H2020
INFN
CEA
CIEMAT
PSI
LBNL
FNAL
Very good: gaining resources and supports by various labs…
But it is wise? Choose a design and concentrate on it? …
This is a personal opinion but seems to me evident... And 16 T will prove to take longer than previous projection  evident by the new strategy by CERN
Construction of hh launched in the 2020s the only way is to aim at 14 T range, 20% above HiLumi

## Slide 26: Progress in magnets R&D
2018: FRESCA2
(14.6 T at 1.9 K, 100 mm)
We need to fill here for FCC/HE
HiLumi

## Slide 27: And the HTS ? Only way to reach 16-25 T
15 T is the HTS crossing point

## Slide 28: 20 T or more: Super proton-proton Collider in China (after CEPC)
 | LHC | FCC | SppC
Circumference (km) | 26.7 | 97.5 | 100
Dipole field (T) | 8.33 | 16 | 12…24
C.o.M. energy (TeV) | 14 | 100 | 70…125
Courtesy of Q. Xu, IHEP, CN

## Slide 29: CN high-field magnet R&D
Baseline design
  Tunnel circumference: 100 km
  Dipole magnet field: 12 T, iron-based HTS technology (IBS)
  Center of Mass energy: >70 TeV
Upgrade phase
  Dipole magnet field: 20…24T, IBS technology
  Center of Mass energy: >125 TeV
Development of high-field superconducting magnet technology
  Starting to develop required HTS magnet technology before applicable iron-based wire is available
  ReBCO & Bi-2212 and LTS wires be used for model magnet studies and as an option for SppC: stress management, quench protection, field quality control and fabrication methods
Conceptual design of common coil 12T dipole
Top priority: reduce cost!
Instead of increasing field
Courtesy of Q. Xu, IHEP
Courtesy of Q. Xu, IHEP, CN
IBS structure

## Slide 30: Comments on HTS (YBCO/REBCO)
Working on new type of cables and magnets: reached 3.5 T, expected 7 T in March 2019
HTS situation and perspective
Very expensive (5 times than Nb3Sn)
Magnets are easier: great stability, no training!
May work in He gas at 20 K: big advantage for power consumption and easier system…
Basic R&D for 5-10 years to reach maturity is needed. Last 3 y has doubled performance! A solenoid of 32 T has been tested successfully.
We would not be alone… plenty of Institute (and companies) work on HTS
This is the ground for basic focus R&D.

## Slide 31
Trying the magnets of the future… 20 tesla or more...
Working on Non-Insulated coils…

## Slide 32
FCC-hh
20+ T is not out of reach

## Slide 33: Conclusion
The program for FCC/He is under scrutiniy by the EU strategy
Maybe a better focus on some objectives and a reduction of those objectives may make the program more feasible.
A 14 T dipole (an HE-LHC of 24 TeV c.o.m., FCC-hh at 85 TeV) based on improved HiLumi superconductor is really feasable for R&D today.
The 16 T is still a long way to be demonstrated: it can, but it needs FOCUS and requires true synergy not just sum of various labs effort;
HE-LHC needs a different optimization for the magnet system and collider than FCC (but the SAME technology R&D) (personal opinion).
If there is an intermediate step (LHeC, or a lepton collider) that pushes 5-10 years back the post-LHc pp collider, then HTS is probably the best solution.
Embracing too large and unfocused R&D (generic High Field magnets) maybe not the best choice now for a project ready in the ‘30s…
From my talk at:

## Slide 35
15 T dipole demonstrator (US-MDP)
All coil parts, structural components and tooling are available at FNAL
Coil fabrication and the work with mechanical structure are in progress
First magnet test in September 2018
Iron Laminations
AL I-Clamps
Fillers
Axial Rods
End Plates
StSt Skin