## Slide 1: Progress of the HTS & HFS Magnet R&D for Future High-energy Accelerators
Qingjin XU
Institute of High Energy Physics (IHEP),
Chinese Academy of Sciences (CAS)
May 25 2018

## Slide 2
SPPC Magnet Design Scope
Domestic Collaboration Towards HTS SPPC
Conceptual Design of the 12T IBS Dipole Magnet
High Field Dipole Magnet R&D
fabrication and test of the 1st model dipole magnet
plan for the 2nd model dipole
CERN-China HL-LHC Collaboration
Summary
Contents

## Slide 3: SPPC Magnet Design Scope (V201701)
Main dipoles
Field strength: 12~24 (Upgrading) Tesla
Aperture diameter: 40~50 mm
Field quality: 10-4 at the 2/3 aperture radius
Outer diameter: 650-900 mm in a 1.5 m cryostat
Tunnel cross section: 6 m wide and 5.4 m high
6-m Tunnel for CEPC-SPPC
SPPC
100 km in circumference
C.M. energy 70-150 (Upgrading) TeV
Timeline
Pre-study: 2013-2020
R&D: 2020-2030
Eng. Design: 2030-2035
Construction: 2035-2042
Conceptual design of the SPPC 12-T magnet with IBS and common coil configuration
SPPC collider
CEPC collider
CEPC booster

## Slide 4: SPPC Magnet Design Scope
Baseline design
  Tunnel circumference: 100 km
  Dipole magnet field: 12 T, iron-based HTS technology (IBS)
  Center of Mass energy: >70 TeV
  Injector chain: 2.1 TeV
Upgrading phase
  Dipole magnet field: 20 -24T, IBS technology
  Center of Mass energy: >125 TeV
  Injector chain: 4.2 TeV (adding a high-energy booster ring in the main tunnel in the place of the electron ring and booster)
Development of high-field superconducting magnet technology
  Starting to develop HTS magnet technology before applicable IBS wire is available
  ReBCO & Bi-2212 and LTS wires be used for model magnet studies and as options for SPPC: stress management, quench protection, field quality control and fabrication methods
Top priority: reducing cost!
Instead of increasing field
Make IBS the high-field “NbTi”
Conductor in 10 years!

## Slide 5
Goal：
1) To increase the Jc of iron-based superconductor (IBS) by 10 times, reduce the cost to 20 Rmb/kAm @ 12T & 4.2K, and realize the industrialization of the conductor;
2) To reduce the cost of ReBCO and Bi-2212 conductors to 20 Rmb/kAm @ 12T & 4.2K;
3) Realization and Industrialization of IBS magnets and SRF cavities.
Working groups：1) Fundamental sciences study; 2) IBS conductor R&D; 3) ReBCO conductor R&D; 4) Bi-2212 conductor R&D; 5) Performance evaluation; 6) Magnet and SRF technology.
Domestic Collaboration for HTS R&D
“Applied High Temperature Superconductor Collaboration (AHTSC)” formed in Oct. 2016.
Including 18 institutions and companies in China. Regular meeting every 3 months.
Proposal for
Strategic Priority Research Program
of Chinese Academy of Sciences (CAS)
Science and Technology Frontier Research
for High Field Applications of High Temperature Superconductors
Ranked No. 1 in 7 candidates
by Academic Committee of CAS !

## Slide 6
Progress on IBS wires
Latest transport property of IBS tape (2017):
Short tape (~4 mm wide, 0.3 mm thick):
Ic~423 A (Jc>1450 A/mm2) @ 4.2 K, 12 T
100 meter long tape:
Jc>200 A/mm2 @ 4.2 K, 12 T
Supercond. Sci. Technol. 31 (2018) 015017
Y. Ma (IEECAS) et al.
115 meter long 7-core tape
IEEE TAS 27 (2017) 7300705
Key steps to the application

## Slide 7
The 12-T Fe-based Dipole Magnet
Yoke OD
500mm
Strand | diam. | cu/sc | RRR | Tref | Bref | Jc@ BrTr | dJc/dB
IBS | 0.802 | 1 | 200 | 4.2 | 10 | 4000 | 111
Design with expected Je of IBS in 2025
Io=9500A
The required length of the 0.8 mm IBS is 6.1 Km/m
For 100-km SPPC, 3000 tons of IBS is needed
Target cost of IBS: 20 RMB (~2.6 Eur) /kAm @12 T

## Slide 8
The 12-T Fe-based Dipole Magnet
Field quality in the aperture
<3*10-4 within 2/3 bore
(ROXIE simulation results)
Field quality | 2D with Rf= 13.3mm | 3D with Rf= 8/13.3 mm
b3 | 0.45 | 0.79/1.91
b5 | 1.01 | -0.65/-2.24
b7 | 0.46 | 0.08/0.67
b9 | -0.27 | -0.13/-0.22
a2 | 3.53 | -1.00/-2.31
a4 | 0.49 | -0.46/0.69
a6 | 0.33 | 0.26/2.49
a8 | 0.58 | -0.12/0.84
a10 | 2.23 | 0.06/2.18
Flare ends

## Slide 9
R&D of 12T Twin-aperture Dipole Magnet
Components and assembly
3d coil layout
NbTi+Nb3Sn, 2*ф10 aperture
All HTS, 2*ф40 aperture
3D magnetic field distribution
Magnetic flux distribution
Nb3Sn+HTS, 2*ф20 aperture
R&D Roadmap for the next 10~15 years

## Slide 10
Cabling Coil winding HT VPI Magnet assembly Test
Fabrication of the 1st model dipole magnet (NbTi+Nb3Sn)
R&D of 12T Twin-aperture Dipole Magnet
Cabling Machine
Rutherford Cable
Coil Winding
Heat Reaction
VPI
Magnet Assembly
VPI Coil Package
Impregnated
Coil

## Slide 11
10.2 T @ 4.2 K dipole field
in two apertures
(Performance limited by NbTi coils)
1st test result of the 1st high-field dipole magnet in China Feb. 2018
Magnet under test @ Hefei
Magnet fabrication @ Beijing
Test system setup @ Hefei
R&D of 12T Twin-aperture Dipole Magnet

## Slide 12
Next step：Replace NbTi coils with new Nb3Sn coils to further increase the field，and insert the IBS coil to test its high field performance.
R&D of 12T Twin-aperture Dipole Magnet
IBS coil
2nd model dipole magnet(Nb3Sn+IBS)
2*100m IBS tapes
IEECAS

## Slide 13
CERN & China Collaboration
Making 12 units CCT corrector magnets for HL-LHC before mid 2021
A 0.5m model magnet to be fabricated and tested by May or June 2018
0.5m model magnet
China Version
0.5m model magnet China Version
0.5m model magnet
CERN Version

## Slide 14: Summary
SPPC design scope: 12 T IBS magnets to reach 70TeV with 100 km circumference. Upgrading phase: 20~24 T IBS magnets to reach 125~150 TeV.
Strong domestic collaboration for the advanced HTS conductor R&D: Make IBS the High-Tc and High-Field “NbTi” conductor in 10 years!
R&D of high field magnet technology: 1st model dipole (NbTi+Nb3Sn) reached 10.2 T @ 4.2 K in two apertures; 2nd model dipole (Nb3Sn+IBS) to be fabricated and tested soon.
CERN & China Collaboration: Making 12 units CCT corrector magnets for HL-LHC before mid 2021.

## Slide 15
Thanks for your attention!