## Slide 1
FOOT calorimeter
Status Report
Crystals
Photodetector
Readout
Mechanics
Contributions by:
S. Argiro’
R. Arteche Diaz
N. Bartosik
G. Giraudo
N. Pastrone
L. Scavarda
P.P. Trapani
Piergiorgio Cerello

## Slide 2
FOOT calorimeter
Status Report
Crystals
Photodetector
Readout
Mechanics

## Slide 3
BGO crystals now available
As many as we need
Stored in polystyrol boxes at CERN (5 crystals/box)
Crystal dimensions:
  Approx. 2.0 ⨉ 24 ⨉ 2.9 cm3
Crystal transmission curves:
  Ongoing Measurement at CERN
2
3
24
BGO Crystals

## Slide 4
BGO Crystals
S08369 Transmission curve – pre/post annealing

## Slide 5
4 quarters of 80 BGO crystals each
20 cm
2.0 cm
2.0 cm
24 cm
FOOT calorimeter
2.9 cm
2.9 cm
Weight: 1027 g
Total weight: 329 Kg

## Slide 6
FOOT calorimeter
Status Report
Crystals
Photodetector
Readout
Mechanics

## Slide 7
SiPM
Crystal 7 cm long
Carbon beam
120 MeV/u
190 MeV/u
400 MeV/u
Proton beam
120 MeV
170 MeV
400 MeV
70 MeV
Calorimeter preliminary test at CNAO

## Slide 8
SiPM test setup
32 channels
8 channels
FAN OUT
Digitizer
Crystal (7 cm)
SiPM
53 V
Amplifier
± 1.75 V
Beam
SiPM Hamamatsu
pitch: 50 μm
voltage breakdown: 52 V
Power supply
Digitizer CAEN
V1742

## Slide 9
Wave Form
Proton beam, 170 MeV, 7 cm crystal long
Same event acquired in the 8 channels of Digitizer
sum over of the whole Tile
No position dependency
Ratio between the sigma and average value of the amplitude distribution of 8 signal channels acquired in one event. Then the distribution is plotted for all events.
Same wave form for all channels

## Slide 10
Protons
Carbons
Signal Integration
Anomalous behaviour for proton beams at 220 MeV: what happened?
Important result: Mean value of signal integrations increases with energy

## Slide 11
Protons
Carbons
Signal Amplitude
Important result: Mean value of signal amplitude increase with energy up to 120 MeV/A carbon
Anomalous behaviour for proton beams at 220 MeV: what happened?

## Slide 12
Energy Resolution - Integration
Protons
Carbons

## Slide 13
Energy Resolution - Amplitude
Protons
Carbons

## Slide 14
Linearity
Amplitude
Linearity between the beam energy and the mean value of the signal
Integration

## Slide 15
PMT
Crystal 24 cm long
Crystal 7 cm long
Carbon beam
120 MeV/u
190 MeV/u
260 MeV/u
330 MeV/u
400 MeV/u
Calorimeter preliminary test at CNAO

## Slide 16
1 channels
Attenuator
Digitizer
Crystal (7 cm)
PMT
+1200V
PMT test setup
1 channels
High Voltage Power Supply
Beam

## Slide 17
1 µs
Carbon beam, 120 MeV, Crystal 7 cm long
Integration of all signals
Integration on all range
PMT Signal Integration

## Slide 18
Fluctuations
maybe attenuator?
PMT Signal Integration
!
Other tests will have to be performed …
Channels
Carbon beam, 120 MeV, Crystal 7 cm long

## Slide 19
SiPM readout board scheme
Readout board for SiPM with 15 um microcell size
will be available in about 2 weeks
Test at CNAO most likely on Jume 24th-25th
Next tests at CNAO:
Test on SiPMs with 15-20 μm pitch with 15 cm and 24 cm long crystals

## Slide 20
FOOT calorimeter
Status Report
Crystals
Photodetector
Readout
Mechanics

## Slide 21
Likely readout scheme, if 15 μm SiPM prove to be linear – as expected
Readout
3x3 readout boards with 9 output channels (1/crystal)
Amplification to be defined
Output to Digitizers
It’s the simplest solution

## Slide 22
FOOT calorimeter
Status Report
Crystals
Photodetector
Readout
Mechanics

## Slide 23
240 (239.9)
The crystals
29 (28.8)
29 (29.1)
20 (20.3)
20 (20.2)

## Slide 24
Matrix 3x3 crystals
Plastic box
Module definition

## Slide 25
arrangement of 32 modules
1 plastic box design
Modules layout – option 1

## Slide 26
Single arrangement of 288 crystals
16 plastic box designs
Modules layout – option 2

## Slide 27
397 mm
Modules layout – front view

## Slide 28
The box houses 9 crystals
ABS reinforced or similar material E≈4 GPa
3D printing (?)
Max displacement ≈ 70μm
Max stress 9,5∙105 Pa
(ABS Tensile strength ≈ 25∙106)
Module case

## Slide 29
FOOT calorimeter
Status Report
Plans
complete crystal transparency measurements
test at CNAO with 15 um SiPM (end of June)
freeze crystal size (test + simulation)
build prototype of 9 modules case
freeze readout chain
start procurement
start crystal calibration
R/O + calibration sw development