## Slide 1
张恒彬
2017年5月23日
Zhang Hengbin
7 / 26 / 2019
Qian Xuesen Laboratory of Space Technology
Two-dimensional graphene superconducting and hot electron bolometer research
based-on metal atoms surface modification

## Slide 2: Graphene
Two-dimensional honeycomb lattice structure composed of single layer carbon atoms
Three σ bonds are formed by the interaction of sp2 hybrid orbitals between adjacent carbon atoms
The basis of the allotropes that make up zero-dimensional fullerenes, one-dimensional carbon nanotubes, and other carbons such as three-dimensional graphite
Wikipedia.org

## Slide 3: Graphene
Zero band gap structure, unique light absorption characteristics, high electron mobility(15000 cm2⋅V−1⋅s−1 ) and high thermal conductivity(5300 W⋅m−1⋅K−1).
Rev.mod.phys.2009,(81),109

## Slide 4: Graphene photodetector
Thomas Mueller et al. NATURE PHOTONICS. 2010, 40
Zheyu Fang et al. NATURE NANOTECHNOLOGY. 2012, 19
Photocurrent enhancement: 800%
transfer of hot electrons generated in the antenna structure upon plasmon decay
direct plasmon-enhanced excitation of intrinsic graphene electrons due to the antenna
Graphene-antenna sandwich
Metal–graphene–metal (MGM)
Asymmetric interdigital electrode
break the mirror symmetry of the internal electric-field
maximum photoresponsivity: 1.5mA⋅W-1
optical communication speed: 10 Gbit s-1

## Slide 5: Graphene photodetector
You-Chia Chang et al. NATURE NANOTECHNOLOGY. 2014, 31
Marco Furchi et al. PHYSICAL REVIEW B. 2011, 12
Distributed Bragg reflectors (DBR)
quarter-wavelength-thick layers of alter­nating materials
light absorption: 60%
Responsivity: 21mA·W–1
Optical microcavity
Graphene double-layer heterostructure
Stacked graphene+Tunnel barrier
photoexcited hot carriers tunnel from top layer into the bottom layer
visible to the midinfrared range
mid-infrared responsivity : 1A·W-1

## Slide 6: Graphene photodetector
Photovoltaic (PV)
Photo-thermoelectric(PTE)
Bolometric
Nat Nanotech. 2014,9,10
Build-in electric field
local chemical doping
split gates
graphene-metal junction
Photocurrent direction
p-n to n-p
p-p+ to p+-p
Seebeck effect
VPTE = (S1 – S2)Δte
Dominate in graphene p-n and suspended graphene
Mott formula
Mechanism: dP~dT
Semiconductor
Superconductor
Without p–n junction

## Slide 7: Graphene HEB
Bolometric(HEB)
Response time:
Sensitivity:
Ideal HEB:
Graphene HEB
Low heat capacity
(T<5K at Vg~10 V, for a 1 um2 sample)
Weak electron-phonon coupling
limitation:
Weak temperature-dependent resistance, no thermometer

## Slide 8: Graphene HEB
1. Strengthen the temperature dependence of the heat
resistance
2. Sense the temperature from noise thermometer
Advantage:
Fast response, low noise, far preceding HEB
Disadvantage:
Complicated fabrication process
Nat Nano 2012, 88,10
Appl. Phys. Lett. 2011, 99, 013504
Phys.Rev.Lett 2012, 109,1056805

## Slide 9: Graphene STJ HEB
Strong tunneling
resistance dependence
Searching for
Strong temperature-dependent resistance
Simple device fabrication
High quality tunnel junctions
Research path :
Strengthen R-T
Thermally isolation
Graphene STJ
Surface modification
The superconducting
proximity effect

## Slide 10: Graphene STJ HEB
Diffusive transport
Appl. Phys. Lett., 2012,100,(15).
Nature., 2007. 446,7131.
Solutions:
Improve the quality of the tunnel junctions
Induce the intrinsic two-dimentional superconducting of graphene
Proximity effect

## Slide 11: Graphene STJ HEB
Hard mask fabrication
ZnO nanowire
Graphene
Al
Sprinkle a handful of zinc oxide nanowires to a free clean substrate
Pick up a suitable nanowire by two glass manipulator arms and put it on top of the graphene block
Cover the graphene all around with scotch tape, and the tape is just pressed on the both ends of the nanowire
Evaporated aluminum (70nm)/ palladium (7nm) membrane on the whole chip
Pull off the tape and remove the nanowire by the manipulator arms

## Slide 12: Graphene STJ HEB
Micromanipulation system
Final optical photograph before and after remove the ZnO nanowire

## Slide 13: Graphene STJ HEB
Transport measurement
High quality:
Dirac point: VD =-10V,
Mobility: 7.9×103 cm2 / V·s
Residual resistance: 90%R0 (130mK)
Oxidation of electrode

## Slide 14: Graphene STJ HEB
superconductor
e
h
x
y
Zero-bias anomaly (ZBA)
Andreev reflection
Precursor of superconducting of graphene!

## Slide 15: The next to do
Further improve the barrier quality to induce the two-dimentional graphene superconducting
Investigate the in situ doping with Ca atoms and the influence to the graphene intrinsic superconducting
Characterize the photon response of the GSTJ and improve its performance

## Slide 16
Thanks for your attention！