## Slide 1: Trapped Flux Sensitivity in the Low Amplitude Radio-Frequency Regime
Mattia Checchin

## Slide 2: Trapped flux surface resistance
⇒ temperature-dependent part of the surface resistance
⇒ intrinsic residual resistance
Trapped flux surface resistance
H. F. Hess et al., Phys. Rev. Lett. 62, 214 (1989)
Cooldown
Pinning points
Trapped vortices
—flux trapping efficiency
—external magnetic field
—trapped flux sensitivity

## Slide 3: —flux trapping efficiency
Seems correlated to higher number of very low angle grain boundaries
Well described by a statistical argumentation of pinning and energetics of vortex stability
Lower
M. Checchin, M. Martinello et al. to be published
M. Martinello, TTC workshop RIKEN, Nishina center, Japan (2018)
S. Posen et al., J. Appl. Phys. 119, 213903 (2016)
Low angle GBs
Bad expulsion
Good expulsion
mis.
angle

## Slide 4
Trapped Flux Sensitivity
——
Experiments

## Slide 5: Trapped flux sensitivity at 1.3 GHz
Trapped flux sensitivity:
Non-monotonic trend of as a function of mean-free-path
  M. Martinello et al., App. Phys. Lett. 109, 062601 (2016)
  D. Gonnella et al., J. App. Phys. 119, 073904 (2016)
N-doping cavities present higher sensitivity than standard treated cavities
Sensitivity is dependent on the accelerating gradient
  C. Benvenuti et al., Physica C 316, 153 (1999)
  M. Martinello et al., App. Phys. Lett. 109, 062601 (2016)
  D. Hall et al., IPAC 2017

## Slide 6: Sensitivity as a function of frequency
  M. Checchin et al., Appl. Phys. Lett. 112, 072601 (2018)
120 C
EP/BCP
2/6 N-doped
Higher low field sensitivity for higher frequency cavities
2/6 N-doped have higher sensitivity, as expected form 1.3 GHz data
Steeper field dependence for high frequency cavities

## Slide 7: Sensitivity at high gradients @ 1.3 GHz
Change of behavior with field:
  At low field S increases linearly with the field
  At higher field the slope of S increases
  Similar trend observed in various treatments
Threshold value due to depinning current?
  M. Martinello, M. Checchin et al., to be published

## Slide 8
Trapped Flux Sensitivity
——
Description at low RF Amplitudes

## Slide 9: Mean-free-path dependent pinning potential
A vortex treated as a flexible flux line oscillating in the plane
2D pinning (elastic) potential:
  Lorentzian/Parabolic
  Dependent on mfp
  Dependent on distance from pinning center
The pinning center is localized at the depth from the RF surface
Pinning potential
Pinning center

## Slide 10: Motion equation of a vortex
Pinning Center
Pinning Center
The pinning constant is depth-dependent
  flexible vortex line
Multiple pinning centers per flux line can be considered
Solution valid for domain
The motion equation has form:

## Slide 11: Vortex surface impedance
The complex resistivity of the vortex line follows from the calculation of the apparent power (active plus reactive power) :
The vortex surface impedance (using the classic definition of ) is then:
Number of vortices
Vortex impedance weighted over normal distributions of pinning positions and strengths
  M. Checchin et al., Supercond. Sci. Technol. 30, 034003 (2017)

## Slide 12: Sensitivity to trapped flux
  M. Checchin et al., Appl. Phys. Lett. 112, 072601 (2018)

## Slide 13: Mean-free-path dependence
Pinning
regime
Flux-flow
regime
Small – pinning regime :
  increases with
Large – flux-flow regime :
  decreases with
Pinning
  M. Checchin et al., Supercond. Sci. Technol. 30, 034003 (2017)
  M. Martinello et al., App. Phys. Lett. 109, 062601 (2016)

## Slide 14: Frequency dependence
– pinning regime:
– flux-flow regime:
Intermediate :
  the frequency dependence is rather complex!
As increases:
  higher peak value
  peak at lower mfp values
  M. Checchin et al., Appl. Phys. Lett. 112, 072601 (2018)
Pinning
regime
Flux-flow
regime
Increasing
frequency

## Slide 15: Pinning center depth dependence
Sensitivity dependent on the pinning site distance from the surface
  Bulk pinning does not affect the vortex dissipation!
Pinning
Pinning
Pinning center
  M. Checchin et al., Supercond. Sci. Technol. 30, 034003 (2017)

## Slide 16: Superficial vs bulk pinning
We must distinguish between bulk and superficial pinning!
Superficial pinning:
Bulk pinning:
Affects sensitivity
——
Affects flux trapping
——
Pinning center

## Slide 17
Perspective on trapped flux sensitivity
in Nb thin films

## Slide 18: Sensitivity in Nb thin films
S. Aull et al., in Proc. SRF 2015
Porosities and defects in a Nb thin film
enhance the pinning force
C. Benvenuti et al., Physica C 316, 153 (1999)
Nb thin films are much more defective than Nb bulk
We can expect higher pinning force for the same mean-free-path
The sensitivity is lower!

## Slide 19: Pinning force dependence
The higher the pinning force, the more constrained the oscillation
S decreases with pinning
Pinning
Typical values for Nb
  L.H. Allen el al., Phys. Rev. B 39, 2054 (1989)
  G. S. Park el al., Phys. Rev. Lett. 68 1920, (1992)
Increasing

## Slide 20: Qualitative description of the data
C. Benvenuti et al., Physica C 316, 153 (1999)
Pinning regime
Flux-flow regime

## Slide 21: Qualitative description of the data
C. Benvenuti et al., Physica C 316, 153 (1999)
Pinning regime
Flux-flow regime
Mean-free-path increases
Pinning force decreases

## Slide 22: Qualitative description of the data
C. Benvenuti et al., Physica C 316, 153 (1999)
Pinning regime
Flux-flow regime
Large scattering in pinning potential?

## Slide 23
Conclusions

## Slide 24: Conclusions
Trapped Flux Sensitivity is a near-surface property
Two regimes of dissipation:
  Pinning regime for or
    increases if and
  Flux-flow regime for or
    decreases if , but independent on
Field dependence:
  Linear dependence up to a threshold field
  Slope increases rapidly after the threshold field
  Similar behavior for different treatments
Pinning dependence:
  The stronger the pinning the lower the sensitivity
  Lower sensitivity in thin films most likely due to stronger pinning points

## Slide 25
M. Martinello, FNAL
A. Grassellino, FNAL
A. Romanenko, FNAL
S. Posen, FNAL
A. Melnychuck, FNAL
D. A. Sergatskov, FNAL
D. Bice, FNAL
S. Chandrasekaran, FNAL
Z.-H. Sung, FNAL
S. Belomestnykh, FNAL
Acknowledgments
Thank you for Your Attention