## Slide 1: Evaluation of the Copper Polishing procedures in the framework of ARIES H2020 Collaboration
C. Pira, C. Antoine, E. Chyhyrynets, A. Katashev, O. Kugeler, O. Malyshev, A. Medvids, V. Palmieri, E. Seiler, F. Stivanello, A. Sublet, R. Valizadeh, M. Vogel
This project has received funding from the European Union’s Horizon 2020 Research and Innovation programme under Grant Agreement No 730871.

## Slide 2: Importance of Surface Treatments in SRF
Used to remove the surface damaged layer, due to cavity fabrication methods
To get high gradient Eacc > 30 MV/m  surface roughness < 2 µm Saito K., Proceedings of the 2003 Workshop on RF Superconductivity, Paris, France

## Slide 3: Importance of Surface Treatments in SRF
On Nb-Cu cavities the thin film is not chemical treated
Different polishing treatments of Cu are used
Morphology of Cu surface is replicated by the Nb film
Direct correlation between Cu surface preparation and Nb films SC performances

## Slide 4: Cu Treatments in Accelerator Cavities
LEP  Chemical Polishing (SUBU5)
Benvenuti et al., Proceedings of the 1987 Workshop on RF Superconductivity, Argonne National Laboratories, Illinois, USA
ALPI  Tumbling + ElectroPolishing + SUBU5
Palmieri et al., Proceedings of the 1997 Workshop on RF Superconductivity, Abano Terme (Padova), Italy
LHC  ElectroPolishing + SUBU5
Calatroni et al., Proceedings of the 1999 Workshop on RF Superconductivity, La Fonda Hotel, Santa Fe, New Mexico, USA
HIE Isolde  SUBU5
Venturini et al., Proceedings of the 2003 Workshop on RF Superconductivity, Paris, France

## Slide 5: ARIES Surface polishing treatments

## Slide 6: Workflow of the experiment
CUTTING
OFE COPPER SHEET

## Slide 7: Workflow of the experiment
Cu Polishing
Cutting
SUBU
OFE COPPER SHEET
SUBU
EP
EP + SUBU
LASER
TUMBLING

## Slide 8: Workflow of the experiment
Cu Polishing
Cutting
SUBU
OFE COPPER SHEET
SUBU
EP
EP + SUBU
LASER
TUMBLING
Talk of Prof. Medvids
today at 15:55

## Slide 9: Workflow of the experiment
Cu Polishing
Nb Coating
Cutting
SUBU
OFE COPPER SHEET
SUBU
EP
EP + SUBU
TUMBLING
DC Magnetron Sputtering
DC Magnetron Sputtering
DC Magnetron Sputtering

## Slide 10: Workflow of the experiment
Cu Polishing
Nb Coating
Cutting
SUBU
OFE COPPER SHEET
SUBU
EP
EP + SUBU
TUMBLING
DC Magnetron Sputtering
DC Magnetron Sputtering
DC Magnetron Sputtering

## Slide 11: Workflow of the experiment
Cu Polishing
Nb Coating
Cutting
Characterization
SUBU
OFE COPPER SHEET
SUBU
EP
EP + SUBU
TUMBLING
DC Magnetron Sputtering
DC Magnetron Sputtering
DC Magnetron Sputtering
PPMS
Morphological
characterization
Exoelectrons

## Slide 12: Workflow of the experiment
Cu Polishing
Nb Coating
Cutting
Characterization
SUBU
OFE COPPER SHEET
SUBU
EP
EP + SUBU
TUMBLING
DC Magnetron Sputtering
DC Magnetron Sputtering
DC Magnetron Sputtering
PPMS
Exoelectrons
Talk of Dr. Katashev tomorrow at 11:10
Morphological
characterization

## Slide 13: Workflow of the experiment
Cu Polishing
Nb Coating
Cutting
Characterization
SUBU
OFE COPPER SHEET
SUBU
EP
EP + SUBU
TUMBLING
DC Magnetron Sputtering
DC Magnetron Sputtering
DC Magnetron Sputtering
PPMS
Morphological
characterization

## Slide 14: Workflow of the experiment
CUTTING
OFE COPPER SHEET

## Slide 15: Copper Samples
50 samples produced from the same sheet of OFE copper at CERN
Dimensions:
53 x 53 mm x 1 mm thick
3 mm hole at one corner (≈ 2,5 mm from edge)
Marked on the back side
CERN Samples: C XX (XX = 01-25)
LNL Samples: L XX (XX = 01-25)
53 mm
53 mm
1 mm thick
Ø 3 mm

## Slide 16: Initial Surface
Rolling texture on the surface

## Slide 17: Characterization of the initial surface
Roughness Ra = 130 ± 30 nm (1 mm scan length)
Evaluated with a Veeco Dektat 8 Profilometer

## Slide 18: Workflow of the experiment
Cu Polishing
Cutting
SUBU
OFE COPPER SHEET
SUBU
EP
EP + SUBU
TUMBLING

## Slide 19: 4 Treatments investigated
SUBU (25 samples at CERN + 4 samples at INFN)
Electropolishing (EP) (8 samples at INFN)
EP+ SUBU (5 samples at INFN)
Tumbling (6 samples at INFN)
40 microns removed (except tumbling)

## Slide 20: Set Up of the 4 polishing treatments investigated

## Slide 21: 1. Chemical Polishing: SUBU5
Developed for LEP2 at CERN
Working temperature = 72° ± 2
Etching rate: (depends on the surface/solution ratio and aging)
SUBU5 composition
  sulfamic acid (5g/l)
  hydrogen peroxide 32% (50ml/l)
  n-butanol 99% (50ml/l)
  ammonium citrate (1g/l)

## Slide 22: 1. Chemical Polishing: SUBU5
Developed for LEP2 at CERN
Working temperature = 72° ± 2
Etching rate: (depend on the surface/solution ratio and aging)
SUBU5 composition
  sulfamic acid (5g/l)  corrodes copper forming copper sulfamate
  hydrogen peroxide 32% (50ml/l)  dissolves the copper
  n-butanol 99% (50ml/l)  moderator of the reaction (limits the pitting process on the surface)
  ammonium citrate (1g/l)  limits the bubble production

## Slide 23: 1. SUBU5 Cleaning Procedure
Degreasing: NGL 1740 bath 2 hours  3' ultra-sonic ON at start and again 3’ min ultra-sonic ON before end
Courtesy of Alban Sublet

## Slide 24: 1. SUBU5 Cleaning Procedure
Degreasing: NGL 1740 bath 2 hours  3' ultra-sonic ON at start and again 3’ min ultra-sonic ON before end
Activation: sulfamic acid (H3NO3S, 5 g/l) for about 3'
Courtesy of Alban Sublet

## Slide 25: 1. SUBU5 Cleaning Procedure
Degreasing: NGL 1740 bath 2 hours  3' ultra-sonic ON at start and again 3’ min ultra-sonic ON before end
Activation: sulfamic acid (H3NO3S, 5 g/l) for about 3'
Polishing: 40' SUBU5 with bath agitation
Courtesy of Alban Sublet

## Slide 26: 1. SUBU5 Cleaning Procedure
Degreasing: NGL 1740 bath 2 hours  3' ultra-sonic ON at start and again 3’ min ultra-sonic ON before end
Activation: sulfamic acid (H3NO3S, 5 g/l) for about 3'
Polishing: 40' SUBU5 with bath agitation
Passivation: sulfamic acid (H3NO3S, 5 g/l) for about 1‘
Courtesy of Alban Sublet

## Slide 27: 1. SUBU5 Cleaning Procedure
Degreasing: NGL 1740 bath 2 hours  3' ultra-sonic ON at start and again 3’ min ultra-sonic ON before end
Activation: sulfamic acid (H3NO3S, 5 g/l) for about 3'
Polishing: 40' SUBU5 with bath agitation
Passivation: sulfamic acid (H3NO3S, 5 g/l) for about 1'
Rinsing with water: demineralized water for about 30s
Courtesy of Alban Sublet

## Slide 28: 1. SUBU5 Cleaning Procedure
Degreasing: NGL 1740 bath 2 hours  3' ultra-sonic ON at start and again 3’ min ultra-sonic ON before end
Activation: sulfamic acid (H3NO3S, 5 g/l) for about 3'
Polishing: 40' SUBU5 with bath agitation, 5 samples in a 10L beaker
Passivation: sulfamic acid (H3NO3S, 5 g/l) for about 1'
Rinsing with water: demineralized water for about 30s
Spaying with alcohol: ethyl alcohol to enhance drying
Drying with N2
Courtesy of Alban Sublet

## Slide 29: 1. SUBU5 Cleaning Procedure
Degreasing: NGL 1740 bath 2 hours  3' ultra-sonic ON at start and again 3’ min ultra-sonic ON before end
Activation: sulfamic acid (H3NO3S, 5 g/l) for about 3'
Polishing: 40' SUBU5 with bath agitation, 5 samples in a 10L beaker
Passivation: sulfamic acid (H3NO3S, 5 g/l) for about 1'
Rinsing with water: demineralized water for about 30s
Spaying with alcohol: ethyl alcohol to enhance drying
Drying with N2
Packing in wafer box and then in plastic bag under N2
Courtesy of Alban Sublet

## Slide 30: 1. SUBU5 Cleaning Procedure
Degreasing: NGL 1740 bath 2 hours  3' ultra-sonic ON at start and again 3’ min ultra-sonic ON before end
Activation: sulfamic acid (H3NO3S, 5 g/l) for about 3'
Polishing: 40' SUBU5 with bath agitation, 5 samples in a 10L beaker
Passivation: sulfamic acid (H3NO3S, 5 g/l) for about 1'
Rinsing with water: demineralized water for about 30s
Spaying with alcohol: ethyl alcohol to enhance drying
Drying with N2
Packing in wafer box and then in plastic bag under N2

## Slide 31: 2. Electropolishing, generalities
Process inverse of electroplating
Sample is connected to + terminal of a DC Power Supply
Redox reactions occur
Current flow beetween two electrodes
The sample works as the anode (oxidised reaction)
A viscous electrolyte is used to moderate the reaction
anode
(oxidation)
catode
(reduction)

## Slide 32: 2. Electropolishing
Key parameter: I-V characteristic curve
A polishing effect is observed between C and D
anode
(oxidation)
catode
(reduction)
Vander Voort G.F. (1999). Metalography Principles and Practice, ASM International

## Slide 33: 2. ARIES Samples EP Set up and Parameters
Solution: Phosphoric acid (85%) : Buthanol (99%), ratio 3:2
Anode: 8 samples at time
Cathode material: OFHC copper
Temperature: Room Temperature
No agitation (could create anisotropy in the treatment)
Process time ≈ 5 hours (2 + 3)
Etching rate ≈ 130 nm/min (Could be higher)

## Slide 34: 2. EP Cleaning Procedure
Degreasing: NGL 1740 bath 2 hours  3' ultra-sonic ON at start and again 3’ min ultra-sonic ON before end
Activation: sulfamic acid (H3NO3S, 5 g/l) for about 3'
Polishing: 5 h EP without bath agitation
Passivation: sulfamic acid (H3NO3S, 5 g/l) for about 1'
Rinsing with water: demineralized water for about 30s
Spaying with alcohol: ethyl alcohol to enhance drying
Drying with N2.
Packing in wafer box and then in plastic bag under N2

## Slide 35: 3. EP+SUBU Cleaning Procedure
EP prevent pitting
SUBU remove EP texture
SUBU also acts on the masked areas during the EP (eg the electrical contacts)

## Slide 36: 3. EP+SUBU Cleaning Procedure
Degreasing: NGL 1740 bath 2 hours  3' ultra-sonic ON at start and again 3’ min ultra-sonic ON before end
Activation: sulfamic acid (H3NO3S, 5 g/l) for about 3'
Polishing: 5 h EP without bath agitation
Rinsing with water: demineralized water for about 1 min
Polishing: 8’ SUBU5 with bath agitation, 5 samples in a 10L beaker
Passivation: sulfamic acid (H3NO3S, 5 g/l) for about 1'
Rinsing with water: demineralized water for about 30s
Spaying with alcohol: ethyl alcohol to enhance drying
Drying with N2.
Packing in wafer box and then in plastic bag under N2

## Slide 37: 4. Tumbling, generalities
Mechanical polishing used to prepare the cavity before chemistry
In ARIES is used to evaluate the effect of mechanical treatment on Nb SC film

## Slide 38: 4. Tumbling, generalities
Mechanical polishing used to prepare the cavity before chemistry
In ARIES is used to evaluate the effect of mechanical treatment on Nb SC film
A barrel, filled whith the samples, is then rotated
Could be added media, water, or other lubricants

## Slide 39: 4. ARIES Samples Tumbling Set Up
Samples keeped in a sample holder to prevent bending
Two different media used:
1. Alumina embedded in ureic resin
2. Coconut powders

## Slide 40: 4. ARIES Samples Tumbling Set Up

## Slide 41: 3. Tumbling Procedure
Degreasing: NGL 1740 bath 2 hours  3' ultra-sonic ON at start and again 3’ min ultra-sonic ON before end
Rinsing with water: demineralized water for about 1 min
Polishing: Tumbling with Alumina embedded media and Roadastel30 bath
Rinsing with water: demineralized water for about 1 min
Polishing: Tumbling with Coconut powders media
Degreasing: Rodastel bath 2 hours  3' ultra-sonic ON at start and again 3’ min ultra-sonic ON before end
Rinsing with water: demineralized water for about 1 min
Passivation: sulfamic acid (H3NO3S, 5 g/l) for about 1'
Rinsing with water: demineralized water for about 30s
Spaying with alcohol: ethyl alcohol to enhance drying
Drying with N2.
Packing in wafer box and then in plastic bag under N2

## Slide 42: Surface Characterization

## Slide 43: Surface Characterizations
Optical Inspection
Reflectivity
SEM
EDS
Roughness

## Slide 44: Optical inspection
Mirror like surface
Reflectivity 65 ± 1 %
Mirror like surface
Texture due to oxygen evolution
Reflectivity 64 ± 1 %
Mirror like surface
Texture due to oxygen evolution reduced by SUBU
Reflectivity 66 ± 1 %
Shining surface
Small visible scratches on surface
Reflectivity 52 ± 1 %
SUBU
EP
EP + SUBU
Tumbling
Initial surface
Rolling texture

## Slide 45: SEM Characterization
SUBU
EP
EP + SUBU
Tumbling
Initial surface

## Slide 46: SEM Characterization
SUBU
EP
EP + SUBU
Tumbling
Initial surface
Rolling texture
Presence of pitting
No pitting
Presence of pitting
Presence of scratches
Possible inclusion of media

## Slide 47: Energy Dispersive Spectroscopy
No visible contaminations are revealed with EDS technique
UNTREATED SAMPLE
POLISHED SAMPLE

## Slide 48: Roughness
Polishing Treatment | Ra
Initial surface | 127 ± 26 nm
SUBU5 | 48 ± 7 nm
EP | 225 ± 80 nm
EP+SUBU5 | 115 ± 80 nm
Tumbling | 48 ± 13 nm
Scan length of 1 mm

## Slide 49: Roughness
Polishing Treatment | Ra | Ra diagonal
Initial surface | 127 ± 26 nm | 
SUBU5 | 48 ± 7 nm | 
EP | 225 ± 80 nm | 86 ± 14 nm
EP+SUBU5 | 115 ± 80 nm | 59 ± 9 nm
Tumbling | 48 ± 13 nm | 
Scan length of 1 mm

## Slide 50: Workflow of the experiment
Cu Polishing
Nb Coating
Cutting
SUBU
OFE COPPER SHEET
SUBU
EP
EP + SUBU
TUMBLING
DC Magnetron Sputtering
DC Magnetron Sputtering
DC Magnetron Sputtering

## Slide 51: Nb coating facilities

## Slide 52: Sputtering parameters
Parameter | STFC | Uni Siegen | INFN
Substrate heated | 650 C for 12 h | 650 C for 1.25 h | 650° for >40 h
Base pressure @ 650 °C on a substrate | <10-9 mbar | 1.22x10-5 mbar | < 9x10-8 mbar
Deposition temperature | 650 °C | 650 °C | 650 °C
Power supply | DC MS | DC MS | DC MS
Current | 0.97 A | 1.34 A | 2.1 A
Current density | 22 mA/cm2 | 15 mA/cm2 | 27 mA/cm2
Voltage | 411 V | 298 V | ≈ 350 V
Target power | 400 W | 400 W | ≈ 750 W
Discharge gas | Kr | Ar | Ar
Discharge gas pressure | 1.5x10-3 mbar | 1.5x10-2 mbar | 5x10-3 mbar
Target-substrate distance | 10 cm | 6 cm | 10 cm
Substrate rotation | 4 rpm | no | no
Deposition time | 480 min | 20 min | 20 min
Deposition rate | 7 nm/min | 150 nm/min | 150 nm/min

## Slide 53: Sputtering parameters
Parameter | STFC | Uni Siegen | INFN
Substrate heated | 650 C for 12 h | 650 C for 1.25 h | 650° for >40 h
Base pressure @ 650 °C on a substrate | <10-9 mbar | 1.22x10-5 mbar | < 9x10-8 mbar
Deposition temperature | 650 °C | 650 °C | 650 °C
Power supply | DC MS | DC MS | DC MS
Current | 0.97 A | 1.34 A | 2.1 A
Current density | 22 mA/cm2 | 15 mA/cm2 | 27 mA/cm2
Voltage | 411 V | 298 V | ≈ 350 V
Target power | 400 W | 400 W | ≈ 750 W
Discharge gas | Kr | Ar | Ar
Discharge gas pressure | 1.5x10-3 mbar | 1.5x10-2 mbar | 5x10-3 mbar
Target-substrate distance | 10 cm | 6 cm | 10 cm
Substrate rotation | 4 rpm | no | no
Deposition time | 480 min | 20 min | 20 min
Deposition rate | 20 nm/min | 150 nm/min | 150 nm/min

## Slide 54: Workflow of the experiment
Nb Coating
Characterization
DC Magnetron Sputtering
DC Magnetron Sputtering
DC Magnetron Sputtering
Morphological
characterization

## Slide 55: Morphology of the Nb coating on different substrate treatments (Low Magnification)
SUBU CERN
SUBU INFN
Tumbling
EP
EP + SUBU

## Slide 56: Morphology of the Nb coating on different substrate treatments (Low Magnification)
SUBU CERN
SUBU INFN
Tumbling
EP
EP + SUBU
PITTING

## Slide 57: Morphology of the Nb coating on different substrate treatments (Medium Magnification)
SUBU CERN
SUBU INFN
EP
EP + SUBU
On STFC samples Pitting is not visible because the Nb film is thicker than INFN and Siegen samples. (10 μm instead of 3 μm)
Also low deposition rate could help to mitigate substrate imperfections

## Slide 58: Morphology of the Nb coating on different substrate treatments (High Magnification)
SUBU CERN
SUBU INFN
Tumbling
EP
EP + SUBU

## Slide 59: Morphology of the Nb coating on different substrate treatments (High Magnification)
SUBU CERN
SUBU INFN
Tumbling
EP
EP + SUBU
pitting
On SUBU samples two different grain structures can be observed

## Slide 60: Roughness of the Nb coating on different substrate treatments
Substrate treatment | AFM Roughness (Ra) [nm] | Profilometer Roughness (Ra) [nm]
SUBU CERN | 21 ± 12.1 | 126 ± 15
SUBU INFN | 6.3 ± 1.2 | 197 ± 98
EP | 11.5 ± 0.7 | 233 ± 66 diag 254 ± 50
EP + SUBU | 14.2 ± 2.4 | 192 ± 64 diag 96 ± 18
Tumbling | 18.3 ± 1.5 | 207 ± 53
Profilometer Roughness
influenced by the sample
bending due to the cutting

## Slide 61: Roughness of the Nb coating on different substrate treatments
Substrate treatment | AFM Roughness (Ra) [nm] | Profilometer Roughness (Ra) [nm]
SUBU CERN | 21 ± 12.1 | 126 ± 15
SUBU INFN | 6.3 ± 1.2 | 197 ± 98
EP | 11.5 ± 0.7 | 233 ± 66 diag 254 ± 50
EP + SUBU | 14.2 ± 2.4 | 192 ± 64 diag 96 ± 18
Tumbling | 18.3 ± 1.5 | 207 ± 53
Profilometer Roughnes
influenced by the sample
bending due to the cutting

## Slide 62: Workflow of the experiment
Cu Polishing
Nb Coating
Cutting
Characterization
SUBU
OFE COPPER SHEET
SUBU
EP
EP + SUBU
TUMBLING
DC Magnetron Sputtering
DC Magnetron Sputtering
DC Magnetron Sputtering
PPMS

## Slide 63: DC Magnetization curves
Chart: T [K]
| 4.22 | 5 | 6 | 7 | 8
C10 (L) CERN subu | 120 | 105 | 80 | 65 | 35
L8 (L) Tumbling | 180 | 150 | 120 | 80 | 45
L16 (L) EP+SUBU | 140 | 115 | 95 | 65 | 35
L21 (L) EP | 180 | 125
L20 (L) SUBU | 200
C1 (S) CERN subu | 155 | 125 | 95 | 45 | 25
L1 (S) SUBU | 145 | 115 | 95 | 65 | 35
L10 (S) EP | 155
L9 (S) Tumbling | 160
L23 (S) EP+SUBU | 150
C7 (D) CERN subu | 241
L13 (D) EP | 220
Field of mag. flux entry Ben 2% criterion
(applied field at which the magnetic flux starts entering the sample’s volume)

## Slide 64: DC Magnetization curves
Chart: T [K]
| 4.22 | 5 | 6 | 7 | 8
C10 (L) CERN subu | 315 | 270 | 205 | 135 | 65
L8 (L) Tumbling | 465 | 395 | 295 | 210 | 110
L16 (L) EP+SUBU | 320 | 265 | 210 | 130 | 60
L20 (L) SUBU | 825
L21 (L) EP | 445 | 295
C1 (S) CERN subu | 850 | 725 | 530 | 355 | 185
L1 (S) SUBU | 795 | 675 | 505 | 340 | 180
L10 (S) EP | 910
L9 (S) Tumbling | 900
L23 (S) EP+SUBU | 870
L19 (D) SUBU | 358
C7 (D) CERN subu | 620
Field of MAX mag. moment in Virgin curve Bp
(proportional to the full penetration field)

## Slide 65: DC Magnetization curves
Chart: T [K]
| 4.22 | 5 | 6 | 7 | 8
C10 (L) CERN subu | 315 | 270 | 205 | 135 | 65
L8 (L) Tumbling | 465 | 395 | 295 | 210 | 110
L16 (L) EP+SUBU | 320 | 265 | 210 | 130 | 60
L20 (L) SUBU | 825
L21 (L) EP | 445 | 295
C1 (S) CERN subu | 850 | 725 | 530 | 355 | 185
L1 (S) SUBU | 795 | 675 | 505 | 340 | 180
L10 (S) EP | 910
L9 (S) Tumbling | 900
L23 (S) EP+SUBU | 870
L19 (D) SUBU | 358
C7 (D) CERN subu | 620
Field of MAX mag. moment in Virgin curve Bp
(proportional to the full penetration field)
slight difference between deposition facilities
rather than different surface preparation

## Slide 66: Conclusions
Surface characterizations show that SUBU5 reduces roughness more than the other treatments
SUBU5 produces pitting on the surface, also if used just for the etching of 5 microns (EP+SUBU)
EP treated surface does not present pitting, but roughness is influenced by the dynamic of the process
Tumbling introduces small scratches on the surface and possible inclusions
PPMS characterizations show slight difference between deposition facilities rather than different surface preparation
QPR measurements are mandatory to evaluate the effect of polishing treatment on Nb thin film SRF properties
WP15 will focus more on EP (pitting free) and SUBU5 (lowest roughness without scratches) polishing treatments

## Slide 67: Thank you very much for your attention!
The authors would like to acknowledge the support provided by European Union’s ARIES collaboration H2020 Research and Innovation Programme under Grant Agreement no. 730871.