## Slide 2: Ar-Nb ion energy distribution and thin film properties in HiPIMS with a positive voltage pulse
Fabio AVINO1, A. Sublet1, S. Calatroni2, P. Costa Pinto1, T. Richard1, G. Rosaz1, M. Taborelli1, W. Vollenberg1, A. Grudiev3, A. Lunt4.
1 CERN, TE/VSC-SCC
2 CERN, TE/VSC-VSM
3 CERN, BE/RF-LRF 4 CERN, EN/MME

## Slide 3: Outline
Framework
R&D simulations
R&D experiments
Next steps
Conclusions

## Slide 4: Outline
Framework
R&D simulations
R&D experiments
Next steps
Conclusions

## Slide 5: The CRAB cavity: what for?
Why CRAB?
HL-LHC upgrade (by 2025) aim at increasing luminosity by a factor of 5.
16 CRAB cavities will be mounted around the two main experiments (CMS-ATLAS).

## Slide 6: The CRAB cavity: what for?
Why CRAB?
HL-LHC upgrade (by 2025) aim at increasing luminosity by a factor of 5.
16 CRAB cavities will be mounted around the two main experiments (CMS-ATLAS).

## Slide 7: The CRAB cavity: what for?
Why CRAB?
HL-LHC upgrade (by 2025) aim at increasing luminosity by a factor of 5.
16 CRAB cavities will be mounted around the two main experiments (CMS-ATLAS).

## Slide 8: The CRAB cavity: what for?
Why CRAB?
HL-LHC upgrade (by 2025) aim at increasing luminosity by a factor of 5.
16 CRAB cavities will be mounted around the two main experiments (CMS-ATLAS).

## Slide 9: The CRAB cavity R&D
1st bulk Nb CRAB cavity for HL-LHC completed and under test in SPS
0.66 m

## Slide 10: The CRAB cavity R&D
1.4 m
1st bulk Nb CRAB cavity for HL-LHC completed and under test in SPS
R&D in the FCC framework for alternative Nb/Cu WOW CRAB cavities
290 kg
1st Cu WOW CRAB cavity prototype to be Nb coated

## Slide 11: The CRAB Cu cavity
CHALLENGES:
Superconducting cavities require high purity and defect-free coatings
Complex shape: avoid shadowing / uniform growth

## Slide 12: The CRAB Cu cavity
CHALLENGES:
Superconducting cavities require high purity and defect-free coatings
Complex shape: avoid shadowing / uniform growth
Total power loss ~ 60W
@ Q0 = 4x108 / 3 MV deflection
Dissipated Psurf [W/m2]

## Slide 13: CRAB cavity coating challenge

## Slide 14: CRAB cavity coating challenge
Cylindrical sputtering source

## Slide 15: CRAB cavity coating challenge
Cylindrical sputtering source
  Coating surfaces at different:
  distances (50 – 150 mm)

## Slide 16: CRAB cavity coating challenge
Cylindrical sputtering source
  Coating surfaces at different:
  distances (50 – 150 mm)
  incident angles (0 – 90 °)

## Slide 17: CRAB cavity coating challenge
Cylindrical sputtering source
  Coating surfaces at different:
  distances (50 – 150 mm)
  incident angles (0 – 90 °)

## Slide 18: CRAB cavity coating challenge
Cylindrical sputtering source
  Coating surfaces at different:
  distances (50 – 150 mm)
  incident angles (0 – 90 °)

## Slide 19
From R&D to scale-1 cavity
Basic tests in a R&D experimental setup:
  Basic plasma physics in HiPIMS
  Optimization of HiPIMS parameters

## Slide 20
From R&D to scale-1 cavity
Basic tests in a R&D experimental setup:
  Basic plasma physics in HiPIMS
  Optimization of HiPIMS parameters
Coating of samples reproducing cavity shape
  Coating of copper strips with the CRAB cavity shape
  Parallel implementation of plasma diagnostics
  New sputtering source development

## Slide 21
From R&D to scale-1 cavity
Basic tests in a R&D experimental setup:
  Basic plasma physics in HiPIMS
  Optimization of HiPIMS parameters
Coating of samples reproducing cavity shape
Coating of the first scale-1 cavity prototype
  Coating of copper strips with the CRAB cavity shape
  Parallel implementation of plasma diagnostics
  New sputtering source development

## Slide 22
From R&D to scale-1 cavity
Basic tests in a R&D experimental setup:
  Basic plasma physics in HiPIMS
  Optimization of HiPIMS parameters
Coating of samples reproducing cavity shape
Coating of the first scale-1 cavity prototype
  Coating of copper strips with the CRAB cavity shape
  Parallel implementation of plasma diagnostics
  New sputtering source development

## Slide 23: Outline
Framework
R&D simulations
R&D experiments
Next steps
Conclusions

## Slide 24: Plasma simulation of 60 mm long cylindrical cathode
Side view of the cylndrical cathode (permanent magnet inside)
Experiment
P = 5.10-3 mbar / Ar / 1kW / DCMS
60 mm
cathode

## Slide 25: Plasma simulation of 60 mm long cylindrical cathode
Side view of the cylndrical cathode (permanent magnet inside)
Plasma simulation
P = 5.10-3 mbar / Ar / 10W / DCMS
N
S
Experiment
P = 5.10-3 mbar / Ar / 1kW / DCMS
Output: Nb sputtering profile
60 mm
cathode

## Slide 26: Plasma simulation of 60 mm long cylindrical cathode
Side view of the cylndrical cathode (permanent magnet inside)
Plasma simulation
P = 5.10-3 mbar / Ar / 10W / DCMS
N
S
Experiment
P = 5.10-3 mbar / Ar / 1kW / DCMS
Output: Nb sputtering profile
x5 cathodes in WOW
60 mm
cathode

## Slide 27: Transport simulation and thickness profile
Nb thickness profile, scaled to an equivalent 15’ coating at 1kW/cathode

## Slide 28: Transport simulation and thickness profile
Nb thickness profile, scaled to an equivalent 15’ coating at 1kW/cathode

## Slide 29: Transport simulation and thickness profile
Dissipated Psurf [W/m2]
Nb thickness profile, scaled to an equivalent 15’ coating at 1kW/cathode
Uniformity copes with peak power density position  layer morphology?
Could HiPIMS ?

## Slide 30: Outline
Framework
R&D simulations
R&D experiments
Next steps
Conclusions

## Slide 31: R&D experimental setup
43 cm high DN150 vacuum chamber

## Slide 32: R&D experimental setup
43 cm high DN150 vacuum chamber
2’’ magnetron source, 15° tilted

## Slide 33: R&D experimental setup
43 cm high DN150 vacuum chamber
2’’ magnetron source, 15° tilted
Mass and energy analyser (MEA):
time integrated + time resolved measurements of ion fluxes

## Slide 34: Samples and holder
View from bottom of the MEA entrance orifice

## Slide 35: Samples and holder
2’’ Nb target
90°
sample
0°
sample
~ 14.5 cm
View from bottom with sample holder

## Slide 36: Samples and holder
15 mm
5 mm
FIB cut
2’’ Nb target
90°
sample
0°
sample
~ 14.5 cm
20 mm
10 mm
View from bottom with sample holder

## Slide 37: HiPIMS configurations
  Duty cycle : 1 kHz
  Main pulse (MP) : 30 ms
-550 V
~20 A
+50 V
MP
+50V PP
0V PP

## Slide 38: HiPIMS configurations
  Duty cycle : 1 kHz
  Main pulse (MP) : 30 ms
  Delay (D) : 4 ms
-550 V
~20 A
+50 V
MP
D
+50V PP
0V PP

## Slide 39: HiPIMS configurations
  Duty cycle : 1 kHz
  Main pulse (MP) : 30 ms
  Delay (D) : 4 ms
  PP duration (PP) : 20 – 250 ms
-550 V
~20 A
+50 V
PP
MP
D
+50V PP
no PP

## Slide 40: Time-integrated IEDF
  By using the MEA
PP
PP

## Slide 41: Time-integrated IEDF
  By using the MEA
  Evidence of a dominant high energy ion population!
PP
PP

## Slide 42: FIB on DCMS coatings
Experimental parameters:
  Argon pressure : 8x10-3 mbar
  Niobium target
  Power : 250 W (1.5 hours)
DCMS with grounded substrate
DCMS with -50V bias on substrate
90°
0°

## Slide 43: FIB on HiPIMS coatings
90°
0°
HiPIMS, no PP, grounded substrate

## Slide 44: FIB on HiPIMS coatings
90°
0°
HiPIMS, no PP, grounded substrate
b) HiPIMS, no PP,
-50 V bias on substrate

## Slide 45: FIB on HiPIMS coatings
90°
0°
HiPIMS, no PP, grounded substrate
b) HiPIMS, no PP,
-50 V bias on substrate
c) HiPIMS, +50 V PP,
grounded substrate
  Biased-like effect with a positive pulse! 90° sample gets densified with 200 ms positive pulse at +50V

## Slide 46: Outline
Framework
R&D simulations
R&D experiments
Next steps
Conclusions

## Slide 47
Basic tests in a R&D experimental setup:
  Basic plasma physics in HiPIMS
  Optimization of HiPIMS parameters
Coating of samples reproducing cavity shape
Coating of the first scale-1 cavity prototype
From R&D to scale-1 cavity
  Coating of copper strips with the CRAB cavity shape
  Parallel implementation of plasma diagnostics
  New sputtering source development

## Slide 48
Basic tests in a R&D experimental setup:
  Basic plasma physics in HiPIMS
  Optimization of HiPIMS parameters
Coating of samples reproducing cavity shape
Coating of the first scale-1 cavity prototype
From R&D to scale-1 cavity
  Coating of copper strips with the CRAB cavity shape
  Parallel implementation of plasma diagnostics
  New sputtering source development

## Slide 49: Validation of coating setup with mockup samples
Mass & Energy Analyser
200 mm stroke
bellow
Sputtering
source
Time- and spatially-resolved (substrate-cathode distance) IEDF measurements
Deposition on samples reproducing the CRAB cavity shape
Assess layer uniformity and SC properties with different coating configurations

## Slide 50: Validation of coating setup with mockup samples
Mass & Energy Analyser
200 mm stroke
bellow
Sputtering
source
WOW-mockup
samples
Time- and spatially-resolved (substrate-cathode distance) IEDF measurements
Deposition on samples reproducing the CRAB cavity shape
Assess layer uniformity and SC properties with different coating configurations

## Slide 51: Conclusions
First indication of coating uniformity with simulations in DCMS
Measured mass-, energy-resolved ion fluxes (Ar+, Nb+) Evidence of a dominant high energy ion population with positive pulse

## Slide 52: Conclusions
First indication of coating uniformity with simulations in DCMS
Measured mass-, energy-resolved ion fluxes (Ar+, Nb+) Evidence of a dominant high energy ion population with positive pulse
Performed sample coatings in different HiPIMS configurations:
  FIB analysis indicates a biased-like effect with a positive pulse! 90° sample gets densified with 200 ms, +50V positive pulse

## Slide 53: Backup Slides

## Slide 54
Process | Sample | XRF [mm] | FIB [mm] | Dr [nm/min]
DCMS (1.5 h / 250W) | 0° | 1.5 | 1.6 | 17.8
 | 90° | 0.5 | 1 | 11.1
DCMS and -50V bias on samples (1.5h / 250W) | 0° | 1.9 | 1.93 | 21.4
 | 90° | 0.6 | 1.3 | 5.4
HiPIMS 30 ms pulse (4h / 250W) | 0° | 2.1 | 2.1 | 8.8
 | 90° | 0.7 | 1.3 | 5.4
HiPIMS 30 ms pulse and -50 V bias on samples (4h / 250W) | 0° | 2 | 2 | 8.3
 | 90° | 0.7 | 0.8 | 3.3
HiPIMS 38 ms pulse and +50V / 200 ms reverse kick (4h / 250W) | 0° | 2 | 2.2 | 9.2
 | 90° | 0.67 | 0.8 | 3.3

## Slide 55: FIB on HiPIMS coatings
90°
0°
HiPIMS (grounded substrate)
b) HiPIMS with -50 V bias on substrate
c) HiPIMS with +100 V positive pulse
(grounded substrate)

## Slide 56: FIB on HiPIMS coatings
90°
0°
HiPIMS (grounded substrate)
b) HiPIMS with -50 V bias on substrate
c) HiPIMS with +100 V positive pulse
(grounded substrate)

## Slide 57: FIB on HiPIMS coatings
90°
0°
HiPIMS (grounded substrate)
b) HiPIMS with -50 V bias on substrate
c) HiPIMS with +100 V positive pulse
(grounded substrate)
  Biased-like effect with a positive pulse! 90° sample gets densified with 200 ms, +100V positive pulse

## Slide 58: 30us MP – 4us D – 200us RK 100V

## Slide 59: How to measure time-resolved ion fluxes
CP400
Ion counter
ECL-TTL
converter
PPM422
acquisition
Multi-channel
Scaler MCS4
Time-Integrated
Measurements
Time-resolved
Measurements:
50ns dwell time

## Slide 60: Time-resolved Ar+ fluxes
30 ms MP
30 ms MP – 25 ms D – 35 ms RK