## Slide 2: HTS superconducting thin films for beam impedance mitigation in the Future Circular Collider
Sergio Calatroni – CERN
On behalf of the collaborations:
CNR-SPIN (Genoa – Italy), TU-Wien (Austria)
and
ALBA, ICMAB-CSIC, IFAE, UPC (Barcelona – Spain)

## Slide 3: Outline
The FCC at CERN
Why a beam screen, and why HTS
Beam impedance and HTS
Strategies:
  ReBCO tapes
  Tl-based coatings
Recent results and challenges
Conclusion and outlook

## Slide 4: Circular Colliders Timeline
Constr.
Physics
LEP
Construction
Physics
Proto
Design
LHC
Construction
Physics
Design
HL-LHC
1980
1985
1990
1995
2000
2005
2010
2015
2020
2025
2030
2035
Conceptual Design Report (CDR) by end 2018
(review of European Strategy for Particle Physics)
now is the time to plan for 2040!
Physics
Construction
Proto
Design
FCC

## Slide 5: The Future Circular Collider Study

## Slide 6: The Future Circular Collider(s)
HE-LHC
International FCC collaboration (CERN as host lab) to study:
pp-collider (FCC-hh)  main emphasis, defining infrastructure requirements
~100 km tunnel infrastructure in Geneva area, site specific
e+e- collider (FCC-ee), as potential first step
HE-LHC with FCC-hh technology
p-e (FCC-he) option, IP integration, e- from ERL
~16 T  100 TeV pp in 100 km

## Slide 7: The FCC-hh: pushing the energy frontier
The raison d’être of a hadron collider is the energy reach
Compared to the LHC  Ecms 100 TeV pp (~6 increase)
factor ~3 in radius  100 km
factor ~2 in field  ~16 T dipoles, Nb3Sn at 1.9 K
Synchrotron radiation 
Conductor R&D
Nb3Sn
Magnet Design
16 T

## Slide 8: Need for a beam screen in a p-p collider
High synchrotron radiation load (SR) of protons @ 50 TeV:
~30 W/m/beam (@16 T)  ~5 MW total in arcs (LHC < 0.2 W/m)
+ Image currents, + electron cloud, + …
The synchrotron radiation cannot be dumped at 1.9 K
Taking into account vacuum requirements, overall cryogenic efficiency and total power consumption of the accelerator, we have two possible operating windows:
40 K ÷ 60 K: Multi-bunch instability growth rate of 25 turns
100 K ÷ 120 K: Multi-bunch instability growth rate of 9 turns
Instabilities are due to transverse beam impedance
Courtesy: C. Garion

## Slide 9: Optimisation of cryo-power, vacuum and impedance
100 MW
200 MW
300 MW
From:
Ph. Lebrun
L. Tavian
V. Baglin
0
500
1000
1500
2000
2500
3000
0
50
100
150
200
Total power to refrigerator [W/m per beam]
Beam-screen temperature Tbs [K]
Tcold mass = 1.9 K, ~30 W/m
Tcold mass = 4.5 K, ~30 W/m
Multi-bunch instability growth time: 25 turns 9 turns (DQ=0.5)

## Slide 10: Beam instabilities in particle accelerators (in 1 slide)
(betatron oscillations)
gives rise to a (complex!)
“Transverse impedance”
F. Sacherer in: Proceedings of the First Course of the International School of Particle Accelerators, CERN 77-13, p. 198

## Slide 11: Surface impedance: the key
Zt: Transverse impedance
Property of the beam
Zs: Surface impedance
Property of the surface
What can be better than copper at 50 K?
: instabilities rise-time
: betatron tune-shift
Ib: bunch current
M: number of bunches
E: beam energy
L: bunch length
R: accelerator radius
c: speed of light
b: vacuum chamber radius
f: wakefields frequency
: electrical resistivity
HTS are the solution

## Slide 12: Current density and frequency spectrum
Beam instantaneous image current
Bunches of 1011 protons, 8 cm rms length
Frequency spectrum
For a beam screen of about 30 mm diameter, and a film thickness / skin depth of 1 µm: J ~ 25 kA/cm2

## Slide 13: Choice of HTS
Nature 414, 368-377 (15 November 2001)
High-Tc superconducting materials for electric power applications
David Larbalestier, Alex Gurevich, D. Matthew Feldmann & Anatoly Polyanskii
Courtesy: E. Bellingeri
Requirements:
HTS operate at 50 K and 16 T
Hc2 , Hirr >> 16T
Jc > 25 kA/cm2 (2.5x108 A/m2)
Rs better than for copper
Superconductor Science and Technology, Volume 11, Number 8
Synthesis and properties of fluorine-doped Tl(1223): bulk materials and Ag-sheathed tapes
E Bellingeri, R E Gladyshevskii, F Marti, M Dhallé and R Flükiger

## Slide 14: Expected performance
Surface resistance at zero Hrf and zero Bext
M. Hein, “High-Temperature Superconductor Thin Films at Microwave Frequencies”, Springer
HTS can have surface resistance lower than Cu
at T< 77 K and 0 T
f < 10 GHz
Sundaresan et al. , IEEE TRANS. APPL. SUPERCOND. 13 (2003) 2913
Tc ~100 K
Tc ~120 K

## Slide 15: Fluxon motion in RF
The rigid fluxon lattice behaves as an harmonic damped oscillator
The “depinning frequency”
Chart: 
d
Flux flow regime
No flux flow
Gittleman and Rosenblum: Phys Rev. Lett. 16, 734 (1966), Journal of Applied Physics 39, 2617 (1968)
Calatroni and Vaglio, IEEE Trans. Appl. Supercond. 27 (2017) 3500506

## Slide 16: Predicted surface resistance of HTS in 16 T field
YBCO at 50 K compared to Cu
Tl-1223 at 50 K compared to Cu
Bc2=70T,=40µcm,Jc=108÷109Am-2 ,0<1GHz
At 1.06 T
(injection)
Bc2=45T, =50µcm, Jc=3x109 Am-2,0=3GHz

## Slide 17: How to make it in practice ?
Coat the inside of the screen
with Tl-1223 films
Manufacture the screen using ReBCO tapes

## Slide 18: ReBCO tapes: ALBA, ICMAB-CSIC, IFAE, UPC
(12 mm width)
A flexible metallic substrate coated with a multilayer of epitaxial multifunctional oxide layers, including a HTS RE(Y, Nd, Sm, Gd, Dy)Ba2Cu3O7-d film…
Capable of carrying 25 times higher current (DC) than the peak induced currents in the FCC.
… scalable technology for growing km-length REBCO CC and is commercially available
Coated Conductors are a revolution
in materials science and engineering

## Slide 19: Collaboration program
Qualification and selection of tapes (Jc, Hc, Tc, magnetization and transport measurements) – (ICMAB)
Validation of RF performance up to 9T and higher (UPC)
Development and assessment of soldering technique preserving the properties (IFAE)
Resistance to synchrotron radiation, and transport + RF properties in-situ (ALBA)
Vacuum compatibility, SEY, outgassing… (CERN)
Goal is to have a demonstrator by end of 2019

## Slide 20: Transport measurements (ICMAB)
Normal resistivity
Critical current density *
*measured with SQUID
Qualification and selection of tapes, evaluation of depinning frequency and estimate RF performance

## Slide 21: Validation of RF performance (UPC - ICMAB)
Copper
CC providers 1 - 5
In house developed 8.05 GHz cavity resonator compatible with 25mm bore 9 T magnet at ICMAB
“Non-optimized” REBCO CCs outperform Cu at 50K and up to 9T
RS is microstructure dependent

## Slide 22: Prediction vs. experiment
w0 scales with experimental Rs
The rigid-fluxon model overestimates REBCO’s Rs
By tuning microstructure  optimize rn, Jc and Birr to maximize w0 and minimize Rs(H,T)
Experimental data

## Slide 23: Development of soldering technology (IFAE)
A cryogenic system to assess 2D /3D stress maps based on optical image correlation with in situ monitoring of the Ic is under its final steps of construction
CC
Solder/glue
beam
HTS tapes
Solders based on Sn / Pb / Cu / Bi & In
will be tested at temperatures < 220ºC

## Slide 24: Synchrotron irradiation
Beam screen coatings have to sustain high synchrotron radiation loads
HTS tapes were irradiated with high energetic electron synchrotron radiation (Ec 130 keV) for four weeks in ALBA synchrotron
Irradiated 5x5 mm2 CC sample
e-beam
X-rays
Absorber (35 mm)
DIPOLE
sample
Courtesy of U.Iriso and M. Pont

## Slide 25: Synchrotron irradiation: first results
SC properties of samples before and after irradiation are compared by means of inductive measurements
does not change within the uncertainties
Field behavior is the same
stays the same within uncertainties
decreases after irradiation slightly

## Slide 26: Cryogenic irradiation tests (ALBA)
Bending magnet @ ALBA
Temperature range 2-500K
DC resistivity online
RF test with synchrotron radiation as final goal

## Slide 27: Tl-1223 tapes: CNR-SPIN, TU-Wien
 | YBCO | Tl-1223
PROs | Very good properties Indiustrially available in tapes | Very high Tc High Jc Very high Bc2 Tolerant for out stoichiometry Substrate-tolerant (Ag coating) Weak link effects my be cured by overdoping
CONs | Very expensive and complex preparation Lower Tc | Tl is toxic Weak link effects may not be overcome easily
May open up the 100-120 K operating window
Power consumption from 100 MW down to 50 MW

## Slide 28: Collaboration program
Construction of a safe laboratory
Definition and selection of precursors for Tl-1223 coating (CNR-SPIN)
Optimization of coating procedure through:
Assessment of transport properties (TU-Wien Atominstitut)
And correlation with microstructural properties (TU-Wien USTEM)
(and repeat)
Produce high-quality coatings by electroplating (few cm2) on untextured substrate (Ag)
Goal is to have a reliable process defined by mid of 2019

## Slide 29: Sample preparation (CNR-SPIN)
Step 1: preparation of the substrate
  Laminated Ag ribbon
  Polishing
  Heat treatments
Step 2: preparation of the precursors
  TlNO3 + Bi(NO3)3 ·5H2O + Sr(NO3)2 + Ba(NO3)2, + CaNO3·H2O + Cu(NO3)2 ·xH2O
  In dimethyl sulfoxide (DMSO)

## Slide 30: Sample preparation (CNR-SPIN)
Flat cell
Step 3 :Electroplating
Step 4: Heat treatment
(Thallium (oxide) is volatile above 700-715°C)

## Slide 31: SQUID measurements (Atominstitut)
Thin film, sample 4x4 mm, Tc and hysteresis loop

## Slide 32: Scanning Hall Probe Microscopy (Atominstitut)
zoom into different areas for high resolution scans

## Slide 33: SEM – EDX elemental mapping (USTEM)

## Slide 34: SEM, TEM (USTEM)
TEM image shows clear evidence of stacking of diﬀerent grains
The superconducting phases of diﬀerent grains can be determined through line scans
TEM investigation shows coexistence of Tl-1223 and Tl-1212 phase

## Slide 35: Tl-1223: Iteration (All)
Focus on Tl-1223 (bulk) to optimize preparation and heat treatments

## Slide 36: Tl-1223: Iteration (All)
Use single crystal TiSrO3 to optimize thin film preparation and growth

## Slide 37: Other requirements
Magnetic field quality
UHV compatibility
Low SEY (e-cloud suppression)
Lifecycle environmental radiation protection
Radiation hardness of HTS (p+, n, photons, …)
…

## Slide 38: Striated configuration to minimize trapped fields
  Screening currents during magnetic field ramping will produce unacceptable field quality effects
  A striated geometry will drastically reduce trapped magnetic fields in the superconductor, recovering acceptable levels of field quality during ramping
J. van Nugteren, S. Bermudez, S. Calatroni, G. Kirby, G. de Rijk
Flux shaking in RF will also take care of suppressing the effect

## Slide 39: Accelerator compatibility: SEY
No degradation of superconducting properties due to amorphous carbon sputter coating

## Slide 40: a-C coating: RF compatibility
In untreated form not suitable for use in the FCC-hh
Coating of a-C decreases SEY under the desired limit
Ti as adhesion and protection layer
NO significant change in surface resistance
Increase of not detrimental
About 85 % of the sample is coated
Uncoated
Copper
a-C coating
Ti + a-C coating
Uncoated
Copper
a-C coating
Ti + a-C coating

## Slide 41: Summary and outlook
Impedance reduction for the FCC-hh: an application which can be done only with HTS
First approach: ReBCO Coated-Conductors
  State-of-the-art tapes, ensure they guarantee the requested performance for FCC (and tailor them if needed), develop soldering technology for beam screen fabrication, maintaining the properties: extensive RF, DC testing
Second approach: Tl-1223 thin films
  Opens-up 100-120 K window, 100 MW  50 MW consumption ! Complex 5-components electroplating and annealing. Once established, should be scalable to large dimensions
We will manufacture a short-sample demonstrator (50 cm length) once the technology is ready.
  At CERN we are preparing a RF impedance test system dedicated to beam screens, at cryo-temperature and high magnetic field

## Slide 42: Acknowledgements
CNR-SPIN: Carlo Ferdeghini, Emilio Bellingeri, Alessandro Leveratto, Marina Putti, Aisha Saba, Ruggero Vaglio
TU-Wien: Michael Eisterer, Thomas Baumgartner, Sigrid Holleis, Johannes Bernardi, Michael Stoeger-Pollach, Alice Moros
ALBA: Francis Peréz, Montse Pons, Patrick Krkotic
ICMAB-CSIC: Teresa Puig, Artur Romanov, Joffre Gutierrez, Xavier Granados, Xavier Obradors
IFAE: Ilya Korolkov, Pedro Gonzalez Melis
UPC: Joan O’Callaghan
CERN: Mauro Taborelli, Pedro Costa Pinto, Pierre Demolon, Danilo Zanin, Elisa Garcia-Tabares Valdivieso, Jeroen van Nugteren, Susana Bermudez, Markus Widorski

## Slide 44: Technical Schedule for each of the 3 options
20
22
24
26
28
30
32
34
38
40
Civil Engineering FCC-hh ring
Dipole short models
16 T dipole indust. prototypes
16 T dipoles preseries
16 T series production
SC Magnets
CE FCC-ee ring + injector
FCC-hh
FCC-ee
HE-LHC
Strategy Update 2026 – assumed project decision
Installation HE-LHC
LHC Modification
42
Technical Design Phase
36
Installation + test FCC-ee
Installation + test FCC-hh
CE TL to LHC
LHC Removal
Dipole long models
Injector
schedule constrained by 16 T magnets & CE
→ earliest possible physics starting dates
FCC-hh: 2043
FCC-ee: 2039
HE-LHC: 2040 (with HL-LHC stop LS5 / 2034)
16 T magnets
FCC-hh
FCC-ee
HE-LHC

## Slide 45: Transverse impedance
F. Sacherer in: Proceedings of the First Course of the International School of Particle Accelerators, CERN 77-13, p. 198

## Slide 46: Betatron motion – simplified model
Unperturbed motion of single particle with and
Adding a perturbation to the beam that changes focussing:
Quadrupoles give the restoring (focussing) force -> harmonic oscillations
Growth rate of instability

## Slide 47: Comparison: Y-123, Bi-2223, Tl-1223
Susanne Tönies, Harald W. Weber, Gerhard Gritzner, Oliver Heiml, and Mario H. Eder,
IEEE TRANSACTIONS ON APPLIED SUPERCONDUCTIVITY, VOL. 13, NO. 2, JUNE 2003

## Slide 48: Comparison: Tl-1223 and Tl-2212
Sundaresan et al. , IEEE TRANS. APPL. SUPERCOND. 13 (2003) 2913

## Slide 49
TlxBa2CayCuy+1Oz
Site | Tlx | Ba2 | Cay | Cuy+1 | Oz
Stoichiometry | X=1 o 2 | 2 | Y=0,1,2 | Y+1=1,2,3 | Z=5…10
Substitution | Pb,Bi,Cu,Hg | Sr | Tl | NONE | F

## Slide 50: Surface impedance: effect of magnetic flux
considering the additional electric field related to the fluxons motion :

## Slide 51: Conductivity: two-fluids
Frequency independent
For perfect metals:
For superconductors: