## Slide 1: Coatings R&D
G. Cagnoli for the VCR&D Collaboration

## Slide 2: The AdV+ objectives

## Slide 3: Timing and strategy of AdV+
Mirror production
Uniformity on selected materials
Post deposition corrective coatings and optical control
Material selection
GC mod.
Substrates purchasing and polishing
Metrology and handling upgrades

## Slide 4: The wide context of Coatings Development
Materials (VCR&D)
Coaters and metrology (LMA)
Pragmatic
Fundamental Physics
Selection and Optimization
Materials
Deposition parameters
Metrology
Density of TLS and structure
TLS distribution and structure
Ongoing
Uniformity
In-situ optical metrology for real time thickness control
Spectrophotometric bench for large optics
Point like defects investigation
Planned
High T deposition
Post deposition coating correction

## Slide 5: The ubiquitous thermal noise
Thermal noise in cavities
  Coating noise dominates between 30 Hz and 300 Hz

## Slide 6: Thermal noise and relaxations
Thermal noise is not thermal agitation
  Random processes brake the coherence of modes and spread the thermal energy over all the frequencies
frequency
energy
kT
Thermal vibrations without noise
frequency
energy
Thermal vibrations with noise

## Slide 7: Coating thermal noise and its parameters
The Power Spectral Density
  : temperature
  : laser beam diameter
  : coating thickness
  : Young’s modulus
  : mechanical loss angle
Fluctuation-Dissipation theorem
Coating development
(LMA)
Material research
( )

## Slide 8: Energy loss in Amorphous Materials (AM) in the acoustic band
Debye
The Asymmetric Double Well Potential model
  AM are populated by Two Level Systems
  The ADWP is perturbed by the external deformation
  Only the TLS that relax with a similar to the period of the external perturbation contribute to the energy loss

## Slide 9: Two ways to reduce thermal noise in coatings
Reducing the density of TLS
Shaping the TLS distribution
Fused silica
High-temperature deposited aSi

## Slide 10
The VCR&D project for AdV+
Proposal made in 3 weeks between may and june
  It details the strategies we are pursuing to reduce the internal friction in coatings
  It gives a detailed list of samples production
  It describes all the characterizations needed
  The WBS is outlined

## Slide 11
The project content
The strategies to reduce for AdV+, 1
Post deposition annealing
  It shapes the TLS distribution
  Not known why in some materials the effect is larger than in others
Mixing of oxides
  To reduce internal friction (unexplained)
  To increase the crystallization temperature
High temperature deposition
  It reduces the TLS density
  Ultra-stable glasses
  Not all amorphous materials are « glasses »

## Slide 12
The project content
The strategies to reduce for AdV+, 2
Deposition parameter optimization
  3 parameters: Vb, Ib, deposition rate Rd
  Indications that for Vb and Rd, the lower the better
  The physics of deposition is lacking
Nano-layering
  Nano layers inhibits crystallization during annealing
  They shape the TLS distribution for a not yet clear relation between relaxation-time to structure-dimension relation

## Slide 13
The project content
The strategies to reduce for AdV+, 3
High coordination-number glasses
  Phillip’s conjecture: coordination number larger than 3 reduces the TLS concentration (example: aSi)
High index silica glasses
  To retain, if possible, the SiO2 TLS distribution
Nitrides
  Optimization of SiNx
  Possibly of GaN

## Slide 14
Missing activities
  Modelling, Molecular dynamics simulation of:
    Deposition
    Structural relaxations
    Mechanical properties
  Characterization:
    Calorimetry
    Dielectric
    Diffusion of Argon
The project content
The strategies to reduce for AdV+, 4

## Slide 15
The Virgo Coatings R&D Collaboration
GENOVA
GENOVA
  Ellipsometry
  Optical properties
  AFM, XPS
  Raman
SALERNO/SANNIO
  IAD
  SEM,TEM,AFM and XRD
  nanolayered composites and Mie-metamaterials
URBINO
URBINO
  GeNS Cryo
  FEA
ROMA 2
SALERNO
SANNIO
PERUGIA
PERUGIA
  Cantilevers & GeNS Cryo
  Physics of Glasses
  Brillouin
ROMA 2
  Laser Polishing
  GeNS 300K 1’’
  FEA
VIRGO
LYON
LYON
  IBS HT, IAD
  GeNS 300K
  FEA
  Optical metrology
  Raman, Brillouin
  Physics of Glasses
  Molecular Dynamics
  Sample production
  Characterization

## Slide 16: Other groups expressing interest recently
GENOVA
URBINO
ROMA 2
SALERNO
SANNIO
PERUGIA
ROMA 1
  Structural characterization
  Thermobalance
  Physics of deposition
VIRGO
LYON
ROMA 1
PISA
PISA
  Study of the crystallization processes
  Physics of deposition and ultrastable glasses
  Modelling
  Calorimetry and Dielectric response

## Slide 17
The project content
The sample production plan
LMA samples
Sannio samples

## Slide 18
The project content
The characterization plan
The Pisa and Roma1 are not yet included

## Slide 19
The WBS of the VCR&D collaboration
WP1 Sample production of co-sputtered coatings (LMA)
WP2 Sample production of nanolayered and co-sputtered coatings (Sannio)
WP3 Chemical characterization (Perugia, Salerno, Genova, Roma1)
WP4 Structural analysis, Raman and Brillouin (ILM, Perugia, Genova, Salerno, Pisa, Roma1)
WP5 Optical characterization (Genova, LMA, Roma ToV )
WP6 Room temperature loss measurements (Roma ToV, LMA, ILM, Urbino, Perugia, Pisa)
WP7 Low temperature loss measurements (Urbino, LMA, ILM, Roma ToV)
WP8 Morphological characterization (Salerno, Perugia, Roma ToV)
WP9 Modelling and calorimetry (Pisa)

## Slide 20: The total budget for coating material research
  Keeping the existing competences
    Sannio: 3yr RTD-A
    Tor Vergata: 3yr RTD-A
  Foster new competences
    Fi/Ur: PhD
    Genova: PhD
    Lyon: PhD
    Perugia: 2 yr post doc
  Developing new tools
    Equipment and consumables
Materials (VCR&D)

## Slide 21
The international context
Advanced Virgo +
  j laser spot
    Labs: 8, 3 coaters
    Funding: pending
LIGO Scientific Collaboration
  Centre of Coating Research
    Labs: 9, 3 coaters
    Funding: 3M$ (postdocs)
    Projects: aLIGO+ Voyager
  Glasgow
    Labs: 2, 2 coaters
    Projects: aLIGO+ Voyager ET
j
j
j

## Slide 22: The Centre for Coating Research, 1

## Slide 23: The Centre for Coating Research, 2

## Slide 24: The current status of material research
Ti:Ta2O5 500°C
SiNx IBS 800°C
aSi 400°C
UWS
loss angle j
SiO2 900°C
SiO2 500°C
aSi 450°C
ATF
aSi dep. 400°C
Berkeley
AlGaAs
G. Cole
Si3N4 LPCVD
Thank you for your attention