## Slide 1: Planning for Planar (Pseudo-)Quad Sensors Production at FBK
M. Backhaus, M. Meschini, A. Messineo, J. Schwandt

## Slide 2: Quad Modules Baseline Options
Two most recent meetings on quad modules on June 20th and on July 17th :
3 quads with 25x100 pixels and no punch through bias. Temporary metal will be used for measurements at FBK premises
5 quads with 50x50 pixels with punch through bias
Clearances between chips
  Four of the 50x50 quads and all 25x100 quads with 350μm inter-chip bump center to bump center distance in x-direction (results in ~200μm clearance)
  One of the 50x50 quads with 250μm or 300 μm inter-chip bump center to bump center distance in x-direction (results in ~100μm clearance) to be decided when dicing precision will be known

## Slide 3: More Options & Decisions
No dicing street in between quad ( doublets cannot be separated)
Clearances between doublets in the quad
  900μm inter-chip bump center to bump center distance in Y-direction
Clearances outside doublets in the quad (for the three sides facing outside)
  500μm from bump center to sensor edge (dicing line)
  ~450um from active matrix edge to physical edge after dicing
long pixels (200 μm) in between chips in X-direction
  Do the same on the outer edges of the sensor? To be decided
PT sensors: design the Punch Through bias rails along Y instead of X as in the present layout

## Slide 4: RD53A
X
Y
Physical dimension including dicing streets not accounted in this figure
Top row pads CANNOT be diced

## Slide 5
A possible layout for pseudo-quads, doublets and single RD53A
Based on ATLAS layout (A. Macchiolo)
8 Quads -> Cyan
7 Doublets -> Yellow
8 Singles -> Grey
Sketch, not yet a real design file

## Slide 6
350 μm distance between centre of bumps
FBK is working on
better bump pad shape and symmetry
reducing opening size
reducing metal overlap on adjacent row pixels to minimize cross-talk between pixel rows
Central zone of a 25 μm * 100 μm pitch doublet without punch through bias

## Slide 7
350 μm distance between centre of bumps
FBK is working on
Two versions, with 250 or 350 μm distance between centre of bumps
Central zone of a 50 μm * 50 μm pitch doublet without punch through bias

## Slide 8
350 μm distance between centre of bumps
Central zone of a 50 μm * 50 μm pitch doublet with punch through bias

## Slide 9: Layout Constraints coming from RD53a chip size
310 mm
45 mm
Distances are taken from center of the last bump to the nominal border In order to assembly two RD53 side-by-side in X or Y:
  Along module width (W or Y):
    310 X 2 + 200 (or 100) = 720-820 mm
  Along the module length (L or X):
    45 X 2 + 200 (or 100) = 190-290 mm
In the front side the center of last bump is 1749 mm far from wire bonding pad (along Y)
Dicing streets still to be accounted in this slide
We got a design file of the top layer, thanks Flavio Loddo

## Slide 10: Center of a RD53a-Quad
190-290 mm
720-820 mm
Top row sensors
Bottom row sensors
Left-side sensor
Right-side sensor
Empty space to be populated
by Bias (in case of PT) + guard rings
Empty space to be populated by Bias ring (in case of PT) + guard rings
Dicing line in case it is planned to
separate Doublets from Quads
No dicing street  We will not cut quads into doublets

## Slide 11: Proposal for Bias/Guard Rings
Profit from experience in FBK R&D planar productions
CMS-diodes : 1 Bias ring or 1 G.R.
Junction implant
+ overhang
Dicing region Ohmic (P+) implant
+ overhang

## Slide 12: Example: 1 Bias ring plus 1 GR
One of the best terminations in the first FBK planar batch

## Slide 13: Dicing Street with P-stop and large metal overhang
Dicing streets with P+ and metal overlap “HPK Old Style” require a lot of space around sensor: how far con we go outside pixel matrix plus GR? 500um total
This is the same sensor of the previous page including the area outside the GRs up to the dicing streets

## Slide 14: Multiple Guard Rings
Try to implement at least 3 or 4 Guard Rings with metal overhang and no p-stop between N+ implants. We will try to fit in the available space between sensors

## Slide 15: Up-to-date Quad Module dimension
Malte B. made the latest update this morning on module size
In blue: sensor
In green: RD53A

## Slide 16: Layout of Quad HDI vs Quad sensor
HDI design from Malte B., dimensions defined, production in progress
Proposal for quad sensor size: L = 41300 mm, W = 21100 mm
W = 19765 mm
L= 40100 mm
275 mm from
wire-bonding-pad
to border

## Slide 17: Planar Quad Sensor Production at FBK
ICEmos is once more delaying wafer delivery… 
  Rescheduled to ship week commencing 16th July 2018: difficult to believe… and indeed the mail from ICEmos today at 12:05 says “I have discussed your order with the production team this morning, we will need until 6th August to complete and ship your order.”
6” Float Zone Si-Si DBW (Direct Bonded Wafer) 150mm thick active device, on 500mm handle
  P type, FZ Sensor resistivity > 5kOhm cm
  Handle wafer: CZ 0.1-1 Ohm cm resistivity, 500mm thick
Layout design in underway, to be completed soon, once all distances and constraints are finalized
If you have comments or suggestions, please speak up, you are still in time!