## Slide 1
25x100_TM_V1
PIXEL
DEAD AREA DOUBLE
«STANDARD» DESIGN
N+: 12.5um
METAL: 4um wider than PASS opening

## Slide 4
25x100_TM_V1r
PIXEL
DEAD AREA DOUBLE
REDUCED OVERLAP:
N+: 10.5um
METAL: 3um wider than PASS opening

## Slide 7
25x100_TM_V1b
PIXEL
DEAD AREA DOUBLE
«BITE» NO OVERLAP:
N+: 12.5um with BITE
METAL: 3um wider than PASS opening

## Slide 10
50x50 PT_V3 DETAIL
PT DOT:
CONTACT diameter: 4um
IMPLANT diameter: 6um
METAL diameter: 8um
PT/PIXEL IMPLANT GAP: 10um
PT/PIXEL METAL GAP: 5um

## Slide 11
450um ATLAS Termination
PSTOP implant: 150um
HALF CUT-LINE: 25um
NO IMPLANT AREA (bulk): 88um
Clearance from bump center to CUT-LINE: 475um
1 BIAS RING (PT-LINE)
3 GR (30um pitch) + 3 GR (34um pitch)

## Slide 12
450um CMS Termination
HALF CUT-LINE: 25um
OHMIC IMPLANT: 140um
FIELD PLATE: 10um
NO IMPLANT GAP: 150um (between FIELD PLATES)
GUARD RINGS:
1 BIAS RING (PT-LINE) + 2 GR
GR EXTENSION: 150um (from PIXEL EDGE to last FIELD PLATE)
TOTAL EXTENSION: 450um + 25um HALF CUT-LINE (if required)

## Slide 13
450um CMS Termination – Ohmic Implant detail
HALF CUT-LINE: 25um
OHMIC IMPLANT: 140um
FIELD PLATE: 10um
CONTACT OPENING: 75um
IMPLANT/METAL CONTACT: 35um

## Slide 14
450um CMS Termination – GR detail
BIAS RING:
  IMPLANT:65um
  CONTACT: 20um
  FIELD PLATE:5um
  PIXEL EDGE GAP: 5um
2x GR:
  IMPLANT:15um
  CONTACT: 5um
  FIELD PLATE:5um
  GR GAP: 10um (between FIELD PLATES)

## Slide 15
50x50 PT_V3 DOUBLE-CHIP
  NOTES:
  DIMENSIONS include HALF-CUTLINE (25um+25um)
  2x RD53A FOOTPRINT over DOUBLE-CHIP are displayed

## Slide 16
50x50 PT_V3 DOUBLE-CHIP – DETAIL 1
  NOTES:
  350um space between last/first pixels
  PT lines interrupted at the center of the pixel matrix

## Slide 17
50x50 PT_V3 DOUBLE-CHIP – DETAIL 2
  NOTES:
  RD53A bumps for BIAS RING connection
  RD53A edges

## Slide 18
50x50 PT_V3 DOUBLE-CHIP – DETAIL 3
  NOTES:
  BIAS RING PASSIVATION OPENING
  (on the 4 doublechip corners)
  RD53A bumps for BIAS RING connection
  RD53A edge

## Slide 19
50x50 PT_V3s DOUBLE-CHIP – «SHORT» LONG PIXELS

## Slide 20
Wafer Assembly
6 DOUBLE CHIPs 25x100_TM_V1? (version TBD)
10 DOUBLE CHIPs 50x50_PT_V3
2 DOUBLE CHIPs 50x50_PT_V3 “ATLAS-like” Termination
2 DOUBLE CHIPs 50x50_PT_V3s (250um “SHORT”)
15 SINGLE chips (TBD)