## Slide 1: Graphene Technology for PTOLEMY Project
Javier Martínez1, R. Santorelli2,, P. Garcia Abia2, I. Garcia-Cortes2, S. Cabrera2, A. Moroño2 , J. P. González2, D. Sanz González2, J. Morales Merino2, S. Fernández2, J. Cárabe2, A. Molinero2, J.M. Barcala2, M.B. Gómez-Mancebo2, R. Fernández2, I. Rucandio2, G. Garcia3, A. Boscá1, J. Pedrós1, F. Calle1
Contact: javier.martinez@upm.es
1 Instituto de Sistemas Optoelectrónicos y Microtecnología, Universidad Politécnica de Madrid, Madrid, Spain
2 CIEMAT, Centro de Investigaciones Energéticas Mediambientales y Tecnológicas Madrid, Spain
3 CSIC, Consejo Superior de Investigaciones Científicas, Madrid, Spain

## Slide 2
MICRO NANO FABRICATION NETWORK
400 m2 Clean Room
300 m2 Characterization Laboratories
200 m2 Instrumentation and electronic Laboratories

## Slide 3
www.isomgraphene.es
Research lines
Green energy
  Supercapacitors
  Solar cells
Information and communication
  Plasmon resonators
  GFETs
  2D materials / III-V devices
Health
  Graphene-macrophage patches

## Slide 4
Exfoliation from pyrolythic graphite
Large area graphitization from polymers
Nomarski x100
50 µm
2 µm
2 µm
Step: 0.5 nm
PECVD on metal foils and foams
 = 4 inch
GRAPHENE FABRICATION
Notes: 25 nm PMMA
50 nm Ni

## Slide 5: GRAPHENE GROWTH BY CVD

## Slide 6
QUALITY IN GRAPHENE FABRICATION
Adapted from K. S. Novoselov, V. I. Fal′ko, L. Colombo, P. R. Gellert, M. G. Schwab, and K. Kim, Nature, vol. 490, no. 7419, pp. 192–200, (2012).

## Slide 7
Gas phase conditions (flux, temperature and pressure) establish growth in solid-gas phase
Reactive H*
  Etch of graphene grain edge
  Nucleation density mitigation
Dissociated C
  Increase growth speed
  Increase nucleation density
GRAPHENE FABRICATION BY CVD

## Slide 8
CVD system: Aixtron Black Magic pro
  Cold wall reactor. Fast ramp-up and cool-down rates
  Industry-ready
  Prepared for 4” wafers. Typically 1/3 of the size of hot wall reactor
  Methane (CH4) and acetylene (C2H2) as gaseous precursors
  In-situ, controlled oxidation is possible
  Showerhead structure for the gas inlet
IMPROVEMENT IN CVD FABRICATION

## Slide 9
CVD is the preferable method for electronics.
  High crystallinity → Increased mobility
  Nucleation density must be decreased
  Large area → Higher throughput
  Lateral growth rate must be increased
  Moderate cost → Scalability
  Cold wall reactors for improved efficiency
Areas of research
  Systematic study of growth thermodynamical conditions
  Pretreatment of the catalytic substrate
    Electropolishing
    Oxidation
    Annealing
  Precursor flux reduction
IMPROVEMENT IN CVD FABRICATION

## Slide 10
SEM Imaging
  Need of partial growth
  Nucleation density (in grains / cm2)
  Lateral growth speed
    Area → Mean diameter → Growth speed (in µm/ min)
Cu foil with small graphene grains. Visible boundaries are from Cu microcrystallinity
CHARACTERIZATION OF CVD GRAPHENE

## Slide 11
No growth for pressure higher than 250 mbar
Best results for the lowest pressure
  Sublimation issues
GROWTH PARAMETERS: PRESSURE

## Slide 12: GRAPHENE TRANSFER TO DIFFERENT SUBSTRATES

## Slide 13
Manual graphene transfer:
  Requires handling skills
  Is laborious and time consuming
  Induces mechanical stress
  Results in off-centered samples
S. Bae, H. R. Kim et al., Nat. Nanotechnol., vol. 5, (2010), p. 574.
STARTING POINT IN THE FABRICATION
Current automatic systems are:
  Designed for flexible substrates (roll-to-roll)
  Not for sale yet
 An automatic transfer for arbitrary substrates is needed

## Slide 14
System outcome
AUTOMATIC SYSTEM PROCESS ALGORITHM

## Slide 15
AUTOMATIC SYSTEM PROCESS ALGORITHM
A. Boscá,, J. Pedros, J. Martínez, T. Palacios, F. Calle, Scientific Reports 6, 21676 (2016)

## Slide 16: GRAPHENE CHARACTERIZATION

## Slide 17
SEM analysis
Images acquired with SEM of the sample with holes and sample with graphene transferred on top of the holes
GRAPHENE SUSPENDED MEMBRANES

## Slide 18
GRAPHENE PATTERNING WITH SEM

## Slide 19
Vacuum annealing for adsorbent removal
Dirac point displacement monitoring
3-terminal characterization
Use of an extraction method for the electrical parameters
JANIS high/low temperature vacuum probe station
A. Boscá, J. Pedrós, J Martínez and F. Calle, J. Appl. Phys., vol. 117, (2015), p. 044504
SYSTEM TEST: COMPARISON WITH GFETs

## Slide 20
OTHER CHARACTERIZATION TECHNIQUES
 Optical Characterization: UV/Vis/NIR and FTIR.
 Electrical Characterization: J-V with or without light
 Photocurrent measurement: QSSPC and SUNS−VOC.
 Laser Beam Induced Current system (LBIC).

## Slide 21: GRAPHENE DEVICE FABRICATION

## Slide 22: Electronic Devices
Hall bars
Van der Pauw
TLMs
Transistors
Flexible electronics
Supercapacitors
GRAPHENE GROUP AT ISOM

## Slide 23: GRAPHENE IRRADIATION WITH DEUTERIUM

## Slide 24
The 2 MeV electron Van de Graaff Accelerator permits material irradiation either by electron beam or by Bremsstrahlung induced by stopping of the electron beam.
High vacuum, air, or controlled atmospheres like D2
Electron energy: 0.25 to 2.0 MeV
Electron current: 10 pA to 150 μA.
Dose rates up to 105 Gy/s.
ELECTRON IRRADIATION FOR DEUTERIUM IN GRAPHENE

## Slide 25
Tritium is radioactive isotope and a laboratory with sufficient radiological protection is necessary in the future experiments.
Meanwhile, D2 loaded in graphene by electron irradiation is being carried out by at CIEMAT (Van de Graaff)
Range of parameters for the experiments:
Temperature ( RT-800 ºC)
dose rate ate up to 10 kGy/s
gas pressure range: 1-1500 mbar
Atmosphere (High vacuum, air, He, etc. in this case D2)
Radiation induced absorption chamber connected to the end of the 2 MeV Van de Graaff Accelerator

## Slide 26
Experiments to study the role of the radiation in D2 absorpcion are underway since June-2018 for different graphite and graphene samples:
Procedure:
The chamber is filled with D2 gas 1250 mbar
Sample holder with and oven (T= 55 ºC)
@1.8 MeV, dose rate 500 Gy/s and total dose: 11 MGy
Other set of samples have been maintained in D2 gas (same P, T and time: 6 hours) without irradiation to compare with D2 loading under irradiation.
Analysis by SIMS, TDS, FTIR, XRD, RAMAN, XPS are available in Ciemat.
Experiments in chamber connected to the end of the 2 MeV Van de Graaff Accelerator

## Slide 27
Preliminary results for GR (Graphite rod) samples
TDS: Thermal Desorption Spectroscopy
SIMS: Secondary Ion Mass Spectrometer
A clear increase of Deuterium absorption due to the electron irradiation is observed by different techniques

## Slide 28: GRAPHENE INTERACTION WITH ELECTRONS

## Slide 29
SETUP FOR ELECTRON-GRAPHENE INTERACTIONS
Low (0-100 eV) and intermediate (1-20 keV) energy electron interactions with graphene

## Slide 30: WORK TO BE DONE IN NEXT SEMESTER

## Slide 31
Graphene growth
  High mobility graphene monolayer in 4”
Graphene Nanoribbons fabrication
  Nanoribbons 100 nm wide in 4” wafer.
Deuterium on Graphene Nanoribbons
  Integration of deuterium in 4” wafer
Electron interaction on Graphene Nanoribbons
  Interaction on devices fabricated in 4” wafer

## Slide 32
ACKNOWLEDGEMENTS
R. Santorelli
P. Garcia Abia
J. Carabe
I. Rucandio
A. J. Quejido
S. Fernandez
A. Molinero
R. Fernandez
T. Palacios
G. Garcia

## Slide 33: Graphene Technology for PTOLEMY Project
Javier Martínez1, R. Santorelli2,, P. Garcia Abia2, I. Garcia-Cortes2, S. Cabrera2, A. Moroño2 , J. P. González2, D. Sanz González2, J. Morales Merino2, S. Fernández2, J. Cárabe2, A. Molinero2, J.M. Barcala2, M.B. Gómez-Mancebo2, R. Fernández2, I. Rucandio2, G. Garcia3, A. Boscá1, J. Pedrós1, F. Calle1
Contact: javier.martinez@upm.es
1 Instituto de Sistemas Optoelectrónicos y Microtecnología, Universidad Politécnica de Madrid, Madrid, Spain
2 CIEMAT, Centro de Investigaciones Energéticas Mediambientales y Tecnológicas Madrid, Spain
3 CSIC, Consejo Superior de Investigaciones Científicas, Madrid, Spain