## Slide 1: Material science and accelerator R&D: Reflectivity and Photo Yield measurements of vacuum chamber technical surfaces
Eliana La Francesca
Dottorato in fisica degli acceleratori
(XXXI ciclo)
Relatore interno: prof. M. Migliorati
Relatore esterno: dott. R. Cimino

## Slide 2
Outline
Synchrotron radiation detrimental effects
Reflectivity and Photo Yield
Bessy II measurements
Conclusions
Eliana La Francesca
Roma, 19 November 2018

## Slide 3: Synchrotron Radiation detrimental effects
Heat load on the accelerator walls
Gas load
Production of photo emitted electrons (e- cloud effect)
Beam instability
Eliana La Francesca
Roma, 19 November 2018

## Slide 4
Synchrotron Radiation interaction with Matter
Reflected + Absorbed + Transmitted
Specular reflected
Scattered
Eliana La Francesca
Roma, 19 November 2018

## Slide 5
Synchrotron Radiation interaction with Matter
Reflected + Absorbed + Transmitted
Electron cloud effect
Photo-electrons
generation
Eliana La Francesca
Roma, 19 November 2018

## Slide 6
Photo-emitted electrons can be:
Produced directly by SR (dipoles): emitted in the orbit plane (not participate to electron cloud build up).
Produced by the reflected or scattered light (dipoles and free field zone): emitted perpendicularly to the orbit plane (generate secondary electrons)
SR and electron cloud generation
Original representation F. Ruggero
Beam instability
Eliana La Francesca
Roma, 19 November 2018
To model the generation of photoelectrons in PyECLOUD build- up simulations are needed paramters like PY and R

## Slide 7
Synchrotron Radiation interaction with Matter
Reflected + Absorbed + Transmitted
Electron cloud effect
Heat Load
Photo-electrons
generation
Eliana La Francesca
Roma, 19 November 2018

## Slide 8: FCC Parameters
Parameters LHC H-L LHC FCC-hh
http://tlep.web.cern.ch/content/fcc-hh
Version 1.0 (2014-02-11)
Dipoles at
1.9 K
Total Power to dissipate such HL at cold bore temperature: 3 GW
Eliana La Francesca
Roma, 19 November 2018
FCC-hh SR incidence angle: 0.077 deg
(0.62 mrad)

## Slide 9: Synchrotron Radiation interaction with Matter
Arc SR Heat Load = 28.4 (44.3) W/m/aperture
Reflected + Absorbed + Transmitted
To be increased in cold parts (Superconductor Magnets)
To be increased in high temperature parts
Specular reflected
Scattered
R. Cimino, V. Baglin and F. Schäfers, PRL. 115 (2015) 264804
Eliana La Francesca
Roma, 19 November 2018

## Slide 10: Reflectivity
X-Ray Reflectivity depends on a limited number of parameters:
Photon energy and light polarization
Angle of incidence
Surface roughness
Material
Eliana La Francesca
Roma, 19 November 2018

## Slide 11: Specular Reflectivity: the case of Carbon
(C) 3.5 nm (X-ray range)
20 nm of C can reflect all photons
R. Cimino, V. Baglin and F. Schäfers, PRL. 115 (2015) 264804
Eliana La Francesca
REFLEC simulations
Attenuation depth ():
P(x)=exp(-x/)
For x= the intensity of X-rays falls to 1/e of its value at the surface.
Roma, 19 November 2018
FCC-hh SR incidence angle: 0.077 deg
(0.62 mrad)
Ra=50 nm

## Slide 12: FCC-hh Beam Screen
Eliana La Francesca
Roma, 19 November 2018

## Slide 13: FCC-hh Beam Screen
Eliana La Francesca
Roma, 19 November 2018

## Slide 14: FCC-hh Beam Screen
Eliana La Francesca
Roma, 19 November 2018
The Science & Technology Facility Council (STFC)

## Slide 15: Samples
two copper sample polished, Cu 1A and Cu 2A (10 cm long), with and without a-C coating;
two copper sample lapped, Cu 1B and Cu 2B (10 cm long), with and without a-C coating;
LHC Beam Screen (BS), flat zone (30 cm long), with and without a-C coating;
LHC Beam Screen (BS), Saw-Tooth zone (30 cm long);
Cu sample treated by Laser Ablation Surface Engineering (LASE, made by the Science & Technology Facility Council (STFC))(30 cm long).
Eliana La Francesca
Roma, 19 November 2018

## Slide 16: AFM measurements
AFM (20x20µm2)

## Slide 17: AFM measurements
AFM (20x20µm2)

## Slide 18: Measured roughness
Sample | RMS Roughness (Ra) | RMS Roughness (Ra) (Carbon Coating)
Cu 1A | 9.6 nm | 13.4 nm
Cu 1B | 25 nm | 31.3 nm
Cu 2A | 27 nm | 28.6 nm
Cu 2B | 643 nm | 648 nm
LHC-Flat | 14.9 nm | 20.1 nm
Side A – means polished
Side B – means lapped
Cu 1A
Cu 2A
Eliana La Francesca
Roma, 19 November 2018
50 nm CC made by
Magneto-sputtering

## Slide 19: BESSY-II Optic Beamline and Reflectometer
A.A.Sokolov,et al,Proc.of SPIE92060J-1-13(2014)
Eliana La Francesca
Roma, 19 November 2018

## Slide 20: BESSY-II Optic Beamline and Reflectometer
Incidence angle θ: -90° – 90°
Detector in-plane 2θ: -180° – 180°
Detector off-plane χ : -4° – 4°
Sample – detector: 310 mm
Six axes sample positioning
Sample current measurement
GaAsP-Photodiodes
Detector slits, pinholes
A.A.Sokolov,et al,Proc.of SPIE92060J-1-13(2014)
Eliana La Francesca
Roma, 19 November 2018

## Slide 21: Bessy II Measurements
Photon Energy range 351800 eV
Beam height h=0.3 mm
Incident Beam measurement
GaAsP Photodiodes (4x4mm) (0.12*4mm)
Incidence angle 0.25, 0.5, 1 deg
Reflectivity measurement
Photo Yield:
PY= Ne/N
Specular Reflectivity
Specular
Total
Detector
Eliana La Francesca
Mirror
Scattered Light
Roma, 19 November 2018

## Slide 22: Flat Copper Samples
Tech. Surf
At grazing incidence angle contaminants are influencing Cu Reflectivity
Eliana La Francesca
Roma, 19 November 2018

## Slide 23: Flat Copper Samples
Photo Yield:
PY= Ne/N
Tech. Surf
Peaks correspond to absorption edge
Eliana La Francesca
Roma, 19 November 2018

## Slide 24: LHC-Flat
Photo Yield:
PY= Ne/N
Tech. Surf
Peaks correspond to absorption edges
At grazing incidence angle contaminants are influencing Cu Reflectivity
Eliana La Francesca
Roma, 19 November 2018

## Slide 25: LHC-Flat
Photo Yield:
PY= Ne/N
Tech. Surf
Eliana La Francesca
Roma, 19 November 2018
Low energy photons can be reflected even at high incidence angles

## Slide 26: Specular and Total Reflectivity
Eliana La Francesca
Roma, 19 November 2018

## Slide 27: Specular and Total Reflectivity
Eliana La Francesca
Roma, 19 November 2018

## Slide 28: Cu Samples with C Coating
Tech. Surf
Coating process increased roughness
Eliana La Francesca
Roma, 19 November 2018

## Slide 29
Tech. Surf
Eliana La Francesca
Roma, 19 November 2018
Cu Samples with C Coating
Carbon coating reduces
Photo Yield at high energy
Peaks correspond to absorption edges

## Slide 30: LHC-Flat with C Coating
Tech. Surf
Peaks correspond to absorption edges
Roma, 19 November 2018
Decreasing of reflectivity at is due to the achievement of the critical angle.
Eliana La Francesca

## Slide 31: LHC-Flat with C Coating
Photo Yield:
PY= Ne/N
Tech. Surf
Eliana La Francesca
Roma, 19 November 2018

## Slide 32: Specular and Total Reflectivity
Eliana La Francesca
Roma, 19 November 2018
Total Reflectivity higher than Specular Reflectivity

## Slide 33: Specular and Total Reflectivity
Eliana La Francesca
Roma, 19 November 2018
CC increases Total Reflectivity and reduce absorption and related Heat Load.

## Slide 34: LHC Saw-Tooth
Roma, 19 November 2018
Tech. Surf
Eliana La Francesca
PY peaks confirm the contaminants presence
Little difference in PY for the three incidence angle

## Slide 35: LHC Saw-Tooth
Roma, 19 November 2018
Tech. Surf
Eliana La Francesca
Total Reflectivity higher than Specular Reflectivity

## Slide 36: LASE
Roma, 19 November 2018
Tech. Surf
Eliana La Francesca
No difference in PY for the three incidence angle
No carbon evidence

## Slide 37: LASE
Roma, 19 November 2018
Tech. Surf
Eliana La Francesca
Total Reflectivity higher than Specular Reflectivity

## Slide 38: Surface modification effects
Photo Yield of LHC S-T and LASE are the same
LHC S-T Specular Reflectiviy is one order of magnitude lower than LASE.
Eliana La Francesca
Roma, 19 November 2018

## Slide 39: Conclusions
At grazing incidence angle air contaminants deeply influence Reflectivity.
For technical surfaces scattered light cannot be neglected.
Photo Yield does not significantly depend on roughness.
Carbon coating increases Total Reflectivity and reduce absorption and related Heat Load (as long as incidence angle is below its critical angle).
Cu LASE Reflectivity is substantially lower than for untreated copper and for LHC Saw-Tooth sample.
The Photo Yield of Saw-Toothed copper and LASE are the same.
Experimental data are important to characterize SR behaviour and HL for all materials to be used in FCC-hh dipoles and IP.
Eliana La Francesca
Roma, 19 November 2018

## Slide 40: Thank you for your attention.
Eliana La Francesca
Roma, 19 November 2018