## Slide 1
Ioan Dafinei
for the CUPID-0 collaboration
CUPID-0, challenges and achievements in the struggle of 0-background double-beta decay experiments
Ioan Dafinei
INFN Sezione di Roma, ITALY
14th Pisa Meeting on Advanced Detectors
La Biodola, Isola d'Elba, May 27 - Jun 2, 2018
14th Pisa Meeting on Advanced Detectors
La Biodola, Isola d'Elba (Italy)
May 27 - Jun 02, 2018

## Slide 2
outline
introduction
bolometric approach in 0νDBD research
CUPID challenge
CUPID-0 achievements
concluding remarks
1/20

## Slide 3
the interest of 0νDBD process
(A;Z) → (A;Z+2) + 2e-
violation of the lepton number conservation laws
proof that neutrino is his own antiparticle (Majorana nature of neutrino)
provide some insight into the absolute mass of neutrinos
Introduction
the interest of bolometric approach
calorimetric technique based on the use of crystals cooled down to mK temperatures where their specific heat is extremely low and goes like T3
small energy deposit can be detected as sizable temperature variation (ΔTΔE/C).
advantages:
energy resolution (as good as 0.1%)
effciency on 0νDBD larger than 80%
crystals available for almost all nuclides of interest
high intrinsic radio-purity affordable
2/20

## Slide 4
challenges
crystals
  radio-purity
  chemical purity
  high production yield (for enriched crystals)
temperature sensors
light detectors
surface detectors
heaters
holding structure (towers)
electronics
cryogenic system
screenings
data acquisition and analysis
…
…
handling
packaging
transport
storage
3/20

## Slide 5
Scintillating bolometers
bolometer
background-free experiment is possible:
α-background: identification and rejection
β/γ-background: ββ isotope with large Q-value
4/20

## Slide 6
CUPID
CUORE (Cryogenic Underground Observatory for Rare Events) Upgrade with Particle IDentification
CUPID is a proposed future tonne-scale bolometric neutrinoless double beta decay (0νDBD) experiment to probe the Majorana nature of neutrinos and discover Lepton Number Violation in the so-called inverted hierarchy region of the neutrino mass. CUPID will be built on experience, expertise and lessons learned in CUORE, and will exploit the current CUORE infrastructure as much as possible. In order to achieve its ambitious science goals, CUPID aims to increase the source mass and dramatically reduce the backgrounds in the region of interest. This requires isotopic enrichment, upgraded purification and crystallization procedures, new detector technologies, a stricter material selection, and possibly new shielding concepts with respect to the state-of-the-art deployed in CUORE.
G. Wang et al. (CUPID interest group), arXiv:1504.03599v1, 14 Apr 2015,
CUPID: CUORE (Cryogenic Underground Observatory for Rare Events) Upgrade with Particle Identification
5/20

## Slide 7
CUPID challenges
large detector mass
  several hundreds kg
  possibly enriched material
background close to zero at the ton ∙ year exposure scale
region of interest of a few keV around 0νDBD transition energy
isotopic enrichment and related improvements regarding crystal production
active alpha rejection
improved material selection
reduced cosmic activation
new with respect to CUORE
see also at this Conference
Wednesday, 30 May, 09:10; Speaker: Antonio Branca
CUORE: the first bolometric experiment at the ton scale for rare decay searches
Wednesday, 30 May, 10:00; Speaker: Nicola Casali
Cryogenic light detectors for background suppression: the CALDER project
6/20

## Slide 8
crystals for 0νDBD
(bolometric approach)
main (CUPID) candidates today: (alphabetic order)
ZnSe
Li2MoO4
7/20
TeO2
particle identification with:
LD: Cherenkov radiation
Surface Effects

## Slide 9
the challenge of large scale 0νDBD experiments
Compact Muon Solenoid
~80tons
PbWO4
~1ton
TeO2
~1ton
TeO2
8/20

## Slide 10
Journal of Crystal Growth 475 (2017) 158–170
Production of 82Se enriched Zinc Selenide (ZnSe) crystals for the study of neutrinoless double beta decay …
Zn82Se crystals production
crystals production cycle
enrichment: 82Se from 8.82% to 96.30% (made at URENCO, Almelo, Holland)
Zn82Se synthesis and crystal growth:
made at ISMA Kharkiv Ukraine with strong INFN contribution
final processing (cutting and polishing):
made at LNGS, INFN Italy
production yields:
synthesis: 98.35%
(99.55% at S-1, 99.40% at VTT and 99.40% at HTT)
crystal growth*: 95%
cutting*: 96,72%
shaping and polishing*: 99%
_________________________
* including recovered material for recycling
similar for any crystal candidate
9/20

## Slide 11
crystal processing:
at LNGS-INFN
Zn82Se crystals production
10/20

## Slide 12
Zn82Se crystals production
ready to use
polished
11/20
radio-purity measured during crystal production
confirmed by CUPID-0 data
https://arxiv.org/pdf/1802.06562.pdf

## Slide 13
mechanical processing
(aiming at maximizing the total mass of 82Se)
Crystal mass*
12/20
*in blue, the 82Se content

## Slide 14
82Se recovery in view of recycling
mass of extracted 82Se ultrapure (99.9999% purity):
6.76.8 kg i.e. 98% to 99% recovery yield
Main reaction:
3ZnSe + 8HNO3  3Zn(NO3)2 + 3Se  + 4H2O + 2NO 
Parasitic reaction:
ZnSe + 8HNO3  Zn(NO3)2 + H2SeO3 + 3H2O + 6NO2 
work performed at Nijnii Novgorod, Russia
82Se extraction from scraps:
chemical + physical (double distillation)
13/20

## Slide 15
light detectors (LD)
(for  background rejection)
CUPID-0 operates 31 LDs
Well established technology for bolometric LDs
LD: Ge wafer + SiO coating (60 nm) + Ge-NTD
Light vs Heat: possible α leakage in β/γ ROI
Pulse Shape Analysis of Light: efficient particle-ID
14/20
LUCIFER: J.W. Beeman et al., 2013 JINST 8 P05021
data from R&D phase!
degraded  source is used

## Slide 16
CUPID-0 detector assembling
(first array of scintillating bolometers based on enriched Zn82Se crystals)
26 bolometers (24 enr + 2 nat) in 5 towers
10.5 kg of ZnSe
5.17 kg of 82Se -> Nββ = 3.8x1025 ββ nuclei
LD: Ge wafer operated as bolometer
Simplest modular detector ➜ scale up
Copper structure (ElectroToughPitch)
PTFE holders
Reflecting foil (VIKUITI 3M)
30cm
15/20

## Slide 17
CUPID-0 detector assembling
(performed in ~2 weeks inside a low-Rn underground clean room at LNGS)
#4 LD installation
#3 Fixing of ZnSe
#5 Tower completed
#1 LD installation
#2 ZnSe and light reflector installation
16/20

## Slide 18
CUPID-0 detector installation
(in the former Cuoricino/CUORE-0 cryostat in hall A at LNGS)
improvements wrt Cuoricino/CUORE-0
double stage pendulum for low vibrational noise
better LD performance
cryostat wiring: can host up to 120 channels
CUPID-0 uses 67 chns
commissioning start in March* 2017
data taking start in June 2017
BKG goal in the Rol ~ 10-3 counts/(keV kg y)
(thanks to  discrimination capability and high Q-Value)
17/20
*data of first month not used for scientific reports

## Slide 19
CUPID-0 results in a glance
O. Azzolini et al., CUPID-0: the first array of enriched scintillating bolometers for 0νββ decay investigations, arXiv:1802.06562, accepted by PRL
O. Azzolini et al., First Result on the Neutrinoless Double Beta Decay of 82Se with CUPID-0, arXiv:1802.07791v2, accepted by EPJC
see more, here
18/20

## Slide 20
CUPID-0 results in a glance
19/20
Single-hit events in the Light Shape Parameter-Energy plane
The energy spectrum in the analysis window.
The blue line is the fitted spectrum together with a hypothetical signal corresponding to the 90% C.I. limit of T1/2(0) = 2.4∙1024 yr

## Slide 21: concluding remarks
20/20
0νDBD is among the most exciting challenges in physics
lately, the conditions have matured for a 1 ton experiment based on enriched bolometers with particle identification
CUPID-0 is the first large array of enriched scintillating bolometers for 0νDBD search, currently taking data from spring 2017
the complete α-background rejection was demonstrated and allowed to reach an unprecedented BKG level for a bolometric experiment
the analysis of the first data (3.44 kg y of ZnSe) allowed to set the best limit on 82Se 0νDBD half-life
energy resolution (exposure weighted)
total signal efficiency

## Slide 22: CUPID-0
O. Azzolini1, M.T. Barrera1, J.W. Beeman2, F. Bellini3,4, M. Beretta5,6, M. Biassoni6, C. Brofferio5,6, C. Bucci7,
L. Canonica7,8, S. Capelli5,6, L. Cardani4, P. Carniti5,6, N. Casali4, L. Cassina5,6, M. Clemenza5,6, O. Cremonesi6,
A. Cruciani4, A. D'Addabbo7, I. Dafnei4, S. Di Domizio9,10, F. Ferroni3,4, L. Gironi5,6, A. Giuliani11,12, P. Gorla7, C. Gotti5,6, G. Keppel1, L. Marini9,10, M. Martinez3,4, S. Morganti4, S. Nagorny7,13, M. Nastasi5,6, S. Nisi7, C. Nones14, D. Orlandi7, L. Pagnanini7,13, M. Pallavicini9,10, V. Palmieri†1, L. Pattavina7,13, M. Pavan5,6, G. Pessina6, V. Pettinacci4, S. Pirro7,
S. Pozzi5,6, E. Previtali6, A. Puiu5,6, F. Reindl4, C. Rusconi7,15, K. Schaeffner7,13, C. Tomei4, M. Vignati4, A. S. Zolotarova14
1INFN Laboratori Nazionali di Legnaro, I-35020 Legnaro (Pd) - Italy
2Lawrence Berkeley National Laboratory , Berkeley, California 94720, USA
3Dipartimento di Fisica, Sapienza Universit_a di Roma, P.le Aldo Moro 2, 00185, Roma, Italy
4INFN, Sezione di Roma, P.le Aldo Moro 2, 00185, Roma, Italy
5Dipartimento di Fisica, Universit_a di Milano Bicocca, I-20126 Milano - Italy
6INFN Sezione di Milano Bicocca, I-20126 Milano - Italy
7INFN Laboratori Nazionali del Gran Sasso, I-67100 Assergi (AQ) - Italy
8Massachusetts Institute of Technology, Cambridge, MA 02139, USA
9Dipartimento di Fisica, Universit_a di Genova, I-16146 Genova - Italy
10INFN Sezione di Genova, I-16146 Genova - Italy
11CNRS/CSNSM, Centre de Sciences Nucl_eaires et de Sciences de la Mati_ere, 91405 Orsay, France
12DISAT, Universit_a dell'Insubria, 22100 Como, Italy
13Gran Sasso Science Institute, 67100, L'Aquila - Italy
14IRFU, CEA, Universit_e Paris-Saclay, F-91191 Gif-sur-Yvette, France
15Department of Physics and Astronomy, University of South Carolina, Columbia, SC 29208 - USA