## Slide 1
Chart: 
A large area SiPM for efficient detection of the fast scintillation component of BaF2
D. G. Hitlin, Lauritsen Laboratory, Caltech M. Hoenk, J. Hennessey, A. Jewell, Jet Propulsion Laboratory, Caltech G. Paternoster, A. Gola, FBK
Arbitrary scale
Native BaF2 spectrum & calculated response with 5 layer filter on 10nm SiN
85%
630ns
15%
600ps
Making use of the very fast barium fluoride scintillation component at 220nm
for fast timing and high rate capability requires a means of suppressing the larger slow component at 300nm
Caltech/JPL and FBK are developing a SiPM with an integrated interference filter for this purpose
This requires reduction of SiN passivation layer on an FBK device and fabrication of an integrated metal/dielectric filter, which has higher efficiency than an external filter
SiPM with thin entrance window and guard ring structure
Wavelength (nm)
Calculated transmittance of several 5 layer filters
Transmission (%)
5 layer (no oxide, no SiN
5 layer (10 nm SiN)
5 layer (20 nm SiN
5 layer (20 nm SiO2, 30 nm SiN)
Wavelength (nm)
t = 0.6/630 ns BaF2
Test wafers are in production