## Slide 1
Radiation hardness investigation of thin and low resistivity bulk Si detectors
Geetika Jain, Surabhi Sharma, Chakresh Jain, Ashutosh Bhardwaj, Kirti Ranjan
Centre for Detector & Related Software Technology, Department of Physics & Astrophysics, University of Delhi, INDIA
Motivation for Study: Si detectors placed close to particle collision point
 Damage to charge collection properties by harsh radiation environment
Development of new Si detector technology mandatory!!
Possible candidate: Low resistivity or High bulk doping concentration () Si substrate
Investigation Technique Used: TCAD Silvaco Simulation Tool!
Non-Irradiated Behaviour of low resisitivity substrate
High charge collection observed at large Nb after a certain applied bias voltage.
Reason: E.field peaks at frontside due to stronger PN junction  leads to charge multiplication, thereby high CC.
Irradiated Behaviour of low resisitivity substrate
CC decreases with fluence but with a characteristic peak in CC before gradually decreasing. This is an observed characteristic for low resistivity substrates – eg. HVCMOS.
RADIATION HARDER THAN HIGH RESISTIVITY SUBSTRATE!*
For Nb = 3 x 1014 cm-3  resistivity = 44 .cm
Fluence
Charge Collected (e)
For d = 100 m
Voltage
Charge Collected (e)
Fluence
Charge Collected (e)
At 500 V
Distance along detector depth
Electric Field (V.cm-1)
For Nb = 1 x 1012 cm-3  resistivity = 13 k.cm