## Slide 1: Micro Patterning Techniques on m-PIC (and MM etc.)
Atsuhiko Ochi
Kobe University
RCGD2019@Bari 13/05/2019

## Slide 2: Micro patterning technique
The m-PIC has very precise pattern, and there are many HV line connections.
In this talk, two type of micro patterning techniques are shown for DLC
  Liftoff patterning
  Connection from metal electrodes to DLC

## Slide 3: Liftoff process using sputtering
Very fine structure (a few tens micro meter) can be formed using photo resist. (same as PCB)
Surface resistivity can be controlled by sputtering material and their thickness
Substrate (polyimide)
Photo resist
Substrate (polyimide)
Carbon sputtering
Substrate (polyimide)
Developing the resists
@PCB company
(Laytech inc.)
@Sputtering
company
(Be-Sputter inc.)
@PCB company
(Laytech inc.)

## Slide 4: Enlarged picture of resistive strip foil
10 mm
1 mm
0.3 mm

## Slide 5: DLC u-PIC in previous production
Fine patterning … μ-PIC with resistive cathode
Drift plane
Anode
Resistive cathode (-HV)
Pickup electrode
Thin
substrate
400 μm
Thick substrate
50 μm

## Slide 6: The problem in liftoff method
The etching for remained resist is effected only from side
For large area (> 5mm) of masked area, those mask cannot be removed
   DLC remained
Substrate (polyimide)
Substrate (polyimide)
DLC and resist can be remained
In thick (negative) pattern
Etching the resist from side

## Slide 7: Manufacturing process of resistive m-PIC (2017-2018)
Liftoff using metal

## Slide 8: Connection between metal & DLC
Anode
Cathode Pickup
DLC cathode
Anode readout

## Slide 9: Prototype Chamber
  Detection area: 10 cm X 10 cm
  2-dimensional, 400 mm spacing
  Cathode: f270 mm
  Anode: f50 mm
  256 x 256 readout
    With APV25 + SRS
2mm

## Slide 10: Signals with / without zigzag connection (HV bias)
Channel number
Channel number

## Slide 12: Imaging using u-PIC

## Slide 13: Summary
For investigating DLC patterning for m-PIC,
  Liftoff process using metal mask
  Zigzag connection between DLC and metal
has been tested and worked well
Liftoff using photo-sensitive resist is still important technique for large size patterning