## Slide 1: THIN FILMS CHARACTERIZATION A. Serra CEDAD - CEnter of Applied Physics, DAting and Diagnostics Department of Mathematics and Physics "Ennio De Giorgi University of Salento INFN-National Institute for Nuclear Physics Via per Arnesano, 73100, Lecce

## Slide 2
Characterization facilities

## Slide 3
Characterization Techniques
Electrical measurements
X-rays diffraction
Transmission electron microscopy
Scanning electron microscopy
Scanning tunneling microscopy and spectroscopy
UV-Vis-NIR and Raman spectroscopy

## Slide 4: From single atom to solid-state
Adapted from Fig. 18.3, Callister & Rethwisch 8e.
Metal semiconductor insulator
Fermi level
BC
BV

## Slide 5: Chemical-physical properties depend on:
-- grain boundaries
-- dislocations
-- impurity atoms
-- vacancies
Modulate the physical features: energy levels
free charges type
mean free path……..

## Slide 6: It is well known that Insulators & Semiconductors ........
• Insulators:
-- wide band gap (> 2 eV)
-- few electrons excited across band gap
Energy
filled
band
filled
valence
band
filled states
GAP
empty
band
conduction
• Semiconductors:
-- narrow band gap (< 2 eV) -- more electrons excited across band gap
Energy
filled
band
filled
valence
band
filled states
GAP
?
empty
band
conduction

## Slide 7: ...........................charge carriers in insulators and semiconductors
Two types of electronic charge carriers:
Free Electron
– negative charge
– in conduction band
Hole
– positive charge – vacant electron state in the valence band
Adapted from Fig. 18.6(b), Callister & Rethwisch 8e.

## Slide 8: Intrinsic semiconduction in terms of electron and hole migration
• Electrical Conductivity given by:
# electrons/m3
electron mobility
# holes/m3
hole mobility
electric field
electric field
electric field
• Concept of electrons and holes:
+
-
electron
hole
pair creation
+
-
no applied
applied
valence
electron
C atom
applied
electron
hole
pair migration

## Slide 9: Number of Charge Carriers
Intrinsic Conductivity
for intrinsic semiconductor n = p = ni
material
Diamond
Si
Ge
GaP
CdS
band gap (eV)
5
1.11
0.67
2.25
2.40

## Slide 10: Intrinsic vs Extrinsic Conduction
Intrinsic:
# electrons = # holes (n = p)
• Extrinsic:
-- electrical behavior is determined by presence of defects
that introduce excess electrons or holes
-- n ≠ p
• p-type Extrinsic: (p >> n)
• n-type Extrinsic: (n >> p)

## Slide 11
Resistivity measurements
Two-point probe
Four-point probe
Rcontact
Rcontact
Rsample
Rcontact
Rcontact
Rsample
Notes: In four-point probe, negligible current flows through the voltmeter, the only voltage drop measured is across Rsample.

## Slide 12
Resistivity
Two-point probe
Four-point probe
Measures sample only
Rcontact
Rcontact
Rsample
Rcontact
Rcontact
Rsample
Measures sample + contact resistance + probe resistance
Notes: In four-point probe, negligible current flows through the voltmeter, the only voltage drop measured is across Rsample.

## Slide 13
Collinear contacts
Semi-infinite sample

## Slide 14
Collinear contacts
Correction factor

## Slide 15
Collinear contacts
For samples thinner than the probe spacing s, F can be written as a product of three independent correction factors.
F1 corrects for sample thickness
F2 corrects for lateral sample dimensions
F3 corrects for placement of probes near edges

## Slide 16
Collinear contacts
For films deposited
on non-conducting substrates:
on conducting substrates replace sinh with cosh.
If

## Slide 17
Collinear contacts
For circular samples of diameter D:
D/s ~ 6
F2 ~ 0.8

## Slide 18
Collinear contacts
F3 accounts for contacts placed near sample edges
d/s ~ 1.7
F31 ~ 0.9
Parallel:
Perpendicular:
d/s ~ 3
F32 ~ 1
conducting substrates
non-conducting substrates

## Slide 19
Van der Pauw method
Van der Pauw found a method to determine the resistivity of an arbitrarily shaped sample subject to the following conditions:
a) the contacts are at the boundary of the sample
b) the contacts are infinitely small (point contacts)
c) the sample has uniform thickness
d) the surface of the sample is singly connected, i.e., the sample does not have isolated holes

## Slide 20
Van der Pauw method
#1
#2
#3
#4
I12
V34

## Slide 21
Van der Pauw method
f must satisfy the relation:
For symmetric contacts f = 1

## Slide 22
Van der Pauw method
The previous equations were formulated assuming that contacts are point contacts. For contacts of finite size d on a circular disc of diameter D with d/D << 1, the percent increase in resistivity per contact can be found:
van der Pauw, Philips Research Reports 13 pg. 1-9
for d/D ~ 0.08 Δρ/ρ ~ 0.000559
total change for 4 contacts ~ 0.224%

## Slide 23
1
2
3
4
Van der Pauw method
Hall effect measurements

## Slide 24
…and from Hall coefficient we determine the free charges concentration:

## Slide 25
In intrinsic semiconductors the main factor that affects mobility is the lattice scattering so that mobility always reduces with temperature.
In extrinsic semiconductors there are two contributions
lattice (μL) and
the impurities (μI ).
So the total mobility is given by Matthiessen’s rule, which is

## Slide 26
A. Serra et al., Modulation of charge transport in diamond- based layers , J. Appl. Phys. 94 (2003) 416
Electrical transport in doped-DLC coating examples
Ionized impurities Nd doped
p-type conduction
W doped percolating network

## Slide 27
A. Serra et al., Electronic properties of individual and assembled homotype SWCNT bundles, Chem. Phys. Lett. 509 (2011) 152
Electrical transport in aligned CNT bundles film examples

## Slide 28
Thermal activated process, with low activation energy,
about 60 meV
Long term stability
For example DLC#9

## Slide 29
Structural and morphological characterization

## Slide 30
X-ray diffraction in the Bragg – Brentano geometry represents the more consolidated method to determine the crystal structure of a sample
Based on Bragg law
One obtain the peaks that allows to determine the lattice spacing set
2d sin q = n l

## Slide 33
K is a factor form (for spherical nanocrystals K=1)

## Slide 34
Turbostratic graphite
HOPG
MWCNT
Microdiamond

## Slide 35
From X-ray diffraction to Raman spectroscopy:
From structure to chemistry

## Slide 36
Raman spectroscopy is particularly well suited to molecular morphology characterization of carbon materials. Every band in the Raman spectrum corresponds directly to a specific vibrational frequency of a bond within the molecule.
Raman spectroscopy

## Slide 37
The graphite spectrum has several bands in the spectrum and the main band has shifted from 1332 cm-1 in diamond to 1582 cm-1 in graphite.
The reason for this is that graphite is composed of sp2 bonded carbon in planar sheets in which the bond energy of the sp2 bonds is higher than the sp3 bonds of diamond.
The higher energy of the sp2 bonds in graphite pushes the vibrational frequency of the bonds and hence the frequency of the band in the Raman spectrum to higher frequency. The 1582 cm-1 band of graphite is known as the G band.

## Slide 38
Raman spectra of DLC films show two contributes G and D peaks.
The simplest fit consists of 2 Lorentzians or 2 Gaussians. In alternative it is used a Breit-Wigner-Fano line for the G peak and a Lorentzian for D peak.

## Slide 39
Sample | ID/IG Gauss | ID/IG Lorentz | ID/IG BWF-L
DLC9 | 0.75 | 0.69 | 0.67
DLC30 | 0.72 | 0.59 | 0.57
DLC38 | 0.78 | 0.53 | 0.54

## Slide 40
Diamond-like carbon is amorphous carbon with a significant sp3 fraction.
Three-stage model:
1) Graphite (G)– nanocrystalline graphite (nc-G)
2) nanocrystalline graphite (nc-G) – amorphous carbon (a-C)
3) amorphous carbon (a-C) – tetrahedral amorphous carbon (ta-C)

## Slide 41
The D and G band ratio can be used to measure the crystalline size La of nanographite.
For stage 1, Tuinstra-Koenig model:
For stage 2 and 3, Ferrari-Robertson model:
The plane size La of crystallites can be determined by using the Raman spectrum of nanographite.
The local arrangement of atoms in nanographite has defined the edges as an armchair or zigzag shape. This local arrangement of atoms can determined by the disorder induced bands in the Raman spectrum of nanographite.

## Slide 42
The shifts of the G band are correlated with stress conditions within the DLC films, so the residual stress s can be calculated by the following relation (Miki, Nishimoto et al. Surf. Coat. Technol. 283 (2015) 274-280)
Where S is the shear modulus about 70 GPa, u is the Poison’s ratio about 0.3, and Dw is the shift in the Raman wavenumber of the G band, w0 is the Raman wavenumber of reference

## Slide 43
 | D cm-1 | G cm-1 | ID/IG | s (GPa) | L (nm) | rsheet (ohm/sq)
#2 | 1391 | 1549 | 0.905 | 5.42 | 1.28 | 2.75x106
#3 | 1387 | 1550 | 0.828 | 5.26 | 1.23 | 1.44x105
#8 | 1392 | 1553 | 0.885 | 4.77 | 1.27 | 1.2x105
#9 | 1391 | 1551 | 0.618 | 5.09 | 1.04 | 1.02x108
#10 | 1401 | 1553 | 0.486 | 4.76 | 0.94 | 1.2x109
HOPG reference

## Slide 44
5 nm
D=(1.8 ±0.5) nm
=(0.020±0.05)

## Slide 45
Thank you for attention