## Slide 1: Multimaterial Coatings for 3rd Generation Gravitational Wave Detectors
Dr Peter G. Murray
Research Fellow
Institute for Gravitational Research

## Slide 2
Peter Murray
on behalf of
Jessica Steinlechner
Iain Martin
Simon Tait
Maya Kinley-Hanlon
Graeme McGhee
Sheila Rowan
Jim Hough
Jessica Steinlechner
Lukas Terkowski
Felix Pein
Roman Schnabel

## Slide 3
Introduce multi-material coatings
Absorption at 2µm
Room temperature mechanical loss measurements
Cryogenic mechanical loss measurements
What do we know so far?
Future Plans
Content

## Slide 4
Silica/(doped) tantala is the coating of choice in current advanced gravitational wave detectors
e.g. low absorption and relatively low mechanical loss
However, the thermal noise performance (due to mechanical loss) will be a limiting factor in their operating sensitivities
Amorphous silicon (a-Si) has been shown to have very low mechanical loss
Unfortunately, it has much higher absorption than both silica and (doped) tantala
So, can we design a coating which can take advantage of the low mechanical loss of a-Si while still using silica/tantala layers to keep low absorption?
Background

## Slide 5
Background

## Slide 6
Since those 2015 papers we have learned:
The optical absorption of ion-plated coatings is ~ 3× lower than for IBS a-Si (at their optimum heat treatment)
The optical absorption (at their optimum heat treatment) of ion-plated a-Si is ~7× lower at 2 μm than at 1550 nm
At 2 μm the absorption also can be reduced by at least 70 % with cryogenic cooling (reduction with cooling previously shown for IBS a-Si at 1550 nm by A. Markosyan)
The cryogenic mechanical loss of as-deposited ion-plated silica found to be lower than IBS silica (R. Robie thesis)
Designed a multi-material coating, deposited using ion-plating, and optimised for use at 2 μm
Background

## Slide 7
Multimaterial coating design

## Slide 8
Multimaterial coating design
 | a-Si | SiO2 | Ta2O5 | SiO2
Lower | 5 | 5 |  | 
Upper |  |  | 5 | 5
Full | 5 | 5 | 5 | 5

## Slide 9
Absorption at 2 µm

## Slide 10
Absorption measured using a Photothermal Common-Path Interferometer
                Peak shows the level of coating absorption
Absorption at 2 µm

## Slide 11
Absorption at 2 µm
Previous work by J. Steinlechner (Phys. Rev. Lett. 120, 263602) also showed a minimum in the absorption of ion-plated deposited a-Si at ~500 °C

## Slide 12
Room Temperature Mechanical Loss

## Slide 13
 | a-Si | SiO2 | Ta2O5 | SiO2
Lower | 5 | 5 |  | 
Upper |  |  | 5 | 5
Full | 5 | 5 | 5 | 5
3in silica discs For measurement on GeNS [Cessarini, E. et al. Rev.Sci.Instrum.80 (2009), 053904]
Silica cantilevers For room temperature mechanical loss and stress measurements
Silicon cantilevers For cryogenic mechanical loss measurement
2in Silicon discs For cryogenic mechanical loss measurement
Mechanical loss samples

## Slide 14
Cantilevers are held tightly on a thicker “clamping” block
Discs are balanced on a convex lens at the centre of the GeNS
System is pumped down to high vacuum <10-6 mBar
Laser light is shone onto the surface of the samples and reflected onto a quad photodiode
Samples are electrostatically driven at resonance via drive place placed nearby
The ring down is recorded
Mechanical loss measurements

## Slide 15
Room Temperature Measurements Full Stack Ta2O5/SiO2/aSi
Preliminary
Developed a new python script to better deal with degenerate modes
Here ~f = 0.16 Hz

## Slide 16
Heat treatment of samples to 300, 400 and 500 °C

## Slide 17
Room Temperature Measurements Full Stack Ta2O5/SiO2/aSi
Preliminary

## Slide 18
Room Temperature Measurements Full Stack Ta2O5/SiO2/aSi
Preliminary

## Slide 19
Room Temperature Measurements Full Stack Ta2O5/SiO2/aSi
Preliminary

## Slide 20
Average coating loss after increased heat treatment

## Slide 21
Average coating loss after increased heat treatment

## Slide 22
Average coating loss after increased heat treatment

## Slide 23
Average coating loss after increased heat treatment
Measurement of mechanical loss of 550, 600 °C + heat treatments currently underway

## Slide 24
Cryogenic Mechanical Loss

## Slide 25
Cryogenic Mechanical Loss
Dual experimental set up
Simultaneous 2× silicon cantilever measurements

## Slide 26
Cryogenic Mechanical Loss
2× independent read out systems
Liquid cryogen (LHe/LN2) cooled
~8 – 300 K PID temperature control

## Slide 27
Measure a range of the bending modes from 500 Hz – 30,000 Hz
These are easily predictable
Also measure a number of torsional modes
These can either be found by running a wide scan or
Use bending mode resonant frequencies to calculate the cantilever thickness which can then be used in finite element models
Cryogenic Mechanical Loss

## Slide 28
Typical Cryogenic Mechanical Loss Measurements Upper Stack Ta2O5/SiO2 ~1.29 kHz

## Slide 29
Predicting mechanical loss
2015 paper written using measured values from IBS coatings

## Slide 30
Single Layer SiO2 ~1.19 kHz

## Slide 31
Single Layer SiO2 ~1.19 kHz

## Slide 32
Single Layer Ta2O5 ~1.27 kHz

## Slide 33
aSi measurements now extended to cover 10-300K
Single Layer aSi ~1.05 kHz

## Slide 34
Single Layer a-Si ~1.05 kHz

## Slide 35
Predicting Multimaterial Mechanical Loss

## Slide 36
Predicted Lower Stack SiO2/a-Si Mechanical Loss

## Slide 37
Predicted Lower Stack SiO2/a-Si Mechanical Loss

## Slide 38
Predicted Upper Stack Ta2O5/SiO2
Mechanical Loss

## Slide 39
Predicted Upper Stack Ta2O5/SiO2
Mechanical Loss

## Slide 40
Predicted Full Stack Ta2O5/SiO2/a-Si
Mechanical Loss
Believe curvature of cantilever is effecting thermoelastic loss
(M. Fletcher PhD thesis 2019)

## Slide 41
Predicted Full Stack Ta2O5/SiO2/a-Si
Mechanical Loss

## Slide 42
Comparison of Ion-plated losses with IBS predictions
2015 paper written using measured values from IBS coatings
These had also been heat treated
We have as-deposited values on IBS samples for comparison

## Slide 43
Comparison of Ion-plated losses with IBS predictions
Lower Stack SiO2/a-Si
?

## Slide 44
Comparison of Ion-plated losses with IBS predictions
Upper Stack Ta2O5/SiO2
?

## Slide 45
Comparison of Ion-plated losses with IBS predictions
Full Stack Ta2O5/SiO2/a-Si
?

## Slide 46
Predicted 500 °C HT
Full Stack Ta2O5/SiO2/a-Si
Mechanical Loss

## Slide 47
Predicted 500 °C HT
Full Stack Ta2O5/SiO2/a-Si
Mechanical Loss

## Slide 48
Predicted 500 °C HT
Full Stack Ta2O5/SiO2/a-Si
Mechanical Loss

## Slide 49
Predicted 500 °C HT
Full Stack Ta2O5/SiO2/a-Si
Mechanical Loss

## Slide 50
Predicted 500 °C HT
Lower Stack SiO2/a-Si
Mechanical Loss

## Slide 51
Predicted 500 °C HT
Upper Stack Ta2O5/SiO2
Mechanical Loss

## Slide 52
Comparison of Ion-plated losses with IBS predictions
Full Stack Ta2O5/SiO2/aSi
At low temperatures as-deposited ion-plated full stack has lower loss than best estimate for an equivalent heat treated IBS coating

## Slide 53
Future Plans: CryoGeNS
Cryogenic mechanical loss measurements of 2” diameter silicon discs is now underway
Results will appear in ~2020 thesis by S. Tait

## Slide 54
Commissioning a new small pulse-cooled cryostat
M. Kinley-Hanlon and 2 MSci students V. Graham and B. McCrindle
Flexible small experimental space
Cryogenic absorption
Silicon Cantilever measurements
Silicon GeNS measurement
Future Plans: Cryogen Free GeNS

## Slide 55
Multimaterial coating behaves as expected based on our predictions from single-layers
A minima in absorption is observed after heat treatment at 500 °C
Mechanical loss also observed to improve with heat treatment
Mechanical loss of the full multimaterial stack is ~40% lower than the “upper” silica/tantala coating
In Summary…

## Slide 56
Shown predictions of mechanical loss of multimaterial coatings from single layers match experimentally measured values
  Both in terms of level of mechanical loss and loss peaks
At low temperatures, even in their as-deposited state ion-plated, these multimaterial coatings perform better than the best theoretical IBS multimaterial coating
Heat treatment of multilayer stacks to 500 °C should further improve the cryogenic mechanical loss
This point towards seeing a real thermal noise reduction for acceptable absorption compared to silica/tantala
Exciting time ahead with cryogenic cantilever, GeNS and absorption measurement capabilities
In Summary…

## Slide 57
#TeamUoG
@UofGravity
Thank you for your attention
peter.murray@glasgow.ac.uk