## Slide 1: Fabrication Test 1
Francesco Mattioli, F. Chiarello, G. Torrioli
1Istituto di Fotonica e Nanotecnologie

## Slide 2: Geometry
Chip 1
300 400 500 600 700 800
Gap (nm)
Dose 718 687 656 625
mC/cm2

## Slide 3: Bilayer and undercutting
COP 33 10% AR-P 617.10 spessore 1031 nm
PMMA 6% AR-P 669.06 spessore totale 1720 nm

## Slide 4: Bilayer and undercutting
COP 33 10% AR-P 617.10 spessore 1031 nm
PMMA 6% AR-P 669.06 spessore totale 1720 nm
Undercutting 360nm

## Slide 5: Bilayer and undercutting
COP 33 10% AR-P 617.10 spessore 1031 nm
PMMA 6% AR-P 669.06 spessore totale 1720 nm

## Slide 6: Fabrication of the tunnel junction
O2 5 min. 1.0 mbar
155° 300 Å Al
90° 300 Å Al

## Slide 7: Fabrication of the tunnel junction
Lift off

## Slide 8: Fabrication of the tunnel junction
300nm

## Slide 9: Fabrication of the tunnel junction
700nm
600nm
500nm
400nm

## Slide 10: Fabrication of the tunnel junction
400nm
500nm
600nm
700nm
400nm
Gap
500nm
600nm
700nm
400nm
800nm

## Slide 11: Fabrication of the tunnel junction
400nm

## Slide 12: Fabrication of the tunnel junction
D 2 656 mC/cm2 | L1 W | R1 W | L2 W | R2 W | L3 W | R3 W | L4 W | R4 W | L5 W | R5 W | L6 W | R6 W
Gap | 300 nm |  | 400 nm |  | 500 nm |  | 600 nm |  | 700 nm |  | 800 nm | 
G1 | 38 | 38 | 42 | 39 | 40 | 38 | 39 | 41 | 68 | 69 | 53 | 64
G2 | 53 | 55 | 51 | 45 | 43 | 43 | 41 | 42 | 64 | 62 | 47 | 50
 | L1 R1 | / | L2 R2 | / | L3 R3 | 11 | L4 R4 | 8 | L5 R5 | 53 | L6 R6 | 37
 | G1 G2 |  |  |  |  |  | 63 |  |  |  |  | 
D 3 687 mC/cm2 | L1 W | R1 W | L2 W | R2 W | L3 W | R3 W | L4 W | R4 W | L5 W | R5 W | L6 W | R6 W
Gap | 300 nm |  | 400 nm |  | 500 nm |  | 600 nm |  | 700 nm |  | 800 nm | 
G1 | 55 | 59 | 64 | 68 | 72 | 77 | 84 | 84 | 85 | 86 | 86 | 87
G2 | 86 | 84 | 84 | 83 | 83 | 83 | 77 | 73 | 69 | 65 | 60 | 57
 | L1 R1 | 55 | L2 R2 | 54 | L3 R3 | 53 | L4 R4 | 53 | L5 R5 | 54 | L6 R6 | 55
 | G1 G2 |  |  |  |  |  | 77 |  |  |  |  | 
D 2 656 mC/cm2 | L1 W | R1 W | L2 W | R2 W | L3 W | R3 W | L4 W | R4 W | L5 W | R5 W | L6 W | R6 W
Gap | 300 nm |  | 400 nm |  | 500 nm |  | 600 nm |  | 700 nm |  | 800 nm | 
G1 | 38 | 38 | 42 | 39 | 40 | 38 | 39 | 41 | 68 | 69 | 53 | 64
G2 | 53 | 55 | 51 | 45 | 43 | 43 | 41 | 42 | 64 | 62 | 47 | 50
 | L1 R1 | / | L2 R2 | / | L3 R3 | 11 | L4 R4 | 8 | L5 R5 | 53 | L6 R6 | 37
 | G1 G2 |  |  |  |  |  | 63 |  |  |  |  |