## Slide 1
R&D for surface properties validation
R. Cimino LNF
The problem from the LHC side: Electron cloud issues
What (I understand) is the problem from LHCspin side
Experimental approach and studies
R&D we plan to do (submitted for funds at NSC5)
Conclusion

## Slide 2
Scientific background
In LHC and in most of the highest performance present and planned circular accelerators of positive particles (positrons, protons) the circulating beam can interact with the accelerator vacuum components causing detrimental effects. Vacuum degradation, beam instabilities up to beam losses may easily occur.
Those interactions strongly depends on material properties.

## Slide 3
Let us see this in details for
the LHC case

## Slide 4: One real example to see what the beam does to Vacuum:
450 GeV – 150 ns bunch spacing: Merged vacuum @ LHC
8-10-2010

## Slide 5: Exotic Vacuum behavior @ LHC:
Beam 1
Beam 2
No pressure Increase
Pressure Increase
450 GeV – 150 ns bunch spacing: Merged vacuum
8-10-2010

## Slide 6: Easily solved: Installation of Solenoids
Solution: Solenoids have been wrapped around the vacuum system!!!

## Slide 7: Solenoids have effect on pressure!!!
Beam Intensity
Solenoid ON
A4L1
Solenoid ON
A4R1
Remove multipacting
Still primary electrons
After 20 min
DP ≈7·10-10
After 20 min
DP ≈7·10-10

## Slide 8
Beam Intensity
Solenoid ON
A4L1
Solenoid ON
A4R1
Remove multipacting
Still primary electrons
After 20 min
DP ≈7·10-10
After 20 min
DP ≈7·10-10
Evidence for:
e-Cloud
Instabilities
due to the interaction between beams and Vacuum system walls
Solenoids have effect on pressure!!!

## Slide 9: Vacuum in new generation accelerators is much “more” than a technical issue!
Let us see what may cause such beam and/or pressure instabilities.
The case of the:
LHC arcs

## Slide 10: Static Vacuum
Cold Bore @ 1.9 K
Extreme High Static Vacuum
(<< 10-13 mbar)

## Slide 11
Cold Bore @ 1.9 K
Radial Distance
T=0, without beam
CB
CB
BS
BS
Need of a Beam Screen
@ 5K< T <20K
to reduce heat load (SR, Eddy current, Impedance, etc…) on Cold bore for thermal load issues

## Slide 12
Pumping slots
Pumping slots
shields
Cu layer
Cooling tubes
“Saw teeth”
The Beam Screen is a complex technological product!

## Slide 13
Why do we need Vacuum???
Radial Distance
CB
CB
BS
BS

## Slide 14: This define: Vacuum Beam Life time (t)
Radial Distance
CB
CB
BS
BS
+ +
+ + + +
+ + + + + +
+ + + +
+ +
p +
The beam interacts with the residual gas:
Where: σ is the cross section i.e. the probability the beam interacts with the atoms of target
I is the beam intensity
        n is the atomic density of a target of thickness dx
        v is the beam velocity
The vacuum life time must be much larger (i.e. >> 24 h) than other life times such as e.g. the particle loss due to the collisions
Beam – Gas Interactions

## Slide 15
Radial Distance
CB
CB
BS
BS
+ +
+ + + +
+ + + + + +
+ + + +
+ +
p +
Ionisation cross section is a function of the speed & the charge of the projectile and of the nature of the residual gas
Chart: Ionisation cross section for proton beam
| 1 | 1.2 | 1.4 | 1.6 | 1.8 | 2 | 2.2000000000000002 | 2.4 | 2.6 | 10 | 26 | 100 | 200 | 450 | 600 | 1000 | 7000
H2 | 1.2494e-22 | 4.3575e-23 | 3.2147e-23 | 2.7791e-23 | 2.5611e-23 | 2.4372e-23 | 2.3616e-23 | 2.3138e-23 | 2.2831e-23 | 2.4297e-23 | 2.7105e-23 | 3.1283e-23 | 3.3448e-23 | 3.5982e-23 | 3.6881e-23 | 3.8478e-23 | 4.456e-23
He | 1.1244e-22 | 4.0149e-23 | 2.9845e-23 | 2.5924e-23 | 2.3976e-23 | 2.2883e-23 | 2.2228e-23 | 2.1825e-23 | 2.1576e-23 | 2.3545e-23 | 2.6604e-23 | 3.1128e-23 | 3.3471e-23 | 3.6213e-23 | 3.7186e-23 | 3.8913e-23 | 4.5495e-23
CH4 | 7.733e-22 | 2.7697e-22 | 2.0609e-22 | 1.7912e-22 | 1.6574e-22 | 1.5824e-22 | 1.5376e-22 | 1.5101e-22 | 1.4932e-22 | 1.6346e-22 | 1.8499e-22 | 2.168e-22 | 2.3327e-22 | 2.5255e-22 | 2.5939e-22 | 2.7154e-22 | 3.1781e-22
H2O | 6.0006e-22 | 2.1416e-22 | 1.5917e-22 | 1.3825e-22 | 1.2785e-22 | 1.2202e-22 | 1.1852e-22 | 1.1636e-22 | 1.1503e-22 | 1.2547e-22 | 1.4174e-22 | 1.6581e-22 | 1.7827e-22 | 1.9285e-22 | 1.9803e-22 | 2.0722e-22 | 2.4223e-22
CO | 6.4194e-22 | 2.3166e-22 | 1.7278e-22 | 1.5039e-22 | 1.3931e-22 | 1.3313e-22 | 1.2946e-22 | 1.2722e-22 | 1.2588e-22 | 1.3882e-22 | 1.5768e-22 | 1.8551e-22 | 1.9992e-22 | 2.1678e-22 | 2.2277e-22 | 2.3339e-22 | 2.7387e-22
O2 | 7.031e-22 | 2.5509e-22 | 1.9058e-22 | 1.6605e-22 | 1.5394e-22 | 1.4719e-22 | 1.4321e-22 | 1.408e-22 | 1.3937e-22 | 1.5449e-22 | 1.7592e-22 | 2.0752e-22 | 2.2388e-22 | 2.4302e-22 | 2.4981e-22 | 2.6187e-22 | 3.0782e-22
CO2 | 1.0284e-21 | 3.6949e-22 | 2.752e-22 | 2.3934e-22 | 2.2156e-22 | 2.1161e-22 | 2.0568e-22 | 2.0206e-22 | 1.9985e-22 | 2.1945e-22 | 2.4873e-22 | 2.9198e-22 | 3.1437e-22 | 3.4058e-22 | 3.4988e-22 | 3.6639e-22 | 4.2929e-22
Heavy gas must be avoided
Beam – Gas Interactions: ion production

## Slide 16
Radial Distance
CB
CB
BS
BS
+ +
+ + + +
+ + + + + +
+ + + +
+ +
p +
Ions interact with accelerator wall: Ion desorption yield
Several molecules can be desorbed per ion  Sputtering
A.G. Mathewson, CERN ISR-VA/76-5
Unbaked
stainless steel
N2+
Varies with: - the material,
- the ion energy
- and ion species
induced ion desorption: pressure, beam-ion interaction (and desorption) increase.
It is a resonant phenomenon causing Vacuum instability
Above a certain critical beam current, there will be a pressure runaway.

## Slide 17
Cold Bore @ 1.9 K
Radial Distance
T=0, without beam
CB
CB
BS
BS
Let us see what happens during operation and beam passage to:
The vacuum system
the Beam screen Surface

## Slide 18: calculation
Radial Distance
CB
CB
BS
BS
Time = 0
+ +
+ + + +
+ + + + + +
+ + + +
+ +
p +
Synchrotron Radiation
A charged particle which is accelerated produce radiation
For a relativistic particle, the radiation is highly peaked (opening angle ~ 1/g)
Critical energy:
divide the power spectrum in two equals parts

## Slide 19: calculation
Radial Distance
CB
CB
BS
BS
Time = 0
+ +
+ + + +
+ + + + + +
+ + + +
+ +
p +
Synchrotron Radiation
The average power
emitted by the beam
per unit length is:
For LHC: P = 0.17 W/m/apert.

## Slide 20
Radial Distance
CB
CB
BS
BS
+ +
+ + + +
+ + + + + +
+ + + +
+ +
Photo-desorption:
O. Gröbner et. al. EPAC 1992

## Slide 21
Radial Distance
CB
CB
BS
BS
+ +
+ + + +
+ + + + + +
+ + + +
+ +
Photo-desorption:
O. Gröbner et al.
J.Vac.Sci. 12(3), May/Jun 1994, 846-853
Cu baked at 150°C
The dynamic pressure decrease by several orders of magnitude with photon dose: “photon conditioning”
The photon desorption yield is characterised by ηphoton
See: talk from Marco Angelucci on “Windy”

## Slide 22
Radial Distance
CB
CB
BS
BS
+ +
+ + + +
+ + + + + +
+ + + +
+ +
Photo-desorption at LT:
See: talk from Marco and Luisa
Initial yield, η0, are smaller than at room T temperature
BUT at LT:
presence of physisorbed molecule
DAFNE-L Beamlines & setups are unique tools to perform those studies at LT

## Slide 23
Radial Distance
CB
CB
BS
BS
Parameters LHC H-L LHC FCC-hh
Photons induce Heat load:
+ +
+ + + +
+ + + + + +
+ + + +
+ +
PTOT
Power to dissipate 1W (W)
Heat Load Dissipation VS Temperature
PTOT

## Slide 24
Radial Distance
CB
CB
BS
BS
+ +
+ + + +
+ + + + + +
+ + + +
+ +
Photon reflectivity:
N. Mahne et al. App. Surf. Sci. 235, 221-226, (2004).
PS: reflected photons do NOT induce HL.
See: R. Cimino V. Baglin and F. Schäfers PRL 2015
See Andrea Liedl talk
The LHC BS has a Sow tooth structure in the h plane

## Slide 25
Radial Distance
CB
CB
BS
BS
Time = 5 ns
+ +
+ + + +
+ + + + + +
+ + + +
+ +
p +
    R. Cimino, V. Baglin, I. R. Collins.
    Phys.Rev. ST-AB 2 63201 (1999).
SR induce Photoemission:(vs. hn, Q, E,T, B)
Produced e- (PY): important for single beam instabilities (K.Ohmi PRL 2000)

## Slide 26
Radial Distance
CB
CB
BS
BS
Time = 10 ns
+ +
+ + + +
+ + + + + +
+ + + +
+ +
Beam induced el. acceleration
p +
(F.Zimmermann)
At the moment of creation
After acceleration
100
0
20
40
60
80
Energy (eV)

## Slide 27
Radial Distance
CB
CB
BS
BS
Time = 15 ns
+ +
+ + + +
+ + + + + +
+ + + +
+ +
R. Cimino et al Phys. Rev. Lett. 93, 14801 (2004).
e- induced e- emission
SEY (Secondary El Yield)

## Slide 28
Radial Distance
CB
CB
BS
BS
Time = 25 ns
+ +
+ + + +
+ + + + + +
+ + + +
+ +
P +
e- cloud Build-up
+ +
+ + + +
+ + + + + +
+ + + +
+ +
Time structure & simulations.
P +
(F. Zimmermann)

## Slide 29
Radial Distance
CB
CB
BS
BS
Time = 25 ns
+ +
+ + + +
+ + + + + +
+ + + +
+ +
P +
e- cloud Build-up
+ +
+ + + +
+ + + + + +
+ + + +
+ +
P +
R. Cimino et al
Phys. Rev. Lett. 93, 14801 (2004).
e-cloud build up causes Heat load!

## Slide 30
Radial Distance
CB
CB
BS
BS
Time = 25 ns
+ +
+ + + +
+ + + + + +
+ + + +
+ +
P +
e- cloud Build-up
+ +
+ + + +
+ + + + + +
+ + + +
+ +
P +
Dynamic
pressure
increase !!!
Desorbed gas
It is a beam/Vacuum issue!
Governed by: h
Electron Desorption Yield
See: Luisa Spallino Talk

## Slide 31
Radial Distance
CB
CB
BS
BS
Time = 25 ns
+ +
+ + + +
+ + + + + +
+ + + +
+ +
P +
e- cloud induced Beam blow up
+ +
+ + + +
+ + + + + +
+ + + +
+ +
P +
e-cloud build up It affects beam quality!
!
+ +
+ + + +
+ + + + + +
+ + + +
+ +
+ +
+ + + +
+ + + + + +
+ + + +
+ +
+ +
+ + + +
+ + + + + +
+ + + +
+ +
+ +
+ + + +
+ + + + + +
+ + + +
+ +
+ +
+ + + +
+ + + + + +
+ + + +
+ +
+ +
+ + + +
+ + + + + +
+ + + +
+ +
+ +
+ + + +
+ + + + + +
+ + + +
+ +
+ +
+ + + +
+ + + + + +
+ + + +
+ +
+ +
+ + + +
+ + + + + +
+ + + +
+ +
Jean-Luc Vay
IPAC’2012

## Slide 32: Electron cloud in accelerators
The Surface Science properties of relevance:
SEY (Secondary Electron Yield);
PY (Photo Yield);
R (photon Reflectivity)
Data are needed to correctly simulate accelerator behaviour but also to trigger R&D on various mitigation strategies
Low SEY materials - Low Desorption – Low/high Reflectivity and PY
R. Cimino and T. Demma
“Electron cloud in Accelerators” Int. J. Mod. Phys. A 29 (2014) 1430023 (pag. 65).

## Slide 33: Surface sensitivity of SEY
L. A. Gonzalez et al., AIP Adv. (2017)
SEY is an intrinsic material property strongly sensitive to the surface composition and chemical state
Chemisorbed/physisorbed compounds modify the metal surface
Effect of contaminants of the atmosphere at room temperature

## Slide 34: Surface sensitivity of SEY
L. A. Gonzalez et al., AIP Adv. (2017)
Kuzucan et al., J. Vac. Sci. Technol. A (2012)
SEY of cold surfaces influenced by gas physisorption
SEY is highly sensitive to the presence of adsorbates, even at sub-monolayer coverage
Residual gas in cryogenic vacuum
CO thick layer coverage
SEY is an intrinsic material property strongly sensitive to the surface composition and chemical state

## Slide 35: Surface sensitivity of SEY
e- cloud mitigation strategies
SEY is an intrinsic property of materials, strongly sensitive to the surface morphology
R. Valizadeh et al. , Appl. Surf. Sci. (2017)
Laser ablation on Cu substrate
(LASE-Cu)
Engineering the surface morphology

## Slide 36: Strategy and experimental set-up at LNF
Low Temperature
Gas Adsorption
Gas Desorption
SEY variation
Temperature variations/photons/electrons
Pressure variation
SEY, Mass Spectrometry, Thermal Programmed Desorption (TPD) and XPS (as soon)
as useful techniques to quantitatively follow adsorption/desorption kinetics

## Slide 37: Strategy and experimental set-up at LNF
Temperature Programmed Desorption (TPD) and Mass Spectrometry measurements
Equipment : QMS (Hiden HAL 101 Pic)
Secondary Electron Yield (SEY) measurements
Equipment : Electron gun, Faraday cup
LNF-cryogenic manipulator
Sample at 15-300 K
Ultra high vacuum systems
main chamber
preparation
chamber
fast-entry lock

## Slide 38: Strategy and experimental set-up at LNF
Screen
Sample
Sample Holder
Heater
T Sensor

## Slide 39: Strategy and experimental set-up at LNF
Retractile gas dosing system
Electron gun

## Slide 40: Strategy and experimental set-up at LNF
+
-
ISam
Vbias
+
-
Iin
Vbias
SEY = δ =
Iout
Iin
Faraday
Sample
Sample
Faraday Cup

## Slide 41
+
-
ISam
Vbias
+
-
Iin
Vbias
SEY = δ =
Iout
Iin
Faraday
Sample
=
Iin - Isam
Iin
Sample
Faraday Cup
Strategy and experimental set-up at LNF

## Slide 42: Results
  TPD from LASE-Cu for temperature induced vacuum transients study
  SEY to probe the surface coverage
  Electron desorption studies: preliminary results

## Slide 43: TPD from LASE-Cu for temperature induced vacuum transients study
poly-Cu
Representative of Laser treated Cu
What about the influence of the surface features on the vacuum stability?
Comparative study of Ar TPD from flat poly-Cu and LASE-Cu samples

## Slide 44: TPD from LASE-Cu for temperature induced vacuum transients study
L. Spallino et al. , Appl. Phys. Lett. (2019)
Single TPD peak at ~30 K corresponding to the desorption of a condensed thick Ar layer
Desorption temperature determined by the weak Ar-Ar van der Waals interaction energies
TPD peak at ~30 K corresponding to the desorption of a condensed thick Ar layer together with a broad TPD profiles, whose peak temperatures and widths depend on the Ar dose
TPD characteristics determined by the sponge-like structural features
poly-Cu
LASE-Cu

## Slide 45: TPD from LASE-Cu for temperature induced vacuum transients study
Conceptually identical results have been obtained with CO and CH4
poly-Cu
LASE-Cu
L. Spallino, M. Angelucci and R. Cimino, to be published
+ CO
+ CO
+ CH4
+ CH4

## Slide 46: TPD from LASE-Cu for temperature induced vacuum transients study
L. Spallino, M. Angelucci and R. Cimino, to be published
TPD of 100 L H2 dosed on poly-Cu and LASE-Cu samples held at T~15-18 K
No TPD signal should be observed by considering the H2 vapor suture pressure curve!!!
The wide distribution of high energy adsorption sites within the inner pore is responsible for the H2 TPD signal from LASE-Cu sample
H2

## Slide 47: SEY to probe surface coverage
Ar adsorption on polycrystalline-Cu substrate as a test system
SEY strongly changes with adsorbed gas
SEY could be used to follow gas coverage variations and make coverage calibration
J. Cazaux et al.; Phys. Rev. B, 71 (2005)
L. Spallino, M. Angelucci and R. Cimino, to be published

## Slide 48: How a Coating modify SEY? (the case of c on Cu)
We followed the growth of thin C layers on Cu with XPS to measure its thickness
Increasing C
We simultaneously follow SEY changes

## Slide 49: How a Coating modify SEY? (the case of c on Cu)
Could follow dmax vs C coverages
Emax
dmax
Could follow Emax vs C coverages
15-20 Ml (~ 5-6 nm) of C determines SEY properties.
What about Water on C (or on Cu)?

## Slide 50: What about Water on Cu?
V . Baglin, J. Bojko1, O. Gröbner, B. Henrist
THE SECONDARY ELECTRON YIELD OF TECHNICAL MATERIALS AND ITS VARIATION WITHSURFACE TREATMENTSV Proceedings of EPAC 2000, Vienna, Austria
Moreover It
charges up!

## Slide 51: (Tentative) Work to do for LHCspin:
Given the facts (to be better identified) that:
Water Ice grow differently ad different T
Water will affect SEY (as a function of thickness and growth morphology)
Thick Ice will charge up (no good) and may have high SEY
We need to study, as a function of substrate (best if flat) and substrate Temperature:
  SEY as a function of Water thickness (the idea is to choose a T where Ice is compact and the thickness is optimum for maintaining H polarization with minimum influence on SEY)
  See whether the interaction with of Atomic H modifies SEY and other surface Properties.
  ...?

## Slide 52
SurfAce and mateRial studies for Accelerator TechnologY And related topics
INFN has a longstanding tradition and a series of highly developed competences on issues related to various aspects of accelerator’s R&D.
The ARYA project is subdivided in Working Packages (WP’s).
All the WP’s will tackle research ew challenges which are studied in international collaborations, more specifically, for HL LHC, FCC and others.
The goal of this proposal is to grant the necessary resources to best contribute to the ongoing and future collaborations highlighting INFN role on studies on collective effects and of material properties for future accelerators.
New experiment for 2020-2024:
ARYA

## Slide 53: ARYA WP’S
WP | TITLE | UNITS INVOLVED | RESPONSIBLE
WP1 | Electron Stimulated desorption studies | LNF-INFN CERN | L. Spallino & R. Cimino
WP2 | Material properties under photon irradiation. | LNF-INFN CERN | M. Angelucci & R. Cimino
WP3 | LHCspin: surface properties validation | LNF-INFN CERN | P. Di Nezza & R. Cimino
WP4 | Beam dynamics studies and material properties for future accelerators | Rome1-INFN Na-INFN LNF-INFN CERN | M. Migliorati
WP5 | Impedance Study and measurements of new LESS | Na-INFN Rome1-INFN CERN LNF-INFN | M.R. Masullo
WP6 | Low SEY thin films technology for aerospace applications | GSSI, Uni Aquila e LNF-INFN | M. Passacantando & R. Cimino

## Slide 54
WP3 | LHCspin: surface properties validation | LNF-INFN CERN | P. Di Nezza & R. Cimino
This WP will be an R&D for the storage cell to be placed in front of LHCb detector during the long shutdown 3. This new vacuum chamber will be filled with various gasses and, in particular, with polarized atomic Hydrogen and Deuterium, bringing, for the first time, polarized physics at the LHC.
Define a cold narrow coated tube to inhibit recombination.
Should fulfill LHC requirements on Vacuum, e- cloud etc.
Graphite, covered by a thin water layer should be the solution to be studied, optimized and validated.

## Slide 55
WP3 | LHCspin: surface properties validation | LNF-INFN CERN | P. Di Nezza & R. Cimino
This WP will be only on NSC5. It will use the Set-up at LNF. We need a UHV H cracker and the H or D supply.
Coverage and T dependent SEY studies should be conducted on H2O on differently compact a-C substrate (from graphite to highly disordered porous a-C) .
The effect of Absorption on those Surfaces of atomic Hydrogen (or Atomic Deuterium) to see if they remain unperturbed or are somehow perturbed by it.
WP3: Foreseen Requests 2020
    Mobility: 10 k€
    Consumable: 10 k€
    H cracker 32 k€

## Slide 56
Conclusion:
There is a lot to do!
LHCspin community have a lot to teach us!
The R&D needed is extremely challenging but of great (general) interest
Experimental set-up mainly there (?)
Man power is THE issue!

## Slide 57
Tanks to the technical support of DAФNE-L Team:
A. Grilli, M. Pietropaoli, A. Raco, V. Tullio, V. Sciarra and G. Viviani
Thank you for your attention
Thanks to EuroCirCol project and to its scientific community
Thanks to the low temperature team at LNF:
M. Angelucci, A. Liedl, R. Larciprete e L. Spallino.
Thanks to MICA supporting project funded by INFN-SNC5