## Slide 1: Ferrimagnetic switching driven by stochastic resonance in multiferroic (Ge,Mn)Te
Juraj Krempaský :: Photon Science Division :: LNO :: Paul Scherrer Institut
LEAPS meets Quantum Technology, Elba Island, Italy

## Slide 2
From GeTe to (Ge,Mn)Te
JK. et al., PRX 8, 021067 (2018)
Simplest binary ferroelectric material
Di Sante et al., Adv. Mat. 25, 509 (2013)
JK et al, PRR , 003000 (2020)

## Slide 3
(1) H. Przybylinska et al., PRL.112, 047202 (2014) (2) JK. et al., PRB 94 205111 (2016)
(3) JK. et al., PRX 2018
(4) JK. et al., Nat. Comm. 7 13071 (2016)
(5) JK. et al., JPChS 1–8 (2017)
Magnetoelectric switching entangled with Rashba-Zeeman splitting

## Slide 4: (Ge,Mn)Te
E-EF (eV)
JK et al., Nat. Comm. 7 13071 (2016)
L. Brey, Nano Lett. 2017, 17
R. Yoshimi et al., arXiv2022
Nonreciprocal electrical transport
Yoshimi et al., Sci. Adv. 2018; 4
Current driven magnetization switching

## Slide 5: IV-VI MBE (Ge,Mn)Te
„epi-taxis“ = on top,
in perfect military formation
ATOMIS
GROWER
GeTe
Mn
Slide courtesy of G. Springholz, JKU Linz

## Slide 6: (Ge,Mn)Te: the SPR-KKR-CPA model
≈0.5 eV
SPR-KKR-CPA: scattering model based on occupation probability rather than a superlattice
2:1

## Slide 7: Light-induced magnetization switching
Sign of XMCD signal switches spontaneously
Collective bulk effect
Switching is also observed when only one light helicity is used!
Mn1
Mn2
Mn3
J. Stöhr, JMM 200 (1999) 470}497
Non-thermal switching

## Slide 8: Stochastic Resonance (SR) in a nutshell
For bistable systems SR are ‘‘noise benefit effects’’ where input/output signal performance is tunable via a combination of a periodic single-frequency TW input signal and broadband noise DkBT. SR effects can be controlled by:
T= ½TW optimal synchronization of the driving signal with the switching process
tuning the noise level with temperature D  kBT (TW held constant)
periodic drive TW (noise D held constant)
If the “stochastic switch” does no happen here…
…next chance is here!
Gammaitoni et al.: Stochastic resonance, RMP, Vol. 70, No. 1, 1998

## Slide 9: Stochastic Magnetization Resonance (1)
we observe oscillatory TEY

## Slide 10: Stochastic Magnetization Resonance (2)
P
V

## Slide 11: Stochastic Magnetization Resonance (3)
TW
C+ E1  E2
TW/2
TW/2
C- E1  E2
E2E1
E2E1
XMCD1
XMCD2
XMCD3…
TW
…very short TEY increase during Mn(L3) absorption
J. Krempaský et al.,, “Synchronized monochromator and insertion device energy scans at SLS,” AIP Conference Proceedings, vol. 1234, no. 1, Jun. 2010.

## Slide 12: Stochastic Magnetization Resonance (4)
TEYBKG
TEYMnL3 and TEYBKG are TWO “synchronized” signals SMR ON
TEYBKG is a frequency modulated signal
TEYMnL3 is an amplitude modulated signal (TEYMnL3 ≈2xTEYBKG)
TEYMnL3

## Slide 13: Stochastic Magnetization Resonance (5)
TEYMnL3 and TEYBKG are TWO non-synchronized signals
SMR OFF
T2
T1
T2
T1
E1
E2
E3
E4
XMCD

## Slide 14: Stochastic Magnetization Resonance on/off
TW
C+ E1  E2
T2
T1
C- E1  E2
E2E1
E2E1
XMCD1
TW
TW
T2
T1
T2
T1
XMCD2
XMCD3…
Stochastic Magnetization Resonance ON T1=T2=T  T= ½TW
Stochastic Magnetization Resonance OFF T1>T2 T1,T2 ≠ ½TW
*
*Rule #1: optimal stochastic resonance condition

## Slide 15: Stochastic resonance on/off comparison
0T (≈6%)
≈6%

## Slide 16: Quantifying the SMR switching
We count AFM switching events, i.e. evaluate a binomial distribution as “switch” or “no switch” in a set of n*TW XMCD measurements
We count SR retention times, i.e. how many TW cycles it takes before an AFM switch occurs
6
5
0
3
2
1
2
0
0
3
1
1
0
0
1
switches
Retention
times
Example: In these series of 40 XMCD measurements there are 15 switches out of 40 measurements, so the switching probability is 15/40=0.375. Retention time estimates: bottom-up I see that before the first switch there are 6 spectra that look the same, or without switching, and the next switch happens after 5 XMCD cycles, etc… The retention times are summed for all experiments made at the same temperatures and TW.

## Slide 17: Switching probability and spin glass
Switching probability follows M(T) curves below T=35K
Above 35K thermally activated
Switching has to be collective !
Splitting of FC and ZFC curves indicates spin glass
mSR ”negative B-shift” of local B-mean field is characteristic to diluted magnetic semiconductors where magnetic clusters form out of spin glass
≈35 K

## Slide 18: Spin and Orbital moments under SMR
measurements
measurements
init
fluctuations
coalescence
FH-FC @ 6T, 10K

## Slide 19: Spin and Orbital moments under SMR
measurements
Yoshimi et al., Sci. Adv. 2018
Coercive field of ~0.05T
Saturation at ~0.1T
Cusps in magnetisation before reaching remanence, also observed in anomalous Hall coefficient
Suggested to be related to skyrmions
F. Büttner et al., Nat. Mat. 20, 2021

## Slide 21: Conclusions
Direct evidence of light-induced, non-thermal ferrimagnetic switching
Theoretical model of magnetostochastic resonance is developed. It is shown that in the presence of noise the signal-to-noise ratio for a bistable uniaxial ferromagnet can be a million times greater than that for a one-stable ferromagnet.
Combination of FM and AM frequency signal can turn stochastic resonance on and off

## Slide 22: Conclusions
Direct evidence of light-induced, non-thermal ferrimagnetic switching
Spin glass collective magnetization switching
Spin glass collective dynamics with skyrmion-like excitations

## Slide 23: Acknowledgements
Spin-Orbit Interaction Spectroscopy group
Hugo Dil
Martin Gmitra
Gunther Springholz
PSI: SIS beamline
COPHEE
Jan Minar Sunil D’Souza
Ondrej Caha
Masaryk Univ. Brno
XMCD support and PSI sample characterization
Cinthia Piamonteze
Valerio Scagnoli
Carlos Vaz
µSR experiments and analysis
Zaher Salman