Reinforcement of paper artworks with cellulose nanocrystals

C. Mazzuca1, L. Micheli1, A. Operamolla2, M. Titubante1,  F. Di Benedetto3, L. Capodieci3,  L. Severini1, A. Palleschi1 .

1Dipartimento di Scienze e Tecnologie Chimiche, Università di Roma Tor Vergata, Via della Ricerca Scientifica, 00173 Rome, Italy

2Dipartimento di Chimica, Università degli Studi di Bari Aldo Moro, via Orabona 4, I-70126, Bari, Italy

3ENEA - Italian National Agency for New Technologies, Energy and Sustainable Economic Development, SSPT-PROMAS-MATAS, S.S. 7 "Appia" km 706, I-72100 Brindisi (Br), Italy

# The reinforcement of  degraded paper artworks using functionalized cellulose nanocrystals (CNCs) as sustainable fillers. CNCs are nano-dimensioned rods with average length of few hundreds of nanometers and width corresponding to that of an elementary fibril (10 nm). Due to their dimension  they can fill water pools found in amorphous cellulose that is present in degraded and fragile paper artworks. Thus, CNCs can be applied to repair high quality paper. In this context, we propose a new procedure to restore the paper materials, using CNCs, which were prepared and functionalized ad hoc in laboratory as “chemically interacting filler”. CNCs are also transparent, and thus their deposition on the paper artwork will not compromise the optical properties of the artworks that, by definition, a restoration process must preserve. The conservation strategy, proposed herein, is followed using a disposable and compatible real time monitoring tool, made up of an amperometric biosensor coupled with a sampling flow system/Gellan gel (used in the past to monitor the cleaning process of paper artworks). In order to assess the validity of this approach, several invasive and not invasive techniques, such as, fluorescence microscopy, SEM, FTIR-ATR, HPLC, XRD have been used .