## Multifunctional properties of nanocomposites at very high content of Graphene Nanoplatelets

## Fabrizia Cilentoa, Alfonso Martoneb, Francesco Bertocchic and Michele Giordano*b,

a Department of Chemical, Materials and Production Engineering, University of Naples Federico II, Napoli, Italy P.le Tecchio, 80125 Naples, Italy

b CNR-IPCB, Institute of Polymers, Composite and Biomaterials, Consiglio Nazionale delle Ricerche, P.le E Fermi, 80055 Portici (Naples), Italy

cJaber Innovation srl,Rome, Italy

*corresponding author: michele.giordano@cnr.it

Graphene has unsurpassed mechanical, electrical, thermal and barrier properties: it owns the highest Young modulus, it supports a lossless electron transport and shows the highest electrical conductivity, the conductive energy transport is characterised by the highest thermal diffusivity and it is impervious to other penetrant molecules[1]. Nevertheless, the production of graphene is still a challenge and the industrial applications seem very far [2].  Composites at very high content of graphene analogues may be the answer to obtain materials that maintain some properties of the magic graphene.

Graphene Nanoplatelets, GNP, can be produced at a reasonable cost for immediate industrial applications. Composite materials with a content of Graphene Nanoplatelets up to 99.9% can be manufactured having a highly oriented structure. Polymer pre-impregnated foils, Gpreg, with large area (square centimeters) and hundreds of microns thick can manufactured (maintaining its highly ordered structure, as showed in picture 1-a) that can be readily integrated in conventional composite manufacturing processes [3,4].

Mechanical, thermal, electrical and barrier properties of polymer pre-impregnated foils at very high content of Graphene Nanoplatelets are here presented and discussed. Figure 1-b shows the interplay of properties of Gpreg films. Potential industrial applications of such class of materials are illustrated.

Figure 1 -  Inner structure of Gpreg laminate (a), Multifunctional properties of GPregs

Acknowledgement: Activities were carried out in the framework of an Italian grant “AMICO”. PhD grant of Fabrizia Cilento is supported by the programme “PON Ricerca e Innovazione 2014-2020”

References

[1]	A.H. Castro Neto, F. Guinea, N.M.R. Peres, K.S. Novoselov, A.K. Geim, The electronic properties of graphene, Rev. Mod. Phys. 81 (2009) 109–162. doi:10.1103/RevModPhys.81.109.

[2]	M.R. Ricciardi, A. Martone, F. Cristiano, F. Bertocchi, M. Giordano, Nacre-like composites made by graphite nanoplatelets, in: AIP Conf. Proc.,  AIP Publishing LLC  , 2018: p. 020072. doi:10.1063/1.5045934.

[3]	M.R. Ricciardi, F. Cristiano, F. Bertocchi, A. Martone, M. Giordano, Manufacturing and properties of biomimetic graphite nanoplatelets foils, Polym. Eng. Sci. (2019) pen.25200. doi:10.1002/pen.25200.

[4]	H. Wu, L.T. Drzal, Graphene nanoplatelet paper as a light-weight composite with excellent electrical and thermal conductivity and good gas barrier properties, Carbon N. Y. 50 (2012) 1135–1145. doi:10.1016/j.carbon.2011.10.026.