## Slide 1: Material science and accelerator R&D: Reflectivity and Photo Yield measurements of vacuum chamber technical surfaces
Dottorato in fisica degli acceleratori
(XXXI ciclo)
Candidata:
Eliana La Francesca
Relatore interno: prof. M. Migliorati
Relatore esterno: dott. R. Cimino

## Slide 2
Outline
Synchrotron radiation detrimental effects
Reflectivity and Photo Yield
Bessy II measurements
Conclusions

## Slide 3
Outline
Synchrotron radiation detrimental effects
Reflectivity and Photo Yield
Bessy II measurements
Conclusions

## Slide 4: Synchrotron Radiation detrimental effects
Heat load on the accelerator walls
Gas load
Production of photo emitted electrons (e- cloud effect)
Beam instability

## Slide 5
Synchrotron Radiation interaction with Matter
Electron cloud effect
Photo-electrons
generation
Absorbed + Reflected + Transmitted

## Slide 6
Photo-emitted electrons can be:
Produced directly by SR (dipoles): emitted in the orbit plane (not participate to electron cloud build up).
Produced by the reflected or scattered light (dipoles and free field zone): emitted perpendicularly to the orbit plane (generate secondary electrons)
SR and electron cloud generation
Original representation F. Ruggero
Beam
instability

## Slide 7
Synchrotron Radiation interaction with Matter
Electron cloud effect
Photo-electrons
generation
Absorbed + Reflected + Transmitted
Heat Load

## Slide 8: FCC Parameters
Parameters LHC H-L LHC FCC-hh
http://tlep.web.cern.ch/content/fcc-hh
Version 1.0 (2014-02-11)
Dipoles at 1.9 K
FCC-hh SR incidence angle: 0.077 deg
(0.62 mrad)
Total Power to dissipate such HL at cold bore temperature: 3 GW

## Slide 9: FCC-hh Synchrotron Radiation
R. Cimino, V. Baglin and F. Schäfers, PRL. 115 (2015) 264804
FCC-hh SR incidence angle: 0.077 deg (0.62 mrad)
21 m from source
Photon fan strip 2mm
X-Ray Range
FCC-hh needs a Beam Screen at the highest possible temperature compatible with vacuum stability, impedance…
Notes: Let’s focus about FCC SR with more detail.
FCC SR is expected to impinge accelerators walls at 21 m from source, with a very grazing angle (0.035 degree) and with 2mm of photon fan strip.
Critical energy is in X-ray range. SR Power is principally carried by high energy photons.

## Slide 10: FCC-hh Beam Screen

## Slide 11: FCC-hh Beam Screen

## Slide 12: FCC-hh Beam Screen
Roma, 19 November 2018
The Science & Technology Facility Council (STFC)

## Slide 13
Synchrotron Radiation interaction with Matter
Absorbed + Reflected + Transmitted
Specular reflected
Scattered

## Slide 14
Arc SR Heat Load = 28.4 (44.3) W/m/aperture
To be increased in cold parts (Superconductor Magnets)
To be increased in high temperature parts
Specular reflected
Scattered
R. Cimino, V. Baglin and F. Schäfers, PRL. 115 (2015) 264804
Absorbed + Reflected + Transmitted
Synchrotron Radiation interaction with Matter

## Slide 15: Specular Reflectivity: the case of Carbon
(C) 3.5 nm (X-ray range)
20 nm of C can reflect all photons
R. Cimino, V. Baglin and F. Schäefers, PRL. 115 (2015) 264804
REFLEC simulations
Attenuation depth ():
P(x)=exp(-x/)
For x= the intensity of X-rays falls to 1/e of its value at the surface.
FCC-hh SR incidence angle: 0.077 deg
(0.62 mrad)
Ra=50 nm

## Slide 16
Outline
Synchrotron radiation detrimental effects
Reflectivity and Photo Yield
Bessy II measurements
Conclusions

## Slide 17: Reflectivity (R) and Photo Yield (PY)
Two main properties of material needs to be
carefully investigated:
Reflectivity
Photo Yield
How many electrons are
produced per incident photon
The part of incident radiation which is reflected by the wall
chambers
To model the generation of photoelectrons in PyECLOUD build- up simulations are needed paramters like PY and R

## Slide 18: Reflectivity (R) and Photo Yield (PY)
X-Ray Reflectivity and PY depends on a limited number of parameters:
Photon energy and light polarization
Angle of incidence
Surface roughness and treatment
Chemical composition of surface
Material (coating)

## Slide 19: Specular VS Total Reflectivity
Usually, analytical programs are used for optical calculation to calculate Specular Reflectivity
R (specular reflectivity) is the normalized number of photons emerging from the sample with the same divergence of the incoming beam and at the geometrical
Reflection
Rt (total reflectivity) is the normalized (to the incoming flux) number of photons emerging from the sample in all directions.

## Slide 20: Roughness and Reflectivity
In optical simulation codes Ra is a considered as a (Debye-Waller) perturbation.
It does not work for:
• high roughness technical surfaces.
• high photon energies
• grazing angles
• also, at very grazing angles
• Different Surface Geometry
• Treated Surface
contaminants should play a major role (difficult to predict)
Saw-Tooth profile (ST)
Laser Treated Samples (LASE)

## Slide 21
Outline
Synchrotron radiation detrimental effects
Reflectivity and Photo Yield
Bessy II measurements
Conclusions

## Slide 22: Samples
two copper sample polished, Cu 1A and Cu 2A (10 cm long), with and without a-C coating;
one copper sample lapped, Cu 1B (10 cm long), with and without a-C coating;
LHC Beam Screen (BS), flat zone (30 cm long), with and without a-C coating;
LHC Beam Screen (BS), Saw-Tooth zone (30 cm long);
Cu sample treated by Laser Ablation Surface Engineering (LASE, made by the Science & Technology Facility Council (STFC))(30 cm long).

## Slide 23: Samples
Cu Flat samples
LHC Flat
LHC Saw-Tooth
Cu Lase

## Slide 24: AFM measurements
AFM (20x20µm2)

## Slide 25: Measured roughness
Sample | RMS Roughness (Ra) | RMS Roughness (Ra) (Carbon Coating)
Cu 1A | 10 nm | 13 nm
Cu 1B | 25 nm | 31 nm
Cu 2A | 27 nm | 29 nm
LHC-Flat | 15 nm | 20 nm
Samples A: polished
Sample B: lapped
Cu 1A
Cu 2A

## Slide 26: BESSY-II Optic Beamline and Reflectometer
A.A.Sokolov,et al,Proc.of SPIE92060J-1-13(2014)

## Slide 27: BESSY-II Optic Beamline and Reflectometer
Incidence angle θ: -90° – 90°
Detector in-plane 2θ: -180° – 180°
Detector off-plane χ : -4° – 4°
Sample – detector: 310 mm
Six axes sample positioning
Sample current measurement
GaAsP-Photodiodes
Detector slits, pinholes
A.A.Sokolov,et al,Proc.of SPIE92060J-1-13(2014)

## Slide 28: Bessy II Measurements
Photon Energy range 351800 eV
Beam height h=0.3 mm
Incident Beam measurement
GaAsP Photodiodes (4x4mm) (0.12*4mm)
Incidence angle 0.25, 0.5, 1 deg
Reflectivity measurement
Photo Yield:
PY= Ne/N
Specular Reflectivity
Specular
Total
Detector
Scattered Light
Mirror

## Slide 29: Flat samples: Reflectivity (R)
O K edge
C K edge
Cu L2,3 edge
E. La Francesca et al: submitted to PR ST
At grazing
incidence angle contaminants are influencing Cu Reflectivity

## Slide 30: Flat samples: Reflectivity (R)
E. La Francesca et al: submitted to PR ST

## Slide 31: Flat samples:Photo Yield (PY)
O K edge
C K edge
Cu L2,3 edge
E. La Francesca et al: submitted to PR ST

## Slide 32: Angular distribution of Reflectivity
For technical surfaces scattered light cannot be neglected
R Rt
Total Reflectivity (Rt) is calculated integrating the angular distribution in qr and F
Reflectivity
5 10 15
twotheta (deg)
100
10-1
10-2
10-3
10-4
10-5
10-6
= 5 deg
small angle
scatter
wide angle
scatter
Ra=0.5 nm
specular reflection

## Slide 33: Angular distribution of Reflectivity
E. La Francesca et al: submitted to PR ST

## Slide 34: Specular and Total Reflectivity
E. La Francesca et al: submitted to PR ST

## Slide 35: Specular and Total Reflectivity

## Slide 36: Specular and Total Reflectivity VS Ra

## Slide 37: LHC Saw-Tooth
Total Reflectivity higher than Specular Reflectivity
E. La Francesca et al: submitted to PR ST

## Slide 38: LHC Saw-Tooth
Total Reflectivity higher than Specular Reflectivity

## Slide 39: LHC Saw-Tooth
Total Reflectivity higher than Specular Reflectivity

## Slide 40: LHC Saw-Tooth
PY peaks confirm the contaminants presence
Little difference in PY for the three incidence angle
E. La Francesca et al: submitted to PR ST

## Slide 41: Lase
Total Reflectivity higher than Specular Reflectivity
No carbon evidence
E. La Francesca et al: submitted to PR ST

## Slide 42: Lase
Total Reflectivity higher than Specular Reflectivity
No carbon evidence

## Slide 43: Lase
Total Reflectivity higher than Specular Reflectivity
No carbon evidence

## Slide 44: Lase
No difference in PY for the three incidence angle
No carbon evidence
E. La Francesca et al: submitted to PR ST

## Slide 45: Surface modification effects
LHC S-T Specular Reflectiviy is one order of magnitude lower than LASE.
E. La Francesca et al: submitted to PR ST

## Slide 46: Surface modification effects
Photo Yield of LHC S-T and LASE are the same
LHC S-T Specular Reflectiviy is one order of magnitude lower than LASE.
E. La Francesca et al: submitted to PR ST

## Slide 47: AFM measurements (CC)
AFM (20x20µm2)

## Slide 48: Measured roughness
Sample | RMS Roughness (Ra) | RMS Roughness (Ra) (Carbon Coating)
Cu 1A | 10 nm | 13 nm
Cu 1B | 25 nm | 31 nm
Cu 2A | 27 nm | 29 nm
LHC-Flat | 15 nm | 20 nm
Samples A: polished
Sample B: lapped
Cu 1A
Cu 2A
50 nm CC made by
Magneto-sputtering

## Slide 49: Flat samples with carbon coating
Coating process increased roughness
E. La Francesca et al: submitted to PR ST

## Slide 50: LHC-Flat with C Coating
Peaks correspond to absorption edges
Decreasing of reflectivity at is due to the achievement of the critical angle.

## Slide 51: Flat samples with carbon coating
Carbon coating reduces
Photo Yield at high energy
Peaks correspond to absorption edges

## Slide 52: Specular and Total Reflectivity (CC)
Total Reflectivity higher than Specular Reflectivity
E. La Francesca et al: submitted to PR ST

## Slide 53: Specular and Total Reflectivity (CC)
Total Reflectivity higher than Specular Reflectivity

## Slide 54: Specular and Total Reflectivity (CC)
Total Reflectivity higher than Specular Reflectivity
It stays above 80 %

## Slide 55: Specular and Total Reflectivity (CC)
CC increases Total Reflectivity and reduce absorption and related Heat Load.
Does not significantly decreases with Ra
Increases with decreasing qi

## Slide 56: conclusions
R and PY on technically relevant samples can be experimentally measured!
At grazing incidence angle air contaminants deeply influence Reflectivity.
For technical surfaces scattered light cannot be neglected (Total Refletivity instead of Specular Reflectivity)
Cu LASE Reflectivity is substantially lower than for untreated copper and for LHC Saw-Tooth sample.
The Photo Yield of Saw-Toothed copper and LASE are the same.

## Slide 57: Conclusions
Simulation for Machine Design study must be supported by:
• Experimental data of each individual Material Property
• Dedicated experiments are the only way to produce the necessary inputs close to realistic conditions.
Carbon coating increases Total Reflectivity and reduce absorption and related Heat Load (as long as incidence angle is below its critical angle).

## Slide 58: Thank you for your attention.

## Slide 59: Flat samples: Reflectivity (R)
In all cases, R is higher at lower photon energies.
In all cases, R is higher at lower angle of incidence qi.
Reflectivity, after the observed Cu-L2-3 absorption edge at 930-950 eV is much higher than in simulation.
In all spectra we measure a significant effect due to the absorption edges of C K-edge at 280 eV and O Kedge at 530 eV (surf. cont.)
C and O K absorption edges are more effective at lower incidence angles.
Roughness, as expected, plays a major role in determining the ability of a surface to specularly reflect impinging photons.

## Slide 60: Flat samples:Photo Yield (PY)
In all cases, PY is higher at higher photon energies.
The PY dependence on qi is consistently dimmed and finally washed out when surface Ra is increasing.
In all cases, the Cu-L2-3 absorption edge at 930-950 eV is visible and cause an increase in the measured PY.
In all spectra we measure a significant effect due to the C K-edge at 280 eV and O K-edge at 530 eV (surf. Contaminants)
Roughness does influence the PY. The lower is Ra, the highest is the measured PY.
E. La Francesca et al: submitted to PR ST

## Slide 61: LHC Flat
Low energy photons can be reflected even at high incidence angles
Photo Yield:
PY= Ne/N
The maximum of Photo Yield Vs qi depends on the impinging photon energy

## Slide 62: LHC Flat (CC)
Photo Yield:
PY= Ne/N
The maximum of Photo Yield Vs qi depends on the impinging photon energy
Low energy photons can be reflected even at high incidence angles

## Slide 63
5
Heat Load Dissipation VS Temperature
FCC-hh needs a Beam Screen at the highest possible temperature compatible with vacuum stability, impedance…
PTOT
PTOT
Power to dissipate 1W (W)
Notes: If we consider the Power needed to dissipate 1W VS Temperature we can see that at cold bore temperature would be necessary 3 GW for the whole machine. This means that FCC needs a BS at highest possible temperature compatible with all other constraints (vacuum, impedance ecc).
It is important to underline that the majority of this heat load is in Dipoles.