## Slide 1: The coating thermal noise R&D for the 3rd generation: a multitechnique investigation
E. Cesarini1,2), M.Prato3), M. Lorenzini2)
      Università di Urbino
      INFN Firenze
      INFN Genova
on behalf of CoaCh collaboration

## Slide 2: The CoaCh project
Modeling
Hints for
Production/
Post-production
New samples
Single layer
sample set
Characterization
Modification/ alteration
Substrate with a single layer of Ta2O5 , crafted to enhance the layer characteristics and to be easily handled
Mechanical, bulk, optical, surface and interface properties
Global alterations :
  Thermal processing/annealing in vacuum or controlled atmosphere
  EM radiation exposure (X-rays, UV)
Local alterations :
  Laser heating/damaging
  Ion implantation

## Slide 3: The CoaCh for the 3rd generation
High Brownian Coating Noise
Higher Brownian Noise
Simulation at 18K
see talk J. Franc or ET-021-09

## Slide 4: Facilities
Properties |  | Description | Facility
Chemical | Bonding state | To evaluate the presence of dangling bonds or the oxidation state | XPS in Genova
Structural | Short range ordering | To quantify the degree of amorphousness | SEM (Modena/Pisa)
 |  |  | XRD in Pisa
Tribological | Roughness | Nano and micro scale | AFM in Genova
Optical | Index of refraction | 245-1700 nm | SE in Genova
Thermal | Conductivity | Thermal conductivity 4 K | Firenze
Mechanical | Young’s modulus and density | Measured through the effects on mode frequencies | Q measurement setup/AFM
 | Mechanical loss | Loss angle measurements | Q measurement in FI PG & PD (Low & Cryo T)

## Slide 5: Preliminary results on 200 nm Ta2O5 mono-layer
Q-measurements facility in Firenze
Annealing treatment in vacuum
SE analysis in Genova
XPS analysis in Genova
Future upgrades

## Slide 6: Q measurements with GeNS
equilibrium condition:
D>t
GeNS (INFN FI) Q measurements at room temperature with a nodal suspension controlled in temperature
The reproducibility between two different suspensions is within 20%
Q value is not depending on suspension point
The deposited coating is preserved
Maximum measured Q value for a thin disk is about 20∙106
E. Cesarini et al. REVIEW OF SCIENTIFIC INSTRUMENTS 80, 053904 (2009)

## Slide 7
Q measurements with GeNS
Substrate loss angle
Substrate+500nm
Ta2O5 loss angle
Substrate+200nm Ta2O5 loss angle
CORNING substrate
+
Ta2O5 mono-layer ion beam sputtered by ATFilms

## Slide 8: Annealing treatment in vacuum
ANNEALING CURVE
HEATING
500 °C
for 1 h
SLOW COOLING
NATURAL
COOLING
WHY 500°C ?
From literature amorphous Ta2O5 crystallised at ≈650°C so we made a conservative choice
Martin et al. Class. Quantum Grav. 26 (2009) 155012
Martin et al. Class. Quantum Grav. 25 (2008) 055005
VACUUM
SYSTEM
TUBE
FURNACE
Loss angle vs Frequency

## Slide 9: SE analysis
Fresnel reflection coefficients
SE studies the polarization of the beam reflected by the specimen
BEFORE ANNEALING AFTER ANNEALING
OPTICAL MODEL FITTED
not annealed disk:
annealed disk:
Surface roughness d = 1.6 nm
Ta2O5 – thickness = 196 nm (20÷40 nm 1-2% voids layer)
Corning substrate
Surface roughness d = 0.9 nm
Ta2O5 – thickness = 196 nm (20÷40 nm 1-2% voids layer)
Corning substrate

## Slide 10: XPS analysis
X-Rays Photo-electron Spectroscopy (XPS) used to study the chemical composition of the surface
High resolution image of Ta4f and O1s peak
Ta2O5 200 nm amorphous layer
Ta2O5 amorphous powder
metallic Tantalium
NO CHANGING AFTER THE ANNEALING

## Slide 11: further possible investigation
Control of the structural properties XRD (Pisa, M. Tonelli)
Direct measurement of the layers thickness to fit the optical properties (Modena, Pisa SEM)
Changing of the Annealing procedure:
    Annealing temperature
    Quick cooling rate to preserve amorphous structure

## Slide 12: Upgrades
GENS at cryogenic temperatures (see talk by M. Lorenzini), silicon substrates
Furnace chamber to connect to XPS machine, to control any chemical structure changes during the heat treatment
Possibility to introduce a small cryostat to cool the sample during SE analysis to investigate optical properties at low temperature
Introduction of the possibility to do annealing in a controlled atmosphere (e.g. N2)
Correlation with structural properties

## Slide 13: EXAFS
This powerful technique for probing the local structure . It gives information on the number and chemical identities of near neighbours and the average interatomic distances up to 5-6 Å
The X-ray source is synchrotron radiation, allowing the EXAFS technique to be used for atoms in any aggregation state (solid,
liquid or gas) in all kinds of environment: crystalline solids, glasses, amorphous phases, liquids and solutions.
Extended X-ray absorption ﬁne structure spectroscopy
Threshold behaviour
ABSORPTION
interference between scattered photons and photons reflected by neighbouring sites

## Slide 14: Conclusion
A multi-technique approach (CoaCh project) on coating thermal noise problem is on-going for 2nd and 3rd generation of GW detectors
First preliminary results can be useful to understand which properties to correlate and which analyses are needed
Upgrades of set up are beginning