## Slide 1
Implantation of silicon-vacancy single-photon emitters at the Tandetron accelerator of INFN Florence for application in quantum technologies.
Stefano Lagomarsino, Silvio Sciortino,
Nicla Gelli,
Lorenzo Giuntini, Massimo Chiari, Francesco Taccetti, Mirko Massi,
Lukas Hunold,
Florian Sledz,
Haritha Kambalathmana, Assegid M. Flatae, Marco Bellini,
Chiara Corsi,
Mario Santoro,
and Mario Agio

## Slide 2
SiV color centers implantation for QA
Implantation of color centers at INFN-FI
Characterization and post-processing at LENS and CNR-INO Florence
Optical studies and device development with Lab. Of Nano-optics Siegen Univ. - Germany

## Slide 3
Diamond color centers implantation for QA
The interest for (negative) Silicon-Vacancy centers arises from
Strong brightness at room temperature
Emission concentrated in ZPL within down to 0.7 nm at room temperature
Doublet spin state of the gr. state
Possibility to increase the (yet short) coherence time of the spin state (e.g. embedding in a phononic crystal)
Short lifetime of excited state (1ns) high emission rate
Single photon emission
Quantum information storage and manipulation

## Slide 4
Tandetron accelerator facility of LABEC (Florence)*
Solid state sputtering neg. Ion source
Es. Si-, CN-
3MV tandem accelerator
switching magnet
Electrostatic deflector line
Si-
Si3+
Si+
Si2+
Si4+
Si3+
Ar stripper
DC: 10 nA/mm2
(fluence 10111016 cm-2)
Pulsed: duty cicle0.05%:
down to 106 cm-2
We can generate and accelerate a great amount of on species either atomic (Si, Ge-, Sn- ecc.) or in convenient molecular form (CN- ecc.)
Choosing appropriate term. Voltage and charge state, we work on the 0.1 <E<15 MeV range of energies
Chart: 
0.1 MeV - 7020 nm (FWHM)
15 MeV – 3.160.08m
Depth (m)
Prob.dens/ion (m-1)
* The center for production of single-photon emitters at the electrostatic-deflector line of the Tandem accelerator of LABEC (Florence) NIMB 422, 31-40

## Slide 5
Implantation of color centers at INFN-FI
Irradiation time (s)
10-8
10-7
10-6
10-5
10-4
10-3
10-2
10-1
10-0
101
102
103
104
Process time (s)
1 s
(1Hz)
102s
(100Hz)
1 s
Cont.
104 s
Cont.
1 s
(1Hz)
50 s
(10Hz)
Fluence (cm-2)
1011
1016
1011
106
106
104
def+
predef.
predef. only
no-def.
Single shot on a 1m pin-hole
Well separated centers light implantation
Heavy implantation, low damage
Single shot on a 1 cm target
Heavy implantation, strong damage

## Slide 6
Single centers (after proper annealing) were searched for by wide field microscopy and addressed for further measurements*.
60X oil-imm. Obj.
1.5 mm w-dist.
10X Obj.
wide-field-ill.
647 Kr-Ar cw laser
1 ion/m2
10 ion/m2
Implantation of color centers at INFN-FI
Single emitter characterization performed at Laboratory of Nano-Optics, Siegen Univ. (Ge)
*Optical properties of silicon-vacancy color centers in diamond created by ion implantation and post-annealing Diamond and Related Materials 84, 196-203

## Slide 7
FWHM = (1.60.1) nm
60X oil-imm. Obj.
1.5 mm w-dist.
10X Obj.
wide-field-ill.
647 Kr-Ar cw laser
1 ion/m2
10 ion/m2
to spectrometer
647 Kr-Ar cw laser
Then, their spectra has been analysed, revealing a very sharp luminescent peak at 738 nm with an inhomogeneous dispersion of order tenth of nm.
Implantation of color centers at INFN-FI
Single emitter characterization performed at Laboratory of Nano-Optics, Siegen Univ. (Ge)

## Slide 8
(ns)
 = (1.070.01) ns
60X oil-imm. Obj.
1.5 mm w-dist.
1 ion/m2
10 ion/m2
to spectrometer
647 Kr-Ar cw laser
45 ps
50 ns
656 pulsed laser-diode
Time-dependent measurements of excited state lifetime gave  1ns, with a theoretical limit to the emission rate of order 50 MHz (with 5% of Q-efficiency)
Implantation of color centers at INFN-FI
Single emitter characterization performed at Laboratory of Nano-Optics, Siegen Univ. (Ge)

## Slide 9
1 ion/m2
10 ion/m2
60X oil-imm. Obj.
1.5 mm w-dist.
45 ps
50 ns
656 pulsed laser-diode
delay
start
stop
cw excitation
g2 meas.
Antibunching in pulsed excitation
Possibility to produce and address single emitting centers confirmed
Implantation of color centers at INFN-FI

## Slide 10
Two kinds of implantation are performed:
Implantation of color centers at INFN-FI
Statistically uniform over large areas (1-10 mm2)
Color centers are randomly implanted at a low fluence and then searched for and addressed for measurements, or locally activated by pulsed laser irradiation
Wide field images of implanted areas

## Slide 11
Two kinds of implantation are performed:
photoluminescence map (scan. 1m res.)
103
102
10
1
1
30
10
3
1
1
«hot spots» 106 Si implanted
Implantation of color centers at INFN-FI
Implanted over matrices with micrometric resolution

## Slide 12
Implantation of color centers at INFN-FI
1.5 m
FWHM
Two points 10 m apart, each with 100 col. centers
0.6 m
FWHM
Single center
Thus, the dispersion of the ion distribution is about
Due to the pin-hole dimensions (possibility to improve to fractions of m)
Confocal micro-fluorescence scan

## Slide 13
Transparency recovers
(defect annealing)
Before annealing
Annealed 1150°C
- x20 increase of luminescence signal (738 nm ZPL of SiV, negligible sidebands)
Implantation of color centers at INFN-FI
1150°C
20°C
2h
3h
t
After proper annealing at 1150°C

## Slide 14
Characterization and post-processing at Lens and INO-CNR Florence
Recently, a new kind of activation procedure has been employed for Nitrogen-Vacancy centers, based on the effect of localised femtosecond, high intensity laser irradiation of diamond with native Nitrogen impurity level of order ppb.

## Slide 15
Characterization and post-processing at Lens and INO-CNR Florence
Spectr.
entr. slit
TV camera
BS
SF
NF
Dicr. M.
Dicr. M.
Beam exp.
BPF
Ti-Sapphire, 800 nm, 300 mJ, 30 fs pulses
 10 nJ pulses
Weel F
F
Sample
He-Ne excitation laser beam
At the XUV-lab of INO-CNR Florence we are employing a similar procedure for activation experiments of SiV centers after implantation of Si ions.
If succesfull, it would permit to locally address the activation of individual SiV centers (res  1 m) by laser irradiation after diffuse silicon irradiation.

## Slide 16
Where irradiated with Ti-Sapphire for some minutes, the diamond surface partially recovers transparence, indication of vacancy-interstitial recombination
before
during
after
before
max = 741.5 nm
FWHM = 9 nm
The identification of the feature at 741 nm is not trivial. It will require measurement of the excited state lifetime
before
after

## Slide 17
Luminescence is quenched at high temperatures, but still strong at 500K, and recovers at RT
Peak wavelength is a reproducible indicator of temperature, with good sensitivity especially at HT
Characterization and post-processing at Lens and INO-CNR Florence
*Robust luminescence of the silicon-vacancy center in diamond at high temperatures AIP Advances 5 (12), 127117

## Slide 18
Device development with Lab. Of Nano-optics Siegen Univ. - Germany
We are working to the fabrication of single photon light-emitting Schottky diodes based on the implantation of recombination SiV centers in an n-doped diamond
Their emission rate would take advantage of the high temperature robustness of these color centers

## Slide 19
Saturation of
single emitter
background
Device development with Lab. Of Nano-optics Siegen Univ. - Germany
Low fluence (107 cm-2) implantation in Phosphorus doped diamond (grown at 5000 ppm of PH3/CH4)
results in well separated luminescent centers…
… exhibiting 738 nm luminescence with 7.6 nm FWHM, over a background which is separable from signal below saturation.
Anticoincidence measurements shows difinitely single-photon emission conditions.
The first assessment of such a behavior in n-doped diamond.
The work is in progress trying to explore the issue of electrical excitation and detection of single photon emission in the depletion zone of Schottky diodes.
arXiv:1912.09352

## Slide 20
Device development with Lab. Of Nano-optics Siegen Univ. - Germany
We are working also on Si-implantation in polycr. diamond membranes (100 nm thickness)*.
Composite diamond-silica-metal layered structures (Yagi-Uda antenna-like) are capable to increment directionality and efficiency of color centers (two patents, US and EU)
SiV centers embedded in a nano-layered antenna have shown increased directionality.
Work is in progress to improve superficial characteristics of diamond films and optimize optical characteristics of SiV centers.
*Highly efficient light extraction and directional emission from diamond color centers using planar Yagi-Uda antennas arXiv:1905.03363

## Slide 21
Silicon-vacancy color centers in phosphorus-doped diamond Assegid Mengistu Flatae, Stefano Lagomarsino, Florian Sledz, Navid Soltani, Shannon S Nicley, Ken Haenen, Robert Rechenberg, Michael F Becker, Silvio Sciortino, Nicla Gelli, Lorenzo Giuntini, Francesco Taccetti, Mario Agio arXiv preprint arXiv:1912.09352
Exploring ultrafast single-photon emission of silicon-vacancy color centers in diamond nano-membranes coupled with gold nano-cones
H Kambalathmana, AM Flatae, S Lagomarsino, H Galal, F Tantussi, GC Messina, E Wörner, C Wild, N Gelli, S Sciortino, L Giuntini, F De Angelis, M Agio Quantum Nanophotonic Materials, Devices, and Systems 2019 11091, 1109108
Highly efficient light extraction and directional emission from diamond color centers using planar Yagi-Uda antennas Hossam Galal, Assegid M Flatae, Stefano Lagomarsino, Gregor Schulte, Christoph Wild, Eckhard Wörner, Nicla Gelli, Silvio Sciortino, Holger Schönherr, Lorenzo Giuntini, Mario Agio arXiv preprint arXiv:1905.03363
Optical properties of silicon-vacancy color centers in diamond created by ion implantation and post-annealing Stefano Lagomarsino, Assegid M Flatae, Silvio Sciortino, Federico Gorelli, Mario Santoro, Francesco Tantussi, Francesco De Angelis, Nicla Gelli, Francesco Taccetti, Lorenzo Giuntini, Mario Agio Diamond and Related Materials 84, 196-203
The center for production of single-photon emitters at the electrostatic-deflector line of the Tandem accelerator of LABEC (Florence) Stefano Lagomarsino, Silvio Sciortino, Nicla Gelli, Assegid M Flatae, Federico Gorelli, Mario Santoro, Massimo Chiari, Caroline Czelusniac, Mirko Massi, Francesco Taccetti, Mario Agio, Lorenzo Giuntini Nuclear Instruments and Methods in Physics Research Section B: Beam Interactions with Materials and Atoms 422, 31-40
Robust luminescence of the silicon-vacancy center in diamond at high temperaturesS Stefano Lagomarsino, Federico Gorelli, Mario Santoro, Nicole Fabbri, Ahmed Hajeb, Silvio Sciortino, Lara Palla, Caroline Czelusniak, Mirko Massi, Francesco Taccetti, Lorenzo Giuntini, Nicla Gelli, Dmitry Yu Fedyanin, Francesco Saverio Cataliotti, Costanza Toninelli, Mario Agio AIP Advances 5 (12), 127117

## Slide 22
Implantation of silicon-vacancy single-photon emitters at the Tandetron accelerator of INFN Florence for application in quantum technologies.
Stefano Lagomarsino, Silvio Sciortino,
Nicla Gelli,
Lorenzo Giuntini, Massimo Chiari, Francesco Taccetti, Mirko Massi,
Lukas Hunold,
Florian Sledz,
Haritha Kambalathmana, Assegid M. Flatae, Marco Bellini,
Chiara Corsi,
Mario Santoro,
and Mario Agio